Table 2 Catalytic activity evaluation of the Fe3O4@SiO2.DIL nanocatalyst for the synthesis of 1,8-dioxo-decahydroacridines derivativesa

| Entry | Aldehyde | Product | Time (min) | Yield (%)b |
| --- | --- | --- | --- | --- |
| 1 |  |  | 25 | 96 |
| 2 |  |  | 30 | 92 |
| 3 |  |  | 33 | 87 |
| 4 |  |  | 25 | 92 |
| 5 |  |  | 30 | 86 |
| 6 |  |  | 20 | 95 |
| 7 |  |  | 30 | 87 |
| 8 |  |  | 30 | 90 |
| 9 |  |  | 25 | 93 |
| 10 |  |  | 25 | 92 |
| 11 |  |  | 35 | 90 |
| 12 |  |  | 30 | 85 |
| 13 |  |  | 20 | 92 |
| 14 |  |  | 33 | 88 |

a Reaction condition: aldehyde (1 mmol), ammonium acetate (1 mmol), dimedone (2 mmol), 100 C, solvent free, 0.05 g catalyst.

b Isolated yield