Table 1. The results of EDX and atomic absorption tests

| Catalyst |  |  |  | EDX |  |  |  | atomic absorption |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Co K | Ru L | C K | N K | O K | Al K | Si k | Co |
| ZIF-67 | 18 | - | 41.89 | 40.1 | - | - | - | 17.63 |
| Co-Ru@NC | 75.63 | 1.85 | 12.74 | 9.78 | - | - | - | 74.04 |
| Co-Ru@ZSM-5 | 15.05 | 0.44 | 11.05 | - | 36.75 | 4.45 | 32.24 | 14.76 |
| Co-Ru@ɤ-Al2O3 | 21.53 | 0.71 | - | - | 30.09 | 47.83 |  | 20.35 |

Table 2. Textural properties of the ZIF-67 and catalysts.

| Catalyst | BET surface area (m2/g) | Pore Volume (cm3/g) | Pore diameter (nm) |
| --- | --- | --- | --- |
| ZIF-67 | 1487.1 | 0.69 | 1.87 |
| Co-Ru@NC | 254.40 | 0.26 | 4.10 |
| Co-Ru@γ-Al2O3 | 219.12 | 0.42 | 7.70 |
| Co-Ru@ZSM-5 | 220.01 | 0.13 | 2.39 |

Table 3. crystal size of cobalt oxide, metallic cobalt and dispersion of metallic cobalt of the synthesized catalysts

|  | Average Crystallite size of cobalt oxide (nm) | Average Crystallite size of metallic cobalt (nm) | Dispersion of metallic cobalt (%D) |
| --- | --- | --- | --- |
| ZIF-67 | 44.3727 | 33.2795 | 2.8846 |
| Co-Ru@NC | 7.5459 | 5.6594 | 16.9627 |
| Co-Ru@ZSM-5 | 10.7771 | 8.078 | 11.83931 |
| Co-Ru@γ-AL2O3 | 11.654 | 8.7405 | 10.9833 |

Table 4. Hydrogen consumption of catalysts measured by H2-TPR

| Total mmol H2/g | H2 consumption, mmol H2/g | Peak II( T/C°) | H2 consumption, mmol H2/g | Peak I( T/C°) | Catalyst |
| --- | --- | --- | --- | --- | --- |
| 2.82 | 2.05 | 283.8 | 0.77 | 185.5 | ZSM-5@ Co-Ru |
| 3.22 | 2.36 | 443.1 | 0.86 | 229 | Co-Ru@γ-AL2O3 |
| 7.62 | 3.44 | 483.1 | 4.18 | 243.9 | Co-Ru@NC |

Table 5. Detailed FTS performance of the Co-Ru@NC, Co-Ru/ZSM-5 and Co-Ru/ɤ-Al2O3 catalyst

| Catalysts | T(°C) | CO Conversion (%) |  |  | Selectivity (%) |  | α value | Yield (%) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | CO2 | CH4 | C2-4 | C5+ |  |  |
| Co-Ru@NC | 210 220 230 | 65.10 72.29 85.62 | 0.010 0.029 0.046 | 4.89 6.25 8.37 | 1.25 1.86 2.16 | 93.85 91.88 89.45 | 0.91 0.9 0.88 | 61.09 66.42 76.59 |
| Co-Ru/ZSM-5 | 210 220 230 | 55.24 64.58 78.35 | 1.08 1.37 1.76 | 12.74 20.05 25.80 | 6.97 7.27 9.50 | 80.27 72.67 64.69 | 0.88 0.87 0.85 | 44.34 46.93 50.68 |
| Co-Ru/ɤ-Al2O3 | 210 220 230 | 49.12 60.48 72.48 | 1.54 1.76 2.29 | 15.6 20.72 28.98 | 3.90 5.71 6.11 | 80.50 73.56 64.90 | 0.87 0.85 0.83 | 39.50 44.49 47.20 |