## Slide 1
Supplementary material for
Investigation of the mechanism of novel molten salt electrolysis of Cu2S at 473 K
for the production of Cu metal and elemental S
Tae-Hyuk Lee1, Hee-Nam Kang1, Jin-Young Lee1,2, and Jungshin Kang1,2,*
1Korea Institute of Geoscience and Mineral Resources, 124 Gwahak-ro Yuseong-gu, Daejeon 34132, Korea
2University of Science and Technology, 217 Gajeong-ro Yuseong-gu, Daejeon 34113, Korea
3School of Materials Science and Engineering, Pusan National University, 2 Busandaehak-ro, Geumjeong-gu, Busan 44241, Korea

## Slide 2
Figure S-1 Binary phase diagram of the CuCl – KCl system.

## Slide 3
Ecathode
Eanode
Inlet
Outlet
Na2S2O3 solution
C rod
C crucible
CuCl – KCl
Exhaust gas
Figure S-2 Schematic of experimental apparatus for electrolysis in CuCl – KCl molten salt using C crucible cathode and C anode at 473 K

## Slide 4
10 μm
(a)
(b)
(c)
Figure S-3 (a) Photograph of the Na2S2O3 solution after electrolysis and analytical results of (b) microstructure and (c) element distribution of precipitates
10 μm
10 mm
S

## Slide 5
(a)
(b)
10 mm
10 mm
Figure S-4 Photograph of the CuCl – KCl molten salt obtained (a) after pre-electrolysis and (b) after CuCl2 converting to CuCl by chemical reaction with Cu metal at 473 K

## Slide 6
(a)
(b)
1 μm
Concentration of element i, Ci (at.%) |  | 
S | Cu | Cl
10.49 | 48.71 | 40.81
(c)
Figure S-5 (a) Photograph of the lid of the PYREX reactor after electrolysis and analytical results of (b) microstructure, and (c) concentration of elements of particles obtained at the lid of the reactor
20 mm