Table S1: Design of experiments using Box-Behnken design to determine the factors on corrosion inhibition efficiency

| Std | Run | Factor 1 | Factor 2 | Factor 3 | Response 1 |
| --- | --- | --- | --- | --- | --- |
|  |  | A: Concentration (ppm) | B: Temperature (°C) | C: Time (hrs) | Inhibition Efficiency (%) |
| 7 | 1 | 200 | 45 | 24 | 85.4 |
| 14 | 2 | 1100 | 45 | 14 | 96.1 |
| 11 | 3 | 1100 | 25 | 24 | 79.4 |
| 13 | 4 | 1100 | 45 | 14 | 96.8 |
| 5 | 5 | 200 | 45 | 4 | 90.9 |
| 12 | 6 | 1100 | 65 | 24 | 93.9 |
| 4 | 7 | 2000 | 65 | 14 | 97.1 |
| 8 | 8 | 2000 | 45 | 24 | 93.8 |
| 2 | 9 | 2000 | 25 | 14 | 85.3 |
| 1 | 10 | 200 | 25 | 14 | 72.8 |
| 3 | 11 | 200 | 65 | 14 | 94.9 |
| 16 | 12 | 1100 | 45 | 14 | 96.7 |
| 15 | 13 | 1100 | 45 | 14 | 96.7 |
| 17 | 14 | 1100 | 45 | 14 | 96.3 |
| 10 | 15 | 1100 | 65 | 4 | 94.6 |
| 9 | 16 | 1100 | 25 | 4 | 27.3 |
| 6 | 17 | 2000 | 45 | 4 | 95.4 |

Table S2: Summary of the model fitting

| Source | Model p-value | Lack of Fit p-value | Adjusted R² | Predicted R² |  |
| --- | --- | --- | --- | --- | --- |
| Design Model | 0.1980 | < 0.0001 | 0.1006 | -0.2368 |  |
| Linear | 0.0053 | < 0.0001 | 0.5502 | 0.3779 | Suggested |
| 2FI | 0.6563 | < 0.0001 | 0.4942 | -0.1652 |  |
| Quadratic | < 0.0001 | 0.0022 | 0.9749 |  | Suggested |
| Cubic | 0.0022 |  | 0.9982 |  | Aliased |

Table S3: ANOVA and fit statistics for the quadratic regression model

| Source | Sum of Squares | df | Mean Square | F-value | p-value |  |
| --- | --- | --- | --- | --- | --- | --- |
| Model | 769.20 | 9 | 85.47 | 65.78 | < 0.0001 | significant |
| A-Concentration | 95.22 | 1 | 95.22 | 73.29 | 0.0001 |  |
| B-Temperature | 325.52 | 1 | 325.52 | 250.55 | < 0.0001 |  |
| C-Time | 6.60 | 1 | 6.60 | 5.08 | 0.0651 |  |
| AB | 26.52 | 1 | 26.52 | 20.41 | 0.0040 |  |
| AC | 3.80 | 1 | 3.80 | 2.93 | 0.1380 |  |
| BC | 0.0200 | 1 | 0.0200 | 0.0154 | 0.9053 |  |
| A² | 18.57 | 1 | 18.57 | 14.29 | 0.0092 |  |
| B² | 146.74 | 1 | 146.74 | 112.95 | < 0.0001 |  |
| C² | 25.85 | 1 | 25.85 | 19.90 | 0.0043 |  |
| Residual | 7.80 | 6 | 1.30 |  |  |  |
| Lack of Fit | 7.43 | 2 | 3.71 | 40.37 | 0.0022 | significant |
| Pure Error | 0.3680 | 4 | 0.0920 |  |  |  |
| Cor Total | 776.99 | 15 |  |  |  |  |
| Std. Dev. | 1.14 |  | R2 | 0.99 |  |  |
| Mean | 91.63 |  | Adjusted R2 | 0.98 |  |  |
| C.V. % | 1.24 |  | Adeq Precision | 25.34 |  |  |

Table S4: Optimization constraints

| Variable | Objective | Lower Limit | Upper Limit | Lower Weight | Upper Weight | Importance |
| --- | --- | --- | --- | --- | --- | --- |
| A: Concentration | minimize | 200 | 2000 | 1 | 1 | 3 |
| B: Temperature | is in range | 25 | 65 | 1 | 1 | 3 |
| C: Time | maximize | 4 | 24 | 1.20226 | 1 | 3 |
| Inhibition Efficiency | maximize | 72.8 | 97.1 | 1 | 1 | 3 |