Supplementary information

A Robust Lateral Shift Free (LSF) Electrothermal Micromirror With Flexible Multi-Morph Beams

Hengzhang Yang 1, Anrun Ren 1, Yingtao Ding 1, Lei Xiao 1, Teng Pan 1, Yangyang Yan 2, Wenlong Jiao2 and Huikai Xie 1, *

1School of Integrated Circuits and Electronics, Beijing Institute of Technology, Beijing 100081, China

2BIT Chongqing Institute of Microelectronics and Microsystems, Chongqing 400030, China

* hk.xie@ieee.org

Supplementary Materials:

Figures S1, S2.

Table S1, S2.

References S1, S2.

Figure S1. The test method for temperature coefficient of resistance. (a) The whole view of the test setup. A temperature-controlled oven is used to set the temperature, and a multimeter is used to measure the resistance value at the specific temperature. (b) A close view of the device in the oven. To maximize the heat concentration on the micromirror, the TO package is inverted on the bottom heating plate. (c) A close view of the PCB circuit board of the micromirror. (d) The relationship between the resistances and the temperature. The measurement error of the resistance is ±1 Ω. The TCR of the resistance can be calculated as the ratio of the slope to the R-axis intercept of its R-T curve [S1], and the value is 0.0022/K.

Figure S2. Damaged pictures of the two types of micromirrors. (a~f). The PSPI-type micromirrors. (g ~ l). The SiO2-type micromirrors.

Table S1. Comparison of properties of the selected materials

| Material | Young’s modulus (GPa) | CTE (ppm K-1) | Thermal conductivity (W m-1 K-1) | Electrical conductivity (S m-1) |
| --- | --- | --- | --- | --- |
| Al [S2] | 70 | 23.1 | 237 | 35.5 × 106 |
| SiO2 [S2] | 70 | 0.5 | 1.4 | Insulator |
| Pt [S2] | 168 | 8.8 | 71.6 | 8.9 × 106 |
| PSPI [S2] | 2.3 | 20 | 0.15 | Insulator |

Table S2. The resistance and frequency test results of a PSPI-type micromirror in the drop test

| Drop height(cm) | R1 (Ω) | R2 (Ω) | R3 (Ω) | R4 (Ω) | f1(Hz) | f2(Hz) | Microscopic Examination |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 528.6 | 534.1 | 526.7 | 529.2 | 198 | 388 | OK |
| 3 | 528.7 | 533.4 | 525.7 | 528.3 | 198 | 388 | OK |
| 5 | 529.1 | 535.2 | 528.8 | 530.4 | 198 | 387 | OK |
| 7 | 528.3 | 537.7 | 524.3 | 527.4 | 197 | 386 | OK |
| 9 | 530.1 | 536.3 | 527.1 | 529.7 | 197 | 386 | OK |
| 11 | 531.4 | 533.1 | 529.4 | 531.2 | 195 | 385 | OK |
| 13 | 529.7 | 534.7 | 531.2 | 533.4 | 190 | 383 | OK |
| 15 | 530.4 | 537.4 | 527.4 | 530.6 | 184 | 371 | OK |
| 17 | 533.1 | 536.3 | 534.1 | 532.8 | 177 | 366 | OK |
| 19 | 532.6 | 533.9 | 536.5 | 530.3 | 162 | 344 | OK |
| 21 | 531.8 | 535.2 | 537.1 | 533.4 | 155 | 336 | OK |
| 23 | \ | \ | \ | \ | \ | \ | Fail* |

*The mirror plate detached from the device.

Reference

[S1] L. Xiao, Y. Ding, P. Wang & H. Xie. Analog-controlled light microshutters based on electrothermal actuation for smart windows. Opt Express 28, 33106-33122 (2020).

[S2] S. Pal & H. Xie. Fabrication of robust electrothermal MEMS devices using aluminum–tungsten bimorphs and polyimide thermal isolation. Journal of Micromechanics and Microengineering 22, (2012).