Table 1. Optimization of the conditions for the model reaction in the presence of TA/PEI and TA/PEI/ Magnetic, TPMS.

| Entry | Catalyst | Product | Catalyst loading | Conditions | Time(min) | Yield (%) |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | TA/PEI | 5a | 0.01 | EtOH / 80 ˚C | 45 | 70 |
| 2 | TA/PEI/M | 5a | 0.01 | EtOH / 80 ˚C | 30 | 80 |
| 3 | TPMS | 5a | 0.01 | EtOH / 80 ˚C | 15 | 94 |
| 4 | TPMS | 0.01 | EtOH | Reflux | 15 | 94 |
| 5 | TPMS | 0.01 | EtOH | r.t | 35 | 80 |
| 6 | TPMS | 0.01 | H2O | Reflux | 25 | 85 |
| 7 | TPMS | 0.01 | H2O | r.t. | 45 | 65 |
| 8 | TPMS | 0.01 | EtOH / H2O (1:1) | Reflux | 25 | 75 |
| 9 | TPMS | 0.01 | EtOH / H2O (1:1) | r.t. | 60 | 55 |
| 10 | TPMS | 0.007 | EtOH | Reflux | 45 | 84 |
| 11 | TPMS | 0.005 | EtOH | Reflux | 70 | 70 |
| 12 | TPMS | 0.003 | EtOH | Reflux | 110 | 55 |

Table 2. Investigation of the synthesis of desired products (5a-m) catalyzed by The TPMS catalyst (1) (Tannic Acid / Polyethylene imine / Magnetic / Sulfone) under the optimized conditions.a

| Entry | Aldehyde | Product | Time (min) | Yieldb (%) | m.p. ˚C (Obs.) | m.p. °C (Lit.) |
| --- | --- | --- | --- | --- | --- | --- |
| 1 |  |  | 15 | 94 | 201-202 | 198-200 116 |
| 2 |  |  | 30 | 88 | 210-217 | 208-210 |
| 3 |  |  | 20 | 90 | 232-235 | 233-234 117 |
| 4 |  |  | 20 | 88 | 193-195 | 192-193 118 |
| 5 |  |  | 15 | 92 | 219-220 | 218-220 |
| 6 |  |  | 15 | 94 | 200-202 | 199-200 119 |
| 7 |  |  | 35 | 87 | 229-230 | 228-229 |
| 8 |  |  | 20 | 89 | 350-352 | 351-352 119 |
| 9 |  |  | 20 | 86 | 217-219 | 216-217 119 |
| 10 |  |  | 30 | 85 | 214-216 | 216-217 119 |
| 11 |  |  | 25 | 92 | 203-205 | 202-204 116 |
| 12 |  |  | 35 | 87 | 167-169 | 165-167 105 |

a Isatoic anhydride (2, 1 mmol), ammonium acetate (3, 1 mmol), 4-chlorobenzaldehyde (4a , 1 mmol) and 0.01g of TPMS for the synthesis of 5a in EtOH at reflux conditions.

b Isolated yields.