Support Materials

High sensitive thermoplastic polyurethane/carbon nanotubes strain sensor fitting by a novel optimization empirical model

Xin Wang,1,2 Muchao Qu,1 Kuangqi Wu,1 Dirk W. Schubert,1,3, Xianhu Liu1,2,

1 Institute of Polymer Materials, Friedrich-Alexander-University Erlangen-Nuremberg, Erlangen 91058, Germany.

2 State Key Laboratory of Structural Analysis, Optimization and CAE Software for Industrial Equipment, National Engineering Research Center for Advanced Polymer Processing Technology, Zhengzhou University, Zhengzhou 450002, China.

3 Bavarian Polymer Institute, Fürth 90762, Germany.

Fig. S1 Ultraviolet transmission (UVT) spectra of pure TPU and TPU/CNTs films in the wavelength range 400-900 nm, the inset is transmittance at 550 nm wavelength.

The UV-analysis results are shown in Fig. S1, which indicate that the T-15 films possess higher transparency clearly during tested wavelength range whether before or after the combination of CNTs. For more accurate comparison, the transmittance data at the wavelength of 550 nm were taken separately, because this wavelength is identified as the average wavelength of visible light that can be recognized by the human eyes as well as the most sensitive light wave region for human beings []. The inset figure summarized the results. At a wavelength around 550 nm, the transmittance of pure T-15 film exhibits 5.08%, providing sufficient optical transparency for distinguishing the logo and patterns of picture behind (Figure 4), whereas pure T-10 film presents 2.06% optical transparency at 550 nm. After incorporating CNTs conductive filler through ultrasonication, both TPU/CNTs composite films display a decreasing transmittance comparing to pure TPU film. Even so, the sensor made from 15 wt% TPU still has a better transmittance, exceeding 1.68%. On the contrary, the transmittance of sensor obtained by 10 wt% TPU is only 0.21%, which reduced almost 1.85% after ultrasonication treatment with CNTs.

Fig. S2 Thermogravimetric analysis (TGA) curves of pure TPU and TPU/CNTs composite films.

The actual amount of CNTs was validated by employing thermogravimetric analysis (TGA). Fig. S2 demonstrates the TGA curves for pure TPU and TPU/CNTs composite films in nitrogen atmosphere. The residue content of pure TPU, TCs-15 and TCs-10 are 0.67%, 1.17% and 5.99%, respectively. According to the following equations,

ms=mc+mT                                                                                                       (1)

b×ms=mc+a×mT                                                                                            (2)

Ø=mcms=b-a1-a                                                                                                             (3)

where ms, mC and mT represent the weight of TPU/CNTs strain sensor, CNTs and TPU in the composites, respectively. a is the ratio of remained pure TPU film in the original TPU film, and b is the fraction of residue TPU/CNTs composite in the initial composite film. The content of CNTs (∅CNTs) can be calculated by Eq. (3), which are 0.50% and 5.36% in TCs-15 and TCs-10 composites, respectively. Based on the same ultrasonication method, the difference in the amount of CNTs adhered to the TPU scaffold was not significant.

Fig. S3 Schematic illustration of the electromechanical property test device

In order to analyze the mechanical properties and determine the sensing behavior of the novel conductive composite strain sensors, electromechanical experiments were carried out using the combination of a universal tensile testing machine and a digit ammeter []. The stretchable TPU/CNTs strain sensors were manufactured with two different concentrations of TPU (10 wt% and 15 wt%). Every sensor experienced a monodirectional stretching process at a stretch rate of 10 mm/min and its resistance change was recorded simultaneously. The schematic of the electromechanical performance test device is displayed in Figure S1. The measured sample was connected to the copper electrode at two ends. Insulating sheets were clamped between the copper electrodes and the clamper to prevent the interference of the metal clamper. By connecting a conductive circuit to the copper electrode and stretching the clamping device at the same time, the relevant computer software recorded every change of the electromechanical properties of the strain sensor.

Fig. S4 The GF value is calculated by using linear fitting of the ΔR/R0-strain plot in every divided 10% strain segment for a TCs-10 and b TCs-15.

To be more specific, the GF value of every 10% strain interval is calculated. Fig. S3 a&b describe the calculation process by using linear fitting of the ΔR/R0-strain plot in every divided 10% strain segment [].

Fig. S5 Schematic mechanism for the sensing behavior of TPU/CNTs strain sensors

The schematic mechanism is shown in Fig. S5. For the TPU/CNTs strain sensor, the three-dimensional scaffold structure built from TPU fibers is like the piers of a highway, and the CNTs are like the road surface of the highway. Each CNTs particle is a section of highway pavement, which is fixed on the surface of TPU scaffold and grid gap, forming a complete “highway”, the conductive pathway. During the stretching process, some CNTs are separated along the stress direction and some CNTs intersect with other particles, leading to the breakage of the conductive pathway and the formation of a new conductive pathway. This explains the insignificant change in sensor resistance at low strain. As the external stress is further increased, the particle spacing becomes larger and the conductive pathway is further disrupted until the sensor fails.

Fig. S6 Schematic of mechanical hysteresis (HM) quantification.

Fig. S6 is the schematic of mechanical hysteresis (HM) quantification. Based on the Mullins effect to explain the reduction in stress, which is commonly occurred in tensile tests of elastomer-based composite material, mechanical hysteresis (HM) is introduced for quantifying the mechanical behavior as the absolute value of the difference under the loading path (AL) and unloading path (AU) curves as a percentage of the area under the loading path curve (HM=(AL-AU)/AL).

References:

. Zhou B, Han XQ, Lia L, Feng YZ, Fang T, Zheng GQ, Wang B, Dai K, Liu CT, Shen CY (2019) Ultrathin, flexible transparent Joule heater with fast response time based on single-walled carbon nanotubes/poly(vinyl alcohol) film. Compos Sci Technol 183: 107796

. Qu MC, Qin YJ, Sun Y, Xu HG, Schubert DW, Zheng K, Xu W, Nilsson F (2020) Biocompatible, flexible strain sensor fabricated with polydopamine-coated nanocomposites of nitrile rubber and carbon black. ACS Appl. Mater Interfaces 12(37): 42140-42152

. Wang X, Liu XH, Schubert DW (2021) Highly sensitive ultrathin flexible thermoplastic polyurethane/carbon black fibrous film strain sensor with adjustable scaffold networks. Nano-Micro Lett 13(1): 1-19

Corresponding authors. E-mail address: xianhu.liu@zzu.edu.cn (X.H. Liu); dirk.schubert@fau.de (D.W. Schubert).