Crystal structure of AgSCN coordination polymers for sensing of iron (III) ions, Nitrobenzene and photocatalytic activity under ultrasonic irradiation

Safaa El-din H. Etaiw1, Mohamed M. Dawood2, Hassan Marie1

1Chemistry Department, Faculty of Science, Tanta University, Tanta, Egypt.

2Tanta Higher Institute of Engineering and Technology (THIET), Tanta, Egypt.

Supplementary materials

Table S1 Bond lengths (Å) and bond angles (deg.) of the SCP1

| Ag1-Ag1 | 3.3429(16) | C3- N4 | 1.166(6) |
| --- | --- | --- | --- |
| Ag1-S2 | 2.8415(16) | Ag1-Ag1-S2 | 67.81(4) |
| Ag1-Ag1 | 3.2593(17) | Ag1-Ag1-Ag1 | 91.73(5) |
| Ag1-Ag1 | 3.4636(17) | S2-Ag1-Ag1 | 158.46(3) |
| Ag1-S2 | 2.9973(17) | Ag1-Ag1-S2 | 165.29(3) |
| Ag1-N4 | 2.156(4) | S2-Ag1-S2 | 107.28(4) |
| Ag1-S2 | 2.4749(13) | Ag1- Ag1- S2 | 94.20(4) |
| S2- C3 | 1.660(4) | Ag1- Ag1- N4 | 79.24(12) |
| S2- Ag1- N4 | 92.13(12) | S2- Ag1- N4 | 87.25(11) |
| Ag1- Ag1- N4 | 90.45(11) | S2- Ag1- S2 | 101.91(4) |
| S2- Ag1- S2 | 97.07(3) | N4- Ag1- S2 | 163.27(11) |
| Ag1- S2 - Ag1 | 125.94(6) | Ag1- S2 - C3 | 100.04(15) |
| Ag1- S2- C3 | 99.55(15) | S2- C3- N4 | 179.9(4) |
| Ag1- N4- C3 | 172.3(4) |  |  |
| Symmetry codes SCP1: +X,+Y,+Z', -X,+Y+ 1/2,-Z' |  |  |  |

Scheme S1 Structure of Acid blue-92 (AB-92) dye used for investigation

Scheme S2 Structure of Eosin-Y (EO) dye used for investigation

Fig. 1. FT-IR Spectra of SCP1 and its nanosized 2

Figure S2 view of the distorted polygonal rings containing 4 atoms (Ag2S2), 8 atoms [Ag2(SCN)2], 12 atoms [Ag4S2(SCN)2],  18 atoms [Ag5S(SCN)4] and 20 atoms [Ag6S2(SCN)4] along the b-axis showing the orientation of the 4- and 8-membered rings

Figure S3 UV-Vis spectra of SCP1 as nujl moll in solid state

Figure S4 (1) Solid state emission spectra of SCP1 and  nanosized 2

Figure S5 Quenching efficiency at different NB concentrations

Figure S6 LOD of SCP1 at different NB concentrations

Figure S7 Quenching efficiency at different Fe3+ concentrations

Figure S8 LOD of SCP1 at different Fe3+ concentrations

Figure S9 The UV-vis absorption spectra of AB-92 dye solution during photocatalytic degradation of the AB-92 solution without using nanosized 1 catalyst in the presence of H2O2 at room temperature

Figure S10 The UV-vis absorption spectra of EO-Y dye solution during photocatalytic degradation of the EO-Y solution without using nanosized 1 catalyst in the presence of H2O2 at room temperature

Fig. S11. Kinetic data for degradation of AB-92 dye under different irradiation sources.

Fig. S12. Kinetic data for degradation of EO-Y dye under different irradiation sources.

Figure S13 The UV-vis absorption spectra of EO-Y dye solution during photocatalytic degradation using nanosized 1 in the presence of H2O2 and 20 mg of AO as scavengers for holes (h+) radical under uV-light irradiation

Figure S14 The UV-vis absorption spectra of EO dye solution during photocatalytic degradation using nanosized 1 in the presence of H2O2 and 20 mg of BQ as scavengers for (.O2–) radical under UV-light irradiation

Figure S15 The UV-vis absorption spectra of EO-Y dye solution during photocatalytic degradation using nanosized 1 in the presence of H2O2 and 2 gm of IPA as scavengers for (.OH) radical under UV-light irradiation

Figure S16 kinetic data for the photodegradation of  EO-Y dye under scavenger experiments