Supplementary Information

Dual photo-enhanced interpenetrating network hydrogel with biophysical and biochemical signals for infected bone defect healing

Guangyu Jian1, #, Dize Li1, #, Qiwei Ying2, Xu Chen1, Qiming Zhai1, Si Wang1, Li Mei3, Richard D. Cannon3, Ping Ji1, *, Huanan Wang2, *, and Tao Chen1, *

1. Stomatological Hospital of Chongqing Medical University, Chongqing Key Laboratory of Oral Diseases and Biomedical Sciences, Chongqing Municipal Key Laboratory of Oral Biomedical Engineering of Higher Education, Chongqing, 401147, P. R. China

2. Key State Laboratory of Fine Chemicals, School of Bioengineering, Dalian University of Technology, Dalian, 116023, P. R. China

3. Department of Oral Sciences, Sir John Walsh Research Institute, Faculty of Dentistry, University of Otago, Dunedin 9054, New Zealand

*E-mail: chentao1985@hospital.cqmu.edu.cn (Tao Chen);

huananwang@dlut.edu.cn (Huanan Wang);

jiping@hospital.cqmu.edu.cn (Ping Ji).

# These authors contributed equally to the work.

1. Supplementary Materials and Methods

1.1. Synthesis of SilMA

Both the silk fibroin (SF) and SilMA solutions were made in the same way. After being cut into thin slices (≈0.25cm2), the cocoons were boiled in 2 litres of 0.02 M Na2CO3 solution for 1 h before being rinsed three times with distilled water. The silk that had been degummed was then left at room temperature to dry. The dried silk was dissolved in LiBr (9.3mM) at 60°C for 4 h using a ratio of 1 g silk to 5 ml LiBr ratio. Immediately after the SF was dissolved by LiBr, 3 ml of glycidyl methacrylate (GMA) solution (424 mM) (Sigma-Aldrich, USA) was added to 50 ml of the SF solution. The mixture was then stirred intermittently at 300 rpm at 60°C for 3 h, resulting in a high-yield reaction between the GMA and the SF. The resultant solution was centrifuged, and then dialyzed for 3 d against distilled water using Slide-A-Lyzer dialysis cassettes (MWCOs of 14000 Da for SilMA and 3500 Da for the SF solution). The SilMA and SF solutions were then frozen at -80°C for 12 h and freeze-dried for 48 h before being stored at 4°C.

1.2. Synthesis of MA-GNPs

Gelatin (20 g) was dissolved in 400 ml of water, and incubated at 50°C for 30 min with stirring. After cooling to room temperature, 1 ml of methacrylic anhydride was added in the dark, and the pH of the solution was constantly adjusted to between 6 and 8. After reacting for 6 h, 1.2 l of acetone was added. The precipitate was re-dissolved in deionized water at 50°C, and freeze-dried. The lyophilized nanoparticles were dissolved in deionized water (50°C) at 5% wt/v. After the nanoparticles were completely dissolved, a peristaltic pump was used to gradually drop in acetone with stirring until it was is 7.5 times that of the solution. After the solution was completely emulsified, 1 ml pentadiene aldehyde was added and reacted for 4 h. Then 40 g glycine was added with stirring at room temperature, and the reaction continued for 2 h, and washed three times with ethanol and water.

1.3. Synthesis of CuBGs

CuBGs (95SiO2:2.5CaO:2.5CuO (in mol%)) was synthesized by a modified Stöber method. First, 25 ml of ethanol and 3 ml of tetraethyl orthosilicate (TEOS) were added to a previously mixed solution of 15 ml of deionized water, 10 ml of ethanol, and 4.5 ml of ammonium hydroxide. After 30 min of stirring, 1.59 g of calcium nitrate tetrahydrate and 0.52 g of copper (II) nitrate hemi(pentahydrate) were added to the solution. After 90 min of mixing, the suspension was centrifuged at 5,000 rpm for 10 minutes, and the resulting slurry was washed with a solution of water and ethanol (2:10, v/v). The slurry was frozen and then freeze-dried for one day.

1.4. Lap shear test and mechanical test

Lap shear testing was performed to measure the tensile strength of the bond between the hydrogel and the bone tissue, and the force required to detach the bond. Two bovine bone blocks were coated evenly with either SilMA, MA-GNPs or SGC hydrogel on the parts (1 cm × 2 cm) that were to be overlapped. Then, the coated blocks were photocured with UV light irradiation (30 s). The blocks were assembled and loaded on a universal testing machine (E42, Meters Instruments, USA) and shear tested by tensile loading at a strain rate of 2 mm/min. The separation point was fixed at the maximum load. The shear strength (KPa) was the maximum load (N) divided by the bond area (2 cm2).

For the deformation recovery test, a 500g weight was placed on the hydrogel with or without light curing (30 s), and the diameter and height of the hydrogel was measured before and after removing the weight. The compression and tensile test were undertaken with a universal mechanical testing machine; the loading rate of the compression and tensile test was 0.5mm/min.

1.5. Bacterial Live and dead staining

A Live/Dead BacLight® Bacterial Viability Kit (Thermo Fisher, USA) was used to evaluate bacterial viability. E. coli or S. aureus cells (1x106 CFU/ml) were incubated with hydrogel at 37°C for 24 h. Then the bacterial solution was collected, centrifuged (10,000 g, 1 0min), and the supernatant was discarded. The pellet was resuspended in 2 ml of saline and centrifuged again. Finally, the pellet was resuspended in 1 ml of saline. An equal volume of SYTO® 9 and propidium iodide was mixed to form a dye solution, and 3 μl of the dye mixture was added. After incubation at room temperature in the dark for 15 min, 5 μl of the stained bacterial suspension was transferred to a glass slide and photographed with an EVOS multi-function microscope.

1.6. Biofilm assay of antibacterial activity

Wells in a 48-well microtiter plate were inoculated with 500 µl of an overnight TSB culture of E. coli or S. aureus cells (1x106 CFU/ml) and incubated at 37°C for 48h to develop a static biofilm. Then 1g hydrogel was added and the plates were incubated for a further 24 h at 37°C. Crystal violet（CV）was used to count bacteria in biofilms. Biofilms were fixed using 500 µl of formaldehyde and then washed three times with PBS buffer. The bacteria were stained with 0.2% (w/v) CV for 15 min. Excess dye was washed off by rinsing the plate wells three times with PBS after the biofilms had dried. The amount of biofilm was quantified by solubilizing the CV using 30% acetic acid and measuring the absorbance at 595 nm.

1.7. The measurement of bacterial ROS levels

The samples were subjected to a 2',7'-dichlorodihydrofluorescein diacetate (DCFH-DA) assay (Reactive Oxygen Species Assay Kit, cat#S0033; Beyotime) to determine the amount of ROS produced by the bacteria. First, the bacteria treated with the hydrogel were washed twice with saline in a refrigerated centrifuge (6,000 rpm, 4°C) for 5 min, then the pellet was resuspended in saline, and DCFH-DA was added at a ratio of 1:1000 or probe loading (37°C, 30 min). Finally, excess DCFH-DA was removed by centrifugation (6,000 rpm, 4°C) for 5 min. The pellet was resuspended and photographed using a fluorescence microscope. In addition, 100 µL of the treated bacteria were put in the wells of a 96-well microtiter plate, and a microplate reader (Perkin Elmer, USA) was used to measure the fluorescence intensity at 525 nm after excitation at 488 nm.

1.8. Hydrogel cell biocompatibility

A live/dead staining kit (Solarbio, China) was used to evaluate tissue culture cell viability. After 7 days of culture, 100 μl of live/dead solution was added to each well of the plates. After incubation at 37°C for 2 h, cells were observed using EVOS multi-function microscope. In addition, the biocompatibility of hydrogels was also evaluated using a cell counting kit-8 (CCK-8, Solarbio, China) assay. Briefly, MC3T3-E1, HUVECs and Raw264.7 cells were cultured with hydrogels and CCK-8 agent were added (10% of well volume) into well plates at certain time points and incubated for 2h. Then the absorbance at 450 nm of the colored culturing media was measured with a multimode plate reader (PerkinElmer).

1.9. qRT-PCR

Total RNA was extracted from Raw264.7, HUVECs and MC3T3-E1 cells using the RNAiso Plus reagent (Takara, Japan) for mRNA analysis. Total RNA (500 ng) was reverse transcribed into cDNA using 5X PrimeScript RT Master Mix (Takara, Japan). For qRT-PCR analysis, a 10 µl reaction volume was used that included cDNA, TB Green™ Premix Ex Taq™ (Takara, Japan), forward and reverse primers, and RNase-free water. Expression of M1 markers (CD86, TNF-α, IL-6), M2 markers (Arg, CD206, TGF-β), markers of osteogenic differentiation (ALP, Runx2, OPN, OSX and COL-1) and markers of angiogenic differentiation (CD31, VEGF and ANG1) were measured using the primers in Table S1; GAPDH acted as the housekeeping gene.

2. Supplementary Fig.

Table S1 Primer sequences for qRT-PCR analysis.

Mouse

| Gene | Forward primer | Reverse prism |
| --- | --- | --- |
| GAPDH | 5’TGAGGTGACCGCATCTTCTTG3’ | 5’TGGTAACCAGGCGTCCGATA3’ |
| CD86 | 5’TGGTAACCAGGCGTCCGATA3’ | 5’CGGCAGATATGCAGTCCCAT3’ |
| TNF-α | 5’CTGAACTTCGGGGTGATCGG3’ | 5’GGCTTGTCACTCGAATTTTGAGA3’ |
| IL-6 | 5’ATAGTCCTTCCTACCCCAATTTCC3’ | 5’GATGAATTGGATGGTCTTGGTCC3’ |
| Arg | 5’GGAATCTGCATGGGCAACCTGTGT3’ | 5’AGGGTCTACGTCTCGCAAGCCA3’ |
| CD206 | 5’AGACGAAATCCCTGCTACTG3’ | 5’CACCCATTCGAAGGCATTC3’ |
| TGF-β | 5’CAGTACAGCAAGGTCCTTGC3' | 5’ACGTAGTAGACGATGGGCAG3’ |
| ALP | 5’CCAGAAAGACACCTTGACTGTGG3’ | 5’TCTTGTCCGTGTCGCTCACCAT3’ |
| COL-Ⅰ | 5’TCGTGGTGAGACTGGTCCTG3’ | 5’TGTCACCTTGTTCGCCTGTC3’ |
| OPN | 5’GCTTGGCTTATGGACTGAGGTC3’ | 5’CCTTAGACTCACCGCTCTTCATG3’ |
| Runx-2 | 5’GAATGGCAGCACGCTATTAAATCC3’ | 5’GCCGCTAGAATTCAAAACAGTTGG3’ |
| OSX | 5’CCTCTCGACCCGACTGCAGATC3’ | 5’AGCTGCAAGCTCTCTGTAACCATGAC3’ |

Human

| Gene | Forward primer | Reverse prism |
| --- | --- | --- |
| GAPDH | 5’ACAACTTTGGTATCGTGGAAGG3’ | 5’GCCATCACGCCACAGTTTC3’ |
| VEGF | 5’CTACCTCCACCATGCCAAGT3’ | 5’CACACAGGATGGCTTGAAGA3’ |
| ANG-1 | 5’TCACATAGGGTGCAGCAATC3’ | 5’ACAGTTGCCATCGTGTTCTG3’ |
| CD31 | 5’CCAAGGTGGGATCGTGAGG3’ | 5’CGGAAGGATAAAACGCGGTC3’ |

Fig. S1 Photographs of the self-healing property of the hybrid hydrogel.

Fig.S2 Time-dependent rheological studies to evaluate the photo-enhanced mechanical property of the S20-GC hybrid hydrogel (n=3) (**** p＜0.0001 using one-way ANOVA test ).

Fig.S3 Rheological studies to evaluate the mechanical properties of the SGC, SilMA and MA- GNP hydrogels.

Fig. S4 Representative stress–strain curves for SGC hydrogels with and without light-curing and the hysteresis curves of SGC hydrogels with and without light-curing upon cyclic loading and unloading.

Fig. S5 Agar plate assay for S. aureus showing the antibacterial properties of SGC hydrogels containing different concentrations of CuBGs (0.5, 1, 2% wt).

Fig. S6 DAF-FM staining of bacteria showing the formation of NO.

Fig. S7 (A) Live/dead staining of MC3T3 cells cultured with various hydrogels for 1, 4, and 7 days. (B) CCK-8 analysis of MC3T3 cells cultured with various hydrogels for 1, 4, and 7 days. (C) Live and dead staining of RAW264.7 cells cultured with various hydrogels for 1, 4, and 7 days. (D) CCK-8 analysis of HUVECs cultured with various hydrogels for 1, 4, and 7 days. (**** p＜0.0001 using one-way ANOVA test )

Fig. S8 The hemostatic effect of the SCG hydrogel after curing with UV light in bone defects.