Supplementary Material

For Research on Chemical Intermediates

Efficient Removal of Methylene Blue by Micro-/Mesoporous Heteroatom-doped Biochar Derived from Waste Bovine Horn

Qifan Peng a, 1, Zhen Du a, 1, Chaoqiang Ma a, Yuepeng Guan b, *, Zhenxing Feng c, *,Yaqin Huang a, *

a Beijing Laboratory of Biomedical Materials, Beijing Key Laboratory of Electrochemical Process and Technology for Materials, Beijing University of Chemical Technology, Beijing 100029, China

b Beijing Key Laboratory of Clothing Materials R&D and Assessment, Beijing Engineering Research Center of Textile Nano Fiber, Beijing Institute of Fashion Technology, Beijing 100029, China

c School of Chemical, Biological, and Environmental Engineering, Oregon State University, Corvallis, Oregon, USA Oregon State University

* Corresponding author.

E-mail address:

Yaqin Huang: huangyq@mail.buct.edu.cn

Yuepeng Guan: 20210007@bift.edu.cn

Zhenxing Feng: zhenxing.feng@oregonstate.edu

1 Both authors contributed equally to this work.

Fig. S1 Element distribution on surface of (a-d) BHB-Air and (e-h) BHB-N2

Fig. S2 Raman spectra of (a) BHB-Air and (b) BHB-N2

Fig. S3 Fitting curves of pseudo-first-order and pseudo-second-order kinetic models for adsorption of MB on (a, b) BHB-Air and (c, d) BHB-N2

Fig. S4 Fitting curves of Langmuir isotherm model and Freundlich isotherm model for adsorption of MB on BHB-Air at (a, b) 30 ℃, (c, d) 40 ℃ and (e, f) 50 ℃

Fig. S5 Fitting curves of Langmuir isotherm model and Freundlich isotherm model for adsorption of MB on BHB-N2 at (a, b) 30 ℃, (c, d) 40 ℃ and (e, f) 50 ℃

Fig. S6 Structural properties of BHBs after adsorption

Fig. S7 XPS spectra of N1s and O 1s from (a, b) BHB-N2 and (c, d) BHB-N2-MB

Table S1 Thermodynamic constants for the adsorption of MB on BHBs

| Adsorbents | ΔG (kJ/mol) |  |  | ΔH (kJ/mol) | ΔS [J/ (mol K)] |
| --- | --- | --- | --- | --- | --- |
|  | 303K | 313K | 323K |  |  |
| BHB-Air | -5.97 | -6.24 | -6.51 | 2.13 | 26.73 |
| BHB-N2 | -4.88 | -5.34 | -5.80 | 9.05 | 45.96 |

Table S2 Structural properties of BHBs after MB adsorption

| Samples | SBET a (m2/g) | Vtotal b (cm3/g) | Vmicro c (cm3/g) | Dp 4 (nm) |
| --- | --- | --- | --- | --- |
| BHB-Air-MB | 434.04 | 0.22 | 0.0092 | 2.21 |
| BHB-N2-MB | 509.31 | 0.32 | -0.011 | 2.74 |

Note: SBET is the specific surface area calculated from BET method, Vtotal is the total pore volume measured at P/P0 = 0.99; Vmicro is the micropore volume calculated by t-Plot method, and Dp is the average pore width calculated from the equation of 4Vtotal/SBET.