- The precipitation of Cu in the inclusion was beneficial to the reduction of grain boundary segregation. And Cu had the ability to capture Sb and Ni.

- Cu was involved in the local corrosion initiation of inclusions, during which Cu and Sb were oxidized to corresponding Cu2O and Sb2O3, and distributed in the corrosion products.

- Under the influence of the segregation of elements at the grain boundaries, the local corrosion spreading process was carried out, and the internal part of the crystal was preferentially corroded.

- Cr was enriched in the cementite of pearlite and took part in the corrosion process, resulting in the formation of CrO3.