Supplementary Information

Stereocomplexed microparticles loaded with Salvia cadmica extracts for enhancement of immune response towards Helicobacter pylori

Weronika Gonciarz, Magdalena Chmiela, Bartłomiej Kost, Ewelina Piątczak, and Marek Brzeziński

Table of Contents

Figure S1. 1H NMR of used PLAs for MPs preparation with low molar mass.

Figure S2. 1H NMR of used PLAs for MPs preparation with medium molar mass.

Figure S3. SEC chromatograms of PLA with low molar mass and PLA with medium molar mass.

Figure S4. Exemplary FTIR spectra of sterecomplexed microparticles showing the presence of a band at 909 cm-1.

Figure S5. DSC thermograms of blank and extracts-loaded microparticles composed of low molecular mass PLAs.

Figure S6. DSC thermograms of blank and extracts-loaded microparticles composed of medium molecular mass PLAs.

Figure S6. TGA curves of blank and extracts-loaded stereocomplexed microparticles.

Table S1. Thermal parameters of obtained stereocomplexed microparticles (I and II heating run), before and after loading of the extracts.

Table S2. The decomposition temperature values for obtained blank and microparticles loaded with extracts.

Figure S1. 1H NMR of used PLAs for MPs preparation with low molar mass.

Figure S2. 1H NMR of used PLAs for MPs preparation with medium molar mass.

Figure S3. SEC chromatograms of PLA with low molar mass and PLA with medium molar mass.

Figure S4. Exemplary FTIR spectra of sterecomplexed microparticles (sc-PLA-SCAPE (mmm)) showing the presence of a band at 909 cm-1.

Figure S5. DSC thermograms of blank and extracts-loaded microparticles composed of low molecular mass PLAs showing the formation of stereocomplex crystallites since their melting is above 200 °C (II heating run).

Figure S5. DSC thermograms of blank and extracts-loaded microparticles composed of medium molecular mass PLAs showing the formation of stereocomplex crystallites since their melting is above 190 °C.

Figure S6. TGA curves of blank and extracts-loaded stereocomplexed microparticles.

Table S1. Thermal parameters of obtained stereocomplexed microparticles (I and II heating run), before and after loading of the extracts.

| Sample | Tm I heating [°C] | Hm I heating [J/g] | Tm II heating [°C] | Hm II heating [J/g] |
| --- | --- | --- | --- | --- |
| sc-PLA (lmm) | 212 | 105 | 213 | 113 |
| sc-PLA-SCAPE (lmm) | 211 159 | 102 7 | 208 | 95 |
| sc-PLA-SCRE (lmm) | 212 | 108 | 214 | 104 |
| sc-PLA (mmm) | 231 | 110 | 226 | 82 |
| sc-PLA- SCAPE (mmm) | 232 | 99 | 195 | 48 |
| sc-PLA- SCRE (mmm) | 233 | 75 | 211 | 62 |

Table S2. The decomposition temperature values for obtained blank and microparticles loaded with extracts.

| sc-PLA (lmm) | sc-PLA-SCAPE (lmm) | sc-PLA-SCRE (lmm) | sc-PLA (mmm) | sc-PLA- SCAPE (mmm) | sc-PLA- SCRE (mmm) |
| --- | --- | --- | --- | --- | --- |
| 257 °C | 280 °C | 283 °C | 288 °C | 302 °C | 353 °C |