Supplementary Information

A High-Sensitivity Ionization Humidity Sensor Based on Carbon Nanotubes

Yong Zhang1, 2, *, Zhenzhen Cheng3, Yuangang Deng1, 2, Ruizhe Wang1, 2, Saif aldeen Saad Obayes ALKADHIM1, 2, *, Waqas Muhammad1, 2, Xiaoyu Li1, 2, Chunqi Wang1, 2, Shudong Wang1, 4, Yunjia Li1.

1School of Electrical Engineering, Xi’an Jiaotong University, Xi’an,710049, P. R. China.

2 State Key Laboratory of Electrical Insulation and Power Equipment, Xi’an Jiaotong University,710049, P. R. China.

3School of Electrical and Control Engineering, Henan University of Urban Construction, Pingdingshan, Henan, 467041, China.

4State Key Laboratory for Manufacturing Systems Engineering, Xi'an Jiaotong University, Xi'an, 710049 China.
* Corresponding author; Y.Z. (zhyong@mail.xjtu.edu.cn ) or S.S.A.(saifaldeen.saad@ieee.org; alkadhim@stu.xjtu.edu.cn )

- Experiment on high relative humidity single-value sensitive characteristics (silicon strip CNT, gold film CNT).

Table 1. Experimental conditions for single-value sensitive characteristics of high relative humidity (silicon strip CNT, gold film CNT).

| No. | Experiment time | electrode spacing (μm). | Electrode structure |  |  | Electrode voltage (V). |  |  | Temperature, pressure, gas |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | cathode | extracting electrode | collecting electrode | cathode | extracting electrode | collecting electrode |  |
| 1 | 2022.10.18. | 200a 100b | ×4 mm, round holes silicon strip | 6 mm | 6×8 mm, 200 m deep groove | 0 | 90 | 10 | 23.7 ℃ 93.7 Kpa air |
| 2 | 2022.10.22. | 200a 100b | ×4 mm, round holes gold film | 6 mm | 6×8 mm, 200 m deep groove | 0 | 90 | 10 | 23.7 ℃ 93.7 Kpa Pure N2 |

a, electrode separation between cathode and the extracting electrode.

b, electrode separation between collecting electrode and the extracting electrode.

Table 2. Single-value sensitive experimental data of high relative humidity in air (silicon strip CNT).

| No. | Relative humidity (%) | Collects current (nA). | No. | Relative humidity (%) | Collects current (nA). |
| --- | --- | --- | --- | --- | --- |
| 1 | 30.0 | 0.61847 | 23 | 70.0 | 1.72837 |
| 2 | 32.0 | 0.63609 | 24 | 72.0 | 1.93903 |
| 3 | 33.3 | 0.65301 | 25 | 74.0 | 2.35880 |
| 4 | 34.0 | 0.66662 | 26 | 76.0 | 2.67520 |
| 5 | 34.8 | 0.67441 | 27 | 78.0 | 3.19650 |
| 6 | 35.6 | 0.69496 | 28 | 80.0 | 3.76730 |
| 7 | 36.4 | 0.70590 | 29 | 82.0 | 4.69800 |
| 8 | 40.0 | 0.71602 | 30 | 84.0 | 5.42960 |
| 9 | 41.0 | 0.73671 | 31 | 86.0 | 7.14640 |
| 10 | 42.0 | 0.75745 | 32 | 88.0 | 7.51510 |
| 11 | 43.0 | 0.76180 | 33 | 90.3 | 8.82470 |
| 12 | 44.0 | 0.76531 | 34 | 92.0 | 9.54830 |
| 13 | 48.0 | 0.77804 | 35 | 94.0 | 11.0635 |
| 14 | 50.0 | 0.78852 | 36 | 95.0 | 14.2929 |
| 15 | 52.0 | 0.79603 | 37 | 96.0 | 17.5499 |
| 16 | 55.0 | 0.83548 | 38 | 97.0 | 80.022 |
| 17 | 56.2 | 0.86478 | 39 | 97.5 | 86.146 |
| 18 | 58.0 | 0.90884 | 40 | 98.7 | 97.018 |
| 19 | 60.0 | 0.95448 | 41 | 99.0 | 100.290 |
| 20 | 62.0 | 1.03616 | 42 | 99.5 | 438.91 |
| 21 | 64.0 | 1.16702 | 43 | 100 | 512.68 |
| 22 | 66.0 | 1.28794 |  |  |  |

Cathode

Extracting Electrode

Collecting Electrode

Cathode

Extracting Electrode

Collecting Electrode

Figure 1. Single-value sensitive characteristic curve of high relative humidity in air (silicon strip CNT).

Cathode

Extracting Electrode

Collecting Electrode

Deep Groove

Figure 2. Single-value sensitive characteristic curve of pure N2 high relative humidity (gold film CNT).

Table 3. Single-valued sensitive experimental data of pure N2 high relative humidity (gold film CNT).

| No. | Relative humidity (%) | Collects current (nA). | No. | Relative humidity (%) | Collects current (nA). |
| --- | --- | --- | --- | --- | --- |
| 1 | 25.8 | 0.01196 | 14 | 65.0 | 0.87838 |
| 2 | 26.5 | 0.02978 | 15 | 70.0 | 1.42468 |
| 3 | 28.0 | 0.04875 | 16 | 73.0 | 1.99251 |
| 4 | 30.0 | 0.06742 | 17 | 75.0 | 2.87925 |
| 5 | 33.0 | 0.09025 | 18 | 78.0 | 3.92135 |
| 6 | 36.0 | 0.13451 | 19 | 80.0 | 4.97251 |
| 7 | 39.0 | 0.17252 | 20 | 85.0 | 10.9285 |
| 8 | 42.0 | 0.21216 | 21 | 88.0 | 20.8275 |
| 9 | 45.0 | 0.26327 | 22 | 91.0 | 40.9235 |
| 10 | 48.0 | 0.29987 | 23 | 95.0 | 100.290 |
| 11 | 53.0 | 0.33789 | 24 | 98.0 | 189.385 |
| 12 | 57.0 | 0.38325 | 25 | 100.0 | 338.720 |
| 13 | 61.7 | 0.45412 | 26 |  |  |

Figure 3. Comparison of pure N2 and air high relative humidity collection current (silicon strip CNT, gold film CNT).

- Experiment on single-value sensitivity characteristics of low relative humidity in air (gold film CNT).

Table 4. Experimental conditions for single-value sensitivity characteristics of low relative humidity in air (gold film CNT).

| Experiment time | Pole spacing (μm). | Electrode structure |  |  | Electrode voltage (V). |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | cathode | extracting electrode | collecting electrode | cathode | extracting electrode | collecting electrode | Experimental conditions |
| 2022.10.13. | 200a 100b | ×4 mm | 6 mm | 6×8 mm, 200 m deep groove | 0 | 90 | 10 | 22.8℃ 93.8Kpa air |

a, electrode separation between cathode and the extracting electrode.

b, electrode separation between collecting electrode and the extracting electrode.

Table 5. Single value sensitive experimental data of low relative humidity in air (gold film CNT).

| No. | Relative humidity (%) | Collects current (nA). | No. | Relative humidity (%) | Collects current (nA). |
| --- | --- | --- | --- | --- | --- |
| 1 | 24.8 | 0.20475 | 16 | 15.4 | 7.85920 |
| 2 | 24.6 | 0.21471 | 17 | 15.1 | 9.30570 |
| 3 | 24.2 | 0.22125 | 18 | 14.7 | 11.2583 |
| 4 | 23.4 | 0.22162 | 19 | 14.3 | 14.0398 |
| 5 | 22.9 | 0.22410 | 20 | 14.0 | 17.9020 |
| 6 | 22.3 | 0.22848 | 21 | 13.6 | 22.6250 |
| 7 | 21.5 | 0.23440 | 22 | 13.2 | 26.7860 |
| 8 | 20.9 | 0.24626 | 23 | 12.9 | 30.4700 |
| 9 | 20.2 | 0.26783 | 24 | 12.5 | 33.1260 |
| 10 | 19.5 | 0.31656 | 25 | 12.3 | 34.0430 |
| 11 | 18.8 | 0.42056 | 26 | 12.2 | 34.5190 |
| 12 | 18.1 | 0.68096 | 27 | 12.1 | 34.7040 |
| 13 | 17.3 | 1.39148 | 28 | 12.0 | 34.8660 |
| 14 | 16.1 | 5.23813 | 29 | 11.9 | 35.9570 |
| 15 | 15.7 | 6.81530 |  |  |  |

Cathode

Extracting Electrode

Collecting Electrode

Deep Groove

Figure 4. Single-value sensitive characteristic curve of low relative humidity in air (gold film CNT).