Table 2: Optimisation for the sulfoxidation reaction

| S.No. | Catalyst | Oxidant | Temp (oC) | Time (h) | Yield (%)b |
| --- | --- | --- | --- | --- | --- |
| 1 | none | H2O2 | 25 | 12 | Trace |
| 2 | 1 | H2O2 | 25 | 12 | 80 |
| 3 | 2 | H2O2 | 25 | 12 | 54 |
| 4 | 3 | H2O2 | 25 | 12 | 95 |
| 5 | 3 | H2O2 | 40 | 12 | 99 |
| 6 | 3 | H2O2 | 40 | 6 | 99 |
| 7 | 3 | H2O2 | 40 | 3 | 82 |
| 8 | 3 | TBHP | 40 | 6 | 99 |
| 9 | 3 | UHP | 40 | 6 | 58 |
| 10 | 1 | H2O2 | 40 | 6 | 91 |
| aReaction condition: substrate (0.5 mmol), catalyst (10mg), H2O2 (1.8 eq), H2O (2ml). bIsolated conversion was calculated by GC |  |  |  |  |  |

Table 3: Solvent screening for the sulfoxidation reaction.

| Entry | Solvent | Conversion (%)b | Selectivity (%) |
| --- | --- | --- | --- |
| 1 | H2O | 99 | 95 |
| 2 | DMSO | 99 | 81 |
| 3 | Ethanol | 82 | 95 |
| 4 | Ethyl Acetate | 71 | 94 |
| aReaction condition: substrate (0.5 mmol), catalyst (3) (10mg) H2O2 (1.8 eq), Solvent (2ml). bIsolated conversion was calculated by GC. Table 4 Substrate scope for sulfoxidation reaction using a catalyst (3). S.No.; Sulfoxide; Time [h]; Yieldb [%]. 1; 6.0; 99. 2; 6.0; 91. 3; 6.0; 81. 4; 6.0; 81. 5; 8.0; 75. aReaction condition: substrate (0.5 mmol), catalyst (10mg), H2O2 (1.8 eq), H2O (2ml), bIsolated Yield.. |