Mechanical properties of the antlion larva Euroleon nostras (Neuroptera, Myrmeleontidae) jaws correlate with the amount of inorganic content

1Department of Cariology, Endodontology and Periodontology, Universität Leipzig, Liebigstraße 12, 04103 Leipzig, Germany

2Department of Behavioral Biology, Institute of Cell and Systems Biology of Animals, Universität Hamburg, Martin-Luther-King-Platz 3, 20146 Hamburg, Germany

3Department of Mammalogy and Paleoanthropology, Leibniz Institute for the Analysis of Biodiversity Change, Martin-Luther-King-Platz 3, 20146 Hamburg, Germany

4Department of Functional Morphology and Biomechanics, Zoological Institute, Christian-Albrechts-Universität zu Kiel, Am Botanischen Garten 1–9, 24118 Kiel, Germany

*corresponding author: wencke.krings@uni-hamburg.de

Supplementary material

Supplementary Table 1. Results from the EDX analysis (in atomic %) and nanoindentation (hardness H and Young’s modulus E, both in GPa) for each tested region are given. Abbreviations: Md, mandible; Mx, maxilla; N, quantity of measurements; SD, standard deviation.

| Mouthpart | Region | Parameter | N | Mean | SD |
| --- | --- | --- | --- | --- | --- |
| Md | Outer edge dorsal | Ae | 132 | 3.77 | 0.43 |
| Md | Outer edge ventral | Ae | 132 | 3.25 | 0.45 |
| Md | Central region dorsal | Ae | 132 | 3.87 | 0.40 |
| Md | Central region ventral | Ae | 132 | 2.65 | 0.46 |
| Md | Inner edge dorsal | Ae | 132 | 4.97 | 0.33 |
| Md | Inner edge ventral | Ae | 132 | 3.80 | 0.32 |
| Md | Tooth I dorsal | Ae | 18 | 6.26 | 0.83 |
| Md | Tooth I ventral | Ae | 18 | 7.49 | 2.97 |
| Md | Tooth II dorsal | Ae | 18 | 5.71 | 0.50 |
| Md | Tooth II ventral | Ae | 18 | 6.37 | 2.42 |
| Md | Tooth III dorsal | Ae | 18 | 5.91 | 0.95 |
| Md | Tooth III ventral | Ae | 18 | 7.52 | 3.95 |
| Md | Tip dorsal | Ae | 60 | 10.19 | 3.16 |
| Md | Tip ventral | Ae | 60 | 9.55 | 3.95 |
| Md | Outer edge dorsal | Ca | 132 | 0.09 | 0.05 |
| Md | Outer edge ventral | Ca | 132 | 0.06 | 0.02 |
| Md | Central region dorsal | Ca | 132 | 0.08 | 0.05 |
| Md | Central region ventral | Ca | 132 | 0.04 | 0.02 |
| Md | Inner edge dorsal | Ca | 132 | 0.19 | 0.11 |
| Md | Inner edge ventral | Ca | 132 | 0.10 | 0.03 |
| Md | Tooth I dorsal | Ca | 18 | 0.49 | 0.30 |
| Md | Tooth I ventral | Ca | 18 | 1.09 | 0.89 |
| Md | Tooth II dorsal | Ca | 18 | 0.33 | 0.14 |
| Md | Tooth II ventral | Ca | 18 | 0.81 | 0.84 |
| Md | Tooth III dorsal | Ca | 18 | 0.38 | 0.28 |
| Md | Tooth III ventral | Ca | 18 | 0.99 | 1.08 |
| Md | Tip dorsal | Ca | 60 | 1.46 | 0.72 |
| Md | Tip ventral | Ca | 60 | 1.68 | 1.00 |
| Md | Outer edge dorsal | Cl | 132 | 0.15 | 0.07 |
| Md | Outer edge ventral | Cl | 132 | 0.12 | 0.06 |
| Md | Central region dorsal | Cl | 132 | 0.14 | 0.08 |
| Md | Central region ventral | Cl | 132 | 0.11 | 0.06 |
| Md | Inner edge dorsal | Cl | 132 | 0.18 | 0.10 |
| Md | Inner edge ventral | Cl | 132 | 0.15 | 0.08 |
| Md | Tooth I dorsal | Cl | 18 | 0.21 | 0.11 |
| Md | Tooth I ventral | Cl | 18 | 0.17 | 0.09 |
| Md | Tooth II dorsal | Cl | 18 | 0.22 | 0.14 |
| Md | Tooth II ventral | Cl | 18 | 0.18 | 0.12 |
| Md | Tooth III dorsal | Cl | 18 | 0.22 | 0.13 |
| Md | Tooth III ventral | Cl | 18 | 0.17 | 0.10 |
| Md | Tip dorsal | Cl | 60 | 0.23 | 0.16 |
| Md | Tip ventral | Cl | 60 | 0.20 | 0.13 |
| Md | Outer edge dorsal | Cu | 132 | 0.24 | 0.06 |
| Md | Outer edge ventral | Cu | 132 | 0.18 | 0.04 |
| Md | Central region dorsal | Cu | 132 | 0.23 | 0.06 |
| Md | Central region ventral | Cu | 132 | 0.13 | 0.05 |
| Md | Inner edge dorsal | Cu | 132 | 0.31 | 0.04 |
| Md | Inner edge ventral | Cu | 132 | 0.22 | 0.03 |
| Md | Tooth I dorsal | Cu | 18 | 0.41 | 0.12 |
| Md | Tooth I ventral | Cu | 18 | 0.58 | 0.34 |
| Md | Tooth II dorsal | Cu | 18 | 0.35 | 0.03 |
| Md | Tooth II ventral | Cu | 18 | 0.47 | 0.27 |
| Md | Tooth III dorsal | Cu | 18 | 0.37 | 0.10 |
| Md | Tooth III ventral | Cu | 18 | 0.58 | 0.47 |
| Md | Tip dorsal | Cu | 60 | 0.92 | 0.54 |
| Md | Tip ventral | Cu | 60 | 0.83 | 0.48 |
| Md | Outer edge dorsal | E | 132 | 8.25 | 1.08 |
| Md | Outer edge ventral | E | 132 | 5.56 | 0.62 |
| Md | Central region dorsal | E | 132 | 8.16 | 1.10 |
| Md | Central region ventral | E | 132 | 4.89 | 0.59 |
| Md | Inner edge dorsal | E | 132 | 10.00 | 1.38 |
| Md | Inner edge ventral | E | 132 | 6.43 | 0.76 |
| Md | Tooth I dorsal | E | 18 | 13.07 | 1.87 |
| Md | Tooth I ventral | E | 18 | 10.98 | 1.57 |
| Md | Tooth II dorsal | E | 18 | 11.67 | 1.59 |
| Md | Tooth II ventral | E | 18 | 10.05 | 1.77 |
| Md | Tooth III dorsal | E | 18 | 11.90 | 2.48 |
| Md | Tooth III ventral | E | 18 | 10.36 | 2.33 |
| Md | Tip dorsal | E | 60 | 16.78 | 1.82 |
| Md | Tip ventral | E | 60 | 12.12 | 1.63 |
| Md | Outer edge dorsal | F | 132 | 1.23 | 0.17 |
| Md | Outer edge ventral | F | 132 | 1.07 | 0.21 |
| Md | Central region dorsal | F | 132 | 1.23 | 0.20 |
| Md | Central region ventral | F | 132 | 1.09 | 0.22 |
| Md | Inner edge dorsal | F | 132 | 1.20 | 0.23 |
| Md | Inner edge ventral | F | 132 | 1.05 | 0.24 |
| Md | Tooth I dorsal | F | 18 | 1.30 | 0.08 |
| Md | Tooth I ventral | F | 18 | 1.06 | 0.12 |
| Md | Tooth II dorsal | F | 18 | 1.11 | 0.33 |
| Md | Tooth II ventral | F | 18 | 0.94 | 0.23 |
| Md | Tooth III dorsal | F | 18 | 1.31 | 0.18 |
| Md | Tooth III ventral | F | 18 | 1.26 | 0.22 |
| Md | Tip dorsal | F | 60 | 0.69 | 0.45 |
| Md | Tip ventral | F | 60 | 0.59 | 0.38 |
| Md | Outer edge dorsal | Fe | 132 | 0.15 | 0.03 |
| Md | Outer edge ventral | Fe | 132 | 0.12 | 0.02 |
| Md | Central region dorsal | Fe | 132 | 0.14 | 0.03 |
| Md | Central region ventral | Fe | 132 | 0.10 | 0.03 |
| Md | Inner edge dorsal | Fe | 132 | 0.19 | 0.03 |
| Md | Inner edge ventral | Fe | 132 | 0.14 | 0.01 |
| Md | Tooth I dorsal | Fe | 18 | 0.25 | 0.03 |
| Md | Tooth I ventral | Fe | 18 | 0.32 | 0.23 |
| Md | Tooth II dorsal | Fe | 18 | 0.22 | 0.02 |
| Md | Tooth II ventral | Fe | 18 | 0.24 | 0.08 |
| Md | Tooth III dorsal | Fe | 18 | 0.22 | 0.04 |
| Md | Tooth III ventral | Fe | 18 | 0.35 | 0.35 |
| Md | Tip dorsal | Fe | 60 | 0.53 | 0.48 |
| Md | Tip ventral | Fe | 60 | 0.48 | 0.38 |
| Md | Outer edge dorsal | H | 132 | 0.76 | 0.16 |
| Md | Outer edge ventral | H | 132 | 0.57 | 0.08 |
| Md | Central region dorsal | H | 132 | 0.75 | 0.17 |
| Md | Central region ventral | H | 132 | 0.45 | 0.12 |
| Md | Inner edge dorsal | H | 132 | 0.95 | 0.11 |
| Md | Inner edge ventral | H | 132 | 0.66 | 0.07 |
| Md | Tooth I dorsal | H | 18 | 1.15 | 0.10 |
| Md | Tooth I ventral | H | 18 | 1.12 | 0.17 |
| Md | Tooth II dorsal | H | 18 | 1.07 | 0.09 |
| Md | Tooth II ventral | H | 18 | 1.03 | 0.19 |
| Md | Tooth III dorsal | H | 18 | 1.07 | 0.15 |
| Md | Tooth III ventral | H | 18 | 1.07 | 0.26 |
| Md | Tip dorsal | H | 60 | 1.36 | 0.15 |
| Md | Tip ventral | H | 60 | 1.25 | 0.19 |
| Md | Outer edge dorsal | K | 132 | 0.17 | 0.15 |
| Md | Outer edge ventral | K | 132 | 0.15 | 0.13 |
| Md | Central region dorsal | K | 132 | 0.13 | 0.07 |
| Md | Central region ventral | K | 132 | 0.11 | 0.06 |
| Md | Inner edge dorsal | K | 132 | 0.18 | 0.10 |
| Md | Inner edge ventral | K | 132 | 0.15 | 0.09 |
| Md | Tooth I dorsal | K | 18 | 0.18 | 0.09 |
| Md | Tooth I ventral | K | 18 | 0.16 | 0.09 |
| Md | Tooth II dorsal | K | 18 | 0.21 | 0.13 |
| Md | Tooth II ventral | K | 18 | 0.17 | 0.10 |
| Md | Tooth III dorsal | K | 18 | 0.19 | 0.11 |
| Md | Tooth III ventral | K | 18 | 0.17 | 0.10 |
| Md | Tip dorsal | K | 60 | 0.56 | 0.49 |
| Md | Tip ventral | K | 60 | 0.47 | 0.43 |
| Md | Outer edge dorsal | Mg | 132 | 0.23 | 0.14 |
| Md | Outer edge ventral | Mg | 132 | 0.18 | 0.10 |
| Md | Central region dorsal | Mg | 132 | 0.22 | 0.14 |
| Md | Central region ventral | Mg | 132 | 0.08 | 0.09 |
| Md | Inner edge dorsal | Mg | 132 | 0.36 | 0.04 |
| Md | Inner edge ventral | Mg | 132 | 0.27 | 0.06 |
| Md | Tooth I dorsal | Mg | 18 | 0.41 | 0.02 |
| Md | Tooth I ventral | Mg | 18 | 0.43 | 0.04 |
| Md | Tooth II dorsal | Mg | 18 | 0.40 | 0.02 |
| Md | Tooth II ventral | Mg | 18 | 0.41 | 0.05 |
| Md | Tooth III dorsal | Mg | 18 | 0.39 | 0.04 |
| Md | Tooth III ventral | Mg | 18 | 0.42 | 0.06 |
| Md | Tip dorsal | Mg | 60 | 0.46 | 0.02 |
| Md | Tip ventral | Mg | 60 | 0.46 | 0.04 |
| Md | Outer edge dorsal | Mn | 132 | 0.27 | 0.10 |
| Md | Outer edge ventral | Mn | 132 | 0.21 | 0.04 |
| Md | Central region dorsal | Mn | 132 | 0.30 | 0.11 |
| Md | Central region ventral | Mn | 132 | 0.16 | 0.05 |
| Md | Inner edge dorsal | Mn | 132 | 0.43 | 0.15 |
| Md | Inner edge ventral | Mn | 132 | 0.26 | 0.04 |
| Md | Tooth I dorsal | Mn | 18 | 0.45 | 0.13 |
| Md | Tooth I ventral | Mn | 18 | 0.85 | 0.56 |
| Md | Tooth II dorsal | Mn | 18 | 0.51 | 0.22 |
| Md | Tooth II ventral | Mn | 18 | 0.69 | 0.50 |
| Md | Tooth III dorsal | Mn | 18 | 0.45 | 0.11 |
| Md | Tooth III ventral | Mn | 18 | 0.82 | 0.68 |
| Md | Tip dorsal | Mn | 60 | 1.26 | 0.71 |
| Md | Tip ventral | Mn | 60 | 1.20 | 0.68 |
| Md | Outer edge dorsal | Na | 132 | 0.00 | 0.00 |
| Md | Outer edge ventral | Na | 132 | 0.00 | 0.00 |
| Md | Central region dorsal | Na | 132 | 0.00 | 0.00 |
| Md | Central region ventral | Na | 132 | 0.00 | 0.00 |
| Md | Inner edge dorsal | Na | 132 | 0.01 | 0.08 |
| Md | Inner edge ventral | Na | 132 | 0.01 | 0.06 |
| Md | Tooth I dorsal | Na | 18 | 0.00 | 0.00 |
| Md | Tooth I ventral | Na | 18 | 0.00 | 0.00 |
| Md | Tooth II dorsal | Na | 18 | 0.05 | 0.15 |
| Md | Tooth II ventral | Na | 18 | 0.05 | 0.14 |
| Md | Tooth III dorsal | Na | 18 | 0.00 | 0.00 |
| Md | Tooth III ventral | Na | 18 | 0.00 | 0.00 |
| Md | Tip dorsal | Na | 60 | 0.05 | 0.16 |
| Md | Tip ventral | Na | 60 | 0.05 | 0.15 |
| Md | Outer edge dorsal | P+Pt | 132 | 0.46 | 0.08 |
| Md | Outer edge ventral | P+Pt | 132 | 0.60 | 0.10 |
| Md | Central region dorsal | P+Pt | 132 | 0.63 | 0.04 |
| Md | Central region ventral | P+Pt | 132 | 0.48 | 0.12 |
| Md | Inner edge dorsal | P+Pt | 132 | 0.76 | 0.04 |
| Md | Inner edge ventral | P+Pt | 132 | 0.71 | 0.07 |
| Md | Tooth I dorsal | P+Pt | 18 | 0.83 | 0.01 |
| Md | Tooth I ventral | P+Pt | 18 | 0.89 | 0.07 |
| Md | Tooth II dorsal | P+Pt | 18 | 0.85 | 0.01 |
| Md | Tooth II ventral | P+Pt | 18 | 0.86 | 0.05 |
| Md | Tooth III dorsal | P+Pt | 18 | 0.87 | 0.01 |
| Md | Tooth III ventral | P+Pt | 18 | 0.88 | 0.10 |
| Md | Tip dorsal | P+Pt | 60 | 0.97 | 0.10 |
| Md | Tip ventral | P+Pt | 60 | 0.94 | 0.10 |
| Md | Outer edge dorsal | S | 132 | 0.11 | 0.05 |
| Md | Outer edge ventral | S | 132 | 0.08 | 0.02 |
| Md | Central region dorsal | S | 132 | 0.10 | 0.05 |
| Md | Central region ventral | S | 132 | 0.05 | 0.03 |
| Md | Inner edge dorsal | S | 132 | 0.17 | 0.04 |
| Md | Inner edge ventral | S | 132 | 0.10 | 0.02 |
| Md | Tooth I dorsal | S | 18 | 0.24 | 0.04 |
| Md | Tooth I ventral | S | 18 | 0.26 | 0.12 |
| Md | Tooth II dorsal | S | 18 | 0.21 | 0.03 |
| Md | Tooth II ventral | S | 18 | 0.22 | 0.09 |
| Md | Tooth III dorsal | S | 18 | 0.21 | 0.06 |
| Md | Tooth III ventral | S | 18 | 0.26 | 0.17 |
| Md | Tip dorsal | S | 60 | 0.42 | 0.15 |
| Md | Tip ventral | S | 60 | 0.36 | 0.16 |
| Md | Outer edge dorsal | Si | 132 | 0.19 | 0.08 |
| Md | Outer edge ventral | Si | 132 | 0.15 | 0.04 |
| Md | Central region dorsal | Si | 132 | 0.18 | 0.09 |
| Md | Central region ventral | Si | 132 | 0.09 | 0.06 |
| Md | Inner edge dorsal | Si | 132 | 0.32 | 0.12 |
| Md | Inner edge ventral | Si | 132 | 0.19 | 0.03 |
| Md | Tooth I dorsal | Si | 18 | 0.66 | 0.27 |
| Md | Tooth I ventral | Si | 18 | 0.75 | 0.43 |
| Md | Tooth II dorsal | Si | 18 | 0.48 | 0.19 |
| Md | Tooth II ventral | Si | 18 | 0.57 | 0.36 |
| Md | Tooth III dorsal | Si | 18 | 0.54 | 0.30 |
| Md | Tooth III ventral | Si | 18 | 0.69 | 0.55 |
| Md | Tip dorsal | Si | 60 | 1.29 | 0.42 |
| Md | Tip ventral | Si | 60 | 1.07 | 0.51 |
| Md | Outer edge dorsal | Zn | 132 | 0.50 | 0.12 |
| Md | Outer edge ventral | Zn | 132 | 0.34 | 0.09 |
| Md | Central region dorsal | Zn | 132 | 0.49 | 0.12 |
| Md | Central region ventral | Zn | 132 | 0.22 | 0.11 |
| Md | Inner edge dorsal | Zn | 132 | 0.66 | 0.11 |
| Md | Inner edge ventral | Zn | 132 | 0.43 | 0.07 |
| Md | Tooth I dorsal | Zn | 18 | 0.82 | 0.08 |
| Md | Tooth I ventral | Zn | 18 | 0.92 | 0.43 |
| Md | Tooth II dorsal | Zn | 18 | 0.76 | 0.06 |
| Md | Tooth II ventral | Zn | 18 | 0.76 | 0.23 |
| Md | Tooth III dorsal | Zn | 18 | 0.75 | 0.12 |
| Md | Tooth III ventral | Zn | 18 | 0.93 | 0.62 |
| Md | Tip dorsal | Zn | 60 | 1.35 | 0.65 |
| Md | Tip ventral | Zn | 60 | 1.23 | 0.66 |
| Mx | Inner edge dorsal | Ae | 132 | 4.02 | 1.19 |
| Mx | Inner edge ventral | Ae | 132 | 4.98 | 1.54 |
| Mx | Outer edge dorsal | Ae | 132 | 4.57 | 2.22 |
| Mx | Outer edge ventral | Ae | 132 | 4.60 | 1.09 |
| Mx | Tip dorsal | Ae | 60 | 7.74 | 3.69 |
| Mx | Tip ventral | Ae | 60 | 5.86 | 2.08 |
| Mx | Inner edge dorsal | Ca | 132 | 0.18 | 0.28 |
| Mx | Inner edge ventral | Ca | 132 | 0.39 | 0.44 |
| Mx | Outer edge dorsal | Ca | 132 | 0.30 | 0.58 |
| Mx | Outer edge ventral | Ca | 132 | 0.30 | 0.34 |
| Mx | Tip dorsal | Ca | 60 | 0.96 | 0.93 |
| Mx | Tip ventral | Ca | 60 | 0.60 | 0.62 |
| Mx | Inner edge dorsal | Cl | 132 | 0.09 | 0.04 |
| Mx | Inner edge ventral | Cl | 132 | 0.07 | 0.04 |
| Mx | Outer edge dorsal | Cl | 132 | 0.16 | 0.08 |
| Mx | Outer edge ventral | Cl | 132 | 0.13 | 0.06 |
| Mx | Tip dorsal | Cl | 60 | 0.26 | 0.17 |
| Mx | Tip ventral | Cl | 60 | 0.21 | 0.14 |
| Mx | Inner edge dorsal | Cu | 132 | 0.23 | 0.12 |
| Mx | Inner edge ventral | Cu | 132 | 0.34 | 0.16 |
| Mx | Outer edge dorsal | Cu | 132 | 0.27 | 0.26 |
| Mx | Outer edge ventral | Cu | 132 | 0.31 | 0.11 |
| Mx | Tip dorsal | Cu | 60 | 0.59 | 0.49 |
| Mx | Tip ventral | Cu | 60 | 0.41 | 0.21 |
| Mx | Inner edge dorsal | E | 132 | 6.41 | 1.46 |
| Mx | Inner edge ventral | E | 132 | 9.22 | 1.31 |
| Mx | Outer edge dorsal | E | 132 | 6.31 | 1.79 |
| Mx | Outer edge ventral | E | 132 | 8.61 | 1.34 |
| Mx | Tip dorsal | E | 60 | 8.48 | 1.41 |
| Mx | Tip ventral | E | 60 | 9.86 | 1.56 |
| Mx | Inner edge dorsal | F | 132 | 1.25 | 0.15 |
| Mx | Inner edge ventral | F | 132 | 1.09 | 0.20 |
| Mx | Outer edge dorsal | F | 132 | 1.19 | 0.18 |
| Mx | Outer edge ventral | F | 132 | 1.05 | 0.21 |
| Mx | Tip dorsal | F | 60 | 0.89 | 0.49 |
| Mx | Tip ventral | F | 60 | 0.76 | 0.43 |
| Mx | Inner edge dorsal | Fe | 132 | 0.16 | 0.05 |
| Mx | Inner edge ventral | Fe | 132 | 0.21 | 0.10 |
| Mx | Outer edge dorsal | Fe | 132 | 0.17 | 0.15 |
| Mx | Outer edge ventral | Fe | 132 | 0.19 | 0.04 |
| Mx | Tip dorsal | Fe | 60 | 0.35 | 0.36 |
| Mx | Tip ventral | Fe | 60 | 0.24 | 0.12 |
| Mx | Inner edge dorsal | H | 132 | 0.65 | 0.12 |
| Mx | Inner edge ventral | H | 132 | 0.94 | 0.14 |
| Mx | Outer edge dorsal | H | 132 | 0.62 | 0.18 |
| Mx | Outer edge ventral | H | 132 | 0.88 | 0.14 |
| Mx | Tip dorsal | H | 60 | 0.80 | 0.11 |
| Mx | Tip ventral | H | 60 | 1.01 | 0.16 |
| Mx | Inner edge dorsal | K | 132 | 0.10 | 0.07 |
| Mx | Inner edge ventral | K | 132 | 0.09 | 0.06 |
| Mx | Outer edge dorsal | K | 132 | 0.15 | 0.08 |
| Mx | Outer edge ventral | K | 132 | 0.13 | 0.07 |
| Mx | Tip dorsal | K | 60 | 0.48 | 0.42 |
| Mx | Tip ventral | K | 60 | 0.43 | 0.42 |
| Mx | Inner edge dorsal | Mg | 132 | 0.28 | 0.13 |
| Mx | Inner edge ventral | Mg | 132 | 0.38 | 0.04 |
| Mx | Outer edge dorsal | Mg | 132 | 0.26 | 0.16 |
| Mx | Outer edge ventral | Mg | 132 | 0.37 | 0.04 |
| Mx | Tip dorsal | Mg | 60 | 0.41 | 0.07 |
| Mx | Tip ventral | Mg | 60 | 0.40 | 0.05 |
| Mx | Inner edge dorsal | Mn | 132 | 0.31 | 0.16 |
| Mx | Inner edge ventral | Mn | 132 | 0.46 | 0.25 |
| Mx | Outer edge dorsal | Mn | 132 | 0.37 | 0.37 |
| Mx | Outer edge ventral | Mn | 132 | 0.41 | 0.18 |
| Mx | Tip dorsal | Mn | 60 | 0.80 | 0.64 |
| Mx | Tip ventral | Mn | 60 | 0.56 | 0.35 |
| Mx | Inner edge dorsal | Na | 132 | 0.00 | 0.00 |
| Mx | Inner edge ventral | Na | 132 | 0.00 | 0.00 |
| Mx | Outer edge dorsal | Na | 132 | 0.00 | 0.00 |
| Mx | Outer edge ventral | Na | 132 | 0.00 | 0.00 |
| Mx | Tip dorsal | Na | 60 | 0.04 | 0.14 |
| Mx | Tip ventral | Na | 60 | 0.03 | 0.11 |
| Mx | Inner edge dorsal | P+Pt | 132 | 0.50 | 0.09 |
| Mx | Inner edge ventral | P+Pt | 132 | 0.71 | 0.14 |
| Mx | Outer edge dorsal | P+Pt | 132 | 0.72 | 0.06 |
| Mx | Outer edge ventral | P+Pt | 132 | 0.63 | 0.16 |
| Mx | Tip dorsal | P+Pt | 60 | 0.91 | 0.08 |
| Mx | Tip ventral | P+Pt | 60 | 0.77 | 0.16 |
| Mx | Inner edge dorsal | S | 132 | 0.12 | 0.05 |
| Mx | Inner edge ventral | S | 132 | 0.17 | 0.06 |
| Mx | Outer edge dorsal | S | 132 | 0.13 | 0.09 |
| Mx | Outer edge ventral | S | 132 | 0.15 | 0.04 |
| Mx | Tip dorsal | S | 60 | 0.25 | 0.14 |
| Mx | Tip ventral | S | 60 | 0.20 | 0.08 |
| Mx | Inner edge dorsal | Si | 132 | 0.24 | 0.14 |
| Mx | Inner edge ventral | Si | 132 | 0.40 | 0.24 |
| Mx | Outer edge dorsal | Si | 132 | 0.27 | 0.26 |
| Mx | Outer edge ventral | Si | 132 | 0.33 | 0.18 |
| Mx | Tip dorsal | Si | 60 | 0.62 | 0.45 |
| Mx | Tip ventral | Si | 60 | 0.51 | 0.31 |
| Mx | Inner edge dorsal | Zn | 132 | 0.55 | 0.29 |
| Mx | Inner edge ventral | Zn | 132 | 0.66 | 0.21 |
| Mx | Outer edge dorsal | Zn | 132 | 0.58 | 0.47 |
| Mx | Outer edge ventral | Zn | 132 | 0.60 | 0.12 |
| Mx | Tip dorsal | Zn | 60 | 1.18 | 0.69 |
| Mx | Tip ventral | Zn | 60 | 0.72 | 0.21 |

Supplementary Table 2. Results from nanoindentation (hardness H and Young’s modulus E, both in GPa) for each tested locality are given (see Figure 4 for localities). Abbreviations: Md, mandible; Mx, maxilla; N, quantity of measurements; SD, standard deviation.

| Mouthpart | Region |  | Locality | H mean | H SD | E mean | E SD |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Md | Dorsal | Outer edge | a | 0.73 | 0.06 | 7.80 | 0.40 |
| Md | Dorsal | Outer edge | b | 0.69 | 0.15 | 7.69 | 0.64 |
| Md | Dorsal | Outer edge | c | 0.54 | 0.18 | 7.11 | 0.71 |
| Md | Dorsal | Outer edge | d | 0.62 | 0.13 | 7.31 | 0.70 |
| Md | Dorsal | Outer edge | e | 0.58 | 0.14 | 7.13 | 0.44 |
| Md | Dorsal | Outer edge | f | 0.57 | 0.20 | 7.13 | 0.61 |
| Md | Dorsal | Outer edge | g | 0.63 | 0.20 | 7.42 | 0.64 |
| Md | Dorsal | Outer edge | h | 0.66 | 0.14 | 7.51 | 0.67 |
| Md | Dorsal | Outer edge | i | 0.75 | 0.06 | 7.87 | 0.49 |
| Md | Dorsal | Outer edge | j | 0.79 | 0.06 | 8.25 | 0.54 |
| Md | Dorsal | Outer edge | k | 0.71 | 0.14 | 7.81 | 0.89 |
| Md | Dorsal | Outer edge | l | 0.74 | 0.06 | 7.85 | 0.42 |
| Md | Dorsal | Outer edge | m | 0.80 | 0.07 | 8.32 | 0.55 |
| Md | Dorsal | Outer edge | n | 0.84 | 0.05 | 8.69 | 0.49 |
| Md | Dorsal | Outer edge | o | 0.81 | 0.08 | 8.44 | 0.70 |
| Md | Dorsal | Outer edge | p | 0.82 | 0.10 | 8.56 | 0.96 |
| Md | Dorsal | Outer edge | q | 0.90 | 0.09 | 9.28 | 0.88 |
| Md | Dorsal | Outer edge | r | 0.91 | 0.08 | 9.42 | 0.79 |
| Md | Dorsal | Outer edge | s | 0.91 | 0.07 | 9.42 | 0.81 |
| Md | Dorsal | Outer edge | t | 0.92 | 0.07 | 9.45 | 0.74 |
| Md | Dorsal | Outer edge | u | 0.92 | 0.10 | 9.66 | 1.20 |
| Md | Dorsal | Outer edge | v | 0.89 | 0.10 | 9.33 | 1.14 |
| Md | Dorsal | Central region | a | 0.72 | 0.08 | 7.79 | 0.40 |
| Md | Dorsal | Central region | b | 0.73 | 0.07 | 7.79 | 0.46 |
| Md | Dorsal | Central region | c | 0.41 | 0.12 | 6.59 | 0.27 |
| Md | Dorsal | Central region | d | 0.43 | 0.12 | 6.68 | 0.32 |
| Md | Dorsal | Central region | e | 0.58 | 0.11 | 7.10 | 0.37 |
| Md | Dorsal | Central region | f | 0.60 | 0.12 | 7.21 | 0.45 |
| Md | Dorsal | Central region | g | 0.68 | 0.08 | 7.46 | 0.38 |
| Md | Dorsal | Central region | h | 0.69 | 0.07 | 7.55 | 0.33 |
| Md | Dorsal | Central region | i | 0.69 | 0.09 | 7.56 | 0.44 |
| Md | Dorsal | Central region | j | 0.73 | 0.08 | 7.81 | 0.48 |
| Md | Dorsal | Central region | k | 0.73 | 0.08 | 7.81 | 0.54 |
| Md | Dorsal | Central region | l | 0.74 | 0.03 | 7.82 | 0.27 |
| Md | Dorsal | Central region | m | 0.76 | 0.07 | 8.03 | 0.54 |
| Md | Dorsal | Central region | n | 0.78 | 0.05 | 8.16 | 0.40 |
| Md | Dorsal | Central region | o | 0.75 | 0.05 | 7.93 | 0.44 |
| Md | Dorsal | Central region | p | 0.81 | 0.06 | 8.40 | 0.50 |
| Md | Dorsal | Central region | q | 0.87 | 0.06 | 8.97 | 0.58 |
| Md | Dorsal | Central region | r | 0.91 | 0.05 | 9.39 | 0.54 |
| Md | Dorsal | Central region | s | 0.94 | 0.04 | 9.69 | 0.44 |
| Md | Dorsal | Central region | t | 0.92 | 0.05 | 9.56 | 0.61 |
| Md | Dorsal | Central region | u | 0.95 | 0.04 | 9.85 | 0.50 |
| Md | Dorsal | Central region | v | 0.99 | 0.03 | 10.28 | 0.43 |
| Md | Dorsal | Inner edge | a | 0.89 | 0.07 | 9.14 | 0.65 |
| Md | Dorsal | Inner edge | b | 0.90 | 0.07 | 9.29 | 0.76 |
| Md | Dorsal | Inner edge | c | 0.86 | 0.05 | 8.86 | 0.45 |
| Md | Dorsal | Inner edge | d | 0.81 | 0.05 | 8.40 | 0.41 |
| Md | Dorsal | Inner edge | e | 0.83 | 0.06 | 8.65 | 0.60 |
| Md | Dorsal | Inner edge | f | 0.84 | 0.07 | 8.72 | 0.62 |
| Md | Dorsal | Inner edge | g | 0.87 | 0.08 | 9.02 | 0.81 |
| Md | Dorsal | Inner edge | h | 0.94 | 0.04 | 9.72 | 0.48 |
| Md | Dorsal | Inner edge | i | 0.89 | 0.05 | 9.15 | 0.46 |
| Md | Dorsal | Inner edge | j | 0.91 | 0.07 | 9.37 | 0.76 |
| Md | Dorsal | Inner edge | k | 0.90 | 0.08 | 9.35 | 0.88 |
| Md | Dorsal | Inner edge | l | 0.91 | 0.07 | 9.38 | 0.70 |
| Md | Dorsal | Inner edge | m | 0.95 | 0.04 | 9.81 | 0.54 |
| Md | Dorsal | Inner edge | n | 0.95 | 0.06 | 9.96 | 0.82 |
| Md | Dorsal | Inner edge | o | 0.95 | 0.04 | 9.78 | 0.52 |
| Md | Dorsal | Inner edge | p | 0.98 | 0.04 | 10.30 | 0.67 |
| Md | Dorsal | Inner edge | q | 1.08 | 0.05 | 11.66 | 0.67 |
| Md | Dorsal | Inner edge | r | 1.07 | 0.04 | 11.59 | 0.37 |
| Md | Dorsal | Inner edge | s | 1.09 | 0.07 | 11.95 | 1.04 |
| Md | Dorsal | Inner edge | t | 1.06 | 0.04 | 11.43 | 0.52 |
| Md | Dorsal | Inner edge | u | 1.09 | 0.05 | 11.92 | 0.69 |
| Md | Dorsal | Inner edge | v | 1.13 | 0.06 | 12.55 | 0.96 |
| Md | Dorsal | Tooth I | Basis | 1.05 | 0.06 | 11.17 | 0.79 |
| Md | Dorsal | Tooth I | Stylus | 1.16 | 0.06 | 13.06 | 1.15 |
| Md | Dorsal | Tooth I | Tip | 1.25 | 0.07 | 14.97 | 1.16 |
| Md | Dorsal | Tooth II | Basis | 0.98 | 0.05 | 10.27 | 0.79 |
| Md | Dorsal | Tooth II | Stylus | 1.05 | 0.04 | 11.23 | 0.51 |
| Md | Dorsal | Tooth II | Tip | 1.18 | 0.04 | 13.52 | 1.02 |
| Md | Dorsal | Tooth III | Basis | 0.96 | 0.09 | 9.97 | 1.11 |
| Md | Dorsal | Tooth III | Stylus | 1.03 | 0.14 | 11.13 | 2.13 |
| Md | Dorsal | Tooth III | Tip | 1.23 | 0.04 | 14.61 | 1.09 |
| Md | Dorsal | Tip | a | 1.28 | 0.06 | 15.97 | 0.61 |
| Md | Dorsal | Tip | b | 1.31 | 0.08 | 15.93 | 1.28 |
| Md | Dorsal | Tip | c | 1.29 | 0.10 | 15.68 | 1.63 |
| Md | Dorsal | Tip | d | 1.33 | 0.12 | 16.50 | 1.51 |
| Md | Dorsal | Tip | e | 1.39 | 0.13 | 17.01 | 1.86 |
| Md | Dorsal | Tip | f | 1.32 | 0.13 | 16.27 | 1.75 |
| Md | Dorsal | Tip | g | 1.32 | 0.16 | 16.16 | 2.52 |
| Md | Dorsal | Tip | h | 1.41 | 0.11 | 17.45 | 1.51 |
| Md | Dorsal | Tip | i | 1.43 | 0.12 | 17.96 | 1.78 |
| Md | Dorsal | Tip | j | 1.57 | 0.22 | 18.87 | 1.46 |
| Md | Ventral | Outer edge | a | 0.50 | 0.08 | 5.04 | 0.39 |
| Md | Ventral | Outer edge | b | 0.55 | 0.06 | 5.32 | 0.38 |
| Md | Ventral | Outer edge | c | 0.54 | 0.10 | 5.34 | 0.58 |
| Md | Ventral | Outer edge | d | 0.48 | 0.10 | 4.95 | 0.47 |
| Md | Ventral | Outer edge | e | 0.48 | 0.08 | 4.91 | 0.36 |
| Md | Ventral | Outer edge | f | 0.52 | 0.07 | 5.15 | 0.37 |
| Md | Ventral | Outer edge | g | 0.54 | 0.07 | 5.26 | 0.44 |
| Md | Ventral | Outer edge | h | 0.55 | 0.06 | 5.35 | 0.48 |
| Md | Ventral | Outer edge | i | 0.55 | 0.04 | 5.29 | 0.29 |
| Md | Ventral | Outer edge | j | 0.58 | 0.03 | 5.60 | 0.27 |
| Md | Ventral | Outer edge | k | 0.60 | 0.04 | 5.69 | 0.31 |
| Md | Ventral | Outer edge | l | 0.57 | 0.07 | 5.52 | 0.53 |
| Md | Ventral | Outer edge | m | 0.58 | 0.06 | 5.56 | 0.55 |
| Md | Ventral | Outer edge | n | 0.56 | 0.08 | 5.49 | 0.61 |
| Md | Ventral | Outer edge | o | 0.57 | 0.06 | 5.51 | 0.51 |
| Md | Ventral | Outer edge | p | 0.62 | 0.08 | 6.01 | 0.81 |
| Md | Ventral | Outer edge | q | 0.61 | 0.06 | 5.92 | 0.56 |
| Md | Ventral | Outer edge | r | 0.64 | 0.05 | 6.13 | 0.56 |
| Md | Ventral | Outer edge | s | 0.61 | 0.06 | 5.90 | 0.56 |
| Md | Ventral | Outer edge | t | 0.65 | 0.06 | 6.36 | 0.67 |
| Md | Ventral | Outer edge | u | 0.65 | 0.06 | 6.25 | 0.67 |
| Md | Ventral | Outer edge | v | 0.59 | 0.07 | 5.75 | 0.60 |
| Md | Ventral | Central region | a | 0.28 | 0.07 | 4.18 | 0.28 |
| Md | Ventral | Central region | b | 0.30 | 0.09 | 4.24 | 0.28 |
| Md | Ventral | Central region | c | 0.38 | 0.10 | 4.51 | 0.33 |
| Md | Ventral | Central region | d | 0.37 | 0.13 | 4.50 | 0.42 |
| Md | Ventral | Central region | e | 0.40 | 0.11 | 4.60 | 0.40 |
| Md | Ventral | Central region | f | 0.33 | 0.09 | 4.36 | 0.28 |
| Md | Ventral | Central region | g | 0.38 | 0.08 | 4.53 | 0.26 |
| Md | Ventral | Central region | h | 0.43 | 0.10 | 4.72 | 0.32 |
| Md | Ventral | Central region | i | 0.40 | 0.11 | 4.66 | 0.43 |
| Md | Ventral | Central region | j | 0.41 | 0.11 | 4.67 | 0.45 |
| Md | Ventral | Central region | k | 0.42 | 0.10 | 4.73 | 0.40 |
| Md | Ventral | Central region | l | 0.47 | 0.08 | 4.87 | 0.33 |
| Md | Ventral | Central region | m | 0.40 | 0.11 | 4.64 | 0.38 |
| Md | Ventral | Central region | n | 0.44 | 0.09 | 4.82 | 0.40 |
| Md | Ventral | Central region | o | 0.52 | 0.04 | 5.10 | 0.24 |
| Md | Ventral | Central region | p | 0.46 | 0.09 | 4.88 | 0.41 |
| Md | Ventral | Central region | q | 0.52 | 0.06 | 5.13 | 0.33 |
| Md | Ventral | Central region | r | 0.59 | 0.03 | 5.62 | 0.23 |
| Md | Ventral | Central region | s | 0.58 | 0.05 | 5.61 | 0.39 |
| Md | Ventral | Central region | t | 0.59 | 0.05 | 5.67 | 0.41 |
| Md | Ventral | Central region | u | 0.59 | 0.05 | 5.69 | 0.42 |
| Md | Ventral | Central region | v | 0.61 | 0.04 | 5.86 | 0.39 |
| Md | Ventral | Inner edge | a | 0.60 | 0.04 | 5.73 | 0.46 |
| Md | Ventral | Inner edge | b | 0.60 | 0.03 | 5.76 | 0.34 |
| Md | Ventral | Inner edge | c | 0.57 | 0.05 | 5.52 | 0.38 |
| Md | Ventral | Inner edge | d | 0.60 | 0.05 | 5.78 | 0.40 |
| Md | Ventral | Inner edge | e | 0.62 | 0.03 | 5.93 | 0.38 |
| Md | Ventral | Inner edge | f | 0.64 | 0.06 | 6.16 | 0.60 |
| Md | Ventral | Inner edge | g | 0.64 | 0.06 | 6.21 | 0.65 |
| Md | Ventral | Inner edge | h | 0.63 | 0.03 | 6.04 | 0.28 |
| Md | Ventral | Inner edge | i | 0.64 | 0.03 | 6.17 | 0.34 |
| Md | Ventral | Inner edge | j | 0.62 | 0.06 | 6.00 | 0.59 |
| Md | Ventral | Inner edge | k | 0.67 | 0.05 | 6.48 | 0.58 |
| Md | Ventral | Inner edge | l | 0.67 | 0.04 | 6.51 | 0.49 |
| Md | Ventral | Inner edge | m | 0.64 | 0.04 | 6.15 | 0.46 |
| Md | Ventral | Inner edge | n | 0.65 | 0.04 | 6.29 | 0.47 |
| Md | Ventral | Inner edge | o | 0.67 | 0.04 | 6.54 | 0.48 |
| Md | Ventral | Inner edge | p | 0.65 | 0.04 | 6.31 | 0.47 |
| Md | Ventral | Inner edge | q | 0.73 | 0.05 | 7.20 | 0.55 |
| Md | Ventral | Inner edge | r | 0.76 | 0.05 | 7.49 | 0.53 |
| Md | Ventral | Inner edge | s | 0.76 | 0.06 | 7.45 | 0.62 |
| Md | Ventral | Inner edge | t | 0.76 | 0.09 | 7.48 | 0.82 |
| Md | Ventral | Inner edge | u | 0.72 | 0.04 | 7.02 | 0.45 |
| Md | Ventral | Inner edge | v | 0.74 | 0.05 | 7.27 | 0.47 |
| Md | Ventral | Tooth I | Basis | 0.95 | 0.05 | 9.34 | 0.58 |
| Md | Ventral | Tooth I | Stylus | 1.15 | 0.12 | 11.21 | 1.05 |
| Md | Ventral | Tooth I | Tip | 1.27 | 0.14 | 12.37 | 1.15 |
| Md | Ventral | Tooth II | Basis | 0.93 | 0.15 | 9.12 | 1.48 |
| Md | Ventral | Tooth II | Stylus | 0.95 | 0.17 | 9.29 | 1.59 |
| Md | Ventral | Tooth II | Tip | 1.21 | 0.12 | 11.74 | 0.91 |
| Md | Ventral | Tooth III | Basis | 0.86 | 0.12 | 8.44 | 1.23 |
| Md | Ventral | Tooth III | Stylus | 1.02 | 0.19 | 9.91 | 1.68 |
| Md | Ventral | Tooth III | Tip | 1.33 | 0.22 | 12.73 | 1.64 |
| Md | Ventral | Tip | a | 1.18 | 0.12 | 11.60 | 1.01 |
| Md | Ventral | Tip | b | 1.27 | 0.15 | 12.39 | 1.28 |
| Md | Ventral | Tip | c | 1.13 | 0.14 | 11.03 | 1.26 |
| Md | Ventral | Tip | d | 1.22 | 0.17 | 11.89 | 1.35 |
| Md | Ventral | Tip | e | 1.21 | 0.12 | 11.84 | 1.04 |
| Md | Ventral | Tip | f | 1.24 | 0.17 | 12.12 | 1.52 |
| Md | Ventral | Tip | g | 1.23 | 0.25 | 11.81 | 2.23 |
| Md | Ventral | Tip | h | 1.23 | 0.07 | 12.00 | 0.53 |
| Md | Ventral | Tip | i | 1.25 | 0.27 | 12.06 | 2.34 |
| Md | Ventral | Tip | j | 1.60 | 0.12 | 14.95 | 0.87 |
| Mx | Dorsal | Outer edge | a | 0.79 | 0.09 | 7.74 | 0.90 |
| Mx | Dorsal | Outer edge | b | 0.82 | 0.09 | 8.11 | 0.87 |
| Mx | Dorsal | Outer edge | c | 0.90 | 0.07 | 8.85 | 0.75 |
| Mx | Dorsal | Outer edge | d | 0.86 | 0.10 | 8.39 | 0.91 |
| Mx | Dorsal | Outer edge | e | 0.87 | 0.08 | 8.56 | 0.75 |
| Mx | Dorsal | Outer edge | f | 0.86 | 0.06 | 8.32 | 0.56 |
| Mx | Dorsal | Outer edge | g | 0.91 | 0.12 | 8.94 | 1.22 |
| Mx | Dorsal | Outer edge | h | 0.90 | 0.08 | 8.79 | 0.77 |
| Mx | Dorsal | Outer edge | i | 0.91 | 0.09 | 8.92 | 0.83 |
| Mx | Dorsal | Outer edge | j | 0.93 | 0.08 | 9.09 | 0.77 |
| Mx | Dorsal | Outer edge | k | 0.95 | 0.09 | 9.35 | 0.96 |
| Mx | Dorsal | Outer edge | l | 0.95 | 0.09 | 9.25 | 0.96 |
| Mx | Dorsal | Outer edge | m | 0.89 | 0.14 | 8.78 | 1.36 |
| Mx | Dorsal | Outer edge | n | 0.92 | 0.10 | 8.94 | 0.99 |
| Mx | Dorsal | Outer edge | o | 0.95 | 0.11 | 9.28 | 1.14 |
| Mx | Dorsal | Outer edge | p | 0.95 | 0.08 | 9.35 | 0.76 |
| Mx | Dorsal | Outer edge | q | 0.99 | 0.08 | 9.76 | 0.85 |
| Mx | Dorsal | Outer edge | r | 1.05 | 0.14 | 10.35 | 1.41 |
| Mx | Dorsal | Outer edge | s | 0.99 | 0.11 | 9.82 | 1.08 |
| Mx | Dorsal | Outer edge | t | 1.10 | 0.15 | 10.76 | 1.44 |
| Mx | Dorsal | Outer edge | u | 1.13 | 0.26 | 10.96 | 2.32 |
| Mx | Dorsal | Outer edge | v | 1.07 | 0.16 | 10.48 | 1.43 |
| Mx | Dorsal | Inner edge | a | 0.77 | 0.05 | 7.53 | 0.46 |
| Mx | Dorsal | Inner edge | b | 0.76 | 0.05 | 7.50 | 0.50 |
| Mx | Dorsal | Inner edge | c | 0.80 | 0.11 | 7.89 | 1.10 |
| Mx | Dorsal | Inner edge | d | 0.81 | 0.13 | 7.93 | 1.31 |
| Mx | Dorsal | Inner edge | e | 0.78 | 0.12 | 7.61 | 1.21 |
| Mx | Dorsal | Inner edge | f | 0.77 | 0.10 | 7.56 | 0.88 |
| Mx | Dorsal | Inner edge | g | 0.81 | 0.13 | 8.03 | 1.24 |
| Mx | Dorsal | Inner edge | h | 0.83 | 0.08 | 8.15 | 0.82 |
| Mx | Dorsal | Inner edge | i | 0.83 | 0.06 | 8.19 | 0.58 |
| Mx | Dorsal | Inner edge | j | 0.82 | 0.13 | 8.06 | 1.23 |
| Mx | Dorsal | Inner edge | k | 0.86 | 0.12 | 8.46 | 1.19 |
| Mx | Dorsal | Inner edge | l | 0.88 | 0.07 | 8.57 | 0.64 |
| Mx | Dorsal | Inner edge | m | 0.85 | 0.10 | 8.30 | 0.99 |
| Mx | Dorsal | Inner edge | n | 0.87 | 0.04 | 8.48 | 0.36 |
| Mx | Dorsal | Inner edge | o | 0.92 | 0.07 | 8.96 | 0.69 |
| Mx | Dorsal | Inner edge | p | 0.90 | 0.10 | 8.81 | 1.05 |
| Mx | Dorsal | Inner edge | q | 0.93 | 0.14 | 8.99 | 1.40 |
| Mx | Dorsal | Inner edge | r | 1.06 | 0.13 | 10.36 | 1.30 |
| Mx | Dorsal | Inner edge | s | 1.01 | 0.05 | 9.98 | 0.54 |
| Mx | Dorsal | Inner edge | t | 0.99 | 0.13 | 9.71 | 1.33 |
| Mx | Dorsal | Inner edge | u | 1.06 | 0.17 | 10.34 | 1.74 |
| Mx | Dorsal | Inner edge | v | 1.04 | 0.16 | 10.20 | 1.51 |
| Mx | Dorsal | Tip | a | 1.04 | 0.13 | 10.19 | 1.29 |
| Mx | Dorsal | Tip | b | 1.00 | 0.09 | 9.87 | 0.98 |
| Mx | Dorsal | Tip | c | 0.98 | 0.14 | 9.62 | 1.41 |
| Mx | Dorsal | Tip | d | 1.03 | 0.06 | 9.73 | 0.58 |
| Mx | Dorsal | Tip | e | 1.04 | 0.14 | 10.18 | 1.38 |
| Mx | Dorsal | Tip | f | 1.13 | 0.13 | 11.04 | 1.08 |
| Mx | Dorsal | Tip | g | 1.16 | 0.21 | 11.32 | 1.99 |
| Mx | Dorsal | Tip | h | 0.95 | 0.22 | 9.31 | 2.19 |
| Mx | Dorsal | Tip | i | 0.96 | 0.12 | 9.50 | 1.22 |
| Mx | Dorsal | Tip | j | 0.82 | 0.10 | 7.99 | 1.02 |
| Mx | Ventral | Outer edge | a | 0.69 | 0.03 | 7.01 | 0.60 |
| Mx | Ventral | Outer edge | b | 0.64 | 0.03 | 5.80 | 0.61 |
| Mx | Ventral | Outer edge | c | 0.51 | 0.10 | 4.57 | 0.37 |
| Mx | Ventral | Outer edge | d | 0.46 | 0.13 | 4.39 | 0.29 |
| Mx | Ventral | Outer edge | e | 0.47 | 0.15 | 4.47 | 0.37 |
| Mx | Ventral | Outer edge | f | 0.45 | 0.13 | 4.44 | 0.40 |
| Mx | Ventral | Outer edge | g | 0.57 | 0.08 | 4.97 | 0.39 |
| Mx | Ventral | Outer edge | h | 0.57 | 0.06 | 4.91 | 0.43 |
| Mx | Ventral | Outer edge | i | 0.65 | 0.03 | 5.95 | 0.55 |
| Mx | Ventral | Outer edge | j | 0.67 | 0.04 | 6.47 | 0.81 |
| Mx | Ventral | Outer edge | k | 0.66 | 0.04 | 6.20 | 0.80 |
| Mx | Ventral | Outer edge | l | 0.66 | 0.03 | 6.38 | 0.74 |
| Mx | Ventral | Outer edge | m | 0.67 | 0.04 | 6.44 | 0.83 |
| Mx | Ventral | Outer edge | n | 0.68 | 0.04 | 6.79 | 0.86 |
| Mx | Ventral | Outer edge | o | 0.69 | 0.05 | 6.81 | 0.92 |
| Mx | Ventral | Outer edge | p | 0.72 | 0.06 | 7.32 | 1.08 |
| Mx | Ventral | Outer edge | q | 0.72 | 0.05 | 7.49 | 0.87 |
| Mx | Ventral | Outer edge | r | 0.76 | 0.07 | 8.17 | 0.82 |
| Mx | Ventral | Outer edge | s | 0.76 | 0.06 | 8.27 | 0.71 |
| Mx | Ventral | Outer edge | t | 0.75 | 0.04 | 8.02 | 0.68 |
| Mx | Ventral | Outer edge | u | 0.73 | 0.03 | 7.80 | 0.51 |
| Mx | Ventral | Outer edge | v | 0.77 | 0.07 | 8.31 | 0.90 |
| Mx | Ventral | Inner edge | a | 0.67 | 0.01 | 6.42 | 0.36 |
| Mx | Ventral | Inner edge | b | 0.62 | 0.05 | 5.54 | 0.67 |
| Mx | Ventral | Inner edge | c | 0.43 | 0.15 | 4.32 | 0.30 |
| Mx | Ventral | Inner edge | d | 0.47 | 0.08 | 4.46 | 0.33 |
| Mx | Ventral | Inner edge | e | 0.43 | 0.15 | 4.35 | 0.44 |
| Mx | Ventral | Inner edge | f | 0.31 | 0.16 | 4.09 | 0.69 |
| Mx | Ventral | Inner edge | g | 0.34 | 0.16 | 4.08 | 0.44 |
| Mx | Ventral | Inner edge | h | 0.31 | 0.16 | 4.09 | 0.46 |
| Mx | Ventral | Inner edge | i | 0.63 | 0.02 | 5.65 | 0.43 |
| Mx | Ventral | Inner edge | j | 0.64 | 0.03 | 5.94 | 0.62 |
| Mx | Ventral | Inner edge | k | 0.64 | 0.03 | 5.95 | 0.73 |
| Mx | Ventral | Inner edge | l | 0.65 | 0.03 | 6.11 | 0.67 |
| Mx | Ventral | Inner edge | m | 0.64 | 0.03 | 5.95 | 0.69 |
| Mx | Ventral | Inner edge | n | 0.67 | 0.03 | 6.59 | 0.63 |
| Mx | Ventral | Inner edge | o | 0.69 | 0.01 | 6.92 | 0.37 |
| Mx | Ventral | Inner edge | p | 0.69 | 0.04 | 6.97 | 0.83 |
| Mx | Ventral | Inner edge | q | 0.70 | 0.05 | 7.10 | 0.99 |
| Mx | Ventral | Inner edge | r | 0.81 | 0.05 | 8.85 | 0.50 |
| Mx | Ventral | Inner edge | s | 0.80 | 0.09 | 8.64 | 1.04 |
| Mx | Ventral | Inner edge | t | 0.82 | 0.05 | 9.03 | 0.43 |
| Mx | Ventral | Inner edge | u | 0.81 | 0.09 | 8.80 | 1.10 |
| Mx | Ventral | Inner edge | v | 0.83 | 0.11 | 8.92 | 1.25 |
| Mx | Ventral | Tip | a | 0.80 | 0.05 | 8.64 | 0.58 |
| Mx | Ventral | Tip | b | 0.81 | 0.06 | 8.76 | 0.75 |
| Mx | Ventral | Tip | c | 0.78 | 0.07 | 8.38 | 1.07 |
| Mx | Ventral | Tip | d | 0.80 | 0.08 | 8.75 | 1.00 |
| Mx | Ventral | Tip | e | 0.90 | 0.16 | 9.56 | 1.43 |
| Mx | Ventral | Tip | f | 0.90 | 0.14 | 9.55 | 1.08 |
| Mx | Ventral | Tip | g | 0.85 | 0.10 | 9.30 | 1.10 |
| Mx | Ventral | Tip | h | 0.83 | 0.08 | 9.05 | 0.93 |
| Mx | Ventral | Tip | i | 0.68 | 0.02 | 6.79 | 0.42 |
| Mx | Ventral | Tip | j | 0.65 | 0.03 | 6.06 | 0.63 |

Supplementary Table 3. Results from ANOVA and pairwise comparison by Tukey-Kramer method between the regions for the mechanical properties. Orange p-values = highly significant differences. red p-values = significant differences. black = no significant differences.

| Parameter | Region 1 | Region 2 | ANOVA |  |  | Tukey-Kramer |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  | F-value | df | p-value | p-value |
| H | Md Tip dorsal | Md Central region ventral | 225.4976 | 19 | <.0001* | <.0001* |
| H | Md Tip ventral | Md Central region ventral |  |  |  | <.0001* |
| H | Md Tip dorsal | Md Outer edge ventral |  |  |  | <.0001* |
| H | Md Tip dorsal | Mx Outer edge dorsal |  |  |  | <.0001* |
| H | Md Tip dorsal | Mx Inner edge dorsal |  |  |  | <.0001* |
| H | Md Tooth I dorsal | Md Central region ventral |  |  |  | <.0001* |
| H | Md Tip dorsal | Md Inner edge ventral |  |  |  | <.0001* |
| H | Md Tip ventral | Md Outer edge ventral |  |  |  | <.0001* |
| H | Md Tooth I ventral | Md Central region ventral |  |  |  | <.0001* |
| H | Md Tip ventral | Mx Outer edge dorsal |  |  |  | <.0001* |
| H | Md Tooth III ventral | Md Central region ventral |  |  |  | <.0001* |
| H | Md Tooth III dorsal | Md Central region ventral |  |  |  | <.0001* |
| H | Md Tooth II dorsal | Md Central region ventral |  |  |  | <.0001* |
| H | Md Tip dorsal | Md Central region dorsal |  |  |  | <.0001* |
| H | Md Tip dorsal | Md Outer edge dorsal |  |  |  | <.0001* |
| H | Md Tip ventral | Mx Inner edge dorsal |  |  |  | <.0001* |
| H | Md Tip ventral | Md Inner edge ventral |  |  |  | <.0001* |
| H | Md Tooth I dorsal | Md Outer edge ventral |  |  |  | <.0001* |
| H | Md Tooth II ventral | Md Central region ventral |  |  |  | <.0001* |
| H | Md Tip dorsal | Mx Tip dorsal |  |  |  | <.0001* |
| H | Mx Tip ventral | Md Central region ventral |  |  |  | <.0001* |
| H | Md Tooth I ventral | Md Outer edge ventral |  |  |  | <.0001* |
| H | Md Tooth I dorsal | Mx Outer edge dorsal |  |  |  | <.0001* |
| H | Md Tip ventral | Md Central region dorsal |  |  |  | <.0001* |
| H | Md Tooth I ventral | Mx Outer edge dorsal |  |  |  | <.0001* |
| H | Md Tooth III ventral | Md Outer edge ventral |  |  |  | <.0001* |
| H | Md Tooth I dorsal | Mx Inner edge dorsal |  |  |  | <.0001* |
| H | Md Inner edge dorsal | Md Central region ventral |  |  |  | <.0001* |
| H | Md Tooth III dorsal | Md Outer edge ventral |  |  |  | <.0001* |
| H | Md Tooth II dorsal | Md Outer edge ventral |  |  |  | <.0001* |
| H | Md Tip ventral | Md Outer edge dorsal |  |  |  | <.0001* |
| H | Mx Inner edge ventral | Md Central region ventral |  |  |  | <.0001* |
| H | Md Tooth I dorsal | Md Inner edge ventral |  |  |  | <.0001* |
| H | Md Tip dorsal | Mx Outer edge ventral |  |  |  | <.0001* |
| H | Md Tooth I ventral | Mx Inner edge dorsal |  |  |  | <.0001* |
| H | Md Tooth I ventral | Md Inner edge ventral |  |  |  | <.0001* |
| H | Md Tooth II ventral | Md Outer edge ventral |  |  |  | <.0001* |
| H | Md Tooth III ventral | Mx Outer edge dorsal |  |  |  | <.0001* |
| H | Md Tip ventral | Mx Tip dorsal |  |  |  | <.0001* |
| H | Md Tooth III dorsal | Mx Outer edge dorsal |  |  |  | <.0001* |
| H | Md Tooth II dorsal | Mx Outer edge dorsal |  |  |  | <.0001* |
| H | Mx Tip ventral | Md Outer edge ventral |  |  |  | <.0001* |
| H | Mx Outer edge ventral | Md Central region ventral |  |  |  | <.0001* |
| H | Md Tooth III ventral | Mx Inner edge dorsal |  |  |  | <.0001* |
| H | Md Tip dorsal | Mx Inner edge ventral |  |  |  | <.0001* |
| H | Md Tooth III dorsal | Mx Inner edge dorsal |  |  |  | <.0001* |
| H | Md Tooth II dorsal | Mx Inner edge dorsal |  |  |  | <.0001* |
| H | Md Tip dorsal | Md Inner edge dorsal |  |  |  | <.0001* |
| H | Md Tooth II ventral | Mx Outer edge dorsal |  |  |  | <.0001* |
| H | Md Tooth III ventral | Md Inner edge ventral |  |  |  | <.0001* |
| H | Md Tooth III dorsal | Md Inner edge ventral |  |  |  | <.0001* |
| H | Md Tooth I dorsal | Md Central region dorsal |  |  |  | <.0001* |
| H | Md Tooth II dorsal | Md Inner edge ventral |  |  |  | <.0001* |
| H | Md Tooth I dorsal | Md Outer edge dorsal |  |  |  | <.0001* |
| H | Mx Tip ventral | Mx Outer edge dorsal |  |  |  | <.0001* |
| H | Md Tooth II ventral | Mx Inner edge dorsal |  |  |  | <.0001* |
| H | Md Inner edge dorsal | Md Outer edge ventral |  |  |  | <.0001* |
| H | Md Tooth I ventral | Md Central region dorsal |  |  |  | <.0001* |
| H | Md Tip ventral | Mx Outer edge ventral |  |  |  | <.0001* |
| H | Mx Inner edge ventral | Md Outer edge ventral |  |  |  | <.0001* |
| H | Md Tooth II ventral | Md Inner edge ventral |  |  |  | <.0001* |
| H | Md Tooth I ventral | Md Outer edge dorsal |  |  |  | <.0001* |
| H | Md Tip dorsal | Mx Tip ventral |  |  |  | <.0001* |
| H | Mx Tip ventral | Mx Inner edge dorsal |  |  |  | <.0001* |
| H | Mx Tip dorsal | Md Central region ventral |  |  |  | <.0001* |
| H | Md Tooth I dorsal | Mx Tip dorsal |  |  |  | <.0001* |
| H | Mx Tip ventral | Md Inner edge ventral |  |  |  | <.0001* |
| H | Md Tip dorsal | Md Tooth II ventral |  |  |  | <.0001* |
| H | Md Inner edge dorsal | Mx Outer edge dorsal |  |  |  | <.0001* |
| H | Md Tooth III ventral | Md Central region dorsal |  |  |  | <.0001* |
| H | Md Tooth I ventral | Mx Tip dorsal |  |  |  | <.0001* |
| H | Md Tooth III dorsal | Md Central region dorsal |  |  |  | <.0001* |
| H | Md Tooth II dorsal | Md Central region dorsal |  |  |  | <.0001* |
| H | Mx Inner edge ventral | Mx Outer edge dorsal |  |  |  | <.0001* |
| H | Md Tooth III ventral | Md Outer edge dorsal |  |  |  | <.0001* |
| H | Md Tip ventral | Mx Inner edge ventral |  |  |  | <.0001* |
| H | Md Outer edge dorsal | Md Central region ventral |  |  |  | <.0001* |
| H | Md Tooth III dorsal | Md Outer edge dorsal |  |  |  | <.0001* |
| H | Md Tooth II dorsal | Md Outer edge dorsal |  |  |  | <.0001* |
| H | Mx Outer edge ventral | Md Outer edge ventral |  |  |  | <.0001* |
| H | Md Inner edge dorsal | Mx Inner edge dorsal |  |  |  | <.0001* |
| H | Md Tip ventral | Md Inner edge dorsal |  |  |  | <.0001* |
| H | Md Central region dorsal | Md Central region ventral |  |  |  | <.0001* |
| H | Md Tip dorsal | Md Tooth II dorsal |  |  |  | <.0001* |
| H | Md Tip dorsal | Md Tooth III dorsal |  |  |  | <.0001* |
| H | Mx Inner edge ventral | Mx Inner edge dorsal |  |  |  | <.0001* |
| H | Md Tip dorsal | Md Tooth III ventral |  |  |  | <.0001* |
| H | Md Inner edge dorsal | Md Inner edge ventral |  |  |  | <.0001* |
| H | Md Tooth II ventral | Md Central region dorsal |  |  |  | <.0001* |
| H | Mx Inner edge ventral | Md Inner edge ventral |  |  |  | <.0001* |
| H | Md Tooth I dorsal | Mx Outer edge ventral |  |  |  | <.0001* |
| H | Md Tooth III ventral | Mx Tip dorsal |  |  |  | <.0001* |
| H | Md Tooth II ventral | Md Outer edge dorsal |  |  |  | <.0001* |
| H | Md Tooth III dorsal | Mx Tip dorsal |  |  |  | <.0001* |
| H | Md Tooth II dorsal | Mx Tip dorsal |  |  |  | <.0001* |
| H | Mx Tip ventral | Md Central region dorsal |  |  |  | <.0001* |
| H | Mx Outer edge ventral | Mx Outer edge dorsal |  |  |  | <.0001* |
| H | Md Tooth I ventral | Mx Outer edge ventral |  |  |  | <.0001* |
| H | Md Tip ventral | Mx Tip ventral |  |  |  | <.0001* |
| H | Mx Tip ventral | Md Outer edge dorsal |  |  |  | <.0001* |
| H | Md Tip dorsal | Md Tooth I ventral |  |  |  | <.0001* |
| H | Mx Tip dorsal | Md Outer edge ventral |  |  |  | <.0001* |
| H | Mx Outer edge ventral | Mx Inner edge dorsal |  |  |  | <.0001* |
| H | Md Tooth II ventral | Mx Tip dorsal |  |  |  | <.0001* |
| H | Md Tip ventral | Md Tooth II ventral |  |  |  | <.0001* |
| H | Mx Outer edge ventral | Md Inner edge ventral |  |  |  | <.0001* |
| H | Md Inner edge ventral | Md Central region ventral |  |  |  | <.0001* |
| H | Md Tip dorsal | Md Tooth I dorsal |  |  |  | <.0001* |
| H | Md Tooth I dorsal | Mx Inner edge ventral |  |  |  | <.0001* |
| H | Mx Tip ventral | Mx Tip dorsal |  |  |  | <.0001* |
| H | Md Inner edge dorsal | Md Central region dorsal |  |  |  | <.0001* |
| H | Md Tooth I dorsal | Md Inner edge dorsal |  |  |  | <.0001* |
| H | Mx Inner edge dorsal | Md Central region ventral |  |  |  | <.0001* |
| H | Md Tooth III ventral | Mx Outer edge ventral |  |  |  | <.0001* |
| H | Mx Inner edge ventral | Md Central region dorsal |  |  |  | <.0001* |
| H | Md Tooth III dorsal | Mx Outer edge ventral |  |  |  | <.0001* |
| H | Md Tooth II dorsal | Mx Outer edge ventral |  |  |  | <.0001* |
| H | Md Outer edge dorsal | Md Outer edge ventral |  |  |  | <.0001* |
| H | Md Inner edge dorsal | Md Outer edge dorsal |  |  |  | <.0001* |
| H | Md Tooth I ventral | Mx Inner edge ventral |  |  |  | <.0001* |
| H | Md Tip ventral | Md Tooth II dorsal |  |  |  | 0.0002* |
| H | Md Tip ventral | Md Tooth III dorsal |  |  |  | 0.0002* |
| H | Mx Tip dorsal | Mx Outer edge dorsal |  |  |  | <.0001* |
| H | Mx Inner edge ventral | Md Outer edge dorsal |  |  |  | <.0001* |
| H | Md Tip ventral | Md Tooth III ventral |  |  |  | 0.0004* |
| H | Md Central region dorsal | Md Outer edge ventral |  |  |  | <.0001* |
| H | Md Tooth I ventral | Md Inner edge dorsal |  |  |  | 0.0001* |
| H | Mx Outer edge dorsal | Md Central region ventral |  |  |  | <.0001* |
| H | Mx Tip dorsal | Mx Inner edge dorsal |  |  |  | <.0001* |
| H | Md Tooth II ventral | Mx Outer edge ventral |  |  |  | 0.0024* |
| H | Md Inner edge dorsal | Mx Tip dorsal |  |  |  | <.0001* |
| H | Md Tooth I dorsal | Mx Tip ventral |  |  |  | 0.0139* |
| H | Md Outer edge dorsal | Mx Outer edge dorsal |  |  |  | <.0001* |
| H | Mx Inner edge ventral | Mx Tip dorsal |  |  |  | <.0001* |
| H | Mx Tip dorsal | Md Inner edge ventral |  |  |  | <.0001* |
| H | Md Tooth III ventral | Mx Inner edge ventral |  |  |  | 0.0193* |
| H | Mx Outer edge ventral | Md Central region dorsal |  |  |  | <.0001* |
| H | Md Tooth III dorsal | Mx Inner edge ventral |  |  |  | 0.0290* |
| H | Md Tooth II dorsal | Mx Inner edge ventral |  |  |  | 0.0307* |
| H | Mx Tip ventral | Mx Outer edge ventral |  |  |  | <.0001* |
| H | Md Tip ventral | Md Tooth I ventral |  |  |  | 0.0820 |
| H | Md Central region dorsal | Mx Outer edge dorsal |  |  |  | <.0001* |
| H | Md Tooth III ventral | Md Inner edge dorsal |  |  |  | 0.0550 |
| H | Md Tooth I dorsal | Md Tooth II ventral |  |  |  | 0.4738 |
| H | Md Outer edge ventral | Md Central region ventral |  |  |  | <.0001* |
| H | Md Tooth I ventral | Mx Tip ventral |  |  |  | 0.1465 |
| H | Md Tooth III dorsal | Md Inner edge dorsal |  |  |  | 0.0784 |
| H | Md Tooth II dorsal | Md Inner edge dorsal |  |  |  | 0.0824 |
| H | Mx Outer edge ventral | Md Outer edge dorsal |  |  |  | <.0001* |
| H | Md Tip dorsal | Md Tip ventral |  |  |  | 0.0018* |
| H | Md Outer edge dorsal | Mx Inner edge dorsal |  |  |  | <.0001* |
| H | Md Tip ventral | Md Tooth I dorsal |  |  |  | 0.4557 |
| H | Md Central region dorsal | Mx Inner edge dorsal |  |  |  | <.0001* |
| H | Md Outer edge dorsal | Md Inner edge ventral |  |  |  | <.0001* |
| H | Md Tooth I ventral | Md Tooth II ventral |  |  |  | 0.8794 |
| H | Md Inner edge ventral | Md Outer edge ventral |  |  |  | <.0001* |
| H | Md Tooth II ventral | Mx Inner edge ventral |  |  |  | 0.5299 |
| H | Md Tooth I dorsal | Md Tooth II dorsal |  |  |  | 0.9643 |
| H | Md Central region dorsal | Md Inner edge ventral |  |  |  | 0.0002* |
| H | Md Tooth I dorsal | Md Tooth III dorsal |  |  |  | 0.9666 |
| H | Md Tooth II ventral | Md Inner edge dorsal |  |  |  | 0.7599 |
| H | Mx Inner edge dorsal | Md Outer edge ventral |  |  |  | 0.0007* |
| H | Md Tooth I dorsal | Md Tooth III ventral |  |  |  | 0.9800 |
| H | Mx Outer edge ventral | Mx Tip dorsal |  |  |  | 0.0518 |
| H | Md Inner edge dorsal | Mx Outer edge ventral |  |  |  | 0.0036* |
| H | Md Tooth III ventral | Mx Tip ventral |  |  |  | 0.9597 |
| H | Mx Tip ventral | Mx Inner edge ventral |  |  |  | 0.2100 |
| H | Md Tooth III dorsal | Mx Tip ventral |  |  |  | 0.9782 |
| H | Md Tooth II dorsal | Mx Tip ventral |  |  |  | 0.9802 |
| H | Mx Inner edge ventral | Mx Outer edge ventral |  |  |  | 0.0382* |
| H | Md Tooth I ventral | Md Tooth II dorsal |  |  |  | 0.9997 |
| H | Md Tooth I ventral | Md Tooth III dorsal |  |  |  | 0.9998 |
| H | Mx Tip ventral | Md Inner edge dorsal |  |  |  | 0.5448 |
| H | Mx Tip dorsal | Md Central region dorsal |  |  |  | 0.5466 |
| H | Md Tooth I ventral | Md Tooth III ventral |  |  |  | 0.9999 |
| H | Mx Outer edge dorsal | Md Outer edge ventral |  |  |  | 0.2876 |
| H | Md Inner edge ventral | Mx Outer edge dorsal |  |  |  | 0.5301 |
| H | Md Tooth III ventral | Md Tooth II ventral |  |  |  | 1.0000 |
| H | Mx Tip dorsal | Md Outer edge dorsal |  |  |  | 0.9392 |
| H | Md Tooth III dorsal | Md Tooth II ventral |  |  |  | 1.0000 |
| H | Md Tooth II dorsal | Md Tooth II ventral |  |  |  | 1.0000 |
| H | Mx Inner edge dorsal | Mx Outer edge dorsal |  |  |  | 0.9775 |
| H | Md Tooth I dorsal | Md Tooth I ventral |  |  |  | 1.0000 |
| H | Md Tooth II ventral | Mx Tip ventral |  |  |  | 1.0000 |
| H | Md Inner edge ventral | Mx Inner edge dorsal |  |  |  | 1.0000 |
| H | Md Outer edge dorsal | Md Central region dorsal |  |  |  | 1.0000 |
| H | Md Inner edge dorsal | Mx Inner edge ventral |  |  |  | 1.0000 |
| H | Md Tooth III ventral | Md Tooth II dorsal |  |  |  | 1.0000 |
| H | Md Tooth III ventral | Md Tooth III dorsal |  |  |  | 1.0000 |
| H | Md Tooth III dorsal | Md Tooth II dorsal |  |  |  | 1.0000 |
| E | Md Tip dorsal | Md Central region ventral | 326.8381 | 19 | <.0001* | <.0001* |
| E | Md Tip dorsal | Md Outer edge ventral |  |  |  | <.0001* |
| E | Md Tip dorsal | Mx Outer edge dorsal |  |  |  | <.0001* |
| E | Md Tip dorsal | Mx Inner edge dorsal |  |  |  | <.0001* |
| E | Md Tip dorsal | Md Inner edge ventral |  |  |  | <.0001* |
| E | Md Tip dorsal | Md Central region dorsal |  |  |  | <.0001* |
| E | Md Tip dorsal | Md Outer edge dorsal |  |  |  | <.0001* |
| E | Md Tip dorsal | Mx Tip dorsal |  |  |  | <.0001* |
| E | Md Tooth I dorsal | Md Central region ventral |  |  |  | <.0001* |
| E | Md Tip dorsal | Mx Outer edge ventral |  |  |  | <.0001* |
| E | Md Tip dorsal | Mx Inner edge ventral |  |  |  | <.0001* |
| E | Md Tooth I dorsal | Md Outer edge ventral |  |  |  | <.0001* |
| E | Md Tip ventral | Md Central region ventral |  |  |  | <.0001* |
| E | Md Tooth III dorsal | Md Central region ventral |  |  |  | <.0001* |
| E | Md Tip dorsal | Mx Tip ventral |  |  |  | <.0001* |
| E | Md Tip dorsal | Md Inner edge dorsal |  |  |  | <.0001* |
| E | Md Tooth II dorsal | Md Central region ventral |  |  |  | <.0001* |
| E | Md Tooth I dorsal | Mx Outer edge dorsal |  |  |  | <.0001* |
| E | Md Tip dorsal | Md Tooth II ventral |  |  |  | <.0001* |
| E | Md Tooth I dorsal | Mx Inner edge dorsal |  |  |  | <.0001* |
| E | Md Tooth I dorsal | Md Inner edge ventral |  |  |  | <.0001* |
| E | Md Tip ventral | Md Outer edge ventral |  |  |  | <.0001* |
| E | Md Tip dorsal | Md Tooth III ventral |  |  |  | <.0001* |
| E | Md Tooth III dorsal | Md Outer edge ventral |  |  |  | <.0001* |
| E | Md Tooth II dorsal | Md Outer edge ventral |  |  |  | <.0001* |
| E | Md Tooth I ventral | Md Central region ventral |  |  |  | <.0001* |
| E | Md Tip ventral | Mx Outer edge dorsal |  |  |  | <.0001* |
| E | Md Tip dorsal | Md Tooth I ventral |  |  |  | <.0001* |
| E | Md Tip ventral | Mx Inner edge dorsal |  |  |  | <.0001* |
| E | Md Tip ventral | Md Inner edge ventral |  |  |  | <.0001* |
| E | Md Tooth III dorsal | Mx Outer edge dorsal |  |  |  | <.0001* |
| E | Md Tooth III dorsal | Mx Inner edge dorsal |  |  |  | <.0001* |
| E | Md Tooth III dorsal | Md Inner edge ventral |  |  |  | <.0001* |
| E | Md Tooth III ventral | Md Central region ventral |  |  |  | <.0001* |
| E | Md Tooth I ventral | Md Outer edge ventral |  |  |  | <.0001* |
| E | Md Tooth II dorsal | Mx Outer edge dorsal |  |  |  | <.0001* |
| E | Md Tooth II dorsal | Mx Inner edge dorsal |  |  |  | <.0001* |
| E | Md Tooth II dorsal | Md Inner edge ventral |  |  |  | <.0001* |
| E | Md Tooth II ventral | Md Central region ventral |  |  |  | <.0001* |
| E | Md Tip dorsal | Md Tooth II dorsal |  |  |  | <.0001* |
| E | Md Inner edge dorsal | Md Central region ventral |  |  |  | <.0001* |
| E | Mx Tip ventral | Md Central region ventral |  |  |  | <.0001* |
| E | Md Tooth I dorsal | Md Central region dorsal |  |  |  | <.0001* |
| E | Md Tip dorsal | Md Tooth III dorsal |  |  |  | <.0001* |
| E | Md Tooth I dorsal | Md Outer edge dorsal |  |  |  | <.0001* |
| E | Md Tooth III ventral | Md Outer edge ventral |  |  |  | <.0001* |
| E | Md Tooth I ventral | Mx Outer edge dorsal |  |  |  | <.0001* |
| E | Md Tip dorsal | Md Tip ventral |  |  |  | <.0001* |
| E | Md Tooth I dorsal | Mx Tip dorsal |  |  |  | <.0001* |
| E | Md Tooth I ventral | Mx Inner edge dorsal |  |  |  | <.0001* |
| E | Md Tooth I ventral | Md Inner edge ventral |  |  |  | <.0001* |
| E | Md Tooth II ventral | Md Outer edge ventral |  |  |  | <.0001* |
| E | Md Tooth I dorsal | Mx Outer edge ventral |  |  |  | <.0001* |
| E | Md Inner edge dorsal | Md Outer edge ventral |  |  |  | <.0001* |
| E | Mx Inner edge ventral | Md Central region ventral |  |  |  | <.0001* |
| E | Mx Tip ventral | Md Outer edge ventral |  |  |  | <.0001* |
| E | Md Tooth III ventral | Mx Outer edge dorsal |  |  |  | <.0001* |
| E | Md Tip ventral | Md Central region dorsal |  |  |  | <.0001* |
| E | Md Tooth III ventral | Mx Inner edge dorsal |  |  |  | <.0001* |
| E | Md Tooth III ventral | Md Inner edge ventral |  |  |  | <.0001* |
| E | Md Tip ventral | Md Outer edge dorsal |  |  |  | <.0001* |
| E | Md Tooth I dorsal | Mx Inner edge ventral |  |  |  | <.0001* |
| E | Md Tooth III dorsal | Md Central region dorsal |  |  |  | <.0001* |
| E | Md Tooth II ventral | Mx Outer edge dorsal |  |  |  | <.0001* |
| E | Mx Outer edge ventral | Md Central region ventral |  |  |  | <.0001* |
| E | Md Tip dorsal | Md Tooth I dorsal |  |  |  | <.0001* |
| E | Md Inner edge dorsal | Mx Outer edge dorsal |  |  |  | <.0001* |
| E | Mx Inner edge ventral | Md Outer edge ventral |  |  |  | <.0001* |
| E | Md Tooth III dorsal | Md Outer edge dorsal |  |  |  | <.0001* |
| E | Md Tip ventral | Mx Tip dorsal |  |  |  | <.0001* |
| E | Md Tooth II ventral | Mx Inner edge dorsal |  |  |  | <.0001* |
| E | Md Tooth II ventral | Md Inner edge ventral |  |  |  | <.0001* |
| E | Mx Tip dorsal | Md Central region ventral |  |  |  | <.0001* |
| E | Md Inner edge dorsal | Mx Inner edge dorsal |  |  |  | <.0001* |
| E | Md Inner edge dorsal | Md Inner edge ventral |  |  |  | <.0001* |
| E | Mx Tip ventral | Mx Outer edge dorsal |  |  |  | <.0001* |
| E | Md Tooth II dorsal | Md Central region dorsal |  |  |  | <.0001* |
| E | Md Tip ventral | Mx Outer edge ventral |  |  |  | <.0001* |
| E | Mx Tip ventral | Mx Inner edge dorsal |  |  |  | <.0001* |
| E | Mx Tip ventral | Md Inner edge ventral |  |  |  | <.0001* |
| E | Md Tooth II dorsal | Md Outer edge dorsal |  |  |  | <.0001* |
| E | Md Tooth III dorsal | Mx Tip dorsal |  |  |  | <.0001* |
| E | Md Outer edge dorsal | Md Central region ventral |  |  |  | <.0001* |
| E | Md Tooth III dorsal | Mx Outer edge ventral |  |  |  | <.0001* |
| E | Md Central region dorsal | Md Central region ventral |  |  |  | <.0001* |
| E | Md Tooth I dorsal | Mx Tip ventral |  |  |  | <.0001* |
| E | Md Tooth II dorsal | Mx Tip dorsal |  |  |  | <.0001* |
| E | Md Tooth I dorsal | Md Inner edge dorsal |  |  |  | <.0001* |
| E | Md Tooth II dorsal | Mx Outer edge ventral |  |  |  | <.0001* |
| E | Mx Outer edge ventral | Md Outer edge ventral |  |  |  | <.0001* |
| E | Md Tooth I dorsal | Md Tooth II ventral |  |  |  | <.0001* |
| E | Mx Tip dorsal | Md Outer edge ventral |  |  |  | <.0001* |
| E | Mx Inner edge ventral | Mx Outer edge dorsal |  |  |  | <.0001* |
| E | Md Tip ventral | Mx Inner edge ventral |  |  |  | <.0001* |
| E | Md Tooth I ventral | Md Central region dorsal |  |  |  | <.0001* |
| E | Mx Inner edge ventral | Mx Inner edge dorsal |  |  |  | <.0001* |
| E | Mx Inner edge ventral | Md Inner edge ventral |  |  |  | <.0001* |
| E | Md Tooth I ventral | Md Outer edge dorsal |  |  |  | <.0001* |
| E | Md Tooth I dorsal | Md Tooth III ventral |  |  |  | <.0001* |
| E | Md Outer edge dorsal | Md Outer edge ventral |  |  |  | <.0001* |
| E | Md Tooth III dorsal | Mx Inner edge ventral |  |  |  | <.0001* |
| E | Md Central region dorsal | Md Outer edge ventral |  |  |  | <.0001* |
| E | Md Tooth I ventral | Mx Tip dorsal |  |  |  | <.0001* |
| E | Md Tooth II dorsal | Mx Inner edge ventral |  |  |  | <.0001* |
| E | Md Tooth I ventral | Mx Outer edge ventral |  |  |  | <.0001* |
| E | Mx Outer edge ventral | Mx Outer edge dorsal |  |  |  | <.0001* |
| E | Md Tip ventral | Mx Tip ventral |  |  |  | <.0001* |
| E | Md Tooth III ventral | Md Central region dorsal |  |  |  | <.0001* |
| E | Mx Outer edge ventral | Mx Inner edge dorsal |  |  |  | <.0001* |
| E | Mx Outer edge ventral | Md Inner edge ventral |  |  |  | <.0001* |
| E | Mx Tip dorsal | Mx Outer edge dorsal |  |  |  | <.0001* |
| E | Md Tip ventral | Md Inner edge dorsal |  |  |  | <.0001* |
| E | Md Tooth III ventral | Md Outer edge dorsal |  |  |  | <.0001* |
| E | Md Tooth I dorsal | Md Tooth I ventral |  |  |  | 0.0004* |
| E | Md Tip ventral | Md Tooth II ventral |  |  |  | <.0001* |
| E | Mx Tip dorsal | Mx Inner edge dorsal |  |  |  | <.0001* |
| E | Mx Tip dorsal | Md Inner edge ventral |  |  |  | <.0001* |
| E | Md Tooth III dorsal | Mx Tip ventral |  |  |  | <.0001* |
| E | Md Outer edge dorsal | Mx Outer edge dorsal |  |  |  | <.0001* |
| E | Md Tooth III dorsal | Md Inner edge dorsal |  |  |  | <.0001* |
| E | Md Tooth II ventral | Md Central region dorsal |  |  |  | <.0001* |
| E | Md Tooth III ventral | Mx Tip dorsal |  |  |  | <.0001* |
| E | Md Tooth III dorsal | Md Tooth II ventral |  |  |  | 0.0045* |
| E | Md Central region dorsal | Mx Outer edge dorsal |  |  |  | <.0001* |
| E | Md Inner edge dorsal | Md Central region dorsal |  |  |  | <.0001* |
| E | Md Outer edge dorsal | Mx Inner edge dorsal |  |  |  | <.0001* |
| E | Md Outer edge dorsal | Md Inner edge ventral |  |  |  | <.0001* |
| E | Md Tooth II dorsal | Mx Tip ventral |  |  |  | <.0001* |
| E | Md Tooth II ventral | Md Outer edge dorsal |  |  |  | <.0001* |
| E | Md Tip ventral | Md Tooth III ventral |  |  |  | 0.0002* |
| E | Md Tooth I ventral | Mx Inner edge ventral |  |  |  | <.0001* |
| E | Md Tooth III ventral | Mx Outer edge ventral |  |  |  | <.0001* |
| E | Md Inner edge dorsal | Md Outer edge dorsal |  |  |  | <.0001* |
| E | Md Central region dorsal | Mx Inner edge dorsal |  |  |  | <.0001* |
| E | Md Central region dorsal | Md Inner edge ventral |  |  |  | <.0001* |
| E | Mx Tip ventral | Md Central region dorsal |  |  |  | <.0001* |
| E | Md Tooth II dorsal | Md Inner edge dorsal |  |  |  | 0.0001* |
| E | Md Tooth II dorsal | Md Tooth II ventral |  |  |  | 0.0333* |
| E | Mx Tip ventral | Md Outer edge dorsal |  |  |  | <.0001* |
| E | Md Tooth II ventral | Mx Tip dorsal |  |  |  | 0.0020* |
| E | Md Tooth III dorsal | Md Tooth III ventral |  |  |  | 0.0606 |
| E | Md Inner edge ventral | Md Central region ventral |  |  |  | <.0001* |
| E | Mx Inner edge dorsal | Md Central region ventral |  |  |  | <.0001* |
| E | Md Inner edge dorsal | Mx Tip dorsal |  |  |  | <.0001* |
| E | Md Tooth II ventral | Mx Outer edge ventral |  |  |  | 0.0028* |
| E | Mx Outer edge dorsal | Md Central region ventral |  |  |  | <.0001* |
| E | Md Tooth I dorsal | Md Tooth II dorsal |  |  |  | 0.1599 |
| E | Md Inner edge dorsal | Mx Outer edge ventral |  |  |  | <.0001* |
| E | Mx Tip ventral | Mx Tip dorsal |  |  |  | <.0001* |
| E | Md Tooth II dorsal | Md Tooth III ventral |  |  |  | 0.2536 |
| E | Mx Tip ventral | Mx Outer edge ventral |  |  |  | <.0001* |
| E | Md Tooth I dorsal | Md Tooth III dorsal |  |  |  | 0.4858 |
| E | Md Tip ventral | Md Tooth I ventral |  |  |  | 0.1371 |
| E | Md Tooth III ventral | Mx Inner edge ventral |  |  |  | 0.0731 |
| E | Md Tooth I ventral | Mx Tip ventral |  |  |  | 0.1732 |
| E | Mx Inner edge ventral | Md Central region dorsal |  |  |  | <.0001* |
| E | Md Tooth I ventral | Md Inner edge dorsal |  |  |  | 0.2717 |
| E | Mx Inner edge ventral | Md Outer edge dorsal |  |  |  | <.0001* |
| E | Md Tooth I dorsal | Md Tip ventral |  |  |  | 0.4748 |
| E | Md Tooth III dorsal | Md Tooth I ventral |  |  |  | 0.8567 |
| E | Md Tooth I ventral | Md Tooth II ventral |  |  |  | 0.8578 |
| E | Md Inner edge ventral | Md Outer edge ventral |  |  |  | <.0001* |
| E | Mx Inner edge dorsal | Md Outer edge ventral |  |  |  | <.0001* |
| E | Md Tooth II ventral | Mx Inner edge ventral |  |  |  | 0.5933 |
| E | Md Inner edge dorsal | Mx Inner edge ventral |  |  |  | 0.0003* |
| E | Mx Outer edge dorsal | Md Outer edge ventral |  |  |  | 0.0009* |
| E | Mx Inner edge ventral | Mx Tip dorsal |  |  |  | 0.0469* |
| E | Md Tooth II dorsal | Md Tooth I ventral |  |  |  | 0.9912 |
| E | Md Outer edge ventral | Md Central region ventral |  |  |  | 0.0070* |
| E | Mx Tip ventral | Mx Inner edge ventral |  |  |  | 0.1739 |
| E | Md Tooth I ventral | Md Tooth III ventral |  |  |  | 0.9981 |
| E | Mx Inner edge ventral | Mx Outer edge ventral |  |  |  | 0.0274* |
| E | Md Tooth III ventral | Mx Tip ventral |  |  |  | 0.9979 |
| E | Mx Outer edge ventral | Md Central region dorsal |  |  |  | 0.3713 |
| E | Md Tip ventral | Md Tooth II dorsal |  |  |  | 0.9995 |
| E | Md Tooth III ventral | Md Inner edge dorsal |  |  |  | 0.9999 |
| E | Mx Outer edge ventral | Md Outer edge dorsal |  |  |  | 0.7890 |
| E | Mx Tip dorsal | Md Central region dorsal |  |  |  | 0.9911 |
| E | Md Tooth III ventral | Md Tooth II ventral |  |  |  | 1.0000 |
| E | Mx Tip dorsal | Md Outer edge dorsal |  |  |  | 0.9999 |
| E | Md Tooth III dorsal | Md Tooth II dorsal |  |  |  | 1.0000 |
| E | Md Tip ventral | Md Tooth III dorsal |  |  |  | 1.0000 |
| E | Md Tooth II ventral | Mx Tip ventral |  |  |  | 1.0000 |
| E | Md Inner edge dorsal | Mx Tip ventral |  |  |  | 1.0000 |
| E | Mx Outer edge ventral | Mx Tip dorsal |  |  |  | 1.0000 |
| E | Md Inner edge ventral | Mx Outer edge dorsal |  |  |  | 1.0000 |
| E | Mx Inner edge dorsal | Mx Outer edge dorsal |  |  |  | 1.0000 |
| E | Md Outer edge dorsal | Md Central region dorsal |  |  |  | 1.0000 |
| E | Md Tooth II ventral | Md Inner edge dorsal |  |  |  | 1.0000 |
| E | Md Inner edge ventral | Mx Inner edge dorsal |  |  |  | 1.0000 |

Supplementary Table 4. For the individual elements and the mechanical parameters, correlation coefficients, estimated by row-wise method are shown. Red letters = negative correlation; grey = negligible to low correlation; blue = moderate to very high correlation.

|  | Ae | Ca | Cl | Cu | F | Fe | H | K | Mg | Mn | E | Na | P+Pt | S | Si | Zn |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Ae | 1.00 | 0.95 | 0.20 | 0.97 | -0.31 | 0.87 | 0.80 | 0.41 | 0.67 | 0.91 | 0.80 | 0.09 | 0.72 | 0.97 | 0.97 | 0.95 |
| Ca | - | 1.00 | 0.15 | 0.94 | -0.34 | 0.79 | 0.71 | 0.33 | 0.56 | 0.89 | 0.70 | 0.10 | 0.64 | 0.92 | 0.94 | 0.87 |
| Cl | - | - | 1.00 | 0.13 | -0.11 | 0.09 | 0.09 | 0.31 | 0.03 | 0.18 | 0.15 | -0.13 | 0.16 | 0.13 | 0.15 | 0.13 |
| Cu | - | - | - | 1.00 | -0.33 | 0.93 | 0.75 | 0.36 | 0.61 | 0.87 | 0.75 | 0.09 | 0.63 | 0.95 | 0.95 | 0.95 |
| F | - | - | - | - | 1.00 | -0.30 | -0.31 | -0.50 | -0.27 | -0.40 | -0.28 | -0.35 | -0.37 | -0.35 | -0.36 | -0.30 |
| Fe | - | - | - | - | - | 1.00 | 0.63 | 0.35 | 0.49 | 0.74 | 0.63 | 0.07 | 0.53 | 0.85 | 0.86 | 0.91 |
| H | - | - | - | - | - | - | 1.00 | 0.25 | 0.86 | 0.68 | 0.96 | 0.13 | 0.75 | 0.87 | 0.83 | 0.77 |
| K | - | - | - | - | - | - | - | 1.00 | 0.14 | 0.42 | 0.28 | -0.04 | 0.31 | 0.35 | 0.36 | 0.33 |
| Mg | - | - | - | - | - | - | - | - | 1.00 | 0.54 | 0.77 | 0.11 | 0.71 | 0.74 | 0.66 | 0.71 |
| Mn | - | - | - | - | - | - | - | - | - | 1.00 | 0.68 | 0.15 | 0.62 | 0.85 | 0.86 | 0.83 |
| E | - | - | - | - | - | - | - | - | - | - | 1.00 | 0.14 | 0.71 | 0.87 | 0.84 | 0.76 |
| Na | - | - | - | - | - | - | - | - | - | - | - | 1.00 | 0.13 | 0.11 | 0.13 | 0.10 |
| P+Pt | - | - | - | - | - | - | - | - | - | - | - | - | 1.00 | 0.73 | 0.71 | 0.66 |
| S | - | - | - | - | - | - | - | - | - | - | - | - | - | 1.00 | 0.97 | 0.95 |
| Si | - | - | - | - | - | - | - | - | - | - | - | - | - | - | 1.00 | 0.91 |
| Zn | - | - | - | - | - | - | - | - | - | - | - | - | - | - | - | 1.00 |

Supplementary Figure 1. The relationship between the elemental content of Ae and the mechanical properties for all localities are shown.

Supplementary Figure 2. The relationship between the elemental content of Ca and the mechanical properties for all localities are shown.

Supplementary Figure 3. The relationship between the elemental content of Cl and the mechanical properties for all localities are shown.

Supplementary Figure 4. The relationship between the elemental content of Cu and the mechanical properties for all localities are shown.

Supplementary Figure 5. The relationship between the elemental content of F and the mechanical properties for all localities are shown.

Supplementary Figure 6. The relationship between the elemental content of Fe and the mechanical properties for all localities are shown.

Supplementary Figure 7. The relationship between the elemental content of K and the mechanical properties for all localities are shown.

Supplementary Figure 8. The relationship between the elemental content of Mg and the mechanical properties for all localities are shown.

Supplementary Figure 9. The relationship between the elemental content of Mn and the mechanical properties for all localities are shown.

Supplementary Figure 10. The relationship between the elemental content of Na and the mechanical properties for all localities are shown.

Supplementary Figure 11. The relationship between the elemental content of P+Pt and the mechanical properties for all localities are shown. Pt and P cannot be differentiated, as these elements share one peak. Pt content was however estimated by measuring localities with epoxy (mean ± SD of Pt: 0.15 ± 0.02 atomic %).

Supplementary Figure 12. The relationship between the elemental content of S and the mechanical properties for all localities are shown.

Supplementary Figure 13. The relationship between the elemental content of Si and the mechanical properties for all localities are shown.

Supplementary Figure 14. The relationship between the elemental content of Zn and the mechanical properties for all localities are shown.

Supplementary Figure 15. Hardness H and Young’s modulus E, both given in GPa, versus the elemental proportions of the individual elements, given in atomic %.