Table 1. Optimization of reaction conditions a,b

| Entry | Catalyst | Conversion (%)2 | Yield (%)2 |
| --- | --- | --- | --- |
| 1 | 1a | 99 | 92 |
| 2 | 1b | 63 | 57 |
| 3 | 1c | 65 | 58 |
| 4 | 1d | 48 | 42 |
| 5 | 1e | 51 | 46 |
| 6 | 1f | 53 | 48 |
| 7 | (NH4)6Mo7O24 | 46 | 35 |
| 8 | NiSO4 | 44 | 36 |
| a Reaction conditions: 1a (1.0 mol%), Benzylamine (1.0 mmol), KBH4 (1.0 mmol), acetonitrile (2.0 mL) at 60 oC for 12 h. b Substrate conversion and yields were determined by GC-MS (internal standard is toluene) analysis. Table 2. Formylation of various amines with CO2 catalyzed by 1aa, b a Reaction conditions: 1a (1.0 mol%), Benzylamine (1.0 mmol), KBH4 (1.0 mmol), acetonitrile (2.0 mL) stirring at a reaction tube with a CO2 balloon at 60 oC for 12 h. b Substrate conversion and yields were determined by GC-MS (internal standard is toluene) analysis.. Table 3. Formylation of various diamines with CO2 catalyzed by 1a a, b a Reaction conditions: 1a (1.0 mol%), diamine (1.0 mmol), KBH4 (2.0 mmol), acetonitrile (2.0 mL) stirring at a reaction tube with a CO2 balloon at 60 oC for 12 h. b Substrate yields were determined by GC-MS (internal standard is toluene) analysis, values in parentheses are the isolated yields.. |