Supplementary information

Flexible self-supporting interconnected cobalt sulfide nanosheets enable high-loading and long-cycling Li-S batteries with high areal capacity

Xiaohui Tian 1, Lukang Che 1, Mengdie Liu, Naomie Beolle Songwe Selabi, Yingke Zhou

The State Key Laboratory of Refractories and Metallurgy, Institute of Advanced Materials and Nanotechnology, College of Materials and Metallurgy, Wuhan University of Science and Technology, Wuhan 430081, P. R. China.

Fig. S1. The initial discharge-charge profile (a) and cycling performance (b) of the Co9S8-CC electrode at a current density of 167 mA g-1.

Fig. S2. Galvanostatic discharge-charge profiles of the Co9S8-CC/Li2S6 electrode (a) and CC/Li2S6 electrode (b) at various rates.

Fig. S3. EIS curves of CC/Li2S6 and Co9S8-CC/Li2S6 electrodes before (a) and after (b) 100 cycles at 0.5 C. The inset in (b) corresponds to the equivalent circuit. The relationship between Zre and ω-1/2 before and after 100 cycles at 0.5 C of Co9S8-CC/Li2S6 electrode (c) and CC/Li2S6 electrode (d).

Table S1. Resistance parameters from fitting of EIS spectroscopy.

| Cathode |  |  | Re (Ω) | Rs (Ω) | Rct (Ω) |
| --- | --- | --- | --- | --- | --- |
| CC/Li2S6 | Before cycling |  | 4.5 | - | 34.4 |
|  | After 100 cycles at 0.5 C |  | 5.4 | 12.7 | 13.6 |
| Co9S8-CC/Li2S6 | Before cycling |  | 3.9 | - | 14.6 |
|  | After 100 cycles at 0.5 C |  | 4.3 | 0.9 | 4.4 |

Fig. S4. SEM images of Co9S8-CC/Li2S6 electrode after 1500 cycles at 2 C.

Fig. S5. (a) Galvanostatic discharge-charge profiles and (b) rate performance of Co9S8-CC/Li2S6 electrode with high areal sulfur-loading of 6.2 mg cm-2 at different rates. (c) Cycle performance of Co9S8-CC/Li2S6 electrode with high areal sulfur-loading of 6.2 mg cm-2 at 0.5 C.

Table S2. Performance comparison of Li-S batteries in this work with those previously reported based on Co9S8 composite hosts.

| Host | Sulfur-loading (mg cm-2) | Current density (C) | Initial capacity (mAh g-1) | Areal capacity (mAh cm-2) | Capacity decay rate (%/cycle) | Ref. |
| --- | --- | --- | --- | --- | --- | --- |
| Hollow NiCo-LDH/Co9S8 heterostructure (H-LDH/Co9S8) | 1.5-2 | 0.1 | 1339.1 | 2-2.68 | - | [1] |
|  |  | 0.5 | 963.5 | 1.44-1.93 | 0.07 (500 cycles) |  |
|  |  | 1 | 866.1 | 1.3-1.73 | 0.06 (1500 cycles) |  |
|  |  | 2 | 669.6 | 1-1.34 | - |  |
| Co9S8 inlaid carbon nanoboxes (Co9S8@C NBs) | ~1.6 | 0.1 | 1267 | ~2.03 | - | [2] |
|  |  | 0.5 | 1059 | ~1.69 | 0.06 (100 cycles) |  |
|  |  | 1 | 970 | ~1.55 | 0.043 (400 cycles) |  |
|  |  | 2 | 802 | ~1.28 |  |  |
| Co9S8 nanocrystal coated hollow carbon nanosphere (HCS@Co9S8) | 1-2 | 0.1 | 1285 | 1.29~2.57 | - | [3] |
|  |  | 0.5 | 890 | 0.89-1.78 | 0.033 (400 cycles) |  |
|  |  | 2 | 710 | 0.71-1.42 | - |  |
| Graphene decorated with hetero-Co9S8-NiS sheets (BMS-G) | 1.2-1.5 | 0.2 | 1142.9 | 1.37-1.71 | - | [4] |
|  |  | 1 | 788 | 0.95-1.18 | 0.031 (800 cycles) |  |
|  |  | 2 | 705.8 | 0.85-1.06 | - |  |
| Hollow sphere-like Co9S8 | 1 | 0.1 | 1100 | 1.1 | - | [5] |
|  |  | 0.5 | 836 | 0.84 | 0.36 (100 cycles) |  |
|  |  | 1 | 781 | 0.78 | - |  |
| Co9S8 inlaid carbon hollow nanopolyhedra (Co9S8/C) | 1.5 | 0.2 | 1160 | 1.74 | - | [6] |
|  |  | 2 | 950 | 1.43 | 0.041 (1000 cycles) |  |
|  | 3.0 | 0.1 | 950 | 2.85 | - |  |
| Co9S8 nanoparticle-embedded in N-doped carbon nanotube hollow polyhedron (Co9S8@NCNHP) | 1.3 | 0.2 | 1107 | 1.44 | 0.14 (200 cycles) | [7] |
|  |  | 2 | 689 | 0.9 |  |  |
|  | 2.1 | 0.2 | 910 | 0.91 | 0.11 (200 cycles) |  |
|  | 3.2 | 0.2 | 780 | 2.5 | 0.15 (200 cycles) |  |
| Co9S8 nanotube/GO | 0.7-1 | 0.1 | 1397 | 0.98~1.40 | 0.033 (100 cycles) | [8] |
|  |  | 1 | 513.4 | 0.36~0.51 | 0.027 (200 cycles) |  |
|  |  | 2 | 361 | 0.25~0.36 | - |  |
| Co9S8 nanotubes | 1.5-1.6 | 0.1 | 913 | 1.37~1.46 | 0.28 (100 cycles) | [9] |
|  |  | 2 | 425.7 | 0.64~0.68 | - |  |
| MWCNT/Co9S8 | 1 | 0.1 | 1271 | 1.27 | 0.55 (100 cycles) | [10] |
|  |  | 0.5 | 563 | 0.56 | - |  |
|  |  | 1 | 431 | 0.43 | - |  |
| Graphene-like Co9S8 nanosheet | 1.5 | 0.05 | 1130 | 1.70 | - | [11] |
|  |  | 0.5 | - | - | 0.045 (1500 cycles) |  |
|  | 4.5 | 0.05 | - | 4.30 | - |  |
| Co9S8-CC | 2.5 | 0.1 | 1315.1 | 3.29 | - | This work |
|  |  | 0.5 | 1105.4 | 2.76 | 0.05 (100 cycles) |  |
|  |  | 2 | 872.4 | 2.18 | 0.02 (1500 cycles) |  |
|  | 6.2 | 0.1 | 1115.1 | 6.91 | 0.129 (200 cycles) |  |

Fig. S6. Optical photos of separators used in (a) CC/Li2S6 and (b) Co9S8-CC/Li2S6 cells after 100 cycles at 0.5 C.

Fig. S7. SEM images and the corresponding S element mapping of Li metal anodes used for CC/Li2S6 cell (a, b) and Co9S8-CC/Li2S6 cell (c, d) after 100 cycles at 0.5 C.

Fig. S8. Optimal configurations and corresponding binding energies of (a) Li2S, (b) Li2S2, (c) Li2S4, (d) Li2S6, (e) Li2S8 and (f) S8 adsorbed on graphene (001).

Fig. S9. Isosurface of charge density difference for optimized structures of (a) Li2S, (b) Li2S2, (c) Li2S4, (d) Li2S6, (e) Li2S8 and (f) S8 adsorbed on Co9S8 (311). The isovalues are defined as 0.005 e/Å3 in all cases.

Fig. S10. EIS curves of CC and Co9S8-CC symmetric cells.

Supplementary reference

- Chen SX, Luo JH, Li NY, Han XX, Wang J, Deng Q, Zeng ZL, Deng SG (2020) Multifunctional LDH/Co9S8 heterostructure nanocages as high-performance lithium-sulfur battery cathodes with ultralong lifespan. Energy Storage Mater 30:187-195

- Sun WW, Li YJ, Liu SK, Guo QP, Zhu YH, Hong XB, Zheng CM, Xie K (2020) Catalytic Co9S8 decorated carbon nanoboxes as efficient cathode host for long-life lithium-sulfur batteries. Nano Res 13:2143-2148

- Xu JL, Liu L, Sun YH, Lu RF, Wang ZR, Sun Q (2020) Engineering of three-dimensional nanohybrids: Co9S8 nanocrystal coated hollow carbon nanosphere for advanced lithium storage. Appl Surf Sci 514:146092

- Chen L, Xie XF, Zhang ZA, Kong XZ, Liang SQ, Pan AQ (2020) One-pot synthesis of hetero-Co9S8-NiS sheets on graphene to boost lithium-sulfur battery performance. Inorg Chem Front 7:2160-2167

- Liu XF, Wang D, Yang XZ, Zhao ZZ, Yang H, Feng M, Zhang W, Zheng WT (2019) Synergistic dual-confinement effect: Merit of hollowly metallic Co9S8 in packaging enhancement of electrochemical performance of Li-S batteries. ACS Appl Energy Mater 2:1428-1435

- Chen T, Ma LB, Cheng BR, Chen RP, Hu Y, Zhu GY, Wang YR, Liang J, Tie ZX, Liu J, Jin Z (2017) Metallic and polar Co9S8 inlaid carbon hollow nanopolyhedra as efficient polysulfide mediator for lithium-sulfur batteries. Nano Energy 38:239-248

- Yu Y, Zhan ZH, Tang PJ, Xu QY, Fan Q, Wang W, Shen K (2021) Promoting polysulfide redox kinetics by Co9S8 nanoparticle-embedded in N-doped carbon nanotube hollow polyhedron for lithium sulfur batteries. J Alloys Compd 869:159306

- Wei J, Chen B, Su H, Jiang C, Li XT, Qiao SS, Zhang H (2021) Co9S8 nanotube wrapped with graphene oxide as sulfur hosts with ultra-high sulfur content for lithium-sulfur battery. Ceram Int 47:2686-2693

- Wei J, Su H, Qin CM, Chen B, Zhang H, Wang JM (2019) Multifunctional Co9S8 nanotubes for high-performance lithium-sulfur batteries. J Electroanal Chem 837:184-190

- Tong W, Huang Y, Jia W, Wang X, Guo Y, Sun Z, Jia D, Zong J (2018) Leaf like interconnected network structure of MWCNT/Co9S8/S for lithium-sulfur batteries. J Alloys Compd 731:964-970

- Pang Q, Kundu DP, Nazar LF (2016) A graphene-like metallic cathode host for long-life and high-loading lithium-sulfur batteries. Mater Horiz 3:130-136

1 These authors contributed equally to this work.

Corresponding author. Tel.: +86 2768 862928, Fax: +86 2768 862928. E-mail: zhouyk@wust.edu.cn.