Acetalization of alkyl alcohols with -citronellal over an acidic carbon catalyst: a green and reusable catalyst obtained from bio-oil sulfonation

Neide Paloma Gonçalves Lopes1, Fabiane Carvalho Ballotin2, Ana Paula de Carvalho Teixeira2, Rochel Montero Lago2 and Márcio José da Silva1*

1Chemistry Department, Federal University of Viçosa, Viçosa, Minas Gerais, Brasil. zip-code: 36590-000

2Chemistry Department, Federal University of Minas Gerais, Belo Horizonte, Minas Gerais, Brasil. zip-code: 31270-901

Supplemental material

List of Figures

Figure 1SM. Plots of ln (instantaneous concentration of -citronellal)/ (initial concentration of -citronellal) versus reaction time obtained from sulfated bio-oil-catalyzed -citronellal acetalization reactions with methyl alcohol at different temperatures

Figure 2SM. Comparison of infrared spectra of 120minH bio-oil catalyst

List of Tables

Table 1SM. Effect of sulfated bio-oil catalyst load on the rate constant of acetalization reactions of -citronellal with methyl alcohol

Table 2SM. The kinetic constants of sulfated bio-oil-catalyzed -citronellal acetalization reactions with methyl alcohol at different temperatures.

Figures

Figure 1SM. Plots of ln (instantaneous concentration of -citronellal)/ (initial concentration of -citronellal) versus reaction time obtained from sulfated bio-oil-catalyzed -citronellal acetalization reactions with methyl alcohol at different temperatures (a)

Figure 2SM. Comparison of infrared spectra of 120minH bio-oil catalyst

Tables

Table 1SM. Effect of sulfated bio-oil catalyst load on the rate constant of acetalization reactions of -citronellal with methyl alcohol

| Catalyst load / wt% | k x10-3 / min-1 |
| --- | --- |
| - | 0.25 |
| 0.66 | 8.8 |
| 1.32 | 16.0 |
| 2.64 | 28.1 |
| 3.96 | 30.4 |

Table 2SM. The kinetic constants of sulfated bio-oil-catalyzed -citronellal acetalization reactions with methyl alcohol at different temperatures.

| T/K | k x 10-3(min-) |
| --- | --- |
| 298 | 8.4 |
| 308 | 18.3 |
| 318 | 45.0 |
| 323 | 53.9 |