Electronic supplementary material for:

Solubility of Na2O·xAl2O3 in NaF-KF-AlF3-based low-temperature electrolyte

Ye Kuanga, Hengwei Yana,b＊, Zhanwei Liua,b＊, Yonghui Yanga

a Faculty of Metallurgical and Energy Engineering, Kunming University of Science and Technology, Kunming 650093, China;

b National Engineering Laboratory for Vacuum Metallurgy, Kunming University of Science and Technology, Kunming 650093, China.

Fig. S-1. Crystal structure of β-Al2O3

Fig. S-2. Relationship between alumina concentration and dissolution time of Na2O·70Al2O3 in NaF-KF-AlF3 system

Table S-Ⅰ. Dissolution rate of aluminum oxide with CR is 1.2 and 1.6 in 0-5min

| extracting time(min) | CR | 0 | 1 | 3 | 5 |
| --- | --- | --- | --- | --- | --- |
| Na2O·70Al2O3 dissolution rate (g Al2O3/100g melt) | 1.2 | 0.25 | 0.41 | 0.56 | 1.95 |
|  | 1.6 | 0.41 | 0.73 | 0.95 | 2.67 |

Table S-Ⅱ. Values of Ca-C0 when the CR is 1.2 and 1.6

| extracting time(min) | CR | 2 | 4 | 5 |
| --- | --- | --- | --- | --- |
| Ca-C0 (g Al2O3/100g melt) | 1.2 | -1.43 | -1.58 | -1.87 |
|  | 1.6 | -1.63 | -1.81 | -2.10 |

Fig. S-3. Zero order reaction with CR is 1.2 and 1.6

Where (a): CR=1.2, (b): CR=1.6

Table S-Ⅲ. Dissolution rate of Al2O3 with CR is 1.2 and 1.6 in 30-120min

| extracting time(min) | CR | 30 | 60 | 90 | 120 |
| --- | --- | --- | --- | --- | --- |
| Al2O3 dissolution rate (g Al2O3/100g melt) | 1.2 | 2.94 | 3.24 | 3.35 | 3.57 |
|  | 1.6 | 3.52 | 3.61 | 3.78 | 4.12 |

Table S-Ⅳ. Values of ln(Ca)-ln(C0) when the CR is 1.2 and 1.6

| Time (min) | CR | 0 | 30 | 60 |
| --- | --- | --- | --- | --- |
| ln(Ca)-ln(C0) (g Al2O3/100g melt) | 1.2 | -0.028 | -0.0597 | -0.079 |
|  | 1.6 | -0.041 | -0.0815 | -0.12 |

Fig. S-4. First order reaction with CR is 1.2 and 1.6

Where (a): CR=1.2, (b): CR=1.6