Supporting Information

Fluorine-Doped M-N-C Catalysts for Efficient Oxygen Reduction Reaction

Zhichuan Zheng1,2, Xuekun Hong1,* , Dajun Wu1, Ning Sun2, Yawei Kuang1, Debao Zhang1, Xiaxi Yao3,* , Peng Du2,*, Kai huang2, Ming Lei2

1 School of Electronic and Information Engineering, Changshu Institute of Technology, Changshu, Jiangsu 215500, P. R. China

2 State Key Laboratory of Information Photonics and Optical Communications, School of Science, Beijing University of Posts and Telecommunications, Beijing 100876, PR China

3 School of Materials Engineering, Changshu Institute of Technology, Changshu, Jiangsu 215500, P. R. China

Email: xkhong@cslg.edu.cn; xiaxiyao@cslg.edu.cn; pengdu@bupt.edu.cn

Supplementary Figures

Figure S1. (a-c) SEM images of MnPc/FCNT800, (d-i) EDS elemental mapping images of F, Mn, C and N (scale bar: 200 nm).

Figure S2. (a-c) SEM images of CoPc/FCNT800, (d-i) EDS elemental mapping images of F, Co, C and N (scale bar: 200 nm).

Figure S3. (a-c) SEM images of NiPc/FCNT800, (d-i) EDS elemental mapping images of F, Ni, C and N (scale bar: 200 nm).

Table S1. Comparison of the electrochemical performances with various reported catalysts.

| Catalyst | Electrolyte | Onset potential (V) | Half-wave potential (V) | Tafel Slope (mV dec-1) | Reference |
| --- | --- | --- | --- | --- | --- |
| MnPc/FCNT800 | 1 M KOH | 0.996 | 0.90 | 60.4 | This work |
| CoPc/FCNT800 | 1 M KOH | 0.977 | 0.88 | 91.1 | This work |
| Pt/C | 1 M KOH | 0.961 | 0.87 | 129.8 | This work |
| NiPc/FCNT800 | 1 M KOH | 0.952 | 0.859 | 116.9 | This work |
| Co3N/C | 1 M KOH | N/A | 0.862 | 37 | [1] |
| N−Co−Mo− GF/CNT | 0.1 M KOH | 0.9 | 0.83 | 27 | [2] |
| Co-NCS-2 | 0.1 M KOH | 0.96 | 0.90 | 60 | [3] |
| FeCo-N-HCN | 0.1 M KOH | 0.98 | 0.86 | 52.1 | [4] |
| FeNCS | 0.1 M KOH | N/A | 0.882 | N/A | [5] |
| FeNC-D0.5 | 0.1 M KOH | N/A | 0.866 | 55 | [6] |
| Mn SAs-N4 | 0.1 M KOH | N/A | 0.90 | 69 | [7] |
| FeN4-PN | 0.1 M KOH | N/A | 0.91 | 58 | [8] |
| Fe-ISA/SNC | 0.1 M KOH | N/A | 0.896 | 44 | [9] |
| FePc-HCNTs | 0.1 M KOH | 0.937 | 0.858 | 32 | [10] |
| FeCl1N4/CNS | 0.1 M KOH | N/A | 0.921 | 53 | [11] |
| SACs-Mn-1000@g-C3N4 | 0.1 M KOH | 0.95 | 0.863 | 79 | [12] |
| FePc–Py–CNTs | 0.1 M KOH | N/A | 0.915 | 27 | [13] |
| p-FePc/CNTs | 0.1 M KOH | 0.98 | 0.88 | 31 | [14] |
| FePc@CNT | 0.1 M KOH | 0.98 | 0.91 | N/A | [15] |
| PcCu–O8–Co/CNT | 0.1 M KOH | N/A | 0.83 | 60 | [16] |
| FeAzPc–4N–DMSO/oxMWCNT | 0.1 M KOH | 1.02 | 0.913 | 29.1 | [17] |
| UiO–66–NO2@CoCNT | 0.1 M KOH | N/A | 0.865 | N/A | [18] |
| 1/CNT | 0.1 M KOH | 0.930 | 0.840 | 84 | [19] |
| 1/CNTs | 0.1 M KOH | N/A | 0.810 | 36.9 | [20] |
| (CoP)0.5(FeP)0.5@CNT | 0.1 M KOH | N/A | 0.80 | 70.1 | [21] |
| FePc–RCNTs | 0.1 M KOH | 0.951 | 0.86 | 38 | [22] |

Reference

[S1] Zeng R, Yang Y, Feng X R, Li H Q, Gibbs L M, DiSalvo F J, Abruna H D (2022) Nonprecious transition metal nitrides as efficient oxygen reduction electrocatalysts for alkaline fuel cells. Sci. Adv. 8 (5): eahj1584.

[S2] Tavakkoli M, Flahaut E, Peljo P, Sainio J, Davodi F, Lobiak E V, Mustonen K, Kauppinen E I (2020) Mesoporous single-atom-doped graphene–carbon nanotube hybrid: Synthesis and tunable electrocatalytic activity for oxygen evolution and reduction reactions. ACS Catal. 10 (8): 4647-4658.

[S3] Shi C, Liu Y, Qi R, Li J, Zhu J, Yu R, Li S, Hong X, Wu J, Xi S, Zhou L, Mai L (2021) Hierarchical N-doped carbon spheres anchored with cobalt nanocrystals and single atoms for oxygen reduction reaction. Nano Energy 87: 106153.

[S4] Li H, Wen Y, Jiang M, Yao Y, Zhou H, Huang Z, Li J, Jiao S, Kuang Y, Luo S (2021) Understanding of neighboring Fe‐N4‐C and Co‐N4‐C dual active centers for oxygen reduction reaction. Adv. Funct. Mater. 31 (22): 2011289.

[S5] Li F, Han G F, Bu Y, Noh H J, Jeon J P, Shin T J, Kim S J, Wu Y, Jeong H Y, Fu Z, Lu Y, Baek J B (2020) Revealing isolated M-N3C1 active sites for efficient collaborative oxygen reduction catalysis. Angew. Chem. Int. Ed. Engl. 59 (52): 23678-23683.

[S6] Shao C, Zhuang S, Zhang H, Jiang Q, Xu X, Ye J, Li B, Wang X (2021) Enhancement of mass transport for oxygen reduction reaction using petal-like porous Fe-NC nanosheet. Small 17 (6): 2006178.

[S7] Yang Z, Wang X, Zhu M, Leng X, Chen W, Wang W, Xu Q, Yang L-M, Wu Y (2021) Structural revolution of atomically dispersed Mn sites dictates oxygen reduction performance. Nano Res. 14 (12): 4512-4519.

[S8] Lin Y, Liu K, Chen K, Xu Y, Li H, Hu J, Lu Y-R, Chan T-S, Qiu X, Fu J, Liu M (2021) Tuning charge distribution of FeN4 via external N for enhanced oxygen reduction reaction. ACS Catal.  11 (10): 6304-6315.

[S9] Li Q, Chen W, Xiao H, Gong Y, Li Z, Zheng L, Zheng X, Yan W, Cheong W C, Shen R, Fu N, Gu L, Zhuang Z, Chen C, Wang D, Peng Q, Li J, Li Y (2018) Fe isolated single atoms on S, N codoped carbon by copolymer pyrolysis strategy for highly efficient oxygen reduction reaction. Adv. Mater. 30 (25): 1800588.

[S10] Yan X, Xu X, Zhong Z, Liu J, Tian X, Kang L, Yao J (2018) The effect of oxygen content of carbon nanotubes on the catalytic activity of carbon-based iron phthalocyanine for oxygen reduction reaction. Electrochim. Acta 281: 562-570.

[S11] Han Y, Wang Y, Xu R, Chen W, Zheng L, Han A, Zhu Y, Zhang J, Zhang H, Luo J, Chen C, Peng Q, Wang D, Li Y (2018) Electronic structure engineering to boost oxygen reduction activity by controlling the coordination of the central metal. Energy Environ. Sci. 11 (9): 2348-2352.

[S12] Qin Y, Ou Z, Xu C, Liu J, Lan Q, Jin R, Xu X, Guo C, Li H, Si Y (2022) Highly accessible single Mn-N3 sites-enriched porous graphene structure via a confined thermal-erosion strategy for catalysis of oxygen reduction. Chem. Eng. J. 440: 135850.

[S13] Mustain W E, Chatenet M, Page M, Kim Y S (2020) Durability challenges of anion exchange membrane fuel cells. Energy Environ. Sci. 13 (9): 2805-2838.

[S14] Xu H, Xi S, Li J, Liu S, Lyu P, Yu W, Sun T, Qi D-C, He Q, Xiao H, Lin M, Wu J, Zhang J, Lu J (2020) Chemical design and synthesis of superior single-atom electrocatalysts via in situ polymerization. J. Mater. Chem. A 8 (34): 17683-17690.

[S15] Kumar A, Zhang Y, Jia Y, Liu W, Sun X (2021) Redox chemistry of N4-Fe2+ in iron phthalocyanines for oxygen reduction reaction. Chinese J. Catal. 42 (8): 1404-1412.

[S16] Zhong H, Ly K H, Wang M, Krupskaya Y, Han X, Zhang J, Zhang J, Kataev V, Buchner B, Weidinger I M, Kaskel S, Liu P, Chen M, Dong R, Feng X (2019) A phthalocyanine-based layered two-dimensional conjugated metal-organic framework as a highly efficient electrocatalyst for the oxygen reduction reaction. Angew. Chem. Int. Ed. Engl. 58 (31): 10677-10682.

[S17] Abe H, Hirai Y, Ikeda S, Matsuo Y, Matsuyama H, Nakamura J, Matsue T, Yabu H (2019) Fe azaphthalocyanine unimolecular layers (Fe AzULs) on carbon nanotubes for realizing highly active oxygen reduction reaction (ORR) catalytic electrodes. NPG Asia Mater. 11 (1): 57.

[S18] Zeng S, Lyu F, Sun L, Zhan Y, Ma F-X, Lu J, Li Y Y (2019) UiO-66-NO2 as an oxygen “pump” for enhancing oxygen reduction reaction performance. Chem. Mater. 31 (5): 1646-1654. [S19] Xie L, Zhang X P, Zhao B, Li P, Qi J, Guo X, Wang B, Lei H, Zhang W, Apfel U P, Cao R (2021) Enzyme-inspired iron porphyrins for improved electrocatalytic oxygen reduction and evolution reactions. Angew. Chem. Int. Ed. Engl. 60 (14): 7576-7581.

[S20] Qin H, Wang Y, Wang B, Duan X, Lei H, Zhang X, Zheng H, Zhang W, Cao R (2021) Cobalt porphyrins supported on carbon nanotubes as model catalysts of metal-N4/C sites for oxygen electrocatalysis. J. Energy Chem. 53: 77-81.

[S21] Lei H, Zhang Q, Wang Y, Gao Y, Wang Y, Liang Z, Zhang W, Cao R (2021) Significantly boosted oxygen electrocatalysis with cooperation between cobalt and iron porphyrins. Dalton Trans. 50 (15): 5120-5123.

[S22] Yan X, Xu X, Liu Q, Guo J, Kang L, Yao J (2018) Functionalization of multi-walled carbon nanotubes with iron phthalocyanine via a liquid chemical reaction for oxygen reduction in alkaline media. J. Power Sources 389: 260-266.