Supplementary Information

An Atomically Thin Programmable and Photosensitive Monolayer Vanadium Disulfide Memtransistor

Mayukh Das1,#, Akshay Wali 6,#, Amit Kumar Patel 2#, Suyash Rai2, Anand B Puthirat3,  Pulickel M Ajayan 3, Anchal Srivastava2*, Saptarshi Das1,3 4,5,6,*

1Department of Engineering Science and Mechanics, Penn State University, PA 16802, USA

2Department of Physics, Institute of Science, Banaras Hindu University, Varanasi 221005 , India

3Department of Materials Science and Nano Engineering, Rice University, Houston, 77005, USA

4Materials Science and Engineering, Penn State University, PA 16802, USA

5 Department of Materials Characterization Laboratory, Penn State University, PA 16802, USA

6Department of Electrical Engineering, Penn State University, PA 16802, USA

# Equal Contribution

* Corresponding Author: anchal@bhu.ac.in, sud70@psu.edu

Supplementary Information S1. (a) Schematic illustration of the two zone APCVD synthesis process. (b) Optimized temperature profile of zone-1 and zone -2 for synthesis of monolayer VS2 crystals.

Supplementary Information S2: 3D bar plots of the extracted resistance values as a function of different VBG values for each applied VP/E.

Supplementary Information S3: Transfer characteristics in logarithmic scale of a representative memtransistor for different Pin intensities and Vexp values for red, green and blue wavelengths