Strontium-substituted phosphate-based glass exhibits improved and optimized bioactive in vitro and in vivo responses

Jeong-Hyun Ryu1, #, Myung-Jin Lee2, #, Utkarsh Mangal1, Ji-Young Seo1, Il Jun Jeong3, Jin-Young Park5, Ji-Yeong Na5, Kee-Joon Lee1, Hyung-Seog Yu1, Jae-Kook Cha5, *, Jae-Sung Kwon3, 4, *, Sung-Hwan Choi1, *

1Department of Orthodontics, Institute of Craniofacial Deformity, Yonsei University College of Dentistry, 50-1 Yonsei-ro, Seodaemun-gu, Seoul, 03722, Republic of Korea

2Department of Dental Hygiene, Division of Health Science, Baekseok University, 1 Baekseokdaehak-ro, Dongnam-gu, Cheonan-si, Chungcheongnam-do 31065, Republic of Korea

3Department and Research Institute of Dental Biomaterials and Bioengineering, Yonsei University College of Dentistry, 50-1 Yonsei-ro, Seodaemun-gu, Seoul, 03722, Republic of Korea

4BK21 FOUR Project, Yonsei University College of Dentistry, 50-1 Yonsei-ro, Seodaemun-gu, Seoul, 03722, Republic of Korea

5Department of Periodontology, Research Institute for Periodontal Regeneration, Yonsei University College of Dentistry, 50-1 Yonsei-ro, Seodaemun-gu, Seoul, 03722, Republic of Korea

#These authors contributed equally to this work.

*Corresponding Authors: Jae-Kook Cha (chajaekook@yuhs.ac), Jae-Sung Kwon (jkwon@yuhs.ac), and Sung-Hwan Choi (selfexam@yuhs.ac).

Table S1. Sequence of primer used in qPCR in this study

| Molecules | Primer sequences (5’- 3’) | Product size (bp) | Accession number from NCBI database |
| --- | --- | --- | --- |
| RUNX2 OCN OSX BSP TNF-α IL-1β IL-6 CXCL10 NOS2 CD80 GAPDH | Forward: GGGAACCAAGAAGGCACAGA Reverse: ACTTGGTGCAGAGTTCAGGG Forward: TTGGCCCAGACCTAGCAGA Reverse: CTGGGCTTGGCATCTGTGA Forward: GTCCTCTCTGCTTGAGGAAGAA Reverse: TCTTTGTGCCTCCTTTCCCC Forward: CGGTTTCCAGTCCAGGGAGG Reverse: CGAGAGTGTGGAAAGTGTGGA Forward: TGTAGCCCACGTCGTAGCAAA Reverse: TGTGGGTGAGGAGCACGTA Forward: TGCCACCTTTTGACAGTGATG Reverse: ATGTGCTGCTGCGAGATTTG Forward: TCTTGGGACTGATGCTGGTG Reverse: TTGCCATTGCACAACTCTTTTC Forward: ATGACGGGCCAGTGAGAATG Reverse: AGGAGCCCTTTTAGACCTTTTT Forward: GGTGAAGGGACTGAGCTGTT Reverse: ACGTTCTCCGTTCTCTTGCAG Forward: CACCTGGGAAAAACCCCCA Reverse: ATGACAACGATGACGACGACT Forward: CCCACTCTTCCACCTTCGATG Reverse: CGAGTTGGGATAGGGCCTCT | 152 100 131 174 197 136 178 188 103 105 201 | NM_001271627.1 NM_007541.3 NM_130458.4 NM_008318.3 NM_013693.3 NM_008361.4 NM_001314054.1 NM_021274.2 NM_010927.1 NM_001359898.1 NM_001289726.1 |

Table S2. The composition of BG used in this study

|  | SiO2 | CaO | Na2O | P2O5 |
| --- | --- | --- | --- | --- |
| BG | 46.1 mol% | 26.9 mol% | 24.4 mol% | 2.6 mol% |

BG; 45S5 bioactive glass

To obtain the BG, SiO2 (Sigma Aldrich), CaCO3 (Sigma Aldrich), Na2CO3 (Sigma Aldrich), P2O5 (Sigma Aldrich) were used. The composition of fabricated BG is summarized in Table S2. The mixture was placed in alumina crucible and heated to an intermediate step at 900 °C for 90 min to remove the carbon dioxide and impurity, followed by a second step at 1350 °C for 4h followed by quenching at 25 °C.

Table S3. Energy dispersive spectrometry of PBG and PSr samples

Unit: Atomic %

| Code | P | Ca | Na | Sr |
| --- | --- | --- | --- | --- |
| PBG | 63.41 | 17.58 | 19.01 | 0.00 |
| PSr1.5 | 62.69 | 15.53 | 20.94 | 0.84 |
| PSr3 | 63.17 | 15.61 | 19.59 | 1.63 |
| PSr6 | 63.94 | 12.94 | 19.85 | 3.27 |
| PSr15 | 64.20 | 8.28 | 19.98 | 7.54 |
| PSr30 | 67.95 | 0.00 | 17.70 | 14.35 |

P; Phosphorous; Ca; Calcium; Na; Sodium; Sr; Strontium.

PBG was detected in P, Ca, and Na. PSr samples ranging from 1.5 to 15 mol% SrO were detected to P, Ca, Na, and Sr atoms. According to EDS analysis, it is successfully fabricated to PBG and PSr samples. PBG; Phosphate-based glass; PSr; strontium substituted PBG.

Table S4. Detection of P, Ca, and Sr ion release of PBG and PSr groups on 1 day

Unit: ng/μL

| Day 1 | P | Ca | Sr |
| --- | --- | --- | --- |
| PBG | 226.013 ± 0.335f | 78.757 ± 0.247e | - |
| PSr1.5 | 219.297 ± 1.933e | 67.717 ± 0.289d | 7.773 ± 0.035a |
| PSr3 | 209.913 ± 1.062d | 63.947 ± 0.267c | 15.307 ± 0.068b |
| PSr6 | 190.760 ± 0.317c | 50.033 ± 0.260b | 25.990 ± 0.141c |
| PSr15 | 171.607 ± 0.438b | 29.800 ± 0.078a | 42.700 ± 0.135d |
| PSr30 | 58.620 ± 0.433a | - | 57.790 ± 0.050e |
| p-value | 6.2 × 10-22 | 2.8 × 10-19 | 1.4 × 10-23 |

Data represented the mean and standard deviation and performed to one-way analysis of variance (ANOVA) with Tukey’s post hoc test at a confidence level of 95%. The different small letter was a significant difference. PBG; phosphate-based glass; PSr; strontium substituted PBG.

Table S5. Cumulative ion release of P, Ca, and Sr ion for PBG and PSr groups on 7 days

Unit: ng/μL

| Day 7 | P | Ca | Sr |
| --- | --- | --- | --- |
| PBG | 287.703 ± 0.712e | 104.683 ± 0.359e | - |
| PSr1.5 | 288.990 ± 2.222e | 94.473 ± 0.473d | 10.500 ± 0.061a |
| PSr3 | 279.280 ± 1.259d | 88.817 ± 0.294c | 20.670 ± 0.080b |
| PSr6 | 262.400 ± 1.700c | 73.107 ± 0.405b | 37.343 ± 0.220c |
| PSr15 | 234.123 ± 0.481b | 40.833 ± 0.072a | 74.513 ± 0.217d |
| PSr30 | 105.213 ± 0.675a | - | 79.350 ± 0.095e |
| p-value | 7.7 × 10-21 | 5.4 ×10-19 | 1.8 × 10-23 |

Data represented the mean and standard deviation and performed one-way analysis of variance (ANOVA) with Tukey’s post hoc test at a confidence level of 95%. The different small letter was a significant difference. PBG; phosphate-based glass; PSr; strontium substituted PBG.

Table S6. Cumulative ion release of P, Ca, and Sr ion for PBG and PSr groups on 14 days

Unit: ng/μL

| Day 14 | P | Ca | Sr |
| --- | --- | --- | --- |
| PBG | 292.400 ± 0.882d | 107.200 ± 0.346e | - |
| PSr1.5 | 296.543 ± 2.174e | 97.930 ± 0.529d | 10.920 ± 0.070a |
| PSr3 | 288.880 ± 1.354d | 93.023 ± 0.378c | 21.730 ± 0.105b |
| PSr6 | 277.503 ± 1.822c | 78.477 ± 0.418b | 40.257 ± 0.226c |
| PSr15 | 251.900 ± 0.642b | 44.307 ± 0.051a | 81.650 ± 0.173d |
| PSr30 | 143.357 ± 2.379a | - | 95.727 ± 0.313e |
| p-value | 5.3 × 10-20 | 1.8 × 10-18 | 4.4 × 10-23 |

Data represented the mean and standard deviation and performed to one-way analysis of variance (ANOVA) with Tukey’s post hoc test at a confidence level of 95%. The different small letter was a significant difference. PBG; phosphate-based glass; PSr; strontium substituted PBG.

Table S7. Cumulative ion release of P, Ca, and Sr ion for PBG and PSr group on 21 days

Unit: ng/μL

| Day 21 | P | Ca | Sr |
| --- | --- | --- | --- |
| PBG | 295.483 ± 1.004d | 108.417 ± 0.357e | - |
| PSr1.5 | 300.433 ± 1.963e | 99.390 ± 0.010d | 11.110 ± 0.070a |
| PSr3 | 295.693 ± 1.316d | 94.877 ± 0.363c | 22.207 ± 0.104b |
| PSr6 | 285.167 ± 2.061c | 80.843 ± 0.355b | 41.593 ± 0.200c |
| PSr15 | 264.277 ± 0.656b | 45.943 ± 0.040a | 85.480 ± 0.131d |
| PSr30 | 143.357 ± 2.379a | - | 105.617 ± 0.306e |
| p-value | 8.0 × 10-19 | 1.2 × 10-18 | 7.8 ×10-24 |

Data represented the mean and standard deviation and performed to one-way analysis of variance (ANOVA) with Tukey’s post hoc test at a confidence level of 95%. The different small letter was a significant difference. PBG; phosphate-based glass; PSr; strontium substituted PBG.

Table S8. Cumulative ion release of P, Ca, and Sr ion for PBG and PSr group on 28 days

Unit: ng/μL

| Day 28 | P | Ca | Sr |
| --- | --- | --- | --- |
| PBG | 296.320 ± 1.189d | 109.263 ± 0.067a | - |
| PSr1.5 | 302.147 ± 1.862e | 100.490 ± 0.608d | 11.260 ± 0.078a |
| PSr3 | 298.040 ± 1.083de | 95.953 ± 0.377c | 22.517 ± 0.114a |
| PSr6 | 289.703 ± 1.658c | 82.520 ± 0.426b | 42.647 ± 0.242b |
| PSr15 | 269.007 ± 0.774b | 47.017 ± 0.029a | 88.470 ± 0.147c |
| PSr30 | 154.413 ± 2.681a | - | 114.267 ± 0.193d |
| p-value | 1.5 × 10-18 | 4.9 × 10-18 | 1.3 × 10-24 |

Data represented the mean and standard deviation and performed to one-way analysis of variance (ANOVA) with Tukey’s post hoc test at a confidence level of 95%. The different small letter was a significant difference. PBG; phosphate-based glass; PSr; strontium substituted PBG.

Table S9. pH measurement of PBG and PSr for 28 days

| Code | Day 1 | Day 7 | Day 14 | Day 21 | Day 28 |
| --- | --- | --- | --- | --- | --- |
| PBG | 4.83 ± 0.06a | 4.51 ± 0.01a | 4.32 ± 0.04a | 4.23 ± 0.05a | 4.25 ± 0.01a |
| PSr1.5 | 5.82 ± 0.60b | 4.51 ± 0.01a | 4.21 ± 0.05a | 4.21 ± 0.05a | 4.22 ± 0.03a |
| PSr3 | 6.38 ± 0.13bc | 4.53 ± 0.01a | 4.25 ± 0.01a | 4.22 ± 0.01a | 4.23 ± 0.01a |
| PSr6 | 6.46 ± 0.13bc | 4.60 ± 0.01b | 4.26 ± 0.04b | 4.22 ± 0.01a | 4.23 ± 0.03a |
| PSr15 | 6.74 ± 0.05c | 4.76 ± 0.04c | 4.37 ± 0.01c | 4.24 ± 0.04a | 4.25 ± 0.03a |
| PSr30 | 6.99 ± 0.15c | 5.79 ± 0.03d | 5.28 ± 0.03d | 4.90 ± 0.03b | 4.79 ± 0.01b |
| p-value | 4.6 × 10-6 | 1.1 × 10-16 | 2.2 × 10-13 | 6.1 × 10-11 | 2.2 × 10-13 |

Data represented the mean and standard deviation and performed to one-way analysis of variance (ANOVA) with Tukey’s post hoc test at a confidence level of 95%. The different small letter was a significant difference. PBG; phosphate-based glass; PSr; strontium substituted PBG.