Supplemental Material for “Vacancy-mediated anomalous phononic and electronic transport in defective half-Heusler ZrNiBi”

Wuyang Rena,b,†, Wenhua Xuec,†, Shuping Guod,†, Ran Hed, Liangzi Dengb, Shaowei Songb, Andrei Sotnikovd, Kornelius Nielschd, Jeroen van den Brinkd, Guanhui Gaoe, Shuo Chenb, Yimo Hane, Jiang Wua, Ching-Wu Chub, Zhiming Wanga,*, Yumei Wangc,*, Zhifeng Renb,*

a Institute of Fundamental and Frontier Sciences, University of Electronic Science and Technology of China, Chengdu 610054, People’s Republic of China

b Department of Physics and Texas Center for Superconductivity at the University of Houston (TcSUH), Houston, Texas 77204, United States

c Beijing National Laboratory for Condensed Matter Physics, Institute of Physics, Chinese Academy of Science, Beijing 100190, People’s Republic of China

d Leibniz Institute for Solid State and Materials Research, Dresden 01069, Germany

e Department of Materials Science and Nano-Engineering, Rice University, Houston, Texas 77005, United States

Single parabolic band model

According to the single parabolic band (SPB) model, the Hall carrier concentration (nH) and the Seebeck coefficient (S) are given by1

nH=4π2m*kBT32h34F02(ξF)3F-12(ξF)									(S1)

S=-kBe[2F1ξFF0ξF-ξF]										(S2)

FnξF=0∞χn1+exp⁡(χ-ξF)dχ									(S3)

ξF=EFkBT											(S4)

where h is the Planck constant, kB is the Boltzmann constant, e is the electron charge, m* is the density of states effective mass, Fn(ξF) is the Fermi integral, ξF is the reduced Fermi energy, and χ is the reduced carrier energy.

Deduction for (M)-12 dependence of vs

The relationship between sound velocity (vs) and the average atomic mass in a unit cell (M) can be deduced by interconnecting kinetic and elastic energy as follows2

vs=[13(2vt3+1vl3)]-13										(S5)

vt=(Gρ)1/2											(S6)

vl=(4G+3B3ρ)1/2										(S7)

ρ=nMa3NA											(S8)

where vt is the transversal sound velocity, vl is the longitudinal sound velocity, G is the shear modulus, B is the bulk modulus, ρ is the density, n is the number of atoms in a unit cell, a is the lattice constant, and NA is the Avogadro constant. Following Equations S5-S8, vs shows a (M)-12 dependence:

vs=(M)-12(a3NAn)12(ELA)-1/3								(S9)

ELA=23G-32+13(43G+B)-3/2								(S10)

By comparing the sound velocity of possible ternary half-Heuslers from the AFLOWLIB.org database3 (denoted as vsDB) and that deduced from Equations S9 and S10 (denoted as vsELA), the deviation is within ~3%. The corresponding data are shown in Table S1.

Table S1. Elastic property and sound velocity of possible ternary half-Heuslers from the AFLOWLIB.org database.

| Material | Space group | Lattice constant a (Å) | Shear modulus G (GPa) | Bulk modulus B (GPa) | Sound velocity vs (m s-1) |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | vsDB | vsELA |
| ScNiSb | F43m | 6.16 | 61.92 | 98.84 | 3403 | 3448 |
| TiNiSn | F43m | 6.00 | 60.94 | 134.2 | 3253 | 3314 |
| TiCoSb | F43m | 5.89 | 75.95 | 143.2 | 3499 | 3560 |
| HfPdSn | F43m | 6.37 | 53.74 | 122.7 | 2493 | 2545 |
| TaRuSb | F43m | 6.19 | 72.16 | 176 | 2769 | 2829 |
| NbFeSb | F43m | 5.95 | 79.44 | 166.8 | 3342 | 3406 |
| ZrCoBi | F43m | 6.19 | 62.85 | 122.6 | 2736 | 2786 |
| NbRuSb | F43m | 6.19 | 68.38 | 169.4 | 3046 | 3115 |
| ScNiBi | F43m | 6.30 | 50.3 | 86.94 | 2698 | 2735 |
| YNiSb | F43m | 6.35 | 54.64 | 87.63 | 3062 | 3102 |
| YNiBi | F43m | 6.46 | 49.22 | 83.67 | 2592 | 2629 |
| TiPtSn | F43m | 6.28 | 49.05 | 132.1 | 2465 | 2523 |
| ScPdSb | F43m | 6.41 | 41.98 | 96.36 | 2708 | 2761 |
| ScPtSb | F43m | 6.42 | 51.05 | 110 | 2595 | 2648 |
| YPtSb | F43m | 6.60 | 46.5 | 99.17 | 2440 | 2487 |
| VFeSb | F43m | 5.79 | 62.44 | 155.4 | 3099 | 3165 |
| VRuSb | F43m | 6.05 | 50.04 | 158.6 | 2705 | 2778 |

Figure S1. (A) XRD patterns of Zr0.88NiBi and Zr0.90NiBi with and without an additional annealing process. (B) XRD patterns of Zr0.88Ni1-xCoxBi1-ySby.

Figure S2. HAADF-STEM intensity profile within the Bi-atom plane of Zr0.88NiBi.

Figure S3. Thermal diffusivity (top), total thermal conductivity (middle), and lattice contribution to total thermal conductivity (bottom) for Zr0.88Ni1-xCoxBi at different temperatures.

Figure S4. Temperature-dependent (A) Seebeck coefficient and electrical conductivity and (B) total thermal conductivity and figure-of-merit for Zr0.88Ni0.57Co0.43Bi1-ySby.

References

1.	He, R. et al. Achieving high power factor and output power density in p-type half-Heuslers Nb1-xTixFeSb. Proc. Natl. Acad. Sci. USA 113, 13576-13581 (2016).

2.	Rogl, G. et al. Mechanical properties of half-Heusler alloys. Acta Mater. 107, 178-195 (2016).

3	Curtarolo, S. et al. AFLOW: an automatic framework for high-throughput materials discovery. Comput. Mater. Sci. 58, 218-226 (2012).