# Supplementary Information

# Rheological and spectroscopic study of luminescent Eu3+-doped gellan gum

Francisco R. Torres1; Victor Hugo Vitorino Sarmento2; Hernane S. Barud3; José Maurício A. Caiut1

1Grupo de Nanomateriais e Sistemas Luminescentes, Departamento de Química, Faculdade de Filosofia, Ciências e Letras de Ribeirão Preto, Universidade de São Paulo, 14040-901 Ribeirão Preto, São Paulo, Brasil

2Departamento de Química, Universidade Federal de Sergipe, 49100-000, Itabaiana, Sergipe, Brasil.

3Laboratório de Biopolímeros e Biomateriais, Universidade de Araraquara/Uniara, 14801- 320, Araraquara- São Paulo, Brasil.

* Corresponding author: caiut@ffclrp.usp.br

# 1. Results

## 1.1. FTIR

Fig. S1 FTIR spectra of film samples (a) LAGG and (b) HAGG_ P (black); _Eu_0.5 (blue) and _Eu_2.0 (red)

Table S1 Band assignments of FTIR spectra of LAGG and HAGG samples, according to Silva-Correia et al. and Pereira et al.

| Assignments | Wavenumber (cm-1) |  |
| --- | --- | --- |
|  | LAGG samples | HAGG samples |
| O-H stretching | 3380 | 3389 |
| C-H stretching | 2925 | 2933 |
| C-O stretching | - | 1724 |
| COO- asymmetric stretching | 1608 | 1613 |
| COO- symmetrical stretching | 1409 | 1406 |
| C-O stretching | 1044 | 1030 |

## 1.2. Rheology

Fig. S2 Amplitude sweep test rheogram at 37 °C showing the G’ (filled circles) and G” (outlined circles) curves along the analysis of (a) LAGG_Eu_2.0 sample (red) comparing to LAGG_P (black) and (b) HAGG_Eu_2.0 sample (blue) compared to HAGG_P (gray)

Table S2 Parameters calculated from the intersection points of the G’ and G’’ curves of the LAGG and HAGG gels by varying the Eu3+ ion concentrations in the gels during the amplitude sweep analysis at 37.0 ºC

| Sample | LAGG |  | HAGG |  |
| --- | --- | --- | --- | --- |
|  | Strain in G’=G” (%) | G’=G” (Pa) | Strain in G’=G” (%) | G’=G” (Pa) |
| Pristine | 59.1 | 32.7 | 344.1 | 23.4 |
| Eu_0.1 | 58.6 | 30.0 | 350.5 | 20.9 |
| Eu_0.2 | 36.5 | 41.6 | 365.1 | 10.9 |
| Eu_0.5 | 73.6 | 98.7 | 346.5 | 23.9 |
| Eu_1.0 | 16.5 | 362.6 | 340.9 | 21.8 |
| Eu_2.0 | 8.0 | 3158.0 | 143.0 | 24.5 |

Fig. S3 Frequency sweep test rheogram with the HAGG_Eu_2.0 sample (25 °C - blue and 37°C - cyan) and HAGG_P (25 °C - black and 37 °C - gray) showing the G’ (filled circles) and G” (outlined circles) moduli

Fig. S4 Complex viscosities at 25 °C (a) and 37 °C (b) of pure HAGG (black), HAGG_Eu_0.1 (blue), HAGG_Eu_0.2 (green), HAGG_Eu_0.5 (yellow), HAGG_Eu_1.0 (orange) and HAGG_Eu_2.0 (red) samples

## 1.3. Luminescence

Fig. S5 (a) Excitation spectra (λem 612 nm) and (b) emission spectra (λex 394 nm) of Eu3+-doped LAGG films (% w/w, Eu3+/GG)

Fig. S6 (a) Excitation spectra (λem 612 nm) and (b) emission spectra (λex 394 nm) of Eu3+-doped HAGG films (% w/w, Eu3+/GG)

Fig. S7 Lifetime curves (ln scale) of the (a) LAGG_Eu_2.0 and (b) HAGG_Eu_2.0 (black line – λ 330 nm and red line – λ 394 nm) samples

Fig. S8 Lifetime curves (ln scale) of the sample LAGG_Eu2.0_TTA1 (λ 280 nm - blue; λ 370 nm - black and λ 394 nm- red)