Efficient adsorption on Cr(VI) and electrochemical application of N,P co-doped carbon spheres

Tian Luoa, Xianjun Xinga*, Xuefei Zhangb, Wang Yuec, Xiufen Mab, Peiyong Mab

a School of Chemistry and Chemical Engineering, Hefei University of Technology, Hefei, Anhui 230009, China

b School of Mechanical Engineering, Hefei University of Technology, Hefei, Anhui 230009, China

c Hefei Institutes of Physical Science, Chinese Academy of Sciences, Hefei, Anhui 230009, China

Table S1. Specific surface area and pore size distribution of NxPBC1-400

| Sample | SBET /m2·g-1 | SMic /m2·g-1 | VMic /cm3·g-1 | DAver /nm |
| --- | --- | --- | --- | --- |
| N0PBC1-400 | 1,151.13 | 512.83 | 0.25 | 2.52 |
| N0.5PBC1-400 | 1,213.91 | 672.18 | 0.33 | 2.20 |
| N1PBC1-400 | 1,271.45 | 686.22 | 0.35 | 2.22 |
| N2PBC1-400 | 1,295.48 | 704.34 | 0.40 | 2.30 |
| N3PBC1-400 | 1,198.47 | 425.20 | 0.21 | 2.24 |

Table S2. Surface element composition of NxPBC1-400

| Sample | Distributions of nitrogen species/at.% |  |  |  |
| --- | --- | --- | --- | --- |
|  | Pyridinic-N | Pyrrolic-N | Graphitic-N | Oxidized-N |
| N0PBC1-400 | 12.31 (0.16) | 23.77 (0.32) | 39.33 (0.52) | 24.59 (0.33) |
| N0.5PBC1-400 | 29.19 (0.95) | 28.34 (0.92) | 25.49 (0.83) | 16.95 (0.55) |
| N1PBC1-400 | 27.23 (0.96) | 36.71 (1.29) | 21.56 (0.76) | 14.48 (0.51) |
| N2PBC1-400 | 35.07 (1.54) | 39.35 (1.73) | 15.04 (0.66) | 10.54 (0.46) |
| N3PBC1-400 | 32.92 (1.37) | 35.45 (1.47) | 20.24 (0.84) | 11.38 (0.47) |

Table S3 Pseudo-first-order, Pseudo-second-order, elovich and intraparticle diffusion for the adsorption of Cr(VI) on N2PBC1-400.

| model | C0(mg·L-1) | 20 | 50 | 100 | 200 |
| --- | --- | --- | --- | --- | --- |
|  | qe,exp(mg·g-1) | 10 | 25 | 45 | 77.5 |
| The pseudo-first-order kinetic mode | qe,cal(mg·g-1) | 9.85 | 23.67 | 41.11 | 68.11 |
|  | k1(min-1) | 0.623 | 0.355 | 0.231 | 0.032 |
|  | R2 | 0.98 | 0.91 | 0.91 | 0.84 |
| The pseudo-second-order kinetic model | qe,cal(mg·g-1) | 10.05 | 24.40 | 42.39 | 72.65 |
|  | k2(g·mg-1·min-1) | 0.114 | 0.023 | 0.009 | 0.001 |
|  | R2 | 0.99 | 0.97 | 0.96 | 0.93 |
| Elovich model | A(mg·g-1·min-1) | 7.406 | 13.883 | 27.556 | 11.116 |
|  | B(g·mg-1 ) | 0.471 | 1.894 | 2.582 | 9.726 |
|  | R2 | 0.91 | 0.95 | 0.99 | 0.98 |
| Intraparticle diffusion model | C(mg·g-1) | 7.464 | 15.822 | 28.499 | 30.679 |
|  | kid(mg·g-1·min-1/2) | 0.1184 | 0.408 | 0.661 | 1.738 |
|  | R2 | 0.19 | 0.39 | 0.36 | 0.69 |

Table S4 Parameters of the Langmuir and Freundlich models

| T(K) | qe,exp (mg·g-1) | Langmuir |  |  |  |  | Freundlich |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | KL (L·mg-1) | qmax (mg·g-1) | RL | R2 |  | KF (mg(1-n)·Ln·g-1) | 1/n | R2 |
| 298 | 90 | 0.0771 | 95.5599 | 0.03~0.39 | 0.98 |  | 30.7885 | 0.206 | 0.80 |
| 308 | 98 | 0.1049 | 103.5207 | 0.02~0.32 | 0.99 |  | 36.2221 | 0.197 | 0.83 |
| 318 | 100.55 | 0.1352 | 105.7635 | 0.01~0.26 | 0.99 |  | 39.9790 | 0.186 | 0.84 |

Table S5 The thermodynamic activation parameters of adsorption Cr(VI) onto N2PBC1-400.

|  | ΔH0 (KJ·mol-1) | ΔS0 (J·mol-1·K-1) | ΔG0(KJ·mol-1) |  |  |
| --- | --- | --- | --- | --- | --- |
|  |  |  | 298K | 308K | 318K |
| N2PBC1-400 | 22.07 | 11.02 | -10.76 | -11.91 | -12.97 |

Table S6 The binding energies and relative contents of C, O, N, P and Cr in N2PBC1-400 and N2PBC1-400-Cr

| Element | Assignment | N2PBC1-400 |  |  | N2PBC1-400-Cr |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Binding energy (Ev) | Relative Content (%) | Absolute content (%) | Binding Energy (Ev) | Relative Content (%) | Absolute content (%) |
| C 1s | C=C | 284.67 | 50.35 | 40.21 | 284.70 | 43.29 | 32.81 |
|  | C-O | 285.50 | 23.85 | 19.04 | 285.55 | 19.09 | 14.47 |
|  | C=O | 286.98 | 14.18 | 11.32 | 286.80 | 24.57 | 18.63 |
|  | O=C-OH | 289.20 | 11.62 | 9.27 | 289.20 | 13.05 | 9.89 |
| O 1s | C=O/P=O | 531.20 | 22.08 | 3.23 | 532.67 | 44.13 | 7.54 |
|  | C-O/P-O | 532.76 | 63.45 | 9.27 | - | - |  |
|  | O=C-O /O=P-O | 533.88 | 14.47 | 2.11 | 533.89 | 17.52 | 2.99 |
|  | Cr-O | - | - | - | 531.45 | 38.35 | 6.55 |
| N 1s | pyridinic N | 398.77 | 35.07 | 1.54 | 398.79 | 33.19 | 1.03 |
|  | pyrrolic N | 400.40 | 39.35 | 1.73 | 400.23 | 35.62 | 1.11 |
|  | Graphitic N | 401.46 | 15.04 | 0.66 | 401.26 | 22.27 | 0.69 |
|  | oxidized N | 402.89 | 10.54 | 0.46 | 402.88 | 8.92 | 2.79 |
| P 2p | P-C | 132.80 | 24.08 | 0.48 | 132.79 | 25.43 | 0.33 |
|  | P-N | 133.65 | 37.19 | 0.75 | 133.54 | 27.96 | 0.36 |
|  | P-O | 134.52 | 38.73 | 0.78 | 134.22 | 46.61 | 0.61 |
| Cr 2p1/2 | Cr(Ⅲ) | - | - | - | 587.32 | 19.55 | 0.50 |
|  | Cr(VI) | - | - | - | 588.28 | 17.14 | 0.44 |
| Cr 2p3/2 | Cr(Ⅲ) | - | - | - | 577.62 | 35.12 | 0.90 |
|  | Cr(VI) | - | - | - | 578.99 | 28.19 | 0.73 |

Corresponding author. Tel: 86-0551-62902960. E-mail: xxianjun@hfut.edu.cn (Xianjun Xing)