Supplementary information for

Cubic Fe-bearing majorite synthesized at 18-25 GPa and 1000 °C: implications for element transport, subducted slab rheology and diamond formation

Vincenzo Stagno1,9*, Luca Bindi2, Barbara Bonechi3, Steeve Greaux4,5, Sonja Aulbach6, Tetsuo Irifune4,5, Stefano Lupi7,10, Giulia Marras1, Catherine A. McCammon8, Manuela Nazzari9, Federica Piccirilli F.10, Brent T. Poe11, Claudia Romano12, Piergiorgio Scarlato9

1Dipartimento di Scienze della Terra, Sapienza Università di Roma, Roma, Italy.

2Dipartimento di Scienze della Terra, Università di Firenze, Firenze, Italy.

3University of Manchester, Manchester, United Kingdom.

4Geodynamic Research Center, Ehime University, Matsuyama, Japan.

5Earth-Life Science Institute, Tokyo Institute of Technology, Tokyo, Japan.

6Goethe University, Institute for Geosciences; Frankfurt Isotope & Element Research Center (FIERCE), Altenhöferallee 1, 60438 Frankfurt, Germany.

7Department of Physics, Sapienza University of Rome, 00185 Rome, Italy.

8Bayerisches Geoinstitut, Bayreuth Universität, Bayreuth, Germany.

9Istituto Nazionale di Geofisica e Vulcanologia, Roma, Italy.

10CNR-IOM, Area Science Park, I-34012 Trieste, Italy.

11Dipartimento di Scienze, Università di Chieti, Chieti, Italy.

12Dipartimento di Scienze, Università di Roma Tre, Roma, Italy.

*Corresponding author: Vincenzo Stagno (vincenzo.stagno@uniroma1.it).

Figure S1. Schematic cross section of the cell assembly used in this study.

Figure S2. Selected single-crystal X-ray diffraction peaks of a majorite fragment extracted from run M82.

Figure S3. X-ray powder diffraction pattern collected from the majorite fragment (run M82). All peaks can be assigned to cubic majorite.

M82

M81

Figure S4. Fitted Mössbauer spectra showing the presence of Fe all as Fe3+. Spectra were fitted to one doublet.

Figure S5. Hyperfine parameters (center shift vs quadruple splitting) from our study plotted along with literature data for both natural28,48 and synthetic49,50 majorites.

Figure S6. Longitudinal and Shear velocities of MORB garnet solid solutions as a function of pressure, at 300 K. Plain lines represent our calculated velocities for [CaNaMg][SiAl]Si3O12 majorite (red), pyrolitic (blue) and MORB (thick black) majorite garnet, and an upper mantle MORB garnet (thin black) with an assumed composition (in wt.%) of  43% pyrope, 27% grossular and 30% almandine (e.g. ref. 60, Table 3, 5 GPa, 1200 °C). The open square and circle symbols represent the corresponding experimental data for the pyrolitic and MORB majorite garnet; Our calculated VP and VS are fairly consistent with those of experimental studies at P > 10 GPa, which corresponds to the depths of the mantle transition region.

Table S1.  Chemical composition of the glass used as starting material.

| This study WM6.80 |  | Bobrov et al.39 |
| --- | --- | --- |
|  | Wt% Cpx [15] | Wt% Di40Hd10Jd50 |
| SiO2 | 54.60(42) | 56.55 |
| MgO | 9.43(9) | 7.59 |
| Al2O3 | 10.52(8) | 12 |
| CaO | 15.30(17) | 13.20 |
| FeOtot | 3.36(4) | 3.38 |
| Na2O | 5.63(31) | 7.29 |
| TiO2 | 0.17(2) | - |
| Total | 99.01(44) | 100 |

Notes: In brackets is the number of points analysed by electron microprobe. WM6.80Cpx is synthetic glass with composition similar to natural Cpx reported by Stosch and Lugmair85. Errors in parentheses are 1σ.

Table S2. Experimental run conditions.

| Run | P (ton) | T(°C) | Duration (min) | Pressure marker | Phases |
| --- | --- | --- | --- | --- | --- |
| M81 | 400 | 1000 | 15 | rwd | Cubic majorite |
| M82 | 450 | 1000 | 30 | rwd + pv (+ per) | Cubic majorite |

rwd = ringwoodite; maj = majorite; per = periclase; pv = Mg-perovskite