Schedule. 1. crystallinity of cellulose under different conditions

| Number | reaction condition | crystallinity, % |
| --- | --- | --- |
| A | Not alkali extraction+E65% | 60.75 |
| B | Caustic extraction+E65% | 63.97 |
| C | Caustic extraction+E0% | 68.75 |
| D | Caustic extraction+E10% | 58.33 |
| E | Caustic extraction+E30% | 50.76 |
| F | Not alkali extraction+E65%+U600W | 51.64 |
| G | Caustic extraction+E65%+U600W | 65.62 |
| H | Caustic extraction+E0%+U600W | 41.90 |
| I | Caustic extraction+E10%+U600W | 59.51 |
| J | Caustic extraction+E30%+U600W | 55.42 |

Other conditions. Temperature: 120 oC, Alkali amount: 35%, Ethanol concentration: 65%, Heat preservation time: 180 min, Solid-liquid ratio: 1:8, Oxygen partial pressure: 0.5 MPa.

Schedule. 2. crystallinity of cellulose under different conditions

| Number | reaction condition | crystallinity, % |
| --- | --- | --- |
| a | Not alkali extraction+E65% | 57.79 |
| b | Caustic extraction+E65% | 58.52 |
| c | Caustic extraction+E0% | 52.27 |
| d | Caustic extraction+E10% | 60.98 |
| e | Caustic extraction+E30% | 57.14 |
| f | Not alkali extraction+E65%+U1000W | 53.64 |
| g | Caustic extraction+E65%+U1000W | 42.72 |
| h | Caustic extraction+E0%+U1000W | 59.42 |
| i | Caustic extraction+E10%+U1000W | 62.28 |
| j | Caustic extraction+E30%+U1000W | 43.80 |

Other conditions: Temperature: 120 oC, Alkali amount: 35%, Heat preservation time: 180 min, Solid-liquid ratio: 1:8, Oxygen partial pressure: 0.5 MPa.