Supplementary

Adsorption activity of spent coffee ground biochar for the removal of Vivizole Red 3BS dye from aqueous solution

Admasu Adamu a *, Feleke Zewge a,b, Yonas Chebude a,b,

a Africa Center of Excellence for Water Management, Addis Ababa University, Addis Ababa, Ethiopia

b Department of Chemistry, College of Natural and Computational Sciences, Addis Ababa University, Addis Ababa, Ethiopia

S1 Physicochemical characteristics of real wastewater (VR 3BS 150 % dye) of the cotton industry

Parameter				Value

pH					12.44

COD (mg O2 L-)			6,885

BOD5 (mg O2 L-)			1,377

Dey concentration (mg/L)		665

Turbidity (NTU)			34.4

Conductivity (µS cm-1)		48.4

TDS (mg/L)				28, 600

TOC (ppm)				319

Total alkalinity (mg/L)		4,400

Chloride Concentration (mg/L)	18, 465

Total Hardness as CaCO3 (mg/L)	440

NO3-N (mg/L)				50

SO42- (mg/L)				600

PO43- (mg/L)				2

NH3-N (mg/L)				28.5

S2 Actual versus predicted VR 3BS dye removal from aqueous solution by activated SCG biochar

| Run | Initial Dye concentration (mg/L) | pH | Dose (g/L) | Contact time (min) | VR 3BS dye removal (%) |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | Actual | Predicted |
| 1 | 20 | 6.5 | 7.5 | 90 | 71.6 | 72.53 |
| 2 | 40 | 3 | 10 | 120 | 80.65 | 81.87 |
| 3 | 40 | 6.5 | 7.5 | 90 | 66.33 | 65.71 |
| 4 | 20 | 10 | 5 | 120 | 64.98 | 64.18 |
| 5 | 40 | 10 | 5 | 60 | 61.02 | 60.41 |
| 6 | 20 | 3 | 10 | 120 | 89.32 | 90.30 |
| 7 | 20 | 3 | 10 | 60 | 94.3 | 91.12 |
| 8 | 40 | 3 | 5 | 120 | 64.08 | 61.29 |
| 9 | 30 | 3 | 7.5 | 90 | 75.7 | 76.91 |
| 10 | 30 | 6.5 | 7.5 | 90 | 67.53 | 63.89 |
| 11 | 20 | 3 | 5 | 120 | 89.85 | 89.28 |
| 12 | 40 | 10 | 10 | 60 | 71.9 | 72.02 |
| 13 | 30 | 6.5 | 7.5 | 60 | 71.9 | 70.95 |
| 14 | 20 | 10 | 5 | 60 | 67.3 | 65.62 |
| 15 | 20 | 10 | 10 | 120 | 61.03 | 60.41 |
| 16 | 30 | 6.5 | 7.5 | 90 | 63.9 | 63.89 |
| 17 | 20 | 10 | 10 | 60 | 54.5 | 57.67 |
| 18 | 30 | 6.5 | 7.5 | 90 | 62.7 | 63.89 |
| 19 | 30 | 6.5 | 7.5 | 120 | 69.07 | 70.32 |
| 20 | 20 | 3 | 5 | 60 | 92.5 | 94.28 |
| 21 | 30 | 6.5 | 5 | 90 | 51.97 | 53.74 |
| 22 | 30 | 6.5 | 7.5 | 90 | 60.6 | 63.89 |
| 23 | 30 | 6.5 | 10 | 90 | 61.53 | 60.06 |
| 24 | 40 | 3 | 5 | 60 | 65.13 | 65.30 |
| 25 | 30 | 10 | 7.5 | 90 | 60.43 | 59.52 |
| 26 | 40 | 10 | 10 | 120 | 77.15 | 75.75 |
| 27 | 30 | 6.5 | 7.5 | 90 | 65.97 | 63.89 |
| 28 | 40 | 10 | 5 | 120 | 57.23 | 59.96 |
| 29 | 30 | 6.5 | 7.5 | 90 | 63.57 | 63.89 |
| 30 | 40 | 3 | 10 | 60 | 80.52 | 81.70 |

S3 Relationship plot between (a) Predicted versus actual values of response, (b) normal % probability versus externally studentised residuals, (c) residual versus the run