Supplementary Information

Synergy of monoatomic copper and oxygen vacancy formed in-situ on ultrathin TiO2(B) nanosheet for efficient photocatalytic dehalogenative C−C coupling synthesis of bibenzyl

Peng Zhenga, Yuanrong Zhanga, Shuaitao Lia, Hongpian Guoa, Xun Hua*, Yanfen Fangb*, Ran Duanc, Qifeng Chena*

a MS Peng Zheng, MS Yuanrong Zhang, MS Shuaitao Li, Miss Hongpian Guo, Dr. & Prof. Xun Hu, Dr. & Prof. Qifeng Chen, School of Materials Science & Engineering, University of Jinan, No. 336, West Road of Nan Xinzhuang, Jinan 250022, Shandong, China, qfchen@126.com (Qifeng Chen); mse_hux@ujn.edu.cn (Xun Hu).

b Prof. Yanfen Fang, College of Biological and Pharmaceutical Sciences, China Three Gorges University, Yichang, China, 443002, fangyf@ctgu.edu.cn.

c Ms Ran Duan, Institute of Chemistry, Chinese Academy of Sciences, Zhongguancun North First Street 2, Beijing, 100190, China.

Photoelectrochemical measurement. In the photocurrent measurement process, we used an Ag/AgCl electrode (3.0 M KCl) as the reference electrode and a platinum electrode as the counter electrode. The working electrode was prepared by impregnating the sample on FTO glass. The measurement of the three-electrode system was carried out in Na2SO4 (0.2 M) electrolyte. For the electrochemical impedance test, the three-electrode system was measured in a mixture of 0.1 M potassium ferricyanide and 0.1 M potassium ferrocyanide electrolyte. The measurement frequency of Nyquist plot was 1×106 ~ 0.01 Hz.

The working electrode was prepared as follows: 3.0 mg of photocatalysts were added into a mixture of 0.3 mL ethanol and 0.1 mL Nafion (0.1 wt%, Alfar Aesar). A homogeneous suspension was obtained by using ultrasonic oscillation for 10 min. Then, the photocatalyst suspension was dropped onto the FTO glass under an infrared lamp. After solvent volatilization, the working electrode with an active area (covered by photocatalysts) of 1.0 cm2 was obtained.

Preparation of AFM sample. A specific amount of TiO2(B) was dispersed in ethanol solution under ultrasonic treatment. Drops of the dispersed liquid were then added drop by drop to the mica sheet. After drying, the sample was photographed with a Bruker Dimension Icon AFM instrument.

Computational details. Adsorption energy and possible adsorption sites were carried out by using the Castep and Adsorption Locator modules, respectively. In Castep calculations, the systematic energy calculations were on the basis of the generalized gradient approximation (GGA) with a plane wave basis cutoff energy of 500 eV. Perdew–Burke–Ernzerhof (PBE) exchange–correlation function was used to achieve structure convergence. The energy was calculated by the Monkhorst–Pack k-point of 2  2  1. Structural relaxations could be achieved when the residual stresses on all atoms in the unit were less than 0.05 eV/Å, and the maximum displacement was 0.002 Å. The accuracy of self-consistent convergence was fixed at 1.0e⁻6 eV/atom. In adsorption Locator calculation, COMPASS II was selected as Forcefield with fine quanlity, in which 1.0e⁻4 kcal/mol energy and 0.005 kcal/mol/Å between adjacent molecules, and the displacement was 5.0e⁻5Å.

Fig. S1 XRD patterns of SA-Cux/TiO2(B)-VO photocatalysts

Fig. S2 HAADF-STEM images of SA-Cu1.0/TiO2(B)-VO

Fig. S3 HAADF-STEM image and corresponding EDX-mapping of SA-Cu1.0/TiO2(B)-VO (Ti (green), O (yellow) and Cu (red))

Fig. S4 EDS spectrum and analysis of SA-Cu1.0/TiO2(B)-VO

Fig. S5 AC-HAADF-STEM images of SA-Cu/TiO2(B)-VO

Fig. S6 The result of the Zeta potential test of TiO2(B). 1.0 mg of the samples were dispersed in 5.0 mL H2O, and then performed the test

Fig. S7 Nitrogen adsorption/desorption isotherm and pore size distribution of various photocatalysts

Fig. S8 EPR spectra of pristine TiO2(B) and SA-Cu/TiO2(B)-VO

Fig. S9 The effect of Cu loading on photocatalytic synthesis of bibenzyl under irradiation

Fig. S10 (a-b) GC spectra at different reaction times in pure and aqueous isopropanol in the presence of SA-Cu1.0/TiO2(B)-VO; (c) mass spectrum of the reactant, benzyl bromide; (d) mass spectrum of the product, bibenzyl

Fig. S11 The effect of water concentration on photocatalytic coupling synthesis of bibenzyl after irradiation of 2 h

Fig. S12 The photocatalytic cycle tests for SA-Cu1.0/TiO2(B)-VO

Fig. S13 XRD pattern of SA-Cu1.0/TiO2(B)-VO before and after the photocatalytic reaction

Fig. S14 4-methylbenzene bromide as substrate. (a) GC data. (b) MS data

Fig. S15 (a) PL spectra of SA-Cux/TiO2(B)-VO photocatalysts. (b) PL spectra of SA-Cu1.0/TiO2(B)-VO photocatalyst before and after air annealing

Fig. S16 XPS spectra of SA-Cu1.0/TiO2(B)-VO photocatalyst before and after irradiation

Fig. S17 Changes of C−Br bond length of benzyl bromide before and after introduction of single atom Cu

Table S1 ICP-OES content analysis of Cu on the surface of SA-Cux/TiO2(B)-VO

| Sample | The theoretical loading | The actual loading |
| --- | --- | --- |
| SA-Cu0.5/TiO2(B)-VO | 0.50% | 0.43% |
| SA-Cu1.0/TiO2(B)-VO | 1.00% | 0.83% |
| SA-Cu1.5/TiO2(B)-VO | 1.50% | 1.14% |

Table S2 Pore radius volume, and specific surface area of SA-Cux/TiO2(B)-VO photocatalysts

| Entry | Photocatalysts | Pore Volume (cm3/g) | Pore semidiameter (Å) | BET surface area (m2/g) |
| --- | --- | --- | --- | --- |
| 1 | TiO2(B) | 0.89 | 64.2 | 279.4 |
| 2 | SA-Cu0.5/TiO2(B)-VO | 0.62 | 41.1 | 301.7 |
| 3 | SA-Cu1.0/TiO2(B)-VO | 0.75 | 52.9 | 285.6 |
| 4 | SA-Cu1.5/TiO2(B)-VO | 0.58 | 40.3 | 288.9 |

Table S3 Atom percentages of O 1s peaks determined by the XPS analysis

| Sample | TiO2(B) | SA-Cu1.0/TiO2(B)-VO |
| --- | --- | --- |
| O1 | 530.3 (47.75%) | 530.4 (50.33%) |
| O2 | 531.4 (48.14%) | 531.5 (38.39%) |
| O3 | 532.9 (4.11%) | 532.6 (11.28%) |

Table S4 Photocatalytic conversion of benzyl bromide in different solvents

| Entry | Solvent | Conversion (%) | Selectivity (%) | Yield (%) |
| --- | --- | --- | --- | --- |
| 1 | Isopropanol | 67.38 | 64 | 43.12 |
| 2 | Ethanol | 99.33 | 68.59 | 68.13 |
| 3 | Methanol | 100 | 91.59 | 91.59 |
| 4 | Isopropanol solution (10 vol% water) | 100 | 92.32 | 92.32 |
| 5 | Ethanol solution (10 vol% water) | 100 | 96.78 | 96.78 |
| 6 | Methanol solution (10 vol% water) | 100 | 97.20 | 97.20 |
| 7 | Acetonitrile solution (30 vol% water) | 57.65 | 74.83 | 43.14 |

Table S5 Adsorption energy of benzyl bromide and bibenzyl at different adsorption sites

|  | E(A-B)/(kcal/mol) | EA (kcal/mol) | EB (kcal/mol) | Eint (kcal/mol) |
| --- | --- | --- | --- | --- |
| PhBr@TiO2(B)(010) | −193226.1222 | −193209.4167 | 5.599547 | −22.305034 |
| PhBr@TiO2(B)(010)VO | −192366.4991 | −192348.6626 | 5.600752 | −23.437319 |
| PhBr@TiO2(B)(010)VO+Cu | −67638.52796 | −67601.91634 | 4.905675 | −41.517295 |
| BiPh@TiO2(B)(010)VO+Cu | −67651.62836 | −67651.62836 | 1.086108 | −1.086108 |
| PhBr+BiPh@TiO2(B)(010)+Cu | −68499.3117 | −68499.3117 | 5.565367 | −5.565367 |