Supporting Information

Novel quinoxaline core-conjugated microporous polymer coating for highly sensitive solid-phase microextraction of phthalate esters in liquid food samples

Gang Xianga,b*,WenzhuoLic, QiuxiangNonga, XiansenHed, CuizhongZhanga,b, ZhengfaZhanga,b, Wei Huang a,b, Jinyun Peng a,b, JiangfenXuc, Yiqiu Tana*and Jing Sune

a College of Chemical and Biological Engineering, Guangxi MinZu Normal University, Chongzuo 532200, China

bPhotochemical Sensing and Regional Environmental Analysis Laboratory, Guangxi MinZuNormal University, Chongzuo 532200, China

c Institute for Food and Drug Control of ChongZuo, Chongzuo 532200, China

d School of Pharmacy, Henan University of Traditional Chinese Medicine, Zhengzhou 450046, China

eCollege of Economics and Management, Guangxi MinZu Normal University, Chongzuo 532200, China

*Corresponding author.

E-mail address: xgshmily@163.com (G. Xiang);  170079911@qq.com (Y. q. Tan);

Figure S1 Chemical stability of CMP materials in various organic solvents and in strong acid and alkaline solutions

Figure S2 Ion chromatogram of extraction of nine PAEs

Figure S3 Standard curves of 9 PAEs

Figure S4　X-ray diffraction pattern of polymer BPQ-CMPs

Figure S5 (A) XPS survey spectrum, (B) C 1s and (C) N 1s spectrum of BPQ-CMPs

Figure S6 Chromatograms of PAEs by the developed method for (a) samples (the black line); (b) spiked with 1.0 μg L-1 PAEs (the red line) and (c) spiked with 5.0 μg L-1 PAEs (the blue line). (A) peach juice, (B) cooking wine, (C)soy sauce, (D)blending oil

(1) DMP; (2) DEP; (3) DAP; (4) DPRP; (5) DBP; (6) DCHP; (7) BEHP; (8) DPHP; (9) DIDP

Table S1　Pore properties of polymer BPQ-CMPs

| Material | Sample weight (g) | BET (m2/g) | Slope (g/cm) | Y-Intercept (g/cm) | C | Qm (cm3/g) | Correlation Coefficient |
| --- | --- | --- | --- | --- | --- | --- | --- |
| CMPs | 0.0366 | 601.6196 ± 4.8935 | 0.007235 ± 0.000059 | 0.000000 ± 0.000005 | 31444.84402 | 138.2214 | 0.9998028 |

Table S2 Extraction performance evaluation

|  | DMP | DEP | DAP | DPRP | DBP | DCHP | BEHP | DPHP | DIDP |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| LogKow | 1.61 | 2.38 | 3.20 | 3.27 | 4.83 | 5.60 | 6.43 | 4.50 | 11.2 |
| EFs | 66±12 | 103±24 | 139±39 | 208±9 | 210±15 | 120±9 | 286±38 | 63±22 | 348±9 |

Table S3 Binding energy (BE) and inhibitor constant of BPQ-CMP towards PAEs

| Compounds | BE (kcal mol−1) | Inhibitor constant |
| --- | --- | --- |
| DMP | -3.92 | 1.33 |
| DEP | -3.99 | 1.19 |
| DAP | -4.22 | 803.57 |
| DPRP | -4.41 | 917.64 |
| DBP | -3.95 | 1.27 |
| DCHP | -5.98 | 41.09 |
| BEHP | -4.31 | 695.13 |
| DPHP | -5.98 | 41.46 |
| DIDP | -3.76 | 1.74 |