La doped TiO2 nanoparticles for photocatalysis: Synthesis, activity in terms of degradation of Methylene Blue dye and regeneration of used nanoparticles

Veeresh Verma1, Satya Vir Singh1

1Department of Chemical Engineering, Indian Institute of Technology (BHU), Varanasi, U.P. 221005, India

*Email: satyavirsingh59@rediffmail.com; svsingh.che@iitbhu.ac.in

Supplementary Material

TiO2 powder

Ammonium Sulphate

H2SO4

100 ml

46.9426 g (0.3552 mol)

4.7289g (0.0592 mol)

For 1% La doping 0.2710 g (0.00063 mol) La(NO3)3.6H2O

Heated at 170°C with continuous starring for 2-3 h

La doping (0.005-0.025%)

H2SO4

Heat at 100°C

Formation of Sol

Titaniumoxysulphate

50 ml

Ti1-xLaxO2

x = 0.005, 0.01...0.025

Cooled at room Temp. & dissolve in 500ml DDW

Formation of white

precipitate

Neutralization by 25% ammonia solution

50 ml

Dissolution of Precipitate in HNO3

Formation of TiO(NO3)2

10 g

Addition Citric Acid

Evaporated at 70-80°C & auto-combustion

Formation of dark brown

colour fluffy mass

Calcined at 500oC for 5 h

La doped TiO2 photocatalyst

Fig S1. The synthesis process of La doped TiO2 photocatalysts.