Light-oriented 3D printing of 4'-pentyl-4-cyanobiphenyl (5CB) liquid crystal/photocurable resins and its in-situ enhancement of mechanical performance

Xiaolu Sun 1,2,3,4,✝ ,Shaoyun Chen 1,3,4,✝*, Bo Qu 1,3,4, , Rui Wang 1,3,4,Yanyu Zheng 1,3,4, Xiaoying Liu1,3,4, Wenjie Li 1,3,4, Jianhong Gao1,3,4, Qinhui Chen 2*, Dongxian Zhuo 1,2,3,4*.

1College of Chemical Engineering and Materials Science, Quanzhou Normal University, Quanzhou, Fujian, 362000, P. R. China;

2College of Chemistry and Materials Science, Fujian Normal University, Fuzhou, Fujian, 350007, P. R. China;

3Fujian University Engineering Research Center of Polymer Functional Coating based Graphene, Fujian, 362000, P. R. China;

4Fujian Key Laboratory of New Materials for Light Textile and Chemical Industry, Fujian, 362000, P. R. China.

*Correspondence: chshaoy@qztc.edu.cn; chenqh@fjnu.edu.cn; dxzhuo@qztc.edu.cn;

✝ Co-first authors

Table S1 Different commercial printing formulations with 3% content of 5CB

Figure S1 Stress-strain curves of different commercial printing formulations with 3% content of 5CB

Figure S2 Polarizing optical microscopy (POM) at 0o and 45o of different commercial printing formulations with 3% content of 5CB

Table S1 Different commercial printing formulations with 3% content of 5CB

| F1 | Aliphatic polyether acrylates | CN991 | HPMA | TPO |  |
| --- | --- | --- | --- | --- | --- |
|  | 46 | 5 | 46 | 3 |  |
| F2 | Aliphatic polyether acrylates | CN991 | HEMA | HPMA | TPO |
|  | 36 | 5 | 20 | 36 | 3 |
| F3 | CN9010 | CN991 | HEMA | HPMA | TPO |
|  | 40 | 32 | 15 | 10 | 3 |

Figure S1 Stress-strain curves of different commercial printing formulations with 3% content of 5CB

Figure S2 Polarizing optical microscopy (POM) at 0o and 45o of different commercial printing formulations with 3% content of 5CB