Supplementary Material for

Reversible Elastomer-Fluid Transitions for Metamorphosic Robots

The PDF file includes:

Section S1. SEM images and optical microscope captured images

Section S2. Material setup for MIMMs

Section S3. Stretch results and experimental setup of VSM tests

Section S4. Supplementary introduction of RF heat tests

Section S5. MFR and viscosity results

Section S6. Stiffness-tuning fluid soft actuator

Section S7. Ex-vivo biomedical demonstrations

Fig. S1. SEM and sample used in this work

Figs. S2-S10. Raw SEM images

Figs. S11-S15. Raw OM images

Fig. S16. Part of material preparations for stretch, OM, VSM, and SEM

Fig. S17. Equipment setup of the conducted stretch tests

Figs. S18-S31. Stretch results

Fig. S32. Illustrations of fracture stretch results

Fig. S33. Equipment setup of the VSM tests: installation, equipment, and control platform

Fig. S34. Experimental setup of the fixed-location RF heating tests

Fig. S35. Experimental setup of the location-varied RF heating tests

Fig. S36. Experimental setup of the viscosity tests

Fig. S37. Experimental setup of MFR tests

Fig. S38. The structure of the stiffness-varied fluidic soft actuator. (A) The hollowed elastic shell cannot be magnetically actuated. (B) With MIMMs, the fluidic soft actuator can be therefore actuated, and stiffness is varied by the elastomer-fluid transition.

Fig. S39. The maximum bending performances of the different stiffness-distributed soft actuators. (A) The left-side distributed soft actuator performs delicate bending. (B) Both sides of distributed soft actuators perform central-concentrated bending. (C) The right-side distributed soft actuator performs large-scale bending

Fig. S39. The maximum bending performances of different stiffness-distributed soft actuators. (A) The left-side distributed soft actuator performs delicate bending. (B) Both sides distributed the soft actuator perform central-concentrated bending. (C) The right-side distributed soft actuator performs large-scale bending

Fig. S40. Locally stiffness adjustable fluidic soft actuator. (A) Constraining the tip, stiffness at the center of the actuator is tested at the ambient temperature. (B) In the elastomer state, the center of the actuator is tested with large stiffness (~10 MPa), where maximum bending curvatures are found at low-stiffness (~2 MPa) regions. (C) Constraining the tip, the fluid-stated actuator is tested. (D) The curvature at the studied region is larger than that in the elastomer state

Fig. S41. The ex-vivo trachea was dissected from a pig lung

Fig. S42. The actuator can navigate itself for intubation

Fig. S43. The actuator can move in a pig intestine with friction

Fig. S44. An oropharyngeal phantom was applied to demonstrate Fig. 5E in the main text

Table. S1. Case table for prepared MIMMs

Table S2. Viscosity results

Table S3. MFR results

Other Supplementary Material for this manuscript includes the following:

Movie S1. Elastomer-fluid transitions of MIMMs responding to RF heating

Movie S2. Self-healing enabled by the elastomer-fluid transition

Movie S3. Additive manufacturing by MIMMs

Movie S4. “Let’s collaborate!”-collaboration to repair fractured structures

Movie S5. “Symbiosis”-gain new motion functions by interacting with external objects

Movie S6. “Field explorer!”-flow through a narrow terrain

Movie S7. “Varied stiffness”- soft actuator with varied-stiffness distributions

Movie S8. “Reach and grab out”-field exploration

Movie S9. In situ drug delivery/treatment

Movie S10. Intubation navigation

Movie S11. Electrical wire connection and insulation

Movie S12. Endoscope transportation through a narrow hole

Section 1. SEM images and optical microscope captured images.

All captured SEM images and OM images are provided here for reference.

Fig. S1. SEM and sample used in this work.

Fig. S2. SEM images of 10 g Fe3O4+ 10 g HMA.

Fig. S3. SEM images of 10 g Fe3O4+ 10 g HMA+ 1.2 g wax.

Fig. S4. SEM images of 10 g Fe3O4+ 10 g HMA+ 0.3 g graphene.

Fig. S5. SEM images of 10 g NdFeB + 10 g HMA.

Fig. S6. SEM images of 5 g Fe3O4+5 g NdFeB+0.2 g graphene.

Fig. S7. SEM images of 5 g Fe3O4+5 g NdFeB+0.6 g wax+10 g HMA.

Fig. S8. SEM images of 10 g Fe3O4+10 g EVA.

Fig. S9. SEM images of 5 g Fe3O4+5 g NdFeB+0.6 g wax+10 g EVA.

Fig. S10. SEM images of 5 g Fe3O4+5 g NdFeB+0.6 g wax+10 g PCL.

Fig. S11. OM image of 10 g Fe3O4+ 10 g HMA.       Fig. S12. OM image of 10 g Fe3O4+ 10 g HMA+ 0.3 g graphene.

Fig. S13. OM image of 5 g Fe3O4+5 g NdFeB+10 g HMA       Fig. S14. OM image of 10 g Fe3O4+10 g EVA

Fig. S15. OM image of 5 g Fe3O4+5 g NdFeB+0.6 g wax+10 g PCL

Section 2. Material setup for MIMMs

The case table to prepare the 35 types of MIMMs below for reference.

Table S1. Case table for prepared MIMMs

| No. | Base Material | Base Material Mass (g) | Fe3O4 (g) | NdFeB (g) | Wax (g) | Graphene (g) |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | HMA | 10 | 15 | - | - | - |
| 2 | HMA | 10 | 10 | - | - | - |
| 3 | HMA | 10 | 5 | - | - | - |
| 4 | HMA | 10 | 10 | - | 0.3 | - |
| 5 | HMA | 10 | 10 | - | 0.6 | - |
| 6 | HMA | 10 | 10 | - | 1.2 | - |
| 7 | HMA | 10 | 10 | - | - | 0.1 |
| 8 | HMA | 10 | 10 | - | - | 0.2 |
| 9 | HMA | 10 | 10 | - | - | 0.3 |
| 10 | HMA | 10 | - | 15 | - | - |
| 11 | HMA | 10 | - | 10 | - | - |
| 12 | HMA | 10 | - | 5 | - | - |
| 13 | HMA | 10 | - | 10 | 0.3 | - |
| 14 | HMA | 10 | - | 10 | 0.6 | - |
| 15 | HMA | 10 | - | 10 | 1.2 | - |
| 16 | HMA | 10 | - | 10 | - | 0.1 |
| 17 | HMA | 10 | - | 10 | - | 0.2 |
| 18 | HMA | 10 | - | 10 | - | 0.3 |
| 19 | HMA | 10 | 5 | 5 | - | - |
| 20 | HMA | 10 | 2 | 8 | - | - |
| 21 | HMA | 10 | 8 | 2 | - | - |
| 22 | HMA | 10 | 5 | 5 | - | 0.2 |
| 23 | HMA | 10 | 5 | 5 | 0.6 | - |
| 24 | EVA | 10 | 10 | - | - | - |
| 25 | EVA | 10 | 10 | - | 1.2 | - |
| 26 | EVA | 10 | 10 | - | - | 0.3 |
| 27 | EVA | 10 | - | 10 | - | - |
| 28 | EVA | 10 | 5 | 5 | - | 0.2 |
| 29 | EVA | 10 | 5 | 5 | 0.6 | - |
| 30 | PCL | 10 | 10 | - | - | - |
| 31 | PCL | 10 | 10 | - | 1.2 | - |
| 32 | PCL | 10 | 10 | - | - | 0.3 |
| 33 | PCL | 10 | - | 10 | - | - |
| 34 | PCL | 10 | 5 | 5 | - | 0.2 |
| 35 | PCL | 10 | 5 | 5 | 0.6 | - |

Fig. S16. Part of material preparations for stretch, OM, VSM, and SEM.

Section 3. Stretch results and experimental setup of VSM tests

Stretch tests were conducted by a mechanical test machine (see Fig. S17).

Fig. S17. Equipment setup of the conducted stretch tests.

Fig. S18. Stretch results of Fe3O4-HMA        Fig. S19. Stretch results of wax-Fe3O4-HMA

Fig. S20. Stretch results of graphene-Fe3O4-HMA            Fig. S21. Stretch results of NdFeB-HMA

Fig. S22. Stretch results of wax-NdFeB-HMA           Fig. S23. Stretch results of graphene-NdFeB-HMA

Fig. S24. Stretch results of Fe3O4-NdFeB-HMA   Fig. S25. Stretch results of wax-graphene-Fe3O4-NdFeB-HMA

Fig. S26. Stretch results of Fe3O4-HMA/EVA/PCL   Fig. S27. Stretch results of wax-Fe3O4-HMA/EVA/PCL

Fig. S28. Stretch results of graphene-Fe3O4-HMA/EVA/PCL  Fig. S29. Stretch results of NdFeB-HMA/EVA/PCL

Fig. S30. Stretch results of graphene-Fe3O4-NdFeB-HMA/EVA/PCL

Fig. S31. Stretch results of wax-Fe3O4-NdFeB-HMA/EVA/PCL

Fig. S32. Fracture stretches results of Fe3O4-HMA/EVA/PCL

Fig. S33. Equipment setup of the VSM tests: installation, equipment, and control platform.

Section 4. Supplementary introduction of RF heat tests

Fig. S34. Experimental setup of the fixed-location RF heating tests.

Fig. 35. Experimental setup of the location-varied RF heating tests.

Experimental setups of two RF heating tests are shown in Figs. S34 and S35. To quantitatively conduct experiments for fixed location heating (Fig. S34), a wooden stick was applied to pierce the sample for positioning. Due to the RF non-responsibility and heat resistance, the wooden stick was selected instead of resin-based or metal-based materials. The time was recorded when the first MIMM droplet fell on the ground. Regarding the second RF heating test (location vs. melt time, shown in Fig. S35), a planar coil was applied to perform vertically intense inductions. The time was recorded when the sample height was half the original height.

Section 5. MFR and viscosity results

Experimental setups and raw test data are provided below for reference.

Fig. S36. Experimental setup of the viscosity tests.

Table S2. Viscosity results

| Material No. | Temp. (℃) | RPM | Cut rate | Viscosity (MPa*s) | Cut pressure (MPa) |
| --- | --- | --- | --- | --- | --- |
| 2 | 140 | 5 | 1.2 | 361410.1 | 451762.7 |
| 2 | 140 | 6 | 1.5 | 342579.6 | 513869.4 |
| 2 | 140 | 7 | 1.7 | 327832.8 | 573707.4 |
| 2 | 140 | 8 | 2 | 305712.6 | 611425.2 |
| 2 | 140 | 9 | 2.2 | 312581.8 | 703309.2 |
| 2 | 145 | 5 | 1.2 | 331916.5 | 414895.6 |
| 2 | 145 | 6 | 1.5 | 306468.8 | 459703.3 |
| 2 | 145 | 7 | 1.7 | 287157.5 | 502525.7 |
| 2 | 145 | 8 | 2 | 275368.2 | 550736.4 |
| 2 | 145 | 9 | 2.2 | 280945.5 | 632127.5 |
| 2 | 150 | 5 | 1.2 | 290852.3 | 363565.4 |
| 2 | 150 | 6 | 1.5 | 265820.6 | 398730.9 |
| 2 | 150 | 7 | 1.7 | 231411.4 | 404969.9 |
| 2 | 150 | 8 | 2 | 234105.5 | 468211 |
| 2 | 150 | 9 | 2.2 | 224983.3 | 506212.4 |
| 2 | 155 | 5 | 1.2 | 249561.3 | 311951.6 |
| 2 | 155 | 6 | 1.5 | 229520.8 | 344281.2 |
| 2 | 155 | 7 | 1.7 | 218771.2 | 382849.7 |
| 2 | 155 | 8 | 2 | 213261.4 | 426522.9 |
| 2 | 155 | 9 | 2.2 | 204060.5 | 459136.1 |
| 2 | 160 | 5 | 1.2 | 228462 | 285577.5 |
| 2 | 160 | 6 | 1.5 | 199838.1 | 299757.1 |
| 2 | 160 | 7 | 1.7 | 204672.6 | 358177.2 |
| 2 | 160 | 8 | 2 | 196245.9 | 392491.8 |
| 2 | 160 | 9 | 2.2 | 203556.3 | 458001.7 |
| 5 | 140 | 5 | 1.2 | 338042.1 | 422552.7 |
| 5 | 140 | 6 | 1.5 | 310817.2 | 466225.9 |
| 5 | 140 | 7 | 1.7 | 310493.1 | 543363 |
| 5 | 140 | 8 | 2 | 307839.5 | 615679.1 |
| 5 | 140 | 9 | 2.2 | 275525.7 | 619933 |
| 5 | 145 | 5 | 1.2 | 321934.1 | 402417.6 |
| 5 | 145 | 6 | 1.5 | 302309.5 | 453464.3 |
| 5 | 145 | 7 | 1.7 | 274679.5 | 480689.1 |
| 5 | 145 | 8 | 2 | 259345.2 | 518690.5 |
| 5 | 145 | 9 | 2.2 | 251704 | 566334 |
| 5 | 150 | 5 | 1.2 | 306052.9 | 382566.1 |
| 5 | 150 | 6 | 1.5 | 283025.2 | 424539.8 |
| 5 | 150 | 7 | 1.7 | 265766.6 | 465091.5 |
| 5 | 150 | 8 | 2 | 251830 | 503660.1 |
| 5 | 150 | 9 | 2.2 | 239730.1 | 539392.8 |
| 5 | 155 | 5 | 1.2 | 294028.6 | 367535.7 |
| 5 | 155 | 6 | 1.5 | 266955 | 400432.4 |
| 5 | 155 | 7 | 1.7 | 247778.7 | 433612.7 |
| 5 | 155 | 8 | 2 | 229709.8 | 459419.7 |
| 5 | 155 | 9 | 2.2 | 221454.1 | 498271.8 |
| 5 | 160 | 5 | 1.2 | 266123.1 | 332653.8 |
| 5 | 160 | 6 | 1.5 | 241998.8 | 362998.2 |
| 5 | 160 | 7 | 1.7 | 224767.2 | 393342.6 |
| 5 | 160 | 8 | 2 | 207589.6 | 415179.2 |
| 5 | 160 | 9 | 2.2 | 190215 | 436704.8 |
| 8 | 140 | 5 | 1.2 | 396802.4 | 496003.1 |
| 8 | 140 | 6 | 1.5 | 383038.8 | 574558.2 |
| 8 | 140 | 7 | 1.7 | 360567.4 | 630993.1 |
| 8 | 140 | 8 | 2 | 348109.6 | 696219.3 |
| 8 | 140 | 9 | 2.2 | 339176.5 | 763147.2 |
| 8 | 145 | 5 | 1.2 | 394328.3 | 497555.3 |
| 8 | 145 | 6 | 1.5 | 370749.8 | 566124.7 |
| 8 | 145 | 7 | 1.7 | 354733.5 | 620783.7 |
| 8 | 145 | 8 | 2 | 340736.2 | 681472.5 |
| 8 | 145 | 9 | 2.2 | 329345.2 | 741026.9 |
| 8 | 150 | 5 | 1.2 | 376610.7 | 470763.3 |
| 8 | 150 | 6 | 1.5 | 346549.9 | 519824.9 |
| 8 | 150 | 7 | 1.7 | 327670.7 | 573423.8 |
| 8 | 150 | 8 | 2 | 321168.3 | 642336.7 |
| 8 | 150 | 9 | 2.2 | 312455.8 | 703025.6 |
| 8 | 155 | 5 | 1.2 | 377518.2 | 471897.7 |
| 8 | 155 | 6 | 1.5 | 343524.9 | 515287.4 |
| 8 | 155 | 7 | 1.7 | 328465.2 | 576543.3 |
| 8 | 155 | 8 | 2 | 318899.6 | 637799.3 |
| 8 | 155 | 9 | 2.2 | 295440.2 | 664740.6 |
| 8 | 160 | 5 | 1.2 | 309682.9 | 387103.6 |
| 8 | 160 | 6 | 1.5 | 260337.8 | 390506.7 |
| 8 | 160 | 7 | 1.7 | 274355.3 | 480121.9 |
| 8 | 160 | 8 | 2 | 246441.8 | 492883.6 |
| 8 | 160 | 9 | 2.2 | 235192.6 | 529183.5 |
| 11 | 140 | 5 | 1.2 | 115025 | 143781.3 |
| 11 | 140 | 6 | 1.5 | 111735.4 | 167603.1 |
| 11 | 140 | 7 | 1.7 | 111168.2 | 194544.4 |
| 11 | 140 | 8 | 2 | 110884.6 | 221769.2 |
| 11 | 140 | 9 | 2.2 | 110538 | 248710.5 |
| 11 | 145 | 5 | 1.2 | 94833.3 | 118541.6 |
| 11 | 145 | 6 | 1.5 | 95097.9 | 142646.9 |
| 11 | 145 | 7 | 1.7 | 93666.5 | 163916.4 |
| 11 | 145 | 8 | 2 | 93443.6 | 186887.3 |
| 11 | 145 | 9 | 2.2 | 93144.3 | 209574.7 |
| 11 | 150 | 5 | 1.2 | 85077.7 | 106347.1 |
| 11 | 150 | 6 | 1.5 | 81674.6 | 122511.9 |
| 11 | 150 | 7 | 1.7 | 80054 | 140094.6 |
| 11 | 150 | 8 | 2 | 79405.8 | 158811.7 |
| 11 | 150 | 9 | 2.2 | 79027.7 | 177812.4 |
| 11 | 155 | 5 | 1.2 | 69423.4 | 86779.2 |
| 11 | 155 | 6 | 1.5 | 68251.2 | 102376.8 |
| 11 | 155 | 7 | 1.7 | 67738 | 118541.6 |
| 11 | 155 | 8 | 2 | 67353.1 | 134706.3 |
| 11 | 155 | 9 | 2.2 | 67305.9 | 151438.3 |
| 11 | 160 | 5 | 1.2 | 60121.5 | 75151.9 |
| 11 | 160 | 6 | 1.5 | 58798.1 | 88197.2 |
| 11 | 160 | 7 | 1.7 | 58663.1 | 102660.4 |
| 11 | 160 | 8 | 2 | 58420 | 116840 |
| 11 | 160 | 9 | 2.2 | 58230.9 | 131019.6 |
| 24 | 180 | 5 | 1.2 | 442404.2 | 553005.2 |
| 24 | 180 | 6 | 1.5 | 413288.6 | 619932.9 |
| 24 | 180 | 7 | 1.7 | 391681.6 | 685442.8 |
| 24 | 180 | 8 | 2 | 372356.8 | 744713.6 |
| 24 | 180 | 9 | 2.2 | 354553.5 | 797745.4 |
| 24 | 190 | 5 | 1.2 | 333958.4 | 417448 |
| 24 | 190 | 6 | 1.5 | 339365.4 | 509048.4 |
| 24 | 190 | 7 | 1.7 | 316651.1 | 554139.5 |
| 24 | 190 | 8 | 2 | 292383.7 | 584767.5 |
| 24 | 190 | 9 | 2.2 | 276282 | 621634.5 |
| 24 | 200 | 5 | 1.2 | 326698.4 | 408373 |
| 24 | 200 | 6 | 1.5 | 306847 | 460270.5 |
| 24 | 200 | 7 | 1.7 | 290884.7 | 509048.3 |
| 24 | 200 | 8 | 2 | 284584.9 | 569169.9 |
| 24 | 200 | 9 | 2.2 | 270862.2 | 609440.1 |
| 24 | 210 | 5 | 1.2 | 298566 | 373207.6 |
| 24 | 210 | 6 | 1.5 | 267333.1 | 400999.6 |
| 24 | 210 | 7 | 1.7 | 241782.7 | 423119.8 |
| 24 | 210 | 8 | 2 | 221627.4 | 443254.9 |
| 24 | 210 | 9 | 2.2 | 222084.3 | 499689.8 |
| 24 | 220 | 5 | 1.2 | 227100.7 | 283875.9 |
| 24 | 220 | 6 | 1.5 | 221769.2 | 332653.8 |
| 24 | 220 | 7 | 1.7 | 230439 | 403268.4 |
| 24 | 220 | 8 | 2 | 207123.6 | 406945.6 |
| 24 | 220 | 9 | 2.2 | 183263.7 | 412343.4 |

Fig. S37. Experimental setup of MFR tests.

Table S3. MFR results

| No. | Load (kg) | T (℃) | W-1 (g) | W-2 (g) | W-3 (g) | W-4 (g) | W-5 (g) | W-6 (g) | W-ave (g) | MFR (g/10 min) | Uni-MFR (g/10 min) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 25 | 1.2 | 100 | 0.113 | 0.114 | 0.114 | 0.114 | 0.114 | 0.1 | 0.1115 | 2.23 | 1.858333 |
| 25 | 1.2 | 110 | 0.189 | 0.189 | 0.19 | 0.189 | 0.19 | 0.19 | 0.1895 | 3.79 | 3.158333 |
| 25 | 1.2 | 120 | 0.287 | 0.284 | 0.284 | 0.284 | 0.284 | 0.284 | 0.2845 | 5.69 | 4.741667 |
| 25 | 1.2 | 130 | 0.468 | 0.468 | 0.466 | 0.479 | 0.468 | 0.483 | 0.472 | 9.44 | 7.866667 |
| 25 | 1.2 | 140 | 0.668 | 0.682 | 0.678 | 0.694 | - | - | 0.6805 | 13.61 | 11.34167 |
| 25 | 1.2 | 160 | 1.266 | 1.249 | 1.154 | - | - | - | 1.223 | 24.46 | 20.38333 |
| 30 | 10 | 100 | 0.051 | 0.053 | 0.051 | 0.045 | 0.051 | 0.054 | 0.050833 | 1.016667 | 0.101667 |
| 30 | 10 | 110 | 0.684 | 0.689 | 0.652 | 0.684 | 0.637 | 0.637 | 0.663833 | 13.27667 | 1.327667 |
| 30 | 5 | 120 | 0.787 | 0.764 | 0.768 | 0.79 | 0.794 | 0.794 | 0.782833 | 15.65667 | 3.131333 |
| 30 | 2.16 | 130 | 0.465 | 0.465 | 0.465 | 0.465 | 0.465 | 0.465 | 0.465 | 9.3 | 4.305556 |
| 30 | 2.16 | 140 | 0.695 | 0.728 | 0.741 | 0.741 | 0.741 | 0.741 | 0.731167 | 14.62333 | 6.770062 |
| 2 | 1.2 | 100 | 0.469 | 0.45 | 0.483 | 0.49 | 0.51 | 0.49 | 0.482 | 9.64 | 8.033333 |
| 2 | 1.2 | 110 | 0.783 | 0.839 | 0.848 | 0.865 | 0.865 | 0.865 | 0.844167 | 16.88333 | 14.06944 |
| 2 | 1.2 | 120 | 1.37 | 1.33 | - | - | - | - | 1.35 | 27 | 22.5 |
| 2 | 0.325 | 130 | 0.463 | 0.444 | 0.444 | 0.41 | 0.415 | 0.412 | 0.431333 | 8.626667 | 26.54359 |
| 2 | 0.325 | 140 | 0.658 | 0.636 | 0.646 | - | - | - | 0.646667 | 12.93333 | 39.79487 |
| 2 | 0.325 | 150 | 0.804 | 0.746 | 0.878 | 0.854 | - | - | 0.8205 | 16.41 | 50.49231 |
| 2 | 0.325 | 160 | 1.015 | 1.143 | 0.906 | - | - | - | 1.021333 | 20.42667 | 62.85128 |
| 5 | 0.325 | 100 | 0.548 | 0.548 | 0.53 | 0.534 | - | - | 0.54 | 10.8 | 33.23077 |
| 5 | 0.325 | 110 | 0.739 | 0.791 | 0.779 | - | - | - | 0.769667 | 15.39333 | 47.3641 |
| 5 | 0.325 | 120 | 1.215 | 1.33 | - | - | - | - | 1.2725 | 25.45 | 78.30769 |
| 8 | 0.325 | 100 | 0.078 | 0.078 | 0.095 | 0.089 | 0.089 | 0.095 | 0.087333 | 1.746667 | 5.374359 |
| 8 | 0.325 | 110 | 0.146 | 0.146 | 0.146 | 0.146 | 0.146 | 0.146 | 0.146 | 2.92 | 8.984615 |
| 8 | 0.325 | 120 | 0.188 | 0.188 | 0.188 | 0.188 | 0.188 | 0.188 | 0.188 | 3.76 | 11.56923 |
| 8 | 0.325 | 130 | 0.33 | 0.34 | 0.336 | 0.344 | 0.344 | - | 0.3388 | 6.776 | 20.84923 |
| 8 | 0.325 | 140 | 0.542 | 0.575 | 0.566 | 0.537 | 0.537 | 0.537 | 0.549 | 10.98 | 33.78462 |
| 8 | 0.325 | 150 | 0.732 | 0.72 | 0.76 | 0.8 | - | - | 0.753 | 15.06 | 46.33846 |
| 8 | 0.325 | 160 | 0.906 | 1 | 1.04 | - | - | - | 0.982 | 19.64 | 60.43077 |
| 11 | 0.325 | 100 | 0.175 | 0.176 | 0.175 | 0.178 | 0.178 | 0.167 | 0.174833 | 3.496667 | 10.75897 |
| 11 | 0.325 | 110 | 0.317 | 0.317 | 0.31 | 0.3 | 0.305 | - | 0.3098 | 6.196 | 19.06462 |
| 11 | 0.325 | 120 | 0.444 | 0.444 | 0.444 | 0.42 | 0.42 | 0.42 | 0.432 | 8.64 | 26.58462 |
| 11 | 0.325 | 130 | 0.729 | 0.729 | 0.707 | 0.7 | - | - | 0.71625 | 14.325 | 44.07692 |
| 11 | 0.325 | 140 | 0.898 | 0.903 | - | - | - | - | 0.9005 | 18.01 | 55.41538 |
| 11 | 0.325 | 150 | 1.384 | 1.264 | - | - | - | - | 1.324 | 26.48 | 81.47692 |

Section 6. Stiffness-varied fluid soft actuator

The experimental setup and results are presented below in figure form for reference.

Fig. S38. The structure of the stiffness-varied fluidic soft actuator. (A) The hollowed elastic shell cannot be magnetically actuated. (B) With MIMMs, the fluidic soft actuator can be therefore actuated, and stiffness is varied by the elastomer-fluid transition.

Fig. S39. The maximum bending performances of different stiffness-distributed soft actuators. (A) The left-side distributed soft actuator performs delicate bending. (B) Both sides distributed the soft actuator perform central-concentrated bending. (C) The right-side distributed soft actuator performs large-scale bending.

Fig. S40. Locally stiffness adjustable fluidic soft actuator. (A) Constraining the tip, stiffness at the center of the actuator is tested at the ambient temperature. (B) In the elastomer state, the center of the actuator is tested with large stiffness (~10 MPa), where maximum bending curvatures are found at low-stiffness (~2 MPa) regions. (C) Constraining the tip, the fluid-stated actuator is tested. (D) The curvature at the studied region is larger than that in the elastomer state.

Section 7. Ex-vivo biomedical demonstrations

Experimental setups are presented below for reference.

Fig. S41. The ex-vivo trachea was dissected from a pig lung.

Fig. S42. The actuator can navigate itself for intubation.

Fig. S43. The actuator can move in a pig intestine with friction.

Fig. S44. An oropharyngeal phantom was applied to demonstrate Fig. 5E in the main text.