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SI 1: Characteristic AFM Images of the (top) DH6, (middle) DH6W6, and (bottom) DH6W6F3 samples.


SI 2: A higher resolution AFM image of the DH6W6F3 sample.[image: A picture containing graphical user interface
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[image: ]SI 3: Bagley plots for the 12 and 13 NFC wt% samples. Lower shear rates (blues) show higher mean pressures than the higher shear rates (reds). Solid lines illustrate linear regression fits for a given shear rate. The red dashed line illustrates the lower limit of the pressure transducer, for reference.
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