Supporting Information for

Bamboo fiber-derived bifunctional electrocatalyst for rechargeable Zn-Air batteries

Jian Yu, Zehong Chen, Linxin Zhong, Wu Yang, Tingzhen Li, Yongfa Huang, Yujia Wei, and Xinwen Peng

State Key Laboratory of Pulp and Paper Engineering, South China University of Technology, Guangzhou, 510641, China.
* Corresponding author. E-mail: fexwpeng@scut.edu.cn (X. Peng)

Fig. S1 The XPS survey spectra of CP@900, CP-N-C@900, CP-UN-C@900 and CP-DN-C@900.

Fig. S2 CV curves of (a) Pt/C and (b) CP-N-C@900 under O2 and N2 saturation.

Fig. S3 The Koutecky-Levich plots at different potentials.

Fig. S4 Electron transfers and H2O2 yields of CP-N-C@900 and Pt/C.

Fig. S5 Deconvoluted N 1s spectra of CP-N-C@900 before (a) and after (b) the ORR durable test.

Fig. S6 Methanol tolerance measurements of Pt/C and CP-N-C@900 at the same condition, with the addition of 1 M methanol at 500 s

Fig. S7 The open circuit voltages of CP-N-C@900-based and Pt/C-based liquid ZAB (Inset: the open circuit voltage of CP-N-C@900-based ZAB).

Table. S1 The element contents obtained by elemental analysis.

| Samples | C (wt%) | N (wt%) | O (wt%) |
| --- | --- | --- | --- |
| CP@900 | 94.1 | 0 | 5.9 |
| CP-N-C@900 | 83.2 | 8.6 | 8.2 |
| CP-UN-C@900 | 88.2 | 6.3 | 5.5 |
| CP-DN-C@900 | 86.9 | 5.8 | 7.3 |

Table. S2 Specific surface areas and the element contents obtained by XPS of the electrocatalysts.

| Samples | Specific surface area (m2 g-1) | The element content obtained by XPS (atom%) |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  |  | C | N | O |
| CP@900 | 825.4 | 94.6 | 0 | 5.3 |
| CP-N-C@900 | 1109.23 | 88.57 | 3.62 | 7.81 |
| CP-UN-C@900 | 1028.65 | 90.61 | 2.57 | 6.82 |
| CP-DN-C@900 | 1265.27 | 86.63 | 2.49 | 10.88 |

Table. S3 Summary of the catalytic activities of the reported electrocatalysts in 0.1 M KOH.

| Catalysts | Eonset (V vs. RHE) |  | E1/2 (V vs. RHE) |  | E j=10 (V) | ΔE (E j=10- E1/2) (V) |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| CP-N-C@900 | 1.00 | 0.86 |  | 1.65 |  |  | 0.79 |
| 10 wt% Pt/C | 0.98 | 0.837 |  | — |  |  | — |
| RuO2 | — | — |  | 1.54 |  |  | — |
| S, S′-CNT 1000 °C | 0.87 | 0.79 |  | 1.58 |  |  | 0.79 |
| NGM | 0.89 | 0.77 |  | 1.67 |  |  | 0.90 |
| N-GRW | 0.92 | 0.84 |  | 1.59 |  |  | 0.75 |
| HPNC-2 | 0.96 | 0.86 |  | — |  |  | — |
| N-GDY-900 | 1.01 | 0.83 |  | 1.796 |  |  | 0.966 |
| MCAC | 0.87 | 0.8 |  | 1.56 |  |  | 0.76 |
| Fe@C–NG/NCNTs | 0.93 | 0.84 |  | 1.68 |  |  | 0.84 |
| Co-POC | — | 0.83 |  | 1.70 |  |  | 0.87 |
| MnCo2O4/N-rGO | 0.89 | 0.82 |  | 1.73 |  |  | 0.91 |
| Co@NPC-800 | 0.89 | 0.70 |  | 1.68 |  |  | 0.98 |

References

El-Sawy A. M, Mosa I. M, Su D, Guild C. J, Khalid S, Joesten R, Rusling J. F, Suib S. L (2016) Controlling the active sites of sulfur-doped carbon nanotube-graphene nanolobes for highly efficient oxygen evolution and reduction catalysis. Adv Energy Mater 6 (5):1501966. https://doi.org/10.1002/aenm.201501966

Ge X, Liu Y, Goh F. W, Hor T. S, Zong Y, Xiao P, Zhang Z, Lim S. H, Li B, Wang X, Liu Z (2014) Dual-phase spinel MnCo2O4 and spinel MnCo2O4/nanocarbon hybrids for electrocatalytic oxygen reduction and evolution. ACS Appl Mater Interfaces 6 (15):12684-12691. https://doi.org/10.1021/am502675c

Li B. Q, Zhao C. X, Chen S, Liu J. N, Chen X, Song L, Zhang Q (2019) Framework-porphyrin-derived single-atom bifunctional oxygen electrocatalysts and their applications in Zn-air batteries. Adv Mater 31 (19):1900592. https://doi.org/10.1002/adma.201900592

Lu H.-S, Zhang H, Liu R, Zhang X, Zhao H, Wang G (2017) Macroscale cobalt-MOFs derived metallic Co nanoparticles embedded in N-doped porous carbon layers as efficient oxygen electrocatalysts. App Surf Sci 392:402-409. https://doi.org/10.1016/j.apsusc.2016.09.045

Lu T, Hu X, He J, Li R, Gao J, Lv Q, Yang Z, Cui S, Huang C (2021) Aqueous/solid state Zn-air batteries based on N doped graphdiyne as efficient metal-free bifunctional catalyst. Nano Energy 85:106024. https://doi.org/10.1016/j.nanoen.2021.106024

Liu H, He G, Liu X, Zhu Y, Eigler S, Han L (2021) Ion-induced formation of hierarchical porous nitrogen-doped carbon materials with enhanced oxygen reduction. ChemCatChem 13 (13):3112-3118. https://doi.org/10.1002/cctc.202002045

Liu J, Wang C, Song Y, Zhang S, Zhang Z, He L, Du M (2021) Two-dimensional triazine-based porous framework as a novel metal-free bifunctional electrocatalyst for zinc-air batty. J Colloid Interface Sci 591:253-263. https://doi.org/10.1016/j.jcis.2021.02.007

Tang C, Wang H. F, Chen X, Li B. Q, Hou T. Z, Zhang B, Zhang Q, Titirici M. M, Wei F. (2016) Topological defects in metal-free nanocarbon for oxygen electrocatalysis. Adv Mater 28 (32):6845-6851. https://doi.org/10.1002/adma.201601406

Wang Q, Lei Y, Chen Z, Wu N, Wang Y, Wang B, Wang Y (2018) Fe/Fe3C@C nanoparticles encapsulated in N-doped graphene–CNTs framework as an efficient bifunctional oxygen electrocatalyst for robust rechargeable Zn–air batteries. J Mater Chem A 6 (2):516-526. https://doi.org/10.1039/c7ta08423d

Yang H. B, Miao J, Hung S.-F, Chen J, Tao H. B, Wang X, Zhang L, Chen R, Gao J, Chen H. M (2016) Identification of catalytic sites for oxygen reduction and oxygen evolution in N-doped graphene materials: Development of highly efficient metal-free bifunctional electrocatalyst. Sci Adv 2 (4):1501122. https://doi.org/10.1126/sciadv.1501122

Corresponding author.

E-mail address: fexwpeng@scut.edu.cn (X. Peng)