Supplementary Information

Active site tuning based on pseudo-binary alloys for low-temperature acetylene semihydrogenation

Ma et al.

Supplementary Figure 1. a HAADF–STEM image and the corresponding elemental maps for b Ni, c Cu, d Ga, e Ni+Cu+Ga (magnified for a few particles) for (Ni0.8Cu0.2)3Ga/TiO2.

Supplementary Table 1. Particle size of (Ni0.8Cu0.2)3Ga/TiO2, (Ni0.8Cu0.2)3Ga/SiO2 and Ni3Ga/TiO2 calculated according to Scherrer equation.

| catalysts | Scherrer constant | half with / degree | center / degree | crystallite size / nm |
| --- | --- | --- | --- | --- |
| (Ni0.8Cu0.2)3Ga/TiO2 | 0.849 | 0.76 | 43.52 | 10.6 |
| Ni3Ga/TiO2 |  | 1.03 | 43.74 | 7.8 |
| (Ni0.8Cu0.2)3Ga/SiO2 |  | 1.60 | 43.74 | 5.1 |

Supplementary Figure 2. a Ni, b Cu, and c Ga K-edge XANES spectra of over (Ni0.8Cu0.2)3Ga/TiO2, (Ni0.8Cu0.2)3Ga/SiO2, Ni3Ga/TiO2 and reference compounds.

Supplementary Figure 3. Fourier-transforms of EXAFS in a Ni, b Cu, and c Ga K-edge over (Ni0.8Cu0.2)3Ga/TiO2, (Ni0.8Cu0.2)3Ga/SiO2, Ni3Ga/TiO2. and reference compounds.

Supplementary Figure 4. Curve-fitting results of a Ni b Cu and c Ga K-edge k3-weighted EXAFS of (Ni0.8Cu0.2)3Ga/TiO2. Solid and dashed lines indicate the results of simulation and experiment, respectively.

Supplementary Figure 5. Curve-fitting results of a Ni and b Ga K-edge k3-weighted EXAFS of Ni3Ga/TiO2. Solid and dashed lines indicate the results of simulation and experiment, respectively.

Supplementary Figure 6. Curve-fitting results of a Ni b Cu and c Ga K-edge k3-weighted EXAFS of (Ni0.8Cu0.2)3Ga/SiO2. Solid and dashed lines indicate the results of simulation and experiment, respectively.

Supplementary Table 2. Summary of the EXAFS curve fitting for (Ni0.8Cu0.2)3Ga/TiO2, (Ni0.8Cu0.2)3Ga/SiO2, Ni3Ga/TiO2 catalysts and reference.

| Sample | Edge | Shell | So2 | CN | r (Å) | ∆Eo (eV) | σ2 (Å2) | R-factor |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Ni foil | Ni k | Ni-Ni | 0.846 | 12 | 2.48±0.01 | 5.43±0.7 | 0.00621 | 0.003 |
| Cu foil | Cu k | Cu-Cu | 0.918 | 12 | 2.54±0.02 | 6.26±0.9 | 0.0088 | 0.005 |
| Ga2O3 | Ga k | Ga-O | 1.316 | 3 | 1.91±0.09 | 6.84±1.8 | 0.00657 | 0.014 |
|  |  | Ga-O |  | 1 | 2.12±0.25 |  | 0.00361 |  |
|  |  | Ga-Ga |  | 2 | 3.05±0.01 |  | 0.00338 |  |
| (Ni0.8Cu0.2)3Ga/TiO2 | Ni k | Ni-Ga | 0.846 | 3.50±0.99 | 2.46±0.07 | 5.40±1.5 | 0.00415 | 0.003 |
|  |  | Ni-Ni(Cu) |  | 7.00±0.99 | 2.58±0.08 |  | 0.00472 |  |
|  | Cu k | Cu-Ga | 0.918 | 2.79±0.48 | 2.49±0.04 | 2.81±1.8 | 0.00275 | 0.008 |
|  |  | Cu-Cu(Ni) |  | 8.38±0.48 | 2.60±0.04 |  | 0.00799 |  |
|  | Ga k | Ga-O | 1.316 | 2.11±0.29 | 2.03±0.20 | 0.65±1.7 | 0.0698 | 0.005 |
|  |  | Ga-Ni(Cu) |  | 8.46±0.28 | 2.54±0.00 |  | 0.00914 |  |
| (Ni0.8Cu0.2)3Ga/SiO2 | Ni k | Ni-Ga | 0.846 | 3.29±0.64 | 2.43±0.11 | 4.51±1.1 | 0.00185 | 0.018 |
|  |  | Ni-Ni(Cu) |  | 6.58±0.64 | 2.57±0.04 |  | 0.00323 |  |
|  | Cu k | Cu-Ga | 0.918 | 3.59±0.93 | 2.29±0.24 | 9.38±2.3 | 0.02631 | 0.01 |
|  |  | Cu-Cu(Ni) |  | 10.8±0.93 | 2.50±0.05 |  | 0.00953 |  |
|  | Ga k | Ga-O | 1.316 | 1.47±0.20 | 1.81±0.01 | 1.91±1.6 | 0.00796 | 0.02 |
|  |  | Ga-Ni(Cu) |  | 5.89±0.20 | 2.54±0.00 |  | 0.00897 |  |
| Ni3Ga/TiO2 | Ni k | Ni-Ga | 0.846 | 3.51±1.22 | 2.45±0.09 | 6.27±1.9 | 0.00421 | 0.006 |
|  |  | Ni-Ni |  | 7.03±1.23 | 2.57±0.04 |  | 0.00389 |  |
|  | Ga k | Ga-O | 1.316 | 2.28±1.10 | 1.79±0.04 | 5.20±1.5 | 0.13945 | 0.021 |
|  |  | Ga-Ni |  | 9.11±1.12 | 2.53±0.00 |  | 0.00811 |  |

Supplementary Figure 7. XRD analysis for (Ni1-xCux)3Ga/TiO2 (x = 0, 0.2, 0.25, 0.33, 0.5, 0.6, 0.75) catalysts. Vertical solid lines indicate the diffraction angles of the corresponding (Ni1-xCux)3Ga phases.

Supplementary Figure 8. a C2H2 conversion, b C2H4 selectivity and c carbon balance as a function of reaction temperature over (Ni1-xCux)3Ga/TiO2.

Supplementary Figure 9. a C2H2 conversion and b C2H4 selectivity as a function of reaction temperature in the presence of ethylene (C2H2:H2:He:C2H4 = 1:10:39:5 mLmin-1) over (Ni0.8Cu0.2)3Ga/TiO2 and Ni3Ga/TiO2.

Supplementary Figure 10. Long-term stability test using (Ni0.8Cu0.2)3Ga/TiO2 in the presence of excess ethylene at 180°C. a C2H2 conversion and b C2H4 selectivity.

Supplementary Figure 11. Relationship between the specific activity and ethylene selectivity at high acetylene conversion (>80%) for 3d transition metal-based catalysts that were reported in literature and developed in this study. Numbers correspond to the entries in Supplementary Table 3.

Supplementary Figure 12. Relationship between the specific activity and ethylene selectivity at high acetylene conversion (>80%) at different reaction temperature for 3d transition metal-based catalysts that were reported in literature and developed in this study. Numbers correspond to the entries in Supplementary Table 3.

Supplementary Table 3. Summary of reaction conditions and catalytic performances in acetylene semihydrogenation using 3d transition metal-based catalysts that were reported in literature and developed in this study.

| entry | catalyst | loading (wt%) | amount / mg | C2H2 flow /mLmin-1 | C2H2 : H2 : C2H4 | total flow /mLmin-1 | GHSV / mLg−1h−1 | conv. (%) | sel. (%) | temp. / °C | specific rate / mLC2H2min−1gM−1 | Operation time (h) | ref |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | (Ni0.8Cu0.2)3Ga/TiO2 | 1 | 80 | 1 | 1 : 10 : 0 | 50 | 37500 | 100 | 96 | 150 | 1250.0 | 60 | This work |
| 2 | Ni3GaC0.5/MgAl LDH | 14.88 | 150 | 0.5 | 0.5:2.5:10 | 100 | 40000 | 100 | 90 | 110 | 22.4 | 36 | 1 |
| 3 | Ni1MoS/Al2O3 | 3.5 | 500 | 0.2475 | 1:20:0 | 165 | 19800 | 100 | 90 | 125 | 14.1 | 16 | 2 |
| 4 | NiCu/MgAl-MMO | 9.58 | 100 | 0.558 | 1 : 2 : 103 | 166 | 100500 | 81 | 88 | 140 | 47.2 | 36 | 3 |
| 5 | Cu(OH)2 | 78.9 | 100 | 1 | 1 : 9 : 0 | 10 | 6000 | 100 | 84 | 110 | 12.7 | 250 | 4 |
| 6 | Cu2O | 88.8 | 100 | 0.045 | 1 : 22 : 197 | 10 | 6000 | 100 | 64 | 120 | 0.5 | 100 | 5 |
| 7 | Ni3ZnC0.7/C | 12 | 50 | 1 | 1:15:0 | 100 | 120000 | 100 | 85 | 165 | 166.7 | 10 | 6 |
| 8 | AgNi0.5/SiO2 | 1.09 | 30 | 0.3 | 1:20:0 | 30 | 60000 | 100 | 55 | 180 | 917.4 | 24 | 7 |
| 9 | Ni/g-C3N4-T | 1 | 50 | 0.3 | 1:10:20 | 30 | 36000 | 99 | 84 | 175 | 594.0 | 20 | 8 |
| 10 | NiGa/MgAl-LDH | 10 | 50 | 1.2 | 1 : 10 : 20 | 120 | 144000 | 90 | 82 | 190 | 216.0 | 24 | 9 |
| 11 | 0.5Cu/Al2O3 | 0.5 | 300 | 0.2 | 1 : 10 : 50 | 20 | 4000 | 100 | 91 | 188 | 133.3 | 40 | 10 |
| 12 | Na-Ni/CHA | 3.5 | 200 | 0.5 | 1 : 16 : 0 | 50 | 15000 | 100 | 97 | 170 | 71.4 | 20 | 11 |
| 13 | Ni1Cu2/g-C3N4 | 3.5 | 150 | 0.15 | 1 : 10 : 50 | 30 | 12000 | 100 | 90 | 160 | 28.6 | 400 | 12 |
| 14 | Cu1/ND | 0.25 | 200 | 0.1 | 1 : 10 : 20 | 10 | 3000 | 95 | 98 | 200 | 190.0 | 60 | 13 |
| 15 | Ni–CeO2 | 1.54 | 200 | 0.35 | 1 : 70 : 4 | 70 | 21000 | 100 | 100 | 200 | 113.6 | 3 | 14 |
| 16 | Ni6In/SiO2 | 8 | 500 | 3 | 1 : 10 : 0 | 300 | 36000 | 100 | 64 | 200 | 75.0 | 35 | 15 |
| 17 | Al13Fe4 | 38.9 | 20 | 0.15 | 1 : 10 : 100 | 30 | 90000 | 85 | 84 | 200 | 16.4 | 14 | 16 |
| 18 | Ni-SAs/N-C | 5.67 | 400 | 0.2 | 1 : 20 : 100 | 40 | 6000 | 96 | 91 | 200 | 8.5 | 18 | 17 |
| 19 | Co2FeGe | 47.8 | 400 | 0.03 | 1 : 400 : 100 | 30 | 4500 | 91 | 90 | 200 | 0.1 |  | 18 |
| 20 | Ni3Ga/TiO2 | 1 | 80 | 1 | 2 : 10 : 0 | 50 | 37500 | 100 | 97 | 230 | 1250.0 | 1 | This work |
| 21 | NiCuFeGaGe/SiO2 | 1 | 100 | 1 | 1 : 10 : 0 | 50 | 30000 | 100 | 98 | 220 | 1000.0 | 28 | 19 |
| 22 | NiCu/ZrO2 | 4.6 | 25 | 0.4 | 1:10:20 | 40 | 96000 | 100 | 93 | 220 | 347.8 | 15 | 20 |
| 23 | Ni3Ga/MgAl2O4 | 2 | 100 | 0.33 | 1 : 20 : 100 | 67 | 144000 | 92 | 77 | 220 | 153.3 | 24 | 21 |
| 24 | Ni/MCM-41 | 25 | 100 | 3.7 | 1 : 2 : 0 | 66.6 | 40000 | 96 | 87 | 240 | 142.2 | 10 | 22 |
| 25 | Ni3Ge/MCM-41 | 3.2 | 1500 | 3.9 | 1 : 2.1 : 0 | 29 | 1160 | 94 | 89 | 250 | 76.4 |  | 23 |
| 26 | Cu2.75Ni0.25Fe | - | 150 | 0.63 | 1.5:4.5:8.1 | 42 | 16800 | 100 | 75 | 250 |  | 30 | 24 |
| 27 | Cu/Fe0.16MgOx | 18.0 | 200 | 0.69 | 1 :100 : 3 | 209 | 62700 | 100 | 95 | 215 | 19.2 | 40 | 25 |
| 28 | NiSb/MgAl LDH | 8.58 | 300 | 0.15 | 0.5:2.5:30 | 30 | 6000 | 100 | 93.2 | 260 | 5.8 | 48 | 26 |
| 29 | NiCu0.125/MCM-41 | 1 | 100 | 3.3 | 1 : 3 : 0 | 13.3 | 8000 | 100 | 63 | 250 | 3333.3 | 9 | 27 |

Supplementary Figure 13. a XRD pattern of (Ni0.8Cu0.2)3Ga/SiO2 and b its magnification indicated as the bule square. The center of 111 diffraction was at 43.72° (blue dotted line), which agreed with that of (Ni0.8Cu0.2)3Ga/TiO2 (43.74°).

Supplementary Figure 14. a C2H2 conversion and b C2H4 selectivity as a function of reaction temperature in the absence of ethylene (C2H2:H2:He = 1:10:39 mLmin-1) over (Ni0.8Cu0.2)3Ga/TiO2 and (Ni0.8Cu0.2)3Ga/SiO2.

Supplementary Figure 15. a C2H2 conversion and b C2H4 selectivity as a function of reaction temperature in the presence of ethylene (C2H2:H2:He:C2H4 = 1:10:39:5 mLmin-1) over (Ni0.8Cu0.2)3Ga/TiO2 and (Ni0.8Cu0.2)3Ga/SiO2.

Supplementary Figure 16. a C2H2 conversion and b C2H4 selectivity as a function of reaction temperature over (Ni0.8M0.2)3Ga/TiO2 (M = Cu, Fe, Co, Zn) and Ni3Ga/TiO2.

Supplementary Figure 17. Ethylene temperature programmed surface reaction profiles (TPSR) of the (Ni0.8Cu0.2)3Ga/TiO2 and Ni3Ga/TiO2 catalysts for ethylene hydrogenation.

Supplementary Figure 18. C2H2-TPD profiles of the (Ni0.8Cu0.2)3Ga/TiO2 and Ni3Ga/TiO2 catalysts.

Supplementary Figure 19. Optimized structures of the slab and adsorbates in acetylene hydrogenation to ethane over Ni3Ga(111).

Supplementary Figure 20. Optimized structures of the slab and adsorbates in acetylene hydrogenation to ethane over (Ni0.8Cu0.2)3Ga(111).

Supplementary Figure 21. Relative energy of ethylidene intermediate on Ni3Ga(111) and (Ni0.8Cu0.2)3Ga(111). Sum of gas phase C2H6 and the clean slab was set to zero in energy as in Figure 3a.

Supplementary references

1.	Ge, X. et al. Enhanced acetylene semi-hydrogenation on a subsurface carbon tailored Ni-Ga intermetallic catalyst. J. Mater. Chem. A 19722–19731 (2022).

2.	Fu, B. et al. Highly Selective and Stable Isolated Non-Noble Metal Atom Catalysts for Selective Hydrogenation of Acetylene. ACS Catal. 12, 607–615 (2022).

3.	Liu, Y. et al. Layered double hydroxide-derived Ni-Cu nanoalloy catalysts for semi-hydrogenation of alkynes: Improvement of selectivity and anti-coking ability via alloying of Ni and Cu. J. Catal. 359, 251–260 (2018).

4.	Lu, C., Zeng, A., Wang, Y. & Wang, A. Copper-Based Catalysts for Selective Hydrogenation of Acetylene Derived from Cu(OH)2. ACS Omega 6, 3363–3371 (2021).

5.	Lu, C., Wang, Y., Zhang, R., Wang, B. & Wang, A. Preparation of an Unsupported Copper-Based Catalyst for Selective Hydrogenation of Acetylene from Cu2O Nanocubes. ACS Appl. Mater. Interfaces 12, 46027–46036 (2020).

6.	Wang, Y., Liu, B., Lan, X. & Wang, T. Subsurface Carbon as a Selectivity Promotor to Enhance Catalytic Performance in Acetylene Semihydrogenation. ACS Catal. 11, 10257–10266 (2021).

7.	Liu, H. et al. Effect of IB-metal on Ni/SiO2 catalyst for selective hydrogenation of acetylene. Chinese J. Catal. 41, 1099–1108 (2020).

8.	Zhou, H. et al. Sulfur-Doped g-C3N4-Supported Ni Species with a Wide Temperature Window for Acetylene Semihydrogenation. ACS Sustain. Chem. Eng. 10, 4849–4861 (2022).

9.	Cao, Y. et al. Adsorption Site Regulation to Guide Atomic Design of Ni–Ga Catalysts for Acetylene Semi‐Hydrogenation. Angew. Chemie 132, 11744–11749 (2020).

10.	Shi, X. et al. Copper Catalysts in Semihydrogenation of Acetylene: From Single Atoms to Nanoparticles. ACS Catal. 10, 3495–3504 (2020).

11.	Chai, Y. et al. Acetylene-Selective Hydrogenation Catalyzed by Cationic Nickel Confined in Zeolite. J. Am. Chem. Soc. 141, 9920–9927 (2019).

12.	Gu, J. et al. Synergizing metal–support interactions and spatial confinement boosts dynamics of atomic nickel for hydrogenations. Nat. Nanotechnol. 16, 1141–1149 (2021).

13.	Huang, F. et al. Anchoring Cu1 species over nanodiamond-graphene for semi-hydrogenation of acetylene. Nat. Commun. 10, 4431 (2019).

14.	Riley, C. et al. Synthesis of Nickel-Doped Ceria Catalysts for Selective Acetylene Hydrogenation. ChemCatChem 11, 1526–1533 (2019).

15.	Chen, Y. & Chen, J. Selective hydrogenation of acetylene on SiO2 supported Ni-In bimetallic catalysts: Promotional effect of In. Appl. Surf. Sci. 387, 16–27 (2016).

16.	Armbrüster, M. et al. Al13Fe4 as a low-cost alternative for palladium in heterogeneous hydrogenation. Nat. Mater. 11, 690–693 (2012).

17.	Dai, X. et al. Single Ni sites distributed on N-doped carbon for selective hydrogenation of acetylene. Chem. Commun. 53, 11568–11571 (2017).

18.	Kojima, T., Kameoka, S., Fujii, S., Ueda, S. & Tsai, A. P. Catalysis-tunable Heusler alloys in selective hydrogenation of alkynes: A new potential for old materials. Sci. Adv. 4, (2018).

19.	Ma, J., Xing, F., Nakaya, Y., Shimizu, K. ichi & Furukawa, S. Nickel-Based High-Entropy Intermetallic as a Highly Active and Selective Catalyst for Acetylene Semihydrogenation. Angew. Chemie - Int. Ed. 61, (2022).

20.	Li, Z. et al. Unveiling the origin of enhanced catalytic performance of NiCu alloy for semi-hydrogenation of acetylene. Chem. Eng. J. 450, 138244 (2022).

21.	Liu, Y. et al. Intermetallic NixMy(M = Ga and Sn) Nanocrystals: A Non-precious Metal Catalyst for Semi-Hydrogenation of Alkynes. Adv. Mater. 28, 4747–4754 (2016).

22.	Zhao, J. et al. Preparation of MCM-41 supported nickel NPs for the high-efficiency semi-hydrogenation of acetylene. New J. Chem. 45, 1054–1062 (2021).

23.	Komatsu, T., Kishi, T. & Gorai, T. Preparation and catalytic properties of uniform particles of Ni3Ge intermetallic compound formed inside the mesopores of MCM-41. J. Catal. 259, 174–182 (2008).

24.	Bridier, B. & Pérez-Ramírez, J. Coperative effects in ternary Cu-Ni-Fe catalysts lead to enhanced alkene selectivity in alkyne hydrogenation. J. Am. Chem. Soc. 132, 4321–4327 (2010).

25.	Fu, F. et al. Interfacial Bifunctional Effect Promoted Non-Noble Cu/FeyMgOx Catalysts for Selective Hydrogenation of Acetylene. ACS Catal. 11, 11117–11128 (2021).

26.	Ge, X. et al. Mechanism driven design of trimer Ni1Sb2 site delivering superior hydrogenation selectivity to ethylene. Nat. Commun. 13, 5534 (2022).

27.	Zhou, S., Kang, L., Zhou, X., Xu, Z. & Zhu, M. Pure acetylene semihydrogenation over Ni–Cu bimetallic catalysts: Effect of the Cu/Ni ratio on catalytic performance. Nanomaterials 10, 509 (2020).