Supplementary information for

Blue Quantum Emitters in hexagonal Boron Nitride

Haidong Liang1,2,#,*, Yuan Chen3,#, Leyi Loh2,4, Nicholas Lin Quan Cheng2, Yifeng Chen2,5, Chengyuan Yang1,2, Zhepeng Zhang2, Kenji Watanabe6, Takashi Taniguchi7, Su Ying Quek2,4,5,8, Michel Bosman4, Goki Eda2,3,5, *, Andrew A. Bettiol1,2,*

1 Centre for Ion Beam Applications (CIBA), Department of Physics, National University of Singapore, Singapore 117542, Singapore

2 Department of Physics, National University of Singapore, Singapore 117551, Singapore

3Department of Chemistry, National University of Singapore, 117543, Singapore

4Department of Materials Science and Engineering, National University of Singapore, 117575, Singapore

5Centre for Advanced 2D Materials, National University of Singapore, 117542, Singapore

6Research Centre for Functional Materials, National Institute for Materials Science, Tsukuba 305-0044, Japan;

7International Centre for Materials Nanoarchitectonics, National Institute for Materials Science, Tsukuba 305-0044, Japan

8NUS Graduate School Integrative Sciences and Engineering Programme, National University of Singapore, 117456, Singapore

# These authors contributed equally. * Authors to whom correspondence should be addressed. Electronic mail: haidong@nus.edu.sg, g.eda@nus.edu.sg, a.bettiol@nus.edu.sg

Fig. S1. PL spectra of some other ensembles of emitters in hBN powders.

Spectra obtained from several ensembles of blue emitters exhibit similar properties as the spectrum shown in Fig. 1. The PL emissions cover all the visible range when excited using a 405 nm laser. However, the blue emissions dominate in most cases. Usually, there are two main peaks at around 427 nm and 452 nm. Similar blue emissions was also observed in hBN as reported by Hayee, F. et al.1

Fig. S2. Nearby SPEs have similar emissions. a, PL mapping of four emitters located nearby. b, PL spectra from four emitters selected in a. c, g2(τ) measurements of the four selected emissions.

Most of the blue emitters that are close to each other have similar PL spectra. It is difficult to distinguish them with the objective lens. Fig. S2 shows an example.

Fig. S3. More blue SPEs, with PL spectra (left) and g2(τ) (right) results confirming their single photon emission properties. The blue highlighted part indicates the selected wavelength range for the g2(τ) measurements. SPEs measured with a, 462 nm peak emission, b, 489 nm peak emission. c, 427 nm peak emission, d, 506 nm peak emission, e, 446 nm peak emission, f, 492 nm peak emission.

There are three main types of blue quantum emitters that have been observed. The first has a ZPL peak at around 430 nm, examples include SPE3, SPE8. The second has a peak at around 450-460 nm, examples include SPE1, SPE2, SPE4, SPE5, SPE6, SPE7, SPE9. The third has a peak at around 490 nm, examples are SPE10, SPE11, SPE12.

Fig. S4. SPEs with longer wavelengths. a, PL spectrum of a quantum emitter in hBN powder. b, g(2) measurements with different wavelength range. The top is for the blue wavelength range, highlighted with blue colour in the spectrum, the bottom is for the red wavelength range, highlighted with a red colour in the spectrum.

Unlike blue SPEs, for emissions in hBN powders with longer wavelength, once a sharp PL peaks observed, it is probably a SPE, and it can be accompanied with the blue emissions. Fig. S4 is such an example.

Fig. S5. Details of the irradiation conditions in Fig. 3d-f. The schematic of the irradiation points. The overall scan size is 36×36 µm, with 2048×2048 pixels. The patterned points have three different sizes: 53 nm×53 nm (3×3 pixels), 106 nm×106 nm (6×6 pixels) and 159 nm×159 nm (9×9 pixels), as marked in different columns in the figure. Each two rows are irradiated with different dwell times: from 1 s/pixel to 1 ms pixel (top to bottom), as marked in the figure. The irradiation current is 0.9 pA, and the highest fluence for the spots is ~5.6×106 ions/pixel, and 4.5×107 ions/spot (9× 9 pixels).

Fig. S6. PL spectra of hBN flakes on different substrates irradiated using different energies and ions.

Both proton and helium ion beam irradiation can create the blue emissions in hBN on different substrates. This might suggest that the blue emissions is from the an internal vacancy or intercalant defects.

Fig. S7. PL data from additional high temperature annealed hBN. a, Microscope image of two annealed hBN flakes. b, PL map of the two hBN flakes in a. c, PL spectra of different emissions marked in b. d, Microscope image of another annealed hBN flake. e, PL map of the sample in d. All scale bars are 5µm. f, PL spectra of the emissions marked in e.

Fig. S8. Blue emitters and VB-. a, Microscope image of a patterned irradiated hBN flake using 1.6MeV He+. There are squares and points. The top square and two rows of points have been irradiated with a fluence of 6E16. The top second squares and next two rows of points have been irradiated with a fluence of 3E16, and then 1E16, 5E15, 3E15, 1E15, 3E14 to the bottom square and two rows of points. b, Blue emission PL map of the irradiated hBN flake in a. c, PL spectra of the pristine and irradiated squares with different fluences, excited by 405 nm laser. d, PL spectra of 4 points marked in a and b, excited by 405 nm laser. They are labelled as ‘point1’: an irradiated point in the first row, with a fluence of 6E16, ‘centre1’ an unirradiated point in centre of four irradiated points, close to ‘point1’, ‘point6’: an irradiated point in the 11th row, with a fluence of 1E15, ‘centre6’: an unirradiated point close to ‘point6’. e, ODMR spectrum of the VB- spin defects in the 3E16 square. f, VB- PL map of the same hBN flake, excited by 532 nm laser. g, PL spectra of the pristine and irradiated squares, excited by 532 nm laser. h, PL spectra of 4 points marked in a and b, excited by 532 nm laser. All fluences are in units of ions/cm2.

Both the blue emissions and the VB- spin defects2,3 are created by high energy He+ irradiation. However, the distributions of the two emissions are a slightly different. For the VB-  spin defects, the PL intensity increases up to the highest irradiation fluence 6E16, as shown in Fig. S8g. It means in this fluence range, the He+ irradiation can continue to create more VB-  spin defects without significant damage the overall crystal lattice. However, for the blue emissions, the PL intensity increases with fluence up to 3E15 ions/cm2, and then decreases with increasing fluence, as shown in Fig. S8c. When the fluence is over 1E16 ions/cm2, the blue emissions spread beyond the irradiation area. For example, the unirradiated point ‘centre1’ marked in Fig. S8a is giving the same blue emissions as the irradiated points and squares, as shown in Fig. S8d. However, if it is excited by 532 nm laser, the same point is not giving any emission from VB-  spin defects as shown in Fig. S8h. This is consistent with our assumption that the blue emissions are from Bint and Nint. While for VB-  spin defects, the boron vacancies are confined to the irradiate region only. The knocked out boron and nitrogen atoms can propagate through the crystal, and the Bint and Nint would spread out of the irradiated region, when the irradiation fluence is high.

Figure S9. HAADF-STEM images of 7 areas across the proton-irradiated hBN multilayer. For each area, as-imaged (left panel) and the same image with defects denoted (right panel) of a large-area HAADF-STEM image. Blue circle represents B atoms and yellow circle represents N atoms. In the right panels, filled circles denote missing atoms and dashed unfilled circles denote additional atoms (e.g., adatoms and intercalants).

References

1.	Hayee, F. et al. Revealing multiple classes of stable quantum emitters in hexagonal boron nitride with correlated optical and electron microscopy. Nat. Mater. 19, 534–539 (2020).

2.	Gottscholl, A. et al. Initialization and read-out of intrinsic spin defects in a van der Waals crystal at room temperature. Nat. Mater. 19, 540–545 (2020).

3.	Liang, H. et al. High Sensitivity Spin Defects in hBN Created by High-Energy He Beam Irradiation. Adv. Opt. Mater. 2201941, 1–7 (2022).