Supporting Information

Grafted antimicrobial cotton fabrics with N-halamine groups via atom transfer radical polymerization

Panpan Peng1,  Ziwen Zhang1, Jianjun Yang*1,2, Mingyuan Wu1,2, Qingyun Wu1,2, Jiuyi Liu1,2, Jianan Zhang1, 2

1 School of Chemistry and Chemical Engineering, Anhui University;

2 Anhui Province Key Laboratory of Environment-friendly Polymer Materials, Hefei 230601, China.

*Corresponding Author

Jianjun Yang, E-mail: andayjj@163.com.

Fig S1  Synthesis procedure of SCMHBMA

Fig S2: 1H NMR spectrum of SCMHBMA in CDCl3

2-(3-(6-methyl-4-oxo-1,4-dihydropyrimidin-2-yl)ureido) (SCMHBMA). 1H NMR (400 MHz, CDCl3 ) δ 12.95 (s, 1H), 11.92 (s, 1H), 10.47 (s, 1H), 6.20 (s, 1H), 5.77 (s, 1H), 5.52 (s, 1H), 4.24 (s, 2H), 3.73 (s, 2H), 2.21 (s, 3H), 1.91 (s, 3H).

Table S1 Characteristics of Cotton-g-PSMA

| Monomer | Reaction time (h) | Graft ratio of polymer (%) | Mn (GPC) | Mw/Mn |
| --- | --- | --- | --- | --- |
| SCMHBMA | 48 | 21.6 | 48727 | 1.41 |

In order to calculate the grafting ratio, the polymer grafted Cotton were weighted before and after ATRP. The grafting ratio (%) was calculated as follows:

G=W2-W1W1×100%

where, W1 and W2 are weights of polymer grafted Cotton before and after, respectively.

The grafting ratio and the molecular weight of  Cotton-g-PSMA was presented in Table S1. It can be seen that the grafting ratio and the molecular weight of SCMHBMA was 21.6% and 48727.