Supplementary Materials for

Reconfigurable Geometrical Phase Spatial Light Modulator Using Short-Pitch Ferroelectric Liquid Crystals

Zhi-bo Sun, Zheng-nan Yuan, Vigneshwaran Swaminathan, Valerii Vashchenko, Olena Vashchenko, Alex Yuk Lung Cheung, Lei Lu, Hoi-sing Kwok and Abhishek. K. Srivastava*

State Key Laboratory of Advanced Displays and Optoelectronics Technologies, and Center for Display Research, Department of Electronics and Computer Engineering, Hong Kong University of Science and Technology, Clear Water Bay Road, Kowloon, Hong Kong

Corresponding Author: Abhishek. K. Srivastava (eeabhishek@ust.hk) Phone Number: (852) 3469 2485

Contact Information:

Zhi-bo Sun (zsunak@connect.ust.hk); Zheng-nan Yuan (zyuanae@connect.ust.hk); Vigneshwaran Swaminathan (eeswaminav@ust.hk); Valerii Vashchenko (eevvv@ust.hk); Olena Vashchenko (eeevv@ust.hk); Alex Yuk Lung Cheung (eealexcheung@ust.hk); Lei Lu (lulei@pku.edu.cn); Hoi-sing. Kwok (eekwok@ust.hk)

CONTENT

1	Supplementary Methods	2

1.1	General Methods	2

1.2	Syntheses	2

1.3	Helix pitch measurements	3

2	Supplementary Discussion	4

2.1	Alignment optimization of DHFLC	4

2.2	EO measurement setup	4

2.3	EO performance of different DHFLC	4

2.4	Compensation film design	4

3	Supplementary Discussion and Equation(s)	6

3.1	Study of Fringe Field Effect on FLCs Based on Proposed Dynamic Model	6

3.2	Prototype fabrication using passively driven 64*64 3 µm pixel size	8

3.3	Measurement results of the reference cell using E7 ECB cell.	8

Supplementary Methods

General Methods

1H NMR spectra were recorded on a Bruker AVII 400 (400MHz) spectrometers in CDCl3 using the TMS as the internal standard.

The MALDI-TOF mass spectra were run by a Waters Micromass MALDI micro MXTM Mass Spectrometer operates on the reflectron mode. The DCTB matrix was used. The CI mass spectrum was run by a Waters Micromass GCTTM Premier Mass Spectrometer operated on the positive ion mode with CH4 as the reagent gas.

HPLC experiments were performed with a Thermo Scientific Dionex UltiMate 3000 instrument fitted with Thermo Scientific Accucore C18 reversed phase column (150 x 2.1 mm) using acetonitrile as eluent at 40 oC.

The phase transition temperatures of the materials were determined using differential scanning calorimetry with Thermo Scientific DSC-25 calorimeter at scanning rate 1 or 2 /min. Phase assignment was carried out according to “natural” textures observation using polarization microscopy (POM).

Unless otherwise specified, all reagents were commercially available and used without further purification.

Unless otherwise specified, all reagents were commercially available and used without further purification. If appropriate, solvents were dried by known methods and distilled immediately prior to use. (R)-1,1,1-Trifluoroalkan-2-ols (2a–e) were synthesized and their enantiomeric purity was determined according to Ref. [S].

Syntheses

Syntheis of bis-(S-2-trifluoromethyl-heptyl) 2,2''-difluoro-[1,1':4',1''-terphenyl]-4,4''-dicarboxylate (DFT-TFA-6) was carried out accordingly to the scheme below.

S-2-(trifluoromethyl)heptyl-2-fluoro-4-bromobenzoate. A solution of 3.27 g (15.8 mmol) of dycyclohexyl-carbodiimide (DCC) in 20 ml of dry dichloromethane (DCM) is added dropwise to a stirred and cooled (ice-water) mixture of 2.89 g (13.2 mmol) of 2-fluoro-4-bromobenzoic acid, 2.28 g (12.4 mmol) of S-1-(trifluoromethyl)-heptanol and 5 mg of 4-N,N-dimethylaminopyridine in 30 ml of DCM. After finishing addition, the mixture is stirred while reaction is completed (monitoring by TLC), then filtered through the short plug of silica gel. The silica gel washed additionally with 150 ml of DCM, the combined solutions in DCM is evaporated to dryness furnishing 5.2 g of oil, which is solidified upon storage. The ester was used on the next step without additional purification.

Bis-(S-2-trifluoromethyl-heptyl) 2,2''-difluoro-[1,1':4',1''-terphenyl]-4,4''-dicarboxylate. Mixture of 2.22 g (5.8 mmol) of S-1-(trifluoromethyl)heptyl-2-fluoro-4-bromobenzoate, 0.4 g (2.4 mmol) of 1,4-phenylenediboronic acid, 300 mg of sodium dodecylsulphate (SDS), 171 mg of PdCl2dppf, 5 ml of 1-butanol, 10 ml of water, and 30 ml of toluene is thoroughly degassed (3 cycles of pumping out to ~ 100 mbar and filling with N2), then heated to reflux and added dropwise a degassed solution of 2.9 g (34,8mmol) of NaHCO3 in 20 ml of water. Reaction mixture is refluxed additionally for 2 h, then cooled down to ambient temperature and separated organic layer. The water layer is extracted 3 times with toluene. Combined organic extracts is washed with water, dried over Na2SO4, filtered through short plug of silica gel, washed silica gel with toluene and evaporated toluene filtrate to dryness. The residual yellowish oil is purified by column chromatography on silica gel (502 cm, eluent Toluene:Hexane 1:1 w/w), furnished 1.00 g (62 %) of the product as a colourless oil.

1H NMR (400 MHz, CDCl3) δ 8.09 (t, J = 7.8 Hz, 1H), 7.76 (s, 2H), 7.54 (dd, J = 8.2, 1.7 Hz, 1H), 7.47 (dd, J = 11.7, 1.7 Hz, 1H), 5.61 (h, J = 6.7 Hz, 1H), 1.97 – 1.88 (m, 2H), 1.57 – 1.24 (m, 7H), 0.97 – 0.84 (m, 3H).

Syntheis of bis((S)-1,1,1-trifluorooctan-2-yl) 6,6'-(1,4-phenylene)dipicolinate (PDN-TFA-6) was carried essentially following to the protocol described for DFT-TFA-6.

Quantities: 6-bromonicotinic acid 2.024 g (10 mmol); S-1-(trifluoromethyl)heptanol 1.76 g (9.54 mmol); 1,4-phenylenediboronic acid 0.624 g (3,76 mmol). Yield of the product PDN-TFA-6 is 1.0 g (40.7%), mp. 57 C.

HRMS: Calcd. for M+H C34H39F6N2O4 653.2814; found: 653.2816.

1H NMR (400 MHz, CDCl3) δ 9.37 (dd, J = 2.3, 0.8 Hz, 1H), 8.42 (dd, J = 8.4, 2.2 Hz, 1H), 8.25 (s, 2H), 7.95 (dd, J = 8.4, 0.9 Hz, 1H), 5.60 (h, J = 6.7 Hz, 1H), 1.93 (q, J = 7.2 Hz, 2H), 1.50 – 1.28 (m, 6H), 0.92 – 0.84 (m, 3H).

Helix pitch measurements

The homeotropic (vertical) alignment of SmC* in cells with ~20 µm FLC layer thickness was assured by spin-coating a thin layer of chromium oxostearyl chloride onto the glass substrates [S] and used only for measurements of the p0 in SmC* phase following to known methods [S, S].

The helix pitch (p0) within the range 130–680 nm was measured by the Bragg diffraction of the light in both normal and oblique incidence of light using microscope equipped with thermal stabilized hot stage using Ocean optics USB-4000 spectrometer. The average birefringence n=1.6 was adopted.

The p0 values less than 130 nm were obtained by extrapolation of linear dependencies of HTP(t), see Extended Data Figure 1 as an example.

Supplementary Discussion

Fabrication and alignment optimization of DHFLC

The fabrication process and alignment optimization are shown in Extended Data Figure 2

EO measurement setup

The EO measurement setup (Mach-Zehnder Michelson interferometer and Michelson interferometer) are shown in Extended Data Figure 3 and 4.

EO performance of different DHFLC

The EO performance of different DHFLCs are shown in Extended Data Figure 3 and 4

Compensation film design

The target function is the integration of the deviation of the retardation from the half-wave condition at all the voltage used (for example 0-10V). the optimal condition can be read by the minimum point in the contour map. Retardation of the DHFLC and compensation film, optical axis of the compensation film are simulated for two cases. On the one hand, we compensate the ellipticity for the reflected mode 2pi phase modulation using DHFLC. On other hand, π phase modulation with better ellipticity is also optimized. The simulation results are shown in Extended Data Figure. 5

The optimization code in MATLAB is attached below:

function [out_delta, out_director,Y] = broadsweep(dn,tilt,dmax,lamda)

L = length(dn);

N = 100;

director = linspace(0.1,pi,N);

delta = linspace(0.1,pi,N);

temp_d = linspace(0.1,1,N)*dmax;

out = zeros(N,N);

phase_p1 = zeros(L,1);

phase_p2 = zeros(L,1);

phase_n1 = zeros(L,1);

phase_n2 = zeros(L,1);

for i=1:N

temp_delta = delta(i);

for j=1:N

%d = temp_d(j);

d = 2e-6;

temp_angle = director(i);

%for k=1:N

%temp_twist = twist(k);

%temp_angle = 155.3557/180*pi;

temp_twist = 1e-8;

for e=1:L

temp_tilt = tilt(e);

temp_dn = dn(e);

MDHFLC = R(-temp_tilt)*[exp(-1i*pi*temp_dn*d/lamda),0;0,exp(1i*pi*temp_dn*d/lamda)]*R(temp_tilt);

Mcom1 = R(temp_angle)*Matrix(temp_twist,temp_delta)*R(-temp_angle);

Mcom2 = R(-temp_angle)*Matrix(temp_twist,temp_delta)*R(temp_angle);

M = Mcom2*MDHFLC*Mcom1;

Eout_positive = M*1/sqrt(2)*[1,1i]';

Mcom1 = R(-temp_angle)*Matrix(temp_twist,temp_delta)*R(temp_angle);

Mcom2 = R(temp_angle)*Matrix(-temp_twist,temp_delta)*R(-temp_angle);

M = Mcom2*MDHFLC*Mcom1;

Eout_negative = M*1/sqrt(2)*[1,1i]';

phase_p1(e) = angle(Eout_positive(1));

phase_p2(e) = angle(Eout_positive(2));

phase_n1(e) = angle(Eout_negative(1));

phase_n2(e) = angle(Eout_negative(2));

end

temp_p = abs(abs(phase_p1-phase_p2)-1.57);

temp_n = abs(abs(phase_n1-phase_n2)-1.57);

out(i,j) = integ(dn,temp_p)+ integ(dn,temp_n);

end

end

[X,x] = min(out);

[Y,y] = min(X);

out_delta = delta(x(y));

%out_director = director(y)/pi*180;

out_director = temp_d(y);

figure;

contour(director/pi*180,delta,out);

xlabel('optical axis of compensation film');

ylabel('retardation of compensation film');

tilt('compensation for 2pi phase modulation');

end

Supplementary Discussion and Equation(s)

Study of Fringe Field Effect on FLCs Based on Proposed Dynamic Model

As shown in Extended Data Figure 6, regarding the area between the electrode(labeled in red dosh line) as the closed surface in the whole 3-dimensional cell structure, the electric field flux through the surface S that encloses the volume (Vgap)=ITO gap (W)* cell gap (d)* cell dimension (L) can be written according to Gaussian surface. Moreover, the FLCs filled between the substrate are scads of dipoles, put another way, the free charge (Q) in the volume(V) is zero. So, the field flux in planar aligned FLC cell can be expressed as:

|  | D.dS=Q | (1) |
| --- | --- | --- |
|  | D.dS=2*(0dεxEx*L*dz)-(εzEd*W*L) | (2) |  |

Where the D is the electric displacement field; εx and εz are the dielectric constant along x-axis and z-axis, respectively. L is the dimension of the cell; W is the width between ITO (ITO gap); Ex is the electric field along x-axis. Ed is the maximum electric field in the region between each ITO electrode.

To estimate the fringe field effect origins from the applied electric field and derivate the relationship between Ed,Ex and Ez from equation 2, the electric distribution based on different ITO gaps, cell gaps and positions along z-axis is simulated (Extended Data Figure 6).

According to electric field distribution simulation, the in-plane electric field Ex along x and z-axis is non-uniform. Along the z-axis, the closer to the ITO electrode, the larger Ex. The Ex approximates 0 at the common electrode. To simplify the calculation, the electric flux is calculated at x=d/2. Similarly, due to symmetry, the Ex at the middle of the electrode gap equals 0 along the x-axis, the Ex shows shaper decreasing distribution profile. So, the flux is calculated from the 1/3 max of Ex.

|  | 2*εxEx*L*d*16-εzEd*W*L=0 | (3) |
| --- | --- | --- |

So, it can be simplified to:

|  | εxEx*d≈3εzEd*W | (4) |
| --- | --- | --- |

Based on the simulation shown in Extended Data Figure 6, in the near field of filed, Ex≈Ez, this matches the data derived from the Gaussian theory.  When the position is very close to the electrode surface the electrode density is the same everywhere on the electrode, forming a uniform electric field. The relation between electric fields can be expressed as:

|  | εx3εzdwidthEz≈Ed | (5) |
| --- | --- | --- |

Furthermore, the FFE of different FLC materials is evaluated based on varying the cell gap and ITO gap. As shown in Extended Data Figure 7, different unwinding process brings various FFE. Material with a shorter pitch shows fewer FFE since it has a larger dielectric constant difference along the x and z-axis. Moreover, dielectric anisotropy is also an important factor. This FFE simulation results based on varying material and electrode designs match the experiment results. So far, the simulation focuses on the electric field, the influence of the extra capacitor, and the corresponding TVC shall also be involved in future work. The FLC TVC might change due to the effect of surface anchoring energy and the hysteresis, which requires future study.

According to the simulation results in Extended Data Figure 7 g and h, the maximum PPI is simulated for DHFLC with different birefringence which is the most important parameter to determine the cell gap with designed wavelength. For the DHFLC with birefringence around 0.2, in display panel, the minimum pixel size and maximum PPI are 0.75 μm and 33000 PPI, respectively. Also, in communication wavelength, the minimum pixel size can be below 1.5 μm which can also within the subwavelength range. With increased birefringence of the DHFLC, the cell gap and PPI can be further optimized.

Prototype fabrication using passively driven 64*64 3 µm pixel size

The prototype is shown in Extended Data Figure 8 a-f

Measurement results of the reference cell using E7 ECB cell.

The measurement resutls shown in Extended Data Figure 8 g and h. Phase modulation measurement using electro-controlled birefringence cell which made by an anti-parallel LC cell filled by 5CB (HCCH). The measurement setup is the same as the system in this paper. The measurement results of this reference 5CB LC cell matches well with the theory and EO-performance between cross polarizer.

[S] V. Mikhailenko, D. Yedamenko, G. Vlasenko, A. Krivoshey, V. Vashchenko, Syntheses of (R)- and (S)-enantiomeric 1,1,1-trifluoromethyl-2-alkanols with high enantiomeric purity controlled through derivatization with L-menthyl phthalate, Tetrahedron Lett. 56 (2015) 5956–5959.

[S] Pozhidaev, E.P., Kiselev, A.D., Schrivastava, A.K., Chigrinov, V.G., Kwok, H.S., Minchenko, M., 2013. Orientational Kerr effect and phase modulation of light in deformed-helix ferroelectric liquid crystals with subwavelength pitch. Phys. Rev. E. 87, 052502.

[S] K. Hori, Angular dependence of selective reflection from the chiral smectic C phase, Mol. Cryst. Liq. Cryst. 82 (1982) 13–17.

[S] Mikhailenko, V. et al. The nano-scale pitch ferroelectric liquid crystal materials for modern display and photonic application employing highly effective chiral components: Trifluoromethylalkyl diesters of p-terphenyldicarboxylic acid. Journal of Molecular Liquids 281, 186-195 (2019)