SUPPLEMENTARY INOFORMATION

Innovative low-cost engineered adsorbents based on waste eggshell for nickel removal from aqueous solutions

Adina-Elena SEGNEANU1, Roxana TRUSCA2, Claudiu CEPAN3, Maria MIHAILESCU3,4, 

 Cornelia MUNTEAN3,4 and Ioan GROZESCU3
1
Institute for Advanced Environmental Research-West University of Timisoara (ICAM-WUT) Oituz nr. 4, Timișoara
2 
National Center for Micro and Nanomaterials, Politehnica University of Bucharest
3
 University Politehnica Timisoara, 2 P-ta Victoriei, 300006, Timisoara, Romania

4
Research Institute for Renewable Energy, 138 Gavril Musicescu Str, 300501, Timisoara, Romania

FIGURES
Figure 1S: 
FT- IR spectra of zeolite (A), eggshell (B), EZ (C), and FEZ (D)
Figure 2S: 
EDX spectra of zeolite (A), and eggshell (B), 
Figure 3S: 
SEM Live map (1) and EDX spectra showing the distribution of elements (2) in EZ (A), and FEZ (B)
Figure 4S: 
XRD patterns of zeolite (A), eggshell (B), EZ (C), and ZEF (D)
Figure 5S: 
FT-IR spectra of EZ (A) after adsorption, and (B) before and after adsorption 
Figure 6S: 
FT-IR spectra of FEZ (A) after adsorption, and (B) before and after adsorption
Figure 7S: 
SEM micrographs of EZ (A, 30 μm; C, 50 μm) before adsorption, and (B, 30 μm; D, 50 μm) after adsorption
Figure 8S: 
SEM micrographs of FEZ (A, 30 μm; C, 50 μm) before adsorption, and (B, 30 μm; D-E, 50 μm) after adsorption
Figure 9S: 
SEM Live maps of EZ (A) and FEZ (B) after adsorption
Figure 10S: 
EDX spectrum of EZ (A) and FEZ (B) after adsorption
	[image: image1.png]Si-OH-Si or AI-OH-Al

25— : : ‘
— :
T Loy





	Figure 1SA


	[image: image2.png]




	Figure 1SB


	[image: image3.png]




	Figure 1SC

	

	


	[image: image4.png]o—] i i . L a10
e T B e e e Bl e T e L e B At Tt
o 10 %0 00 2% 20 2% % 1500 125 1000 T






Figure 1SD
[image: image5.png]657K]

584K

365K

073K]
000K
00 77 88

0cnts 0000 ks

Status: die CPS: 10897 DT:22




Figure 2SA
	[image: image6.png]70K

355K

142K

00 13 25 39 52 65 78 91 117

Status: die cps: 114

0cnts 0000 ke






	Figure 2SB



	[image: image7.jpg]



	[image: image8.jpg]. 3% O KISiK/FeK/AIK/CaK (434 Pixels)
. 30% SiK/O K/AIK (3881 Pixels)
. 27% Unallocated (3437 Pixels)
. 23% SiK/O K/AIK (2955 Pixels)

- 13% SiK/AIK/O K/K K/FeK/CaK (1679 Pixels)

. 3% Cak/SiK/O K/K K/FeK/AIK (414 Pixels)




	[image: image9.jpg]




	Figure 3SA(1)


	[image: image10.png]165K]

132

09%]

066K]

0cnts 0000 ks

Status: die CPs:S089  DT:17






	Figure 3SA(2)


	[image: image11.png]



	[image: image12.jpg]. 14% FeK/O K/SIK/CaK (1744 Pixels)
. 10% Cak/FeK/SiK/O K/AIK (1241 Pixels)
. 25% FeK/O K/SIK/CaK (3206 Pixels)
. 19% Unallocated (2459 Pixels)

. 32% O KISiK/FeK/CaK/AIK (4150 Pixels)




	[image: image13.jpg]




	Figure 3SB(1)


	[image: image14.png]08K

072

060K

048K]

02K

012

60 82 96 108

Status: die

0cnts 0000 ke






	Figure 3SB(2)


	[image: image15.png]1004004

5004003

0024000

W0 & £l
24heta (deg)




	[image: image16.png]6084004

5004004

2000004

1004004

00e+000_

%

24heta (deg)







A







B
	[image: image17.png]3es004-

264004
1e4004-
ool ﬂ N
L] o
0

24heta (deg)




	[image: image18.png]2.0e+004

1.50+004-

1.0+004:

Intensity (cps)

5004003

00840004

o T W T TT o TT T 1T

24heta (deg)







C







D
Figure 4S
[image: image19.png]



Figure 5SA

	[image: image20.png]EZ: efore adsorption

EZ after adsorption






	Figure 5SB

	


	[image: image21.png]11067






	Figure 6SA


	[image: image22.png]T T
FEZ after adsorption






	Figure 6SB


	[image: image23.png]det HV spotmage WD ————————30pum
CBS 30.00 kV 3.5 5000 x 10.2 mm www.foodsafety.upb.ro CNpSA





	[image: image24.png]www.foodsafety.upb.ro CNpSA






	A 
	B


	
[image: image25.png]50 um
www.foodsafety.upb.ro CNpSA





	
[image: image26.png]det H spotmag WD 50 pm
CBS|30.00kV| 3.5 2 000 x/10.3 mm www.foodsafety.upb.ro CNpSA






	C
	D


Figure 7S
	
[image: image27.png]det| HV [spotjmag o 30 pm
CBS|30.00 kV 3.5 5000 x www.foodsafety.upb.ro CNpSA




	[image: image28.png]30 pm
www.foodsafet






	A
	B


	[image: image29.png]



	[image: image30.png]



	[image: image31.png]




	C
	D
	E


Figure 8S
	[image: image32.jpg]



	[image: image33.png]23% OK
2% NaK
2% MgK
10% AIK
38% SiK
6% KK
9% CaK
3% MnK

5% FeK

2% NiK




	[image: image34.jpg]



	[image: image35.png]




	A
	B


Figure 9S
	[image: image36.png]46.8K]

41.6K]

36.4K

31.2K

26.0K]

20.8K

15.6K

104K

SiK

00,

oK
Mg K|

K Na K
Cal Al K K Mn K

el CakK Mn K

nL K K FeK

NiL e FeK Nk nik

A -

0 20 40 6.0 8.0 100 120 140 16.0 180






	Figure 10SA


	[image: image37.png]27.0K

24.0K

21.0K

18.0K]

15.0K

12.0K|

9.0K]

6.0K]

3.0K]

oK
L

SiK

FeK

FeK

Ni K NiK

0.0"

6.0 8.0 100

140

16.0






	Figure 10SB



_1743431818

_1743431819

_1743431816

