Supporting Information

The tannic acid-iron dynamic redox self-catalytic system mediated way to simple and rapidly fabricate a multifunctionally conductive hydrogel for wearable strain sensors

Gan Miao a, Fangchao Li a, Xiao Miao b Zhiqiang Hou a, Lide Xu a, Ting Xu a, Guina Ren a,*, Xiaoyang Yang a,* and Xiaotao Zhu a,*

a School of Environmental and Material Engineering, Yantai University, Yantai 264405, China

b Shandong Key Laboratory of Optical Communication Science and Technology, School of Physics Science and Information Technology, Liaocheng University, Liaocheng 252000, China

*Corresponding author. Tel: +86-535-6706038 (X. Zhu)

E-mail: xiaotao.zhu@ytu.edu.cn (X. Zhu)

rgnlicp@126.com (G. Ren)

Self-healing Test

The self-healing test is as follows: the sample is cut, then stitched together, and finally placed under certain conditions for self-healing. The self-healing efficiency is calculated using the following formula:

E=σσ0

where σ is the conductivity after self-healing, σ0 is the conductivity of the original sample, and E is the self-healing efficiency of electrical conductivity. Three samples were tested and the results were averaged.

Table S1. The content of Fe3+ and TA of TA@Fe3+-PAA hydrogels

| Samples | Solution A |  |  | Solution B |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | TA (g) | FeCl3·6H2O (g) | Deionized water(mL) | AA (mL) | APS (g) | Deionized water(mL) |
| 0.1 wt.% Fe3+ | 0.003 | 0.01 | 4 | 2.7 | 0.025 | 3 |
| 0.2 wt.% Fe3+ | 0.003 | 0.02 | 4 | 2.7 | 0.025 | 3 |
| 0.3 wt.% Fe3+ | 0.003 | 0.03 | 4 | 2.7 | 0.025 | 3 |
| 0.4 wt.% Fe3+ | 0.003 | 0.04 | 4 | 2.7 | 0.025 | 3 |
| 0.5 wt.% Fe3+ | 0.003 | 0.05 | 4 | 2.7 | 0.025 | 3 |
| 0.6 wt.% Fe3+ | 0.003 | 0.06 | 4 | 2.7 | 0.025 | 3 |
| 0.7 wt.% Fe3+ | 0.003 | 0.07 | 4 | 2.7 | 0.025 | 3 |
| 0.8 wt.% Fe3+ | 0.003 | 0.08 | 4 | 2.7 | 0.025 | 3 |

Figure S1. (a) The gelation time of TA@Fe3+-PAA hydrogels according to the concentration of Fe3+ and (b) TA content. Photographs of the self-exothermic process of the organohydrogel (Fe3+ = 0.60 wt.%) at room temperature.

Figure S2. Compressive strength of the hydrogels as a function of Fe3+ content.

Figure S3. Proposed adhesion mechanism between the TA@Fe3+-PAA hydrogel and various substrates.

Figure S4. Relative resistance variation of TA@Fe3+-PAA hydrogel at 0-100% strain and the GF values at three different strain ranges.