Supplementary Materials: Anomalous interlayer exciton diffusion in WS2/WSe2 moiré heterostructure

Antonio Rossi*1,2,†‡, Jonas Zipfel1,†, Indrajit Maity*3,†, Monica Lorenzon1, Luca Francaviglia1, Emma C. Regan4, Zuocheng Zhang4, Jacob H. Nie4,5, Edward Barnard1, Kenji Watanabe6, Takashi Taniguchi7, Eli Rotenberg2, Feng Wang4, Johannes Lischner3, Archana Raja1* and Alexander Weber-Bargioni1*

1-The Molecular Foundry, Lawrence Berkeley National Laboratory, Berkeley, USA.

2-Advanced Light Source, Lawrence Berkeley National Laboratory, Berkeley, USA.

3-Imperial College London, South Kensington Campus, London, United Kingdom.

4-Department of Physics, University of California at Berkeley, Berkeley, CA, USA.

5-Department of Physics, University of California at Santa Barbara, Santa Barbara, CA, USA

6-Research Center for Functional Materials, National Institute for Materials Science, 1-1 Namiki, Tsukuba, Japan 8

7-International Center for Materials Nanoarchitectonics, National Institute for Materials Science, 1-1 Namiki, Tsukuba,Japan

†-These authors contributed equally

‡-Current affiliation: Center for Nanotechnology Innovation @ NEST, Instituto Italiano di Tecnologia, Pisa,Italy

*Corresponding authors: antonio.rossi@iit.it, i.maity@imperial.ac.uk, araja@lbl.gov, awb@lbl.gov,

Figure S1: Sample Characterization1

Figure S1. Optical image of the samples used for this work. (a) and (b) are images of the 0° and 60° stacking angle samples respectively. (c-d) Second Harmonic Generation (SHG) analysis confirming the relative orientation of WS2 and WSe2 monolayers to be 0° and 60 respectively. (e-f) Adsorption spectra for the two samples. The sample in panel (a) is the same sample used in Ref.1.

0°

60°

1

Figure S2: PL spectrum multipeak fitting

Figure S2. PL peak fitting for 0° sample at (a) 30 K, (b) 130K and (c) 230 K. The fitting is performed with one, two and three Voigt functions respectively.

Figure S3:

Figure S3. Spatially resolved PL emission from 0° stacking angle sample. Each image is taken at different temperatures, ranging from 30 K to 250 K.

Diffusion Measurements

Figure S4: Diffusion Measurements

Figure S4. Spatially resolved PL emission from 0° stacking angle sample. Each image is taken at different temperatures, ranging from 30 K to 180 K

L=466 nm

t=0.8 ns

Figure S5: Exciton Diffusion single layer

Figure S5. To estimate the exciton diffusivity at cryogenic temperature in monolayer we measure the dark exciton dynamic through their spectrally well separated phonon side-bands (PSB)2. (a)PL spectra of WSe2 (blue) and PSB only (orange). Spatially(b) and (c) time resolved PL from PSB of isolated WSe2 crystal The extracted diffusion length and lifetime are reported in the insets. The calculated Diffusivity is D = 1.35 cm2/s

2

Figures S6-S7-S8: Additional details on DFT Calculations

- Moiré potential using unit-cell calculations

Figure S6. Moiré potential for the 0° and 60° alignment evaluated without atomic reconstruction.

The unit-cell lattice-constants of the WS2 and WSe2 are 3.18 and 3.32 Å, respectively. The lattice mismatch (about 4%) gives rise to a moiré when WS2 and WSe2 are stacked together even without a twist angle. We extract the moiré potential using the approach discussed in the main text. We also strain both the layer (isotropic tensile strain for WS2 and compressive strain for WSe2) and set the unit-cell lattice to 3.25 Å. We find that the qualitative moiré potential differences between 0◦ and 60◦ stacking are similar to experiments (see Fig. S6). However, these unit-cell calculations that do not include atomic reconstructions hugely underestimate the moiré potential for exciton hopping (which were shown in the main text). All the calculations are performed with the Quantum ESPRESSO package3.

- Moiré potential extraction from twisted bilayer

We develop a simple scheme to compute the moiré potential using large-scale DFT calculations by taking into account the full atomic reconstructions. In this approach, we explicitly consider the localization of the electronic wave functions and extract the local band gap for different high symmetry stacking regions. To illustrate this, we plot the electronic wave function |ψΓ|2 for several bands near the band gap (see Fig. S 7). The valence bands are marked as V1, V2,... . V1 corresponds to Valence Band Maximum (VBM). Similarly, the conduction bands are marked as C1, C2,... . C1 corresponds to Conduction Band Minimum (CBM). The local band gap at the red diamond stacking is 0.775 eV and obtained from V2 and C1 bands. The local band gap at the orange diamond stacking is 0.843 eV and obtained from V1 and C4 bands. The local band gap at the green diamond stacking is 0.963 eV and obtained from V3 and C4 bands. Similarly, we obtain the local band-gaps for 0◦ twisted WS2/WSe2 heterobilayer.

Figure S7. |ψΓ|2 averaged in the out-of-plane directions for several bands of 60◦ twisted WS2/WSe2. The unit cell is marked with dashed lines and different high-symmetry stackings are marked with coloured diamonds.

- Moiré movements at different times

Figure S8. Electronic band-structures using density functional theory of the structures obtained from classical molecular dynamics simulations in the canonical ensemble at 175 K. The |ψΓ|2 averaged in the out-of-plane directions for the valence band maximum (VBM) and conduction band minimum (CBM) are shown in the bottom panel for the same structures. The center of different high-symmetry stackings in the moiré pattern is also marked.

Bibliography

1.	Jin, C. et al. Identification of spin, valley and moiré quasi-angular momentum of interlayer excitons. Nat. Phys. 15, 1140–1144 (2019).

2.	Rosati, R. et al. Temporal Evolution of Low-Temperature Phonon Sidebands in Transition Metal Dichalcogenides. ACS Photonics 7, 2756–2764 (2020).

3.	Giannozzi, P. et al. QUANTUM ESPRESSO: a modular and open-source software project for quantum simulations of materials. J. Phys.: Condens. Matter 21, 395502 (2009).