Supplemental Figures

| Figure S1: SN-CNPs have negative charges. The zeta potential of SN-CNPs measured at 50 μg mL-1 indicates that they are negatively charged. Figure S2: Size distribution of SN-CNPs. Analysis of the TEM images of SN-CNPs measured at 100 μg mL-1 shows that the peak distribution for the diameter of the nanoparticles is around 50 nm. |  |  |
| --- | --- | --- |
| (a) | (b) |

Figure S3: SN-CNPs form aggregates at high concentration.

2D (a) and 3D (b) AFM images of dried SN-CNPs on mica slide show sign of aggregation at 150 μg mL-1.

pH 4.7

pH 7.0

pH 8.8

N-CNP + NBT/BCIP

ALP + NBT/BCIP

NBT/BCIP control

BTSSCT control

Figure S4: Phosphatase assay for N–CNPs.

The results show that N-CNPs have low phosphatase activity, especially at pH values that differ from neutral.

| (a) | (b) |
| --- | --- |
| (c) | (d) |
| 0 μg mL-1 (1); 10 μg mL-1 (2); 50 μg mL-1 (3); 100 μg mL-1 (4); 200 μg mL-1 (5) | 0 μg mL-1 (1); 10 μg mL-1 (2); 50 μg mL-1 (3); 100 μg mL-1 (4); 200 μg mL-1 (5) |
| (e) | (f) |

Figure S5: Antibacterial test for N-CNPs against E. coli (left column) and L. lactis (right column).

Antibacterial activity tests for N-CNPs against E. coli (a, c, e) and L. lactis (b, d, f) reveal that N-CNPs have significantly weaker antibacterial properties than SN-CNPs. N-CNPs do not inhibit bacterial growth at concentrations less than 200 μg mL-1, whereas SN-CNPs almost completely inhibit at this concentration.

| (a) | (b) |
| --- | --- |
| 0 μg mL-1 (1); 13 μg mL-1 (2); 25 μg mL-1 (3); 50 μg mL-1 (4); 75 μg mL-1 (5) | 0 μg mL-1 (1); 50 μg mL-1 (2); 100 μg mL-1 (3); 150 μg mL-1 (4); 200 μg mL-1 (5) |

Figure S6. SN-CNPs have antibacterial properties against both E. coli and L. Lactis.

Antibacterial activity tests of SN-CNPs at different concentrations against E. coli (a) and L. lactis (b) reveal that L. Lactis has much more tolerance or resistance to SN-CNPs than E. coli.