List of Tables:

Table 1. Physical properties of Ennore sand

| Parameter | Value |
| --- | --- |
| Coefficient of uniformity, Cu | 1.89 |
| Coefficient of curvature, Cc | 1.13 |
| Specific gravity, GS | 2.65 |
| Minimum unit weight, γd, min (kN/m3) | 15.3 |
| Maximum unit weight, γd, max (kN/m3) (Hariprasad et al., 2016) | 17.4 |
| Relative density, Rd | 85% |
| Friction angle, φ | 42o |
| Sand classification (as per USCS) | SP |