Supporting information for

Highly Active, Ultra-Low Loading Single-Atom Iron Catalysts for Catalytic Transfer Hydrogenation

Zhidong An, a, ∇ Piaoping Yang, b, ∇ Delong Duan, c, ∇ Jiang Li, a, *, Tong Wan, a Yue Kong, a Stavros Caratzoulas, b Shuting Xiang, d Jiaxing Liu, a Lei Huang, a Anatoly I. Frenkel, d Yuan-Ye Jiang, e Ran Long, c, * Zhenxing Li, a, *, and Dionisios G. Vlachos b, *

- College of New Energy and Materials, China University of Petroleum (Beijing), Beijing 102249, China.

- Department of Chemical and Biomolecular Engineering and Catalysis Center for Energy Innovation, University of Delaware, 221 Academy St., Newark, Delaware, 19716, United States.

- School of Chemistry and Materials Science, Frontiers Science Center for Planetary Exploration and Emerging Technologies, and National Synchrotron Radiation Laboratory, University of Science and Technology of China, Hefei, Anhui, 230026, China.

- Department of Materials Science and Chemical Engineering Stony Brook University, Stony Brook, New York, 11794, USA; Chemistry Division Brookhaven National Laboratory Upton, New York, 11973, USA.

- School of Chemistry and Chemical Engineering, Qufu Normal University, Qufu 273165, China.

Corresponding authors: lijiang@cup.edu.cn (Jiang Li), longran@ustc.edu.cn (Ran Long), lizx@cup.edu.cn (Zhenxing Li), vlachos@udel.edu. (Dionisios G. Vlachos).

Figure S1. TEM images of ZIF-8 precursor.

Figure S2. XRD pattern of ZIF-derived iron catalysts prepared at different pyrolysis temperatures.

Figure S3. TGA data for Fe-ZIF-8 precursor.

Figure S4. N2 adsorption isotherms of various MOF-derived catalysts.

Figure S5. NH3-TPD (a) and CO2-TPD (b) patterns of Fe-ZIF-8-800, ZIF-8-800, and Fe-MOF-5-800 catalysts.

Figure S6. O 1s XPS spectra of various MOF-derived catalysts.

Figure S7. C 1s XPS spectra of various MOF-derived catalysts.

Figure S8. Two representative aberration corrected HAADF-STEM images of Fe-ZIF-8-800 catalyst.

Figure S9. Fe K-edge (a) and Zn K-edge (b) normalized X-ray absorption near-edge structure (XANES) spectra of the Fe-MOF-5-800 catalyst. Fourier transform of Fe K-edge (c) and Zn K-edge (d) EXAFS spectra of the Fe-MOF-5-800 catalyst. (e, f) EXAFS fitting of the Fe-MOF-5-800. (g) Wavelet transform of Fe K-edge and Zn K-edge EXAFS for Fe-MOF-5-800.

Figure S10. EXAFS fitting of the Fe-ZIF-8-800 using Fe(II)-N4C12 moiety. The results are similar to that using Fe(I)-N3C10 (Figure 2e), suggesting that the local structures of the Fe-Nx sites in Fe-ZIF-8-800 can be described well by both two porphyrin-based moieties.

Figure S11. (a–b) Experimental Fe K-edge XANES spectra of Fe-ZIF-8-800 and theoretical spectra of the porphyrin-based Fe-NxCy moieties. (c–d) Experimental Zn K-edge XANES spectra of ZIF-8-800 and theoretical spectra of the porphyrin-based Zn-NxCy moieties. Latin numerals in brackets indicate the formal oxidation states of the metal atoms.

Figure S12. (a–d) Experimental Fe K-edge XANES spectra of Fe-ZIF-8-800 and theoretical spectra of the Fe-NxCy moieties involving pyridinic N coordination. (e–h) Experimental Zn K-edge XANES spectra of ZIF-8-800 and theoretical spectra of the Zn-NxCy moieties involving pyridinic N coordination. Latin numerals in brackets indicate the formal oxidation states of the metal atoms.

Figure S13. Time courses for the CTH of FF over Fe-ZIF-8-800 and Fe-phen/C-800 catalysts at 80 (a), 120 (b), and 160 oC (c) (squares: conversion, circles: yield). Reaction conditions: 0.5 mmol FF, 3 mL solvent, 50 mg catalyst.

Figure S14. Fe(I)-plN3, Fe(II)-plN4, and Zn(II)-plN4 models. The grey, blue, white, orange, and light purple spheres represent carbon (C), nitrogen (N), hydrogen (H), iron (Fe), and zinc (Zn), respectively.

Figure S15. Optimized geometries (side and top views) of intermediates and transition states on P1 pathway for Fe(I)-plN3 (a), Fe(II)-plN4 (b), and Zn(II)-plN4 (c).

Figure S16. Optimized geometries (side and top views) of intermediates and transition states on P2 pathway for Fe(I)-plN3 (a), Fe(II)-plN4 (b), and Zn(II)-plN4 (c).

Figure S17. Optimized geometries (side and top views) of intermediates and transition states on P3 pathway for Fe(I)-plN3.

Figure S18. Gibbs free energy profiles along the P1 and P2 pathways for Fe(I)-plN3 at 393 K.

Figure S19. Crystal field splitting diagrams for various configurations of Fe(I) complexes (a) and Fe(II) complexes (b). depIPA_H*, depIPA_H_FF*, IPA*, FF_IPA* denote the trigonal, tetrahedral, square pyramidal, and “ridge-tent” configurations, respectively.

Figure S20. The adsorption geometries (side view) and corresponding adsorption energies of -OH groups in HMF and isopropanol at Fe(I)-plN3.

Figure S21. (a) Recyclability tests of Fe-ZIF-8-800 catalyst. Reaction conditions: 0.5 mmol FF, 3 mL isopropanol solvent, 120 ℃, 15 min, 50 mg Fe-ZIF-8-800 catalyst for the first run, and then reused for 4 runs. To recover the activity of Fe-ZIF-8-800 catalyst, re-calcination of the reused catalyst is proceeded by adding 1 wt% Fe(NO3)3 (the Fe dosage is only 0.14 wt%). (b) XRD pattern of used and fresh Fe-ZIF-8-800 catalysts.

Figure S22. Fe K-edge (a) and Zn K-edge (c) normalized XANES spectra of fresh and used Fe-ZIF-8-800 catalysts. Fourier transform of Fe K-edge (b) and Zn K-edge (d) EXAFS spectra of fresh and used Fe-ZIF-8-800 catalysts.

Figure S23. Experimental and computed Fe K-edge XANES spectra of Fe foil (a) and FeO (b); and Zn K-edge XANES spectra of Zn foil (c) and ZnO (d).

Figure S24. A representative GC spectrum. Reaction condition: 0.5 mmol FF, 3 mL isopropanol solvent, 50 mg Fe-ZIF-8-800 catalyst (0.13mol% Fe), 80 oC, 3 h.

Table S1. Contents of Fe and Zn in various MOF-derived catalysts.

| Entry | Catalyst | Fe Content [%] | Zn Content [%] |
| --- | --- | --- | --- |
| 1 | Fe-ZIF-8-800 | 0.073 | 28.60 |
| 2 | Fe-MOF-5-800 | 5.73 | 63.24 |
| 3 | ZIF-8 | – | 30.81 |
| 4 | ZIF-8-800 | – | 20.79 |
| 5 | Fe-ZIF-8 | 0.037 | 30.48 |
| 6 | Fe-MOF-5 | 0.33 | N.D. |
| 7 | Fe-ZIF-8-400 | N.D. | 30.95 |
| 8 | Fe-ZIF-8-600 | N.D. | 33.29 |
| 9 | Fe-ZIF-8-1000 | N.D. | 1.41 |

N.D.=not determined.

Table S2. Contents of N, C and H in Fe-ZIF-8-800 catalyst.

| Catalyst | N [wt%] | C [wt%] | H [wt%] |
| --- | --- | --- | --- |
| Fe-ZIF-8-800 | 21.98 | 46.34 | 2.374 |

Table S3. Intensity ratio of D-band to G-band in Raman spectra of various MOF-derived catalysts.

| Catalyst | ID/IG | Peak Intensity |  |
| --- | --- | --- | --- |
|  |  | D peak | G peak |
| Fe-ZIF-8-800 | 2.01 | 7.66 | 3.82 |
| Fe-ZIF-8-1000 | 1.6 | 7.43 | 4.64 |
| Fe-MOF-5-800 | 1.03 | 5.71 | 5.55 |
| ZIF-8-800 | 1.38 | 15.03 | 10.89 |

Table S4. N2 adsorption/desorption data of various catalysts.

| Catalyst | BET Surface Area (m2/g) | Pore Size (nm) | Pore Volume (cm3/g) |
| --- | --- | --- | --- |
| Fe-ZIF-8 | 1315 | 9.62 | 0.05 |
| Fe-ZIF-8-400 | 1280 | 7.53 | 0.07 |
| Fe-ZIF-8-600 | 766 | 5.00 | 0.07 |
| Fe-ZIF-8-800 | 403 | 9.75 | 0.07 |
| Fe-ZIF-8-1000 | 991 | 7.83 | 0.05 |
| ZIF-8-800 | 580 | 6.64 | 0.07 |
| Fe-MOF-5-800 | 798 | 7.74 | 1.09 |

Table S5. N speciation (at. %) from XPS analysis for various ZIF-derived catalysts.

| Sample | pyridnic N 398.6 eV | pyrrolic N 400.5 eV | graphitic N 401.2 eV |
| --- | --- | --- | --- |
| Fe-ZIF-8-400 | 93.3 | 6.7 | 0 |
| Fe-ZIF-8-600 | 90.4 | 9.6 | 0 |
| Fe-ZIF-8-800 | 81.1 | 13.1 | 5.8 |
| ZIF-8-800 | 72.8 | 18.5 | 8.7 |

Table S6. O speciation (at. %) from XPS analysis for various MOF-derived catalysts.

| Sample | lattice oxygen | bridging hydroxyls | physically adsorbed water | total O (at. %) |
| --- | --- | --- | --- | --- |
| Fe-ZIF-8-400 | 1.3 | 6.0 | 4.1 | 11.4 |
| Fe-ZIF-8-600 | 1.1 | 5.1 | 6.4 | 12.7 |
| Fe-ZIF-8-800 | 0 | 11.7 | 8.0 | 19.7 |
| Fe-ZIF-8-1000 | 0 | 11.5 | 9.9 | 21.4 |
| Fe-MOF-5-800 | 6.4 | 4.1 | 2.5 | 13.0 |
| ZIF-8-800 | 4.2 | 5.3 | 3.9 | 13.3 |

Table S7. C speciation (at. %) from XPS analysis for various MOF-derived catalysts.

| Sample | C–C/C–H | C–N/C–O | C=O/C=N | O–C=O | total C (at. %) |
| --- | --- | --- | --- | --- | --- |
| Fe-ZIF-8-400 | 46.6 | 15.9 | 0 | 3.0 | 65.5 |
| Fe-ZIF-8-600 | 45.5 | 14.8 | 0 | 3.8 | 64.1 |
| Fe-ZIF-8-800 | 50.1 | 16.3 | 0 | 8.3 | 74.8 |
| Fe-ZIF-8-1000 | 53.2 | 15.7 | 0 | 8.1 | 77.1 |
| Fe-MOF-5-800 | 49.5 | 9.9 | 0 | 2.8 | 62.2 |
| ZIF-8-800 | 55.0 | 9.3 | 4.9 | 6.4 | 75.7 |

Table S8. Fitting results of Fe K-edge EXAFS data.

CN, the coordination numbers; R, the bonding distance; σ2, the Debye-Waller factor.

| Sample | Scattering Path | CN | R(Å) | σ2 (Å) |
| --- | --- | --- | --- | --- |
| Fe-ZIF-8-800 | Fe-N | 3.70 +/– 0.56 | 1.96 +/– 0.02 | 0.00090 |
| Used Fe-ZIF-8-800 | Fe-N | 4.56 +/– 0.58 | 2.00 +/– 0.10 | 0.00593 |
| Fe-MOF-5-800 | Fe-O | 4.78 +/– 1.22 | 2.05 +/– 0.09 | 0.00123 |
|  | Fe-Fe | 4.69 +/– 2.33 | 2.47 +/– 0.06 | 0.01600 |
| Fe2O3 | Fe-O | 6.00 (fixed) | 1.94 +/– 0.01 | 0.01087 |
|  | Fe-Fe | 1.00 (fixed) | 2.70 +/– 0.05 | 0.01270 |
|  | Fe-Fe | 3.00 (fixed) | 2.96 +/– 0.01 | 0.00677 |
|  | Fe-Fe | 3.00 (fixed) | 3.45 +/– 0.09 | 0.00274 |
| FeO | Fe-O | 6.00 (fixed) | 2.11 +/– 0.06 | 0.01557 |
|  | Fe-Fe | 12.00 (fixed) | 3.07 +/– 0.01 | 0.01394 |
| Fe foil | Fe-Fe | 8.00 (fixed) | 2.47 +/– 0.02 | 0.00467 |
|  | Fe-Fe | 6.00 (fixed) | 2.85 +/– 0.02 | 0.00540 |

Table S9. Fitting results of Zn K-edge EXAFS data.

| Sample | Scattering Path | CN | R(Å) | σ2 (Å) |
| --- | --- | --- | --- | --- |
| Fe-ZIF-8-800 | Zn-N | 3.89 +/– 0.32 | 1.97 +/– 0.01 | 0.00748 |
| Used Fe-ZIF-8-800 | Zn-N | 4.07 +/– 0.41 | 1.98 +/– 0.01 | 0.00890 |
| Fe-MOF-5-800 | Zn-O | 4.63 +/– 0.52 | 1.98 +/– 0.17 | 0.00435 |
|  | Zn-Zn | 6.21 +/– 2.63 | 3.22 +/– 0.07 | 0.00876 |
| ZIF-8-800 | Zn-N | 4.10 +/– 0.38 | 1.98 +/– 0.01 | 0.00946 |
| ZnO | Zn-O | 4.00 (fixed) | 1.97 +/– 0.00 | 0.00498 |
|  | Zn-Zn | 12.00 (fixed) | 3.23 +/– 0.02 | 0.00974 |
| Zn foil | Zn-Zn | 12.00(fixed) | 2.65 +/– 0.01 | 0.01249 |

Table S10. Catalytic transfer hydrogenation of FF over various catalysts.a

| Entry | Catalyst | T [oC] | t [h] | Conv. [%] | Yield [%] | Sel. [%] | Yield of solvent-derived products |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | – | 120 | 6 | 9.3 | 1.1 | 12.1 | 1.1 | < 0.1 |
| 2 | Fe-ZIF-8-800 | 120 | 6 | 99.6 | 96.5 | 96.9 | 156.0 | 2.1 |
| 3 | Fe-phen/C-800 | 120 | 6 | 51.5 | 44.0 | 85.4 | 87.9 | 0.3 |
| 4 | Fe-MOF-5-800 | 120 | 6 | 11.4 | 3.3 | 28.9 | 139.4 | 0 |
| 5 | ZIF-8-800 | 120 | 6 | 22.1 | 12.0 | 54.3 | 33.7 | 0.4 |
| 6 | Fe-ZnO-NH3-800b | 120 | 6 | 4.3 | 1.2 | 27.9 | 2.3 | 0 |
| 7 | Fe(acac)3-ZIF-8-800c | 120 | 6 | 95.0 | 74.0 | 77.9 | 112.1 | 4.8 |
| 8 | Fe-ZIF-8 | 120 | 6 | 23.1 | 13.0 | 56.3 | 54.2 | 0.6 |
| 9 | ZIF-8 | 120 | 6 | 14.8 | 5.7 | 38.5 | 22.7 | 0 |
| 10 | Fe-ZIF-8-400 | 120 | 6 | 4.8 | 2.2 | 45.8 | 3.14 | 0 |
| 11 | Fe-ZIF-8-600 | 120 | 6 | 82.0 | 79.6 | 97.1 | 82.1 | 1.8 |
| 12 | Fe-ZIF-8-900 | 120 | 6 | 98.5 | 87.0 | 88.3 | 125.7 | 2.8 |
| 13 | Fe-ZIF-8-1000 | 120 | 6 | 61.8 | 50.1 | 81.1 | 110.3 | 1.6 |
| 14 | Fe-ZIF-8-800 | 120 | 1 | 99.5 | 93.1 | 93.5 | 103.8 | 2.7 |
| 15d | Fe-ZIF-8-800 | 80 | 3 | 96.6 | 90.1 | 93.3 | 103.8 | 3.6 |
| 16 | Pd/C | 120 | 1 | 14.8 | 0.6 | 4.1 | 5.8 | 0 |
| 17 | Pt/C | 120 | 1 | 16.3 | 0.7 | 4.3 | 3.5 | 0 |
| 18 | Ru/C | 120 | 1 | 36.9 | 27.7 | 75.1 | 4.0 | 0 |

aReaction condition: 0.5 mmol FF, 3 mL isopropanol solvent, 50 mg catalyst (0.13mol% Fe). bCalcination of Fe-ZnO precursor under NH3 at 800 oC. The dosage of Fe in Fe-ZnO precursor is the same as Fe-ZIF-8-800 catalyst. cThe synthesis method is the same as Li’s paper [S1] except pyrolysis at 800 oC. dIron loading is 0.3 wt% (0.54 mol% Fe).

The catalytic performance of various MOF-derived catalysts is summarized in Table S10. The formation of acetone (dehydrogenation product of isopropanol solvent) and of (E)-4-(furan-2-yl)but-3-en-2-one (coupling products of FF and acetone) illustrates solvent conversion and side reaction, respectively. Trace FA is observed in the blank test (entry 1). We also tried Li’s method [S1] to prepare Fe SA catalysts using Fe(acac)3 as Fe precursors. The performance is inferior to our Fe SA catalyst although the Fe loading is much higher (2.16 wt%, ca. 30 times higher than our Fe-ZIF-8-800 catalyst) in their work. Control experiments using noble metal catalysts such as Pd, Pt, and Ru are inferior to ZIF-derived catalysts (entries 16–18).

Table S11. Screening of H donor for the CTH of FF over Fe-ZIF-8-800 catalyst.a

| Entry | H-Donor | Conversion [%] | Yield [%] | Selectivity [%] |
| --- | --- | --- | --- | --- |
| 1 | MeOH | 28.8 | 13.4 | 47.1 |
| 2 | EtOH | 42.1 | 33.7 | 80.0 |
| 3 | 1-PrOH | 60.0 | 29.4 | 49.1 |
| 4 | 2-PrOH | 100 | 93.4 | 93.4 |
| 5 | 2-BuOH | 96.2 | 89.1 | 92.7 |
| 6 | Cyclohexanol | 49.3 | 25.7 | 52.1 |
| aReaction conditions: 0.5 mmol FF, 3 mL solvent, 50 mg Fe-ZIF-8-800 catalyst, 120 oC, 6 h. |  |  |  |  |

Various alcohols are examined to explore the effect of H donor (Table S11). Primary alcohols, such as methanol, ethanol, and 1-propanol give FA yields of <35% at FF conversions of <60%. The conversion of FF increases with increasing carbon number. Secondary alcohols, such as 2-propanol and 2-butanol, furnish FA selectivities of >90% at excellent FF conversions of >95%. Cyclohexanol leads to inferior catalytic performance due to the high viscosity that prevents the efficient contact of the catalyst and the substrate. Overall, the results, along with the dehydrogenation of a fraction of the solvent, are consistent with the Meerwein-Ponndorf-Verley (MPV) concerted reaction mechanism [S2,S3].

Table S12. Representative examples of the conversion of FF to FA via catalytic transfer hydrogenation (CTH).

| Entry | Catalyst | Solvent | Ta [K] | Pb [MPa] | tc [h] | XFFd [%] | SFAe [%] | TOF [h–1] | Ref. |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | Pd/NPC | 2-butanol | 393 | – | 10 | 97 | 92 | 876 | 32 |
| 2 | Co-Ru/C | Benzyl alcohol | 423 | – | 12 | 98 | >99.9 | 173.8 | 33 |
| 3 | Au/TiO2-R | Water | 363 | 4f | 4 | >99.9 | >99.9 | 91 | 34 |
| 4 | 15CMA | Formic acid | 483 | – | – | 90 | 99 | ca. 576 | 35 |
| 5 | Ni-SAs/NC | Isopropanol | 403 | 2 | 2 | 85.1 | 97.1 | 832 | 36 |
| 6g | Co-N-C-700 | 1,4-dioxane | 423 | 0.5 | 6 | >99.9 | >99 | 88.2 | 37 |
| 7 | (PhP)-Hf (1:1.5) | Isopropanol | 393 | – | 2 | 99.2 | 98.4 | 16.8 | 38 |
| 8 | ZrPN | Isopropanol | 413 | – | 2 | 98 | >99 | 22.5 | 39 |
| 9 | M-ZrO2-U-N | Isopropanol | 383 | – | 6 | 92.4 | 97.1 | 15.1 | 40 |
| 10 | M-MOF-808 | Isopropanol | 373 | – | 2 | 99.2 | 93.8 | 17.6 | 41 |
| 11 | Al2O3-S(7) | Isopropanol | 403 | 0.4 | 6 | 96.9 | 98.5 | 34 | 42 |
| 12 | Fe-phen/C-800 | Isopropanol | 433 | – | 15 | 91.6 | 83 | 9.1 | 25 |
| 13 | Fe-ZIF-8-800 | Isopropanol | 393 | – | 6 | 99.6 | 96.9 | 2435 | This work |
| 14h | Fe-ZIF-8-800 |  | 353 |  | 3 | 96.6 | 93.3 | – |  |

aReaction temperature. bNitrogen pressure, “–” means not mentioned. cReaction time. dFF conversion. eFA selectivity. fCarbon monoxide atmosphere. gFormic acid is used as hydrogen donor. hFe-ZIF-8-800 has a higher iron loading of 0.54 mol%.

Table S13. CTH of FF to FA over Fe-based catalysts.

| Entry | Catalyst | Solvent | Ta [K] | Pb [MPa] | tc [h] | XFFd [%] | SFAe [%] | TOF [h-1] | Ref. |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | Fe3O4@C | Isopropanol | 473 | 2 | 4 | 93.6 | 98.9 | 0.77f | 43 |
| 2 | Fe3O4-12 | Isopropanol | 433 | – | 5 | 97.5 | 92.4 | 0.101g | 44 |
| 3 | Fe3O4/C | Isopropanol | 473 | 2 | 4 | 76.4 | 98.5 | 0.46h | 45 |
| 4 | LaFeO3 | Isopropanol | 453 | 1 | 3 | 90 | 94 | 1.73i | 46 |
|  |  | Toluene |  | 1j |  | 20 | 18 | 0.074k |  |
| 5 | LaFeO3_N | Isopropanol | 453 | 1 | 3 | 64.5 | 91.1 | 6.11l | 47 |
| 6 | LaFeO3@C-M | Isopropanol | 453 | 1 | 3 | 93.2 | 94.1 | 7.6m | 48 |
| 7 | HT_MgFe-3 | Isopropanol | 443 | –n | 6 | 97 | 92.8 | 0.01o | 49 |
| 8 | Fe-phen/C-800 | Isopropanol | 433 | – | 15 | 91.6 | 83.0 | 9.1p | 25 |
| 9 | Fe-ZIF-8-800 | Isopropanol | 493 | – | 6 | 99.6 | 96.9 | 2435q | This work |

aReaction temperature. bNitrogen pressure, “–” means not mentioned. cReaction time. dFF conversion. eFA selectivity. fTOF was calculated at 22.1% FF conversion and 200 oC for 1 h. gTOF was quoted in ref. [S4]. hTOF was calculated at 26% FF conversion and 200 oC for 1 h. iTOF was calculated at 9.6% FF conversion and 180 oC for 1 h. jHydrogen atmosphere. kTOF was calculated at 20% FF conversion and 180 oC for 3 h. lTOF was calculated at 25.3% FF conversion and 180 oC for 1 h. mTOF was calculated at 22.7% FF conversion and 180 oC for 0.5 h. nHelium atmosphere. oTOF was calculated at 20.2% FF conversion and 170 oC for 0.5 h. pTOF was calculated at 25.6% FF conversion and 120 oC for 0.5 h. fTOF was calculated at 10.7% FF conversion and 120 oC for 2 min.

Table S14. Theoretical values of turnover frequencies (TOFs) on Fe(I)-plN3 and Fe(II)-plN4, and Zn(II)-plN4.

| Models | TOF (s–1) |
| --- | --- |
| Fe(I)-plN3 | 4.41E1 |
| Fe(II)-plN4 | 7.65E–5 |
| Zn(II)-plN4 | 1.15E–5 |

Table S15. The Fe and Zn contents in the reaction liquid after the first two reused cycle. The data were collected by ICP-AES analysis.

| Runs | Fe Content [g] | Zn Content [g] | Percentage of Fe leaching [wt%] | Percentage of Zn leaching [wt%] |
| --- | --- | --- | --- | --- |
| 1 | 0.15 | − | 0.41 | − |
| 2 | 0.05 | 0.25 | 0.14 | 0.003 |

Table S16. Fe contents and textural properties of fresh, reused, and regenerated Fe-ZIF-8-800 catalysts.

| Catalyst | Fe Content [wt%] | BET Surface Area [m2/g] | Pore Size [nm] | Pore Volume [cm3/g] |
| --- | --- | --- | --- | --- |
| fresh Fe-ZIF-8-800 | 0.073 | 403 | 9.75 | 0.07 |
| used Fe-ZIF-8-800 | 0.045 | 33 | 13.2 | 0.11 |
| regenerated Fe-ZIF-8-800 | 0.23 | 99 | 9.87 | 0.08 |

Table S17. Cutting energy and core-level width for XANES simulation of Fe and Zn reference compounds.

| Reference Compounds | Cutting Energy (eV) | Core-level width (eV) |
| --- | --- | --- |
| Fe foil | 0 | 2 |
| FeO | −4 | 2 |
| Zn foil | −1 | 2 |
| ZnO | 1 | 1.5 |

Table S18. Microkinetic model parameters.

| Parameter | Units | Values | Basis |
| --- | --- | --- | --- |
| Temperature | K | 393 | Experiments |
| Pressure | atm | 4.2 | Experiments |
| Feed composition | Molar ratio | IPA:FF=0.987:0.013 | Experiments |
| Feed flow rate | cm3/s | 5E−2 | Maintain conversion below 10% |
| Site density of each site type | mol/cm2 | 7.55E−11 | Model |
| Catalyst area/Volume | cm−1 | 1.34E3 | Experiments |

Table S19. Elementary steps and corresponding kinetic parameters on Fe(I)-plN3, Fe(II)-plN4, and Zn(II)-plN4 (T=393 K).

| Elementary step |  | sticking coefficient/ pre-exponential factor | ΔH (eV) | ΔH≠ (eV) | ΔG (eV) | ΔG≠ (eV) |
| --- | --- | --- | --- | --- | --- | --- |
|  | Fe(I)-plN3 |  |  |  |  |  |
| IPA(g) + * = IPA* |  | 5E−1 | −0.87 |  | −0.16 |  |
| IPA* = depIPA_H* |  | 2.084E+10 | 0.05 | 0.23 | 0.07 | 0.28 |
| depIPA_H* + FF(g) = depIPA_H_FF* |  | 5E−1 | −1.15 |  | −0.35 |  |
| depIPA_H_FF* = ACE_H_FFH* |  | 2.084E+10 | 0.18 | 0.78 | 0.08 | 0.87 |
| ACE_H_FFH* = ACE(g) + H_FFH* |  | 5E−1 | 0.67 |  | 0.07 |  |
| H_FFH* = FA* |  | 2.084E+10 | 0.10 | 0.29 | −0.01 | 0.32 |
| FA* = FA(g) + * |  | 5E−1 | 0.98 |  | 0.26 |  |
| IPA* + FF(g) = FF_IPA* |  | 5E−1 | −1.07 |  | −0.23 |  |
| FF_IPA* = FA_ACE* |  | 2.084E+10 | 0.19 | 1.20 | 0.06 | 1.25 |
| FA_ACE* = ACE* + FA(g) |  | 5E−1 | 0.76 |  | −0.05 |  |
| ACE* = ACE + * |  | 5E−1 | 0.98 |  | 0.34 |  |
| FF(g) + * = FF* |  | 5E−1 | −1.00 |  | −0.24 |  |
| FF* + IPA(g) = IPA_FF* |  | 5E−1 | −0.49 |  | 0.08 |  |
| IPA_FF* = ACE_FA* |  | 2.084E+10 | −0.28 | 0.90 | −0.19 | 1.10 |
| ACE_FA* = FA* + ACE(g) |  | 5E−1 | 0.78 |  | 0.04 |  |
|  | Fe(II)-plN4 |  |  |  |  |  |
| FF(g) + * = FF* |  | 5E−1 | −0.69 |  | 0.00 |  |
| FF* + IPA(g) = IPA_FF* |  | 5E−1 | −0.37 |  | 0.31 |  |
| IPA_FF* = ACE_FA* |  | 2.084E+10 | −0.41 | 0.78 | −0.39 | 0.89 |
| ACE_FA* = FA* + ACE(g) |  | 5E−1 | 0.69 |  | 0.02 |  |
| FA* = FA(g) + * |  | 5E−1 | 0.77 |  | 0.01 |  |
| IPA(g) + * = IPA* |  | 5E−1 | −0.66 |  | 0.01 |  |
| IPA* + FF(g) = FF_IPA* |  | 5E−1 | −0.96 |  | −0.13 |  |
| FF_IPA* = FA_ACE* |  | 2.084E+10 | 0.34 | 1.35 | 0.11 | 1.42 |
| FA_ACE* = ACE* + FA(g) |  | 5E−1 | 0.67 |  | −0.08 |  |
| ACE* = ACE + * |  | 5E−1 | 0.60 |  | 0.03 |  |
|  | Zn(II)-plN4 |  |  |  |  |  |
| FF(g) + * = FF* |  | 5E−1 | −0.68 |  | 0.04 |  |
| FF* + IPA(g) = IPA_FF* |  | 5E−1 | −0.42 |  | 0.18 |  |
| IPA_FF* = ACE_FA* |  | 2.084E+10 | −0.38 | 0.80 | −0.36 | 0.97 |
| ACE_FA* = FA* + ACE(g) |  | 5E−1 | 0.60 |  | 0.10 |  |
| FA* = FA(g) + * |  | 5E−1 | 0.78 |  | −0.02 |  |
| IPA(g) + * = IPA* |  | 5E−1 | −0.70 |  | −0.05 |  |
| IPA* + FF(g) = FF_IPA* |  | 5E−1 | −0.94 |  | −0.14 |  |
| FF_IPA* = FA_ACE* |  | 2.084E+10 | 0.43 | 1.33 | 0.19 | 1.43 |
| FA_ACE* = ACE* + FA(g) |  | 5E−1 | 0.63 |  | −0.06 |  |
| ACE* = ACE + * |  | 5E−1 | 0.58 |  | 0.02 |  |

Computational Details for pKa prediction

The computational study for pKa prediction was performed with Gaussian program [S5], M06-2X method [S6], SMD solvation model [S7] (solvent=2-propanol) for both geometry optimization and energy calculation. Geometry optimization and frequency analysis were conducted with def2-SVP basis set [S8] and solution-phase single-point energies were calculated with a larger basis set def2-TZVP [S8] based on the optimized structures (no imaginary frequency for each species). The thermodynamic correction to Gibbs free energy added by the solution-phase single-point energy and 1.9 kcal/mol (to account for the standard state change from 1 atm. to 1 M at 298.15 K) [S9] was used as the solution-phase Gibbs free energy of each optimized species. The pKa values of HMF, 4-(hydroxymethyl)benzaldehyde and 4-hydroxybenzaldehyde in 2-propanol were calculated based on Eq. (1) by using the experimental pKa value [S10] of 2-propanol in 2-propanol as a reference according to literature [S11]:

pKaHA=22+∆G2.303×RT                   (1)

ΔG is the Gibbs free energy change of the deprotonation of concerned acid by 2-propanolate. However, the prediction based on the reaction formula HA + iPrO–  A– + iPrOH (HA is the concerned acid) has a large error probably because it omits the hydrogen bonding of solvent. For example, the experiment pKa of 4-hydroxybenzaldehyde is 6.84 whereas the prediction based on the above reaction formula give a pKa value of 3.18.

To solve this problem, we referred the cluster-continuum method [S11] and considered the hydrogen bonding of HA, iPrO–, iPrOH and A– with several 2-propanol molecules to found the most stable forms for each of them. According to the number of lone pairs bear on hydroxyl/hydroxylate oxygen, hydrogen bonding with one to two 2-propanol molecules was considered for the neutral species, and hydrogen bonding with one to three 2-propanol molecules was considered for anionic species (Table S20). Thereafter, the ΔG* is calculated based on the corrected reaction formulas (Scheme S1) using the most stable forms to replace the ΔG. With the correction method, the pKa value of 4-hydroxybenzaldehyde in 2-propanol is predicted to be 6.40, being much better.

Table S20. Calculated relative solution-phase Gibbs free energies (in kcal/mol).

| Molecule (M) | M | M(iPrOH) | M(2 iPrOH) | M(3 iPrOH) |
| --- | --- | --- | --- | --- |
|  | 0.0 | 4.6 | 11.7 | N.A. |
|  | 0.0 | –4.4 | –4.2 | –4.0 |
|  | 0.0 | 4.6 | 10.6 | N.A. |
|  | 0.0 | –2.9 | –2.8 | 0.4 |
|  | 0.0 | 5.2 | 11.6 | N.A. |
|  | 0.0 | –4.2 | –3.1 | –2.3 |
|  | 0.0 | 6.8 | 13.8 | N.A. |
|  | 0.0 | 2.8 | 5.6 | 9.2 |

N.A.=not applicable.

Scheme S1. Corrected reaction formulas for pKa prediction.

Table S21. Calculated thermodynamic corrections to Gibbs free energy (ΔGcor), solution-phase single-point energies (ΔEsol) and solution-phase Gibbs free energies (ΔGsol) in Hartree.

| Molecules | ΔGcor | ΔEsol | ΔGsol |
| --- | --- | --- | --- |
| a1 | 0.081019 | -194.3501563 | -194.2661095 |
| a1(iPrOH) | 0.179184 | -388.7071693 | -388.5249575 |
| a1(2 iPrOH) | 0.28218 | -583.0649292 | -582.7797213 |
| b1 | 0.066502 | -193.8330786 | -193.7635488 |
| b1(iPrOH) | 0.166174 | -388.2058761 | -388.0366743 |
| b1(2 iPrOH) | 0.267798 | -582.5732182 | -582.3023923 |
| b1(3 iPrOH) | 0.369531 | -776.9407746 | -776.5682158 |
| c1 | 0.080192 | -457.8964114 | -457.8131916 |
| c1(iPrOH) | 0.180312 | -652.2552573 | -652.0719175 |
| c1(2 iPrOH) | 0.279983 | -846.6114678 | -846.328457 |
| d1 | 0.066504 | -457.393508 | -457.3239761 |
| d1(iPrOH) | 0.166114 | -651.7639102 | -651.5947684 |
| d1(2 iPrOH) | 0.267295 | -846.1309433 | -845.8606205 |
| d1(3 iPrOH) | 0.37024 | -1040.495012 | -1040.121744 |
| e1 | 0.109643 | -460.1043024 | -459.9916316 |
| e1(iPrOH) | 0.207342 | -654.4598862 | -654.2495164 |
| e1(2 iPrOH) | 0.311539 | -848.8199619 | -848.5053951 |
| f1 | 0.096306 | -459.596199 | -459.4968651 |
| f1(iPrOH) | 0.195003 | -653.9676287 | -653.7695979 |
| f1(2 iPrOH) | 0.296759 | -848.3337989 | -848.034012 |
| f1(3 iPrOH) | 0.397524 | -1042.699486 | -1042.298935 |
| g1 | 0.082976 | -420.8065389 | -420.720535 |
| g1(iPrOH) | 0.182262 | -615.1611636 | -614.9758737 |
| g1(2 iPrOH) | 0.281371 | -809.5152167 | -809.2308179 |
| h1 | 0.070637 | -420.3325661 | -420.2589013 |
| h1(iPrOH) | 0.170578 | -614.6941766 | -614.5205707 |
| h1(2 iPrOH) | 0.271065 | -809.0563618 | -808.7822689 |
| h1(3 iPrOH) | 0.371499 | -1003.417163 | -1003.042636 |

Cartesian Coordinates of All Calculated Species (In Angstrom)

a1

C      -0.00247900    0.04553900    0.36251800

H       0.00796200    0.08774300    1.46843000

O       0.10251500    1.35882900   -0.16547900

H       0.95629900    1.72144300    0.10524000

C      -1.34241300   -0.50341600   -0.08815700

H      -1.37574800   -0.55844100   -1.18739700

H      -1.51084300   -1.51031200    0.31846600

H      -2.15924500    0.15084900    0.24938200

C       1.15959700   -0.81805600   -0.10180500

H       2.11855700   -0.39148300    0.23108200

H       1.08378300   -1.83735800    0.30447700

H       1.17088600   -0.87746900   -1.20118400

a1(iPrOH)

C      -2.21519000   -0.21035900   -0.31804200

H      -2.48150600   -0.59468500   -1.31897600

O      -1.20736900    0.79180200   -0.45989100

H      -1.55223300    1.51168700   -1.00738100

C      -1.59860200   -1.33327600    0.49258400

H      -1.33377700   -0.97326600    1.49919200

H      -2.30433700   -2.16896000    0.59679800

H      -0.68741800   -1.70035900   -0.00134700

C      -3.45346000    0.37653900    0.33522600

H      -3.86217900    1.19994900   -0.27012400

H      -4.23716800   -0.38751000    0.44113600

H      -3.20565600    0.76733900    1.33397000

C       1.94939200   -0.09920400    0.21917700

H       1.40244100   -0.61480100    1.03392400

O       1.27268500   -0.30198900   -1.00794900

H       0.39397100    0.11615700   -0.92419000

C       3.32311700   -0.73011000    0.09092500

H       3.89184000   -0.23298800   -0.71061700

H       3.88800300   -0.63904500    1.02956000

H       3.23515600   -1.79726700   -0.16049300

C       2.02757700    1.38267200    0.55943700

H       1.01640100    1.80799600    0.64482800

H       2.55000000    1.54485300    1.51390400

H       2.56693400    1.92482900   -0.23330100

a1(2 iPrOH)

C       0.17784200    2.52625500    0.05235200

H      -0.56281200    3.33126200   -0.09629600

O      -0.08622400    1.48973300   -0.90497800

H       0.04636300    1.84045500   -1.79924600

C      -0.02481400    1.90496500    1.41893000

H       0.69975400    1.08934400    1.56711400

H       0.12164100    2.65409800    2.20926300

H      -1.04432000    1.50084800    1.50365800

C       1.57618200    3.08195700   -0.14505100

H       1.69203700    3.49717200   -1.15795100

H       1.77371200    3.88788500    0.57624100

H       2.32343600    2.28703500   -0.00248400

C      -2.43604900   -0.73977300    0.09822500

H      -1.82344800   -0.69976400    1.02147400

O      -2.67285700    0.57753800   -0.36534000

H      -1.81214000    0.94104400   -0.64305600

C      -3.78021600   -1.35150000    0.44568300

H      -4.41352000   -1.40716300   -0.45359700

H      -3.65847000   -2.36559900    0.85219500

H      -4.29943500   -0.73640000    1.19516100

C      -1.68179800   -1.55326000   -0.94459300

H      -0.72062900   -1.07154000   -1.18488300

H      -1.47583000   -2.57260700   -0.58466000

H      -2.27391600   -1.62055800   -1.87124900

C       2.01510300   -1.61264000   -0.18282900

H       1.46406900   -2.11255700   -1.00289600

O       2.13476400   -0.22940000   -0.46451300

H       1.25358000    0.15973100   -0.60591400

C       3.42087600   -2.18196800   -0.13330900

H       3.99583300   -1.69040000    0.66709300

H       3.40173400   -3.26303100    0.06486100

H       3.94073300   -2.01063000   -1.08708900

C       1.26019600   -1.84615800    1.11734900

H       0.26506200   -1.37787600    1.07884300

H       1.12198600   -2.92109000    1.30843100

H       1.81518000   -1.40989500    1.96308700

b1

C       0.00001100    0.17022500    0.33186600

H       0.00004100    0.10396000    1.47389000

O       0.00007500    1.42188500   -0.14766700

C      -1.25456900   -0.63374700   -0.08638800

H      -1.28726800   -0.70194900   -1.18833000

H      -1.29457900   -1.65504200    0.33101200

H      -2.15861200   -0.09021200    0.23380100

C       1.25450000   -0.63385800   -0.08639500

H       2.15855300   -0.09004900    0.23329500

H       1.29473600   -1.65495000    0.33147600

H       1.28688800   -0.70255800   -1.18831100

b1(iPrOH)

C        1.82895600    0.09134200    0.17301900

H        1.34295300    0.53521600    1.08342500

O        1.02307400    0.19685700   -0.93936900

C        2.13030300   -1.37154700    0.52726500

H        2.63163700   -1.86212400   -0.32419700

H        2.77299700   -1.47117200    1.41734600

H        1.18867700   -1.90800100    0.71997600

C        3.13454500    0.86293900   -0.03607300

H        2.91708700    1.91913900   -0.25999400

H        3.79970500    0.82345100    0.84157100

H        3.67248900    0.44340900   -0.90289100

C       -2.04533400    0.14309800   -0.31508800

H       -2.18633300    0.54550800   -1.34633400

O       -1.07067600   -0.85254900   -0.30121800

H       -0.11256500   -0.39176300   -0.62721700

C       -3.37889300   -0.45162000    0.12092500

H       -3.29541000   -0.83808800    1.15002100

H       -4.19132600    0.29059500    0.09153500

H       -3.65134200   -1.29344700   -0.53392300

C       -1.65057300    1.32623200    0.56918000

H       -0.68636100    1.72760800    0.22461100

H       -2.40099800    2.13208500    0.54223400

H       -1.53440900    0.99045600    1.61316100

b1(2 iPrOH)

C         0.42893000    2.34060000   -0.37410400

H        -0.09647800    2.99694100   -1.11092000

O         0.04941400    1.01813900   -0.54020300

C         0.03576200    2.84999900    1.01609700

H         0.59336000    2.29898200    1.79239900

H         0.23491800    3.92604100    1.14514600

H        -1.03795700    2.67037600    1.18109900

C         1.92689600    2.52726900   -0.61944500

H         2.19887900    2.15416000   -1.61910200

H         2.22596500    3.58563300   -0.55441500

H         2.51074800    1.95846000    0.12238600

C        -2.45337900   -0.60497900    0.21079500

H        -1.80769700   -0.64680900    1.11521000

O        -2.41605500    0.68233600   -0.34670500

H        -1.40630600    0.87283400   -0.48588300

C        -3.87988900   -0.91481200    0.63578400

H        -4.54548900   -0.88826100   -0.24221600

H        -3.95845900   -1.90845600    1.10141200

H        -4.23832000   -0.16331500    1.35535000

C        -1.92599300   -1.63881500   -0.78281400

H        -0.89401700   -1.39255200   -1.07779500

H        -1.93333300   -2.65633200   -0.36088900

H        -2.55159100   -1.63432400   -1.69061700

C         1.68657300   -1.60346400    0.23537100

H         0.66157300   -1.86405600    0.57714900

O         1.62506700   -0.88521900   -0.96962000

H         1.01984600   -0.06592800   -0.81463400

C         2.43431300   -2.90232700   -0.02194300

H         3.45615400   -2.68158900   -0.37036600

H         2.50107900   -3.51959900    0.88606600

H         1.92772400   -3.48650000   -0.80489200

C         2.34032300   -0.78227900    1.34280100

H         1.76583700    0.14228600    1.50113300

H         2.37511900   -1.33757200    2.29286600

H         3.36981800   -0.50961900    1.05848700

b1(3 iPrOH)

C       -0.41097600   -0.20216100    2.38163700

H        0.27430000    0.53144300    2.86495300

O       -0.15160600   -0.25755100    1.00802400

C       -1.84169800    0.27030800    2.63903200

H       -2.55345800   -0.42974900    2.17103000

H       -2.06812600    0.33082000    3.71505100

H       -1.99551500    1.26577600    2.19581300

C       -0.15489500   -1.56301400    3.02762400

H        0.87323800   -1.89652300    2.81912500

H       -0.29629800   -1.53539400    4.11946900

H       -0.84666800   -2.31251500    2.60771700

C        0.46837600    2.64619400   -0.52934500

H        0.69184900    2.11023900   -1.47718700

O       -0.67092500    2.08920700    0.08066700

H       -0.44696600    1.15655300    0.40971800

C        0.15642400    4.09279100   -0.87549800

H       -0.04619000    4.66361700    0.04491300

H        0.99466800    4.56928900   -1.40458400

H       -0.73705100    4.14877400   -1.51524800

C        1.69155200    2.52642200    0.37305500

H        1.90742400    1.47027500    0.59399600

H        2.58228000    2.96773600   -0.10062400

H        1.50821200    3.05120000    1.32510900

C        2.36483400   -1.18937800   -0.76522300

H        1.96352200   -0.32079200   -1.33197300

O        2.27586900   -0.93721100    0.61707700

H        1.30639800   -0.68292600    0.79985400

C        3.83142200   -1.35090700   -1.12837500

H        4.26374800   -2.19351800   -0.56529100

H        3.95996500   -1.54832000   -2.20276400

H        4.39695300   -0.44260700   -0.87140600

C        1.54707800   -2.41951000   -1.14651500

H        0.49091200   -2.28598800   -0.86670700

H        1.59464800   -2.61771000   -2.22872300

H        1.93487400   -3.30305700   -0.61358300

C       -2.36588300   -0.63779200   -1.20294200

H       -2.64133500    0.29002900   -0.66077800

C       -3.60556700   -1.17571400   -1.89631000

H       -4.01277500   -0.44641100   -2.61198600

H       -3.36000900   -2.09998000   -2.44362200

H       -4.38634700   -1.41325300   -1.15860500

C       -1.26854800   -0.27235000   -2.19731300

H       -1.58318500    0.54852100   -2.86091400

H       -0.36640600    0.05135400   -1.65623600

H       -1.00776800   -1.14382600   -2.82016200

O       -1.91259000   -1.60544900   -0.28305400

H       -1.19358600   -1.14436100    0.26297400

c1

C       -0.98276800   -0.08862600    0.02587200

C       -0.64250300    1.23929800    0.03005000

C        0.78005800    1.27520500    0.01650900

C        1.19565800   -0.03088900    0.00523700

O        0.11366500   -0.85838400    0.01074300

H       -1.33601000    2.07519300    0.04020700

H        1.43002200    2.14745200    0.01429400

C        2.51565600   -0.64065000   -0.01729100

H        2.51485300   -1.75303200   -0.02615800

O        3.54526600   -0.00027300   -0.02651000

C       -2.30396800   -0.77766700    0.04219100

H       -2.32498700   -1.51740700   -0.77921100

H       -2.39744100   -1.34313000    0.98764900

O       -3.29665700    0.20318700   -0.09053000

H       -4.15742600   -0.22535100   -0.00182000

c1(iPrOH)

C        0.53628300    1.21464800   -0.02519400

C        0.65311200    1.10288800    1.33505000

C        1.74375900    0.21552900    1.55500800

C        2.20775600   -0.13804700    0.31413000

O        1.46577800    0.47478100   -0.64659300

H        0.02249100    1.58557900    2.07601800

H        2.14494700   -0.12735900    2.50642100

C        3.29374700   -1.01295700   -0.09427000

H        3.84027200   -1.47809500    0.75425100

O        3.59441500   -1.23123500   -1.24832400

C       -0.42310300    1.96619200   -0.88322700

H        0.04907900    2.89874400   -1.23900200

H       -0.65949400    1.35337400   -1.77091700

O       -1.56307000    2.24003400   -0.10239300

H       -2.16381100    2.80328500   -0.60997800

H       -2.15865700    0.67814800    0.76444400

O       -2.28723400   -0.23959700    1.06027100

C       -1.98645100   -1.07674500   -0.04150800

H       -0.93770600   -0.90950900   -0.36272800

C       -2.11193500   -2.51283300    0.43048800

C       -2.90497700   -0.77023800   -1.21610000

H       -3.14155400   -2.70969500    0.76799600

H       -1.86744600   -3.21634000   -0.37785200

H       -1.43038100   -2.69924600    1.27344200

H       -2.82426700    0.29151300   -1.49682100

H       -2.64981500   -1.38027500   -2.09514800

H       -3.95191200   -0.97261500   -0.94007100

c1(2 iPrOH)

C       -1.79745400   -0.44837100    0.40714600

C       -2.29294300    0.18027300    1.51931100

C       -3.70503700    0.22368800    1.33894600

C       -3.95658600   -0.37949900    0.13470100

O       -2.78815900   -0.79002400   -0.42841300

H       -1.71376200    0.56510800    2.35446800

H       -4.45097900    0.64753100    2.00793800

C       -5.19954900   -0.62009300   -0.57995100

H       -6.10357800   -0.25497300   -0.04661200

O       -5.26735800   -1.16599400   -1.66003600

C       -0.40514400   -0.78722700   -0.01343700

H       -0.34364800   -1.85635500   -0.27601600

H       -0.14239200   -0.21255600   -0.91550900

O        0.52259700   -0.44059700    0.99069600

H        0.36019300    1.47496300    0.93155000

O        0.29218500    2.27132700    0.38216800

C        1.47234000    2.32756800   -0.40453900

H        1.53682100    1.42328600   -1.04119000

C        1.35795300    3.54383600   -1.30304500

C        2.71061800    2.37581300    0.47858800

H        1.28815900    4.45877200   -0.69388800

H        2.23337100    3.62853000   -1.96225600

H        0.45547300    3.47663500   -1.92782400

H        2.74852900    1.49804600    1.14247800

H        3.62962500    2.37919900   -0.12605100

H        2.69556300    3.28233600    1.10416800

H        0.40712100   -1.02280400    1.75779400

H        2.14247900   -0.51168500    0.04797800

O        2.82714500   -0.71860800   -0.60989500

C        3.45068100   -1.92752300   -0.20985400

H        2.71240400   -2.75324300   -0.23969600

C        4.54801700   -2.22445300   -1.21367600

C        3.98577900   -1.80856600    1.20942600

H        5.30089100   -1.42101100   -1.19595800

H        5.04642700   -3.17648000   -0.98293900

H        4.13306600   -2.28620900   -2.23022500

H        3.16981600   -1.57485800    1.91130000

H        4.45935800   -2.74555300    1.53781300

H        4.73173000   -1.00018900    1.26482300

d1

C      -0.96176600   -0.07139600    0.00002400

C      -0.83965500    1.29773400   -0.00005800

C       0.55249000    1.57343400    0.00006100

C       1.18630300    0.35357100   -0.00003800

O       0.25666000   -0.64427400    0.00003000

H      -1.67408900    1.99189900   -0.00011200

H       1.04763900    2.54285000    0.00008700

C       2.59146300    0.01602100   -0.00010400

H       3.26275700    0.90338500    0.00001000

O       3.03486200   -1.11639600    0.00009500

C      -2.21848300   -0.91795200    0.00000400

H      -2.05968500   -1.62403600   -0.87703400

H      -2.05974500   -1.62401300    0.87706900

O      -3.33889600   -0.20165000   -0.00004400

d1(iPrOH)

C        1.10149500   -0.47806700    0.26844500

C        1.51678500   -1.51172300   -0.53519200

C        2.87193700   -1.23677700   -0.86194400

C        3.18731200   -0.05663500   -0.23386900

O        2.10299300    0.39944000    0.45386400

H        0.90119700   -2.35297200   -0.83836900

H        3.54672400   -1.82485100   -1.48125900

C        4.41600800    0.70745600   -0.19828500

H        5.24257600    0.25355300   -0.78797400

O        4.56401700    1.74943900    0.40885200

C       -0.22796700   -0.22877200    0.92759800

H       -0.00958900   -0.13420800    2.02122000

H       -0.52338800    0.80872500    0.62292000

O       -1.14671900   -1.18191600    0.62016400

H       -2.01738900   -0.53947200   -0.28457900

O       -2.66929000    0.05168400   -0.87209300

C       -3.64252300    0.54450500    0.00488400

H       -3.16477500    1.11041300    0.83650600

C       -4.54225900    1.50908100   -0.75357200

C       -4.44304300   -0.59276700    0.63611500

H       -5.04653100    0.97914500   -1.57794900

H       -5.31050100    1.95028800   -0.10091700

H       -3.94563300    2.32415800   -1.19023900

H       -3.75373500   -1.27086500    1.16011000

H       -5.18950600   -0.22408300    1.35676900

H       -4.96392900   -1.16681100   -0.14762200

d1(2 iPrOH)

C       1.39496500   -0.74192500    0.52001000

C       1.90899100   -0.13728600    1.64094200

C       3.31428300   -0.06812200    1.43909700

C       3.55505400   -0.63394000    0.21157400

O       2.37995400   -1.04263100   -0.34266200

H       1.32912300    0.20883900    2.49126600

H       4.06882400    0.34605500    2.10507400

C       4.78667200   -0.83210000   -0.52531400

H       5.69084500   -0.46190700    0.00578100

O       4.85718400   -1.35097800   -1.62096600

C      -0.01923700   -1.06495000    0.14171900

H      -0.12707200   -0.78089800   -0.93266500

H      -0.12058800   -2.17468700    0.14774600

O      -0.91680500   -0.44159100    0.97208700

H      -2.15161700   -1.31180300    0.89786200

O      -2.95789600   -1.88979200    0.65790400

C      -3.65357000   -1.17194900   -0.33116400

H      -2.93544600   -0.74709100   -1.06398300

C      -4.57393700   -2.13241000   -1.06715300

C      -4.42529500   -0.00591100    0.28033300

H      -5.30468700   -2.56431000   -0.36439200

H      -5.12501700   -1.62780500   -1.87442600

H      -3.99291800   -2.95828000   -1.50370800

H      -3.73217400    0.68869600    0.77784600

H      -4.97927100    0.56014500   -0.48469400

H      -5.14281200   -0.38059900    1.02820300

H      -1.28754900    0.78411300    0.21273100

O      -1.46808700    1.62926300   -0.34336400

C      -0.44591200    2.54760100   -0.04378100

H      -0.05624500    2.34779800    0.97568500

C       0.71659700    2.41383000   -1.02455700

C      -1.02286400    3.95605200   -0.06402200

H       0.36369900    2.60990700   -2.05014300

H       1.52714400    3.12248600   -0.79380900

H       1.13753300    1.39658500   -1.00052400

H      -1.84380500    4.04424300    0.66278500

H      -0.25995500    4.71100600    0.17758600

H      -1.42729300    4.18000400   -1.06430200

d1(3 iPrOH)

C       -1.76095500    0.38987100   -0.76826800

C       -1.93044900    1.13663900    0.37327600

C       -3.32903600    1.14954700    0.62780700

C       -3.91085200    0.41496900   -0.37518900

O       -2.95006900   -0.04310100   -1.22251700

H       -1.13093800    1.59273900    0.95240400

H       -3.85565600    1.63487500    1.44720400

C       -5.29592200    0.07718800   -0.63785900

H       -6.00887900    0.49094500    0.10839200

O       -5.67235000   -0.59392400   -1.57695300

C       -0.53737600   -0.01162400   -1.54067600

H       -0.74805700   -1.02149400   -1.95539900

H       -0.47536300    0.65811100   -2.42683700

O        0.60878700    0.02319000   -0.77513700

H        1.99355000   -0.20673400   -1.54598200

O        2.89556600   -0.43796700   -1.91774400

C        3.44362000   -1.40673300   -1.04902500

H        2.73129100   -2.24755200   -0.93077900

C        4.71394400   -1.94344000   -1.68534200

C        3.70737400   -0.82548600    0.33619000

H        5.44117800   -1.12673400   -1.81944000

H        5.17590600   -2.72156400   -1.06028900

H        4.49655600   -2.37338000   -2.67438500

H        2.79990100   -0.35011100    0.73903900

H        4.02705700   -1.60842300    1.04139700

H        4.49976300   -0.06077700    0.28472600

H        0.62216900   -1.31602700    0.03135000

O        0.57622100   -2.14832400    0.59852100

C       -0.23070100   -1.84508300    1.71428200

H       -0.23710200   -0.74783400    1.87218400

C       -1.66600100   -2.30652100    1.47861100

C        0.36793100   -2.49877700    2.95108500

H       -1.69180400   -3.40264800    1.36583000

H       -2.32765600   -2.02761100    2.31348200

H       -2.07095000   -1.86430800    0.55488000

H        1.39042700   -2.13020800    3.12134900

H       -0.23290000   -2.29071100    3.84891000

H        0.41647500   -3.59080000    2.81203700

H        0.90442100    1.02167400    0.41514100

O        1.14827200    1.69312800    1.12172200

C        1.50459400    2.87359700    0.43259000

H        0.74988000    3.07982300   -0.35464300

C        1.49184800    4.02573300    1.42255500

C        2.86195400    2.71916500   -0.24298100

H        2.20174800    3.82214200    2.24008700

H        1.78030500    4.97060400    0.93952600

H        0.49142400    4.15212200    1.86288000

H        2.86156700    1.84452400   -0.91084800

H        3.11828600    3.61134500   -0.83483700

H        3.64615800    2.56973800    0.51712900

e1

C        0.81136700   -1.03342400    0.00016600

C       -0.55994200   -1.28859500    0.00002600

C       -1.47158300   -0.23092000   -0.00005100

C       -1.00546200    1.09291000   -0.00007800

C        0.35749300    1.34429500   -0.00006700

C        1.27837800    0.28254100    0.00008500

H        1.52771000   -1.85433400    0.00028100

H       -0.92794500   -2.31791600    0.00002400

H       -1.72893000    1.91056800   -0.00018700

H        0.72475700    2.37368300   -0.00010800

C       -2.92233300   -0.51307500   -0.00002600

H       -3.19392300   -1.59349600    0.00000600

C        2.75264300    0.59109300    0.00023500

H        2.97737400    1.21346200   -0.88566800

H        2.97748900    1.21238000    0.88685300

O        3.50085400   -0.59675600   -0.00039900

H        4.43699800   -0.36053700    0.00016600

O       -3.78046600    0.34016000    0.00001000

e1(iPrOH)

C         0.81364000    0.09355800   -0.73287900

C         1.92576600   -0.73343600   -0.61143900

C         3.03341300   -0.31574800    0.13406400

C         3.01855500    0.93543700    0.76250900

C         1.90594500    1.75950800    0.64311300

C         0.79586900    1.34622800   -0.10569100

H        -0.05486500   -0.23680900   -1.30263900

H         1.94747600   -1.71272300   -1.09370000

H         3.88476900    1.25656400    1.34643800

H         1.89193000    2.73502400    1.13485800

C         4.22067800   -1.18739000    0.26670600

H         5.04675400   -0.76941900    0.88628700

C        -0.38205000    2.27636000   -0.23668100

H        -0.67521000    2.63206000    0.76620300

H        -0.06897700    3.16237100   -0.81633300

O        -1.45218500    1.61795400   -0.87735800

H        -2.17255800    2.24879800   -1.01185700

O         4.32350900   -2.27868600   -0.24540100

H        -1.94499200    0.08182500    0.00081200

O        -2.29922100   -0.77566900    0.29681400

C        -3.65430600   -0.81687100   -0.11274400

H        -3.71573500   -0.67070700   -1.20921100

C        -4.19037700   -2.19627200    0.21959800

C        -4.45313500    0.28763900    0.56594900

H        -4.13814900   -2.36839300    1.30623000

H        -5.23657200   -2.30196500   -0.10049000

H        -3.59204800   -2.97197200   -0.28017400

H        -4.02238600    1.27329200    0.33083100

H        -5.50267700    0.28497300    0.23640200

H        -4.42756800    0.15420500    1.65886800

e1(2 iPrOH)

C        0.49059300   -0.95859200    0.87042200

C        1.47829800   -1.52579700    0.07621400

C        2.77800100   -1.00065300    0.09628800

C        3.07957900    0.09207200    0.91308400

C        2.08357400    0.66744400    1.70007000

C        0.78639700    0.14740800    1.68354700

H       -0.52161900   -1.36951600    0.86699800

H        1.25980600   -2.38233500   -0.56470700

H        4.09486600    0.49655900    0.92149100

H        2.31133000    1.53390100    2.32477900

C        3.84019600   -1.59488600   -0.74568500

H        4.83921400   -1.11079700   -0.65506000

C       -0.29640000    0.77173300    2.52304000

H       -0.50798100    0.13343500    3.39840200

H        0.03727000    1.75291700    2.89291100

O       -1.47073000    0.90941400    1.73111000

H       -2.11297200    1.45652500    2.20810800

O        3.67207100   -2.53568600   -1.48649100

H       -2.45950700   -0.63910200    1.35160200

O       -2.88561800   -1.42084400    0.95902800

C       -3.04680300   -1.15290800   -0.42712400

H       -2.05847800   -0.93851200   -0.87509300

C       -3.61694500   -2.40467800   -1.06552800

C       -3.93605800    0.06289000   -0.64363500

H       -4.59512000   -2.64397200   -0.61941600

H       -3.75088500   -2.26720000   -2.14775000

H       -2.94628400   -3.26129900   -0.90416200

H       -3.50851300    0.94951300   -0.15063600

H       -4.03762900    0.29121700   -1.71503200

H       -4.93894300   -0.11781500   -0.22518000

H       -1.13503200    1.20013000   -0.12153100

O       -0.98352300    1.33943200   -1.07274100

C        0.30421300    1.90563800   -1.24809500

H        1.07705100    1.16957800   -0.95166300

C        0.46796900    2.20341900   -2.72640100

C        0.46611200    3.14949500   -0.38653300

H       -0.29059500    2.93232200   -3.05213700

H        1.46465000    2.61747500   -2.93505700

H        0.34146800    1.28568200   -3.31886600

H        0.28489900    2.91111300    0.67365500

H        1.48115100    3.56502900   -0.47419600

H       -0.25809300    3.92112300   -0.69269000

f1

C       -0.85669800   -1.03399700    0.00020800

C        0.51325900   -1.28899300    0.00025100

C        1.42296800   -0.22605300    0.00004300

C        0.94729400    1.09792700   -0.00000900

C       -0.41719600    1.34120800   -0.00002600

C       -1.33731200    0.27665400    0.00001500

H       -1.60332600   -1.82959200    0.00012000

H        0.88955200   -2.31627100    0.00011500

H        1.66883000    1.91803400   -0.00004600

H       -0.78966800    2.37065800    0.00020600

C        2.86826800   -0.50470600   -0.00010100

H        3.13795700   -1.58646800   -0.00057500

C       -2.85687100    0.50300300    0.00010400

H       -3.00555700    1.21289500    0.87755400

H       -3.00512100    1.21351200   -0.87669100

O       -3.60922100   -0.59004700   -0.00037600

O        3.73485400    0.34341900   -0.00007300

f1(iPrOH)

C       -0.98168300    0.21884500   -1.01526900

C       -2.22090600   -0.40525900   -0.92392800

C       -3.04257400   -0.16922200    0.18619600

C       -2.60960700    0.69775800    1.19977100

C       -1.37027900    1.31860500    1.10120900

C       -0.54116700    1.08521400   -0.00630900

H       -0.31781500    0.05328600   -1.86493500

H       -2.57133500   -1.08270800   -1.70611900

H       -3.25409800    0.87724100    2.06477500

H       -1.03171400    1.99388000    1.89233300

C       -4.35701300   -0.82650000    0.30048700

H       -4.93022400   -0.57717600    1.22350500

C        0.81213700    1.77397000   -0.13574600

H        0.57406200    2.87075200   -0.14937400

H        1.31513400    1.63281900    0.85649100

O        1.57271500    1.36566300   -1.18329400

O       -4.81810900   -1.58706400   -0.52238800

H        2.76220900    0.93583400   -0.57943200

O        3.61183600    0.57901100   -0.05043700

C        3.58996600   -0.81673600   -0.13957600

H        3.54124000   -1.13812100   -1.20443000

C        4.88285400   -1.36398700    0.44741700

C        2.36719300   -1.40121800    0.56505300

H        4.96204200   -1.07282600    1.50742000

H        4.92998400   -2.46149600    0.38331400

H        5.75070400   -0.94537200   -0.08413200

H        1.45225700   -0.97960800    0.12251700

H        2.32491500   -2.49795900    0.47542900

H        2.38757300   -1.13824400    1.63576200

f1(2 iPrOH)

C        0.74925300   -0.72142200   -0.45560200

C        1.92367800   -1.39403800   -0.77342300

C        2.88153800   -1.64239000    0.21851200

C        2.65049100   -1.21032300    1.53104700

C        1.47416700   -0.53837700    1.84320100

C        0.50982600   -0.28827100    0.85617600

H       -0.00071900   -0.51563500   -1.22028100

H        2.11701800   -1.73490800   -1.79284600

H        3.40221200   -1.40237700    2.30145500

H        1.29487100   -0.19708600    2.86655000

C        4.13220100   -2.35391300   -0.10444600

H        4.82483500   -2.50117900    0.75637100

C       -0.78620000    0.42853000    1.21116400

H       -1.36190600   -0.28835700    1.84569300

H       -0.50998300    1.25222100    1.91054000

O       -1.51947700    0.86642500    0.13840200

O        4.42393600   -2.76536300   -1.20577800

H       -2.19253800   -0.38272500   -0.36912800

O       -2.63057400   -1.27447800   -0.62173400

C       -4.02114200   -1.11724800   -0.49680700

H       -4.38808800   -0.35176100   -1.21432100

C       -4.68561300   -2.43865000   -0.84682700

C       -4.39468900   -0.65031100    0.90674600

H       -4.35638100   -3.22002000   -0.14329700

H       -5.78223500   -2.36529900   -0.80040300

H       -4.40038100   -2.75319000   -1.86194300

H       -3.87423000    0.29188500    1.13372100

H       -5.47827000   -0.48406100    1.00641600

H       -4.08765700   -1.40550900    1.64858000

H       -0.59711300    1.72924100   -0.73688400

O        0.07807300    2.30774500   -1.23565700

C        0.74396300    3.07524500   -0.26507600

H        1.24401700    2.40932300    0.47234000

C        1.82167700    3.89361100   -0.95666700

C       -0.24053200    3.95886200    0.49524000

H        1.36260400    4.56383100   -1.70115800

H        2.38756600    4.50524600   -0.23855900

H        2.52618700    3.23218400   -1.48257900

H       -1.04251300    3.33788300    0.92239500

H        0.24952600    4.51416300    1.30960900

H       -0.70420000    4.68367900   -0.19355400

f1(3 iPrOH)

C       -2.13022800   -0.01271300   -0.47738700

C       -3.51290100   -0.07521600   -0.61383400

C       -4.32829700   -0.15094900    0.52199000

C       -3.74488000   -0.16379200    1.79604700

C       -2.36306300   -0.10108000    1.92677800

C       -1.54039100   -0.02414400    0.79358600

H       -1.48865100    0.04734700   -1.35759100

H       -3.97982200   -0.06628000   -1.60100000

H       -4.38430400   -0.22371900    2.68078600

H       -1.90690500   -0.11106100    2.92036300

C       -5.79649800   -0.21804800    0.39102300

H       -6.35265100   -0.27689900    1.35515700

C       -0.03156900    0.05401100    0.96078700

H        0.16489300    0.95933800    1.57904800

H        0.26026600   -0.80142700    1.61078700

O        0.66870000    0.07387900   -0.22634100

O       -6.39228000   -0.21310800   -0.66338500

H        0.29755400    1.45890000   -0.89427600

O        0.05620300    2.37097000   -1.24228300

C        1.18454200    3.20012000   -1.08634300

H        2.06409100    2.74508500   -1.58792300

C        0.88714400    4.52883100   -1.76045900

C        1.53482300    3.37527100    0.38715400

H        0.02310700    5.01036300   -1.27495000

H        1.74618200    5.21272900   -1.70051200

H        0.63901900    4.37193200   -2.82064800

H        1.78438400    2.40097600    0.83255900

H        2.40275700    4.03973100    0.51959200

H        0.67689100    3.80477700    0.92929200

H        0.35989600   -1.34141900   -0.86409100

O        0.14215400   -2.28902200   -1.12109800

C        1.23622600   -3.08538600   -0.73194800

H        1.43763600   -2.94907600    0.35215200

C        0.86585600   -4.54096200   -0.96170300

C        2.49812100   -2.69597800   -1.49602100

H        0.66251100   -4.70965300   -2.03141500

H        1.67612200   -5.21636100   -0.65060900

H       -0.04201800   -4.80124700   -0.39766100

H        2.73879900   -1.63569700   -1.32417300

H        3.36240400   -3.30262200   -1.18300100

H        2.34081700   -2.84448700   -2.57661900

H        2.21484800    0.31533900   -0.11900100

O        3.21820400    0.41565000   -0.07519400

C        3.66925600   -0.34861500    1.01944500

H        3.11573300   -1.31048100    1.05322700

C        5.14362000   -0.65531400    0.81266100

C        3.42676100    0.38252400    2.33589700

H        5.71135100    0.28536300    0.73187300

H        5.55477000   -1.23898000    1.64922000

H        5.29346000   -1.22439600   -0.11698500

H        2.35637100    0.60455900    2.46541600

H        3.75730100   -0.21749700    3.19758200

H        3.97819800    1.33654000    2.34376700

g1

C       -1.21529500    1.18506500   -0.00006000

C        0.16557900    1.33744600   -0.00004500

C        1.00476300    0.21725200   -0.00002700

C        0.44098800   -1.06904200   -0.00007300

C       -0.93336100   -1.23302500   -0.00006900

C       -1.76944300   -0.10249300    0.00001600

H       -1.87731600    2.05385800   -0.00010200

H        0.60223400    2.33952500   -0.00005800

H        1.10320400   -1.93727100   -0.00011500

H       -1.39042300   -2.22368000   -0.00008500

C        2.46581000    0.39534000    0.00004600

H        2.81027200    1.45511200   -0.00006600

O        3.26709900   -0.51370400    0.00009100

O       -3.09599500   -0.31176900    0.00005500

H       -3.57105400    0.53297700    0.00053600

g1(iPrOH)

C       -0.35101800   -0.29975100   -0.73857900

C       -1.54071700   -0.99750000   -0.58176200

C       -2.66630600   -0.37299500   -0.02873000

C       -2.58776100    0.96934400    0.36845200

C       -1.40573700    1.67834200    0.21731200

C       -0.28530700    1.04179500   -0.33812200

H        0.53961200   -0.76495300   -1.16434400

H       -1.60226900   -2.04411800   -0.89098000

H       -3.46954900    1.44886800    0.79813500

H       -1.33327500    2.72443700    0.52299200

C       -3.92155100   -1.12782100    0.13059200

H       -3.88222000   -2.18515700   -0.21849200

O       -4.94015600   -0.67040400    0.60033700

O        0.88838700    1.68515300   -0.51132300

H        0.83954100    2.60080000   -0.19579100

H        2.40012900    0.58074600   -1.12271200

O        2.92625800   -0.23091200   -1.06002800

C        3.13463100   -0.47664900    0.32264100

H        2.15387900   -0.54712700    0.83375700

C        3.84036300   -1.81383700    0.44046500

C        3.93158600    0.65526300    0.95383800

H        4.80866300   -1.77481200   -0.08260500

H        4.02252200   -2.06999400    1.49365200

H        3.23579400   -2.61270500   -0.01306900

H        3.39506700    1.61033700    0.84575300

H        4.09644300    0.47591500    2.02642300

H        4.91065500    0.74992000    0.45875800

g1(2 iPrOH)

C       -0.47961500   -0.79089400   -0.40022800

C       -1.64419600   -1.08681200   -1.09607300

C       -2.87506700   -1.15079600   -0.43017700

C       -2.93093000   -0.91955100    0.95133300

C       -1.77520400   -0.62159300    1.65772000

C       -0.55388400   -0.55218400    0.97573700

H        0.49055800   -0.74291400   -0.89579000

H       -1.60254400   -1.27476400   -2.17187900

H       -3.89426800   -0.97451300    1.46205600

H       -1.80164800   -0.43061700    2.73287900

C       -4.10266100   -1.46596400   -1.18409200

H       -3.95523800   -1.63869700   -2.27473000

O       -5.20565700   -1.54092400   -0.68993000

O        0.60006900   -0.22800400    1.61238800

H        0.46823000   -0.16164400    2.57222000

H        2.11668800   -1.17884000    0.79803300

O        2.67463500   -1.79207600    0.29642300

C        3.93585600   -1.18052200    0.07530000

H        4.33674200   -0.80483100    1.03593600

C        4.86860300   -2.25744800   -0.44626600

C        3.81544000   -0.01154200   -0.89152600

H        4.48317100   -2.66104300   -1.39570800

H        5.87583200   -1.85424800   -0.62242400

H        4.94386900   -3.08448800    0.27448300

H        3.10257000    0.74021700   -0.52093800

H        4.78780100    0.48296500   -1.03609000

H        3.45876900   -0.36764700   -1.87139700

H        1.05666700    1.47837300    0.66276100

O        1.05138400    2.03801200   -0.12826100

C        0.29875400    3.21049300    0.14162800

H        0.84424400    3.84010500    0.87067500

C        0.18234200    3.97315400   -1.16369800

C       -1.05939500    2.85852500    0.72849300

H       -0.36341700    3.36853900   -1.90468600

H       -0.35550900    4.92052900   -1.01851700

H        1.17996100    4.19753200   -1.56833700

H       -0.94266200    2.30029900    1.67093500

H       -1.64213700    3.76645200    0.94348700

H       -1.63139600    2.23397400    0.02315100

h1

C       1.25867500    1.19914700    0.00013600

C      -0.11022800    1.33864600    0.00019900

C      -0.96899500    0.21448500    0.00001000

C      -0.37705000   -1.07353100    0.00038500

C       0.98674100   -1.23278800    0.00019100

C       1.89882500   -0.10180400   -0.00043200

H       1.91320600    2.07480400    0.00034700

H      -0.55592800    2.33939700    0.00031000

H      -1.03696900   -1.94603800    0.00058400

H       1.43654700   -2.22944800    0.00032100

C      -2.40213500    0.38429200   -0.00010100

H      -2.74033400    1.44977800    0.00006900

O      -3.23525000   -0.51305400   -0.00028600

O       3.14381000   -0.24434300   -0.00020700

h1(iPrOH)

C        -0.38683600   -0.47687800   -0.64084700

C        -1.60628800   -1.08880000   -0.43806800

C        -2.72885500   -0.36200800    0.01003800

C        -2.57716700    1.02261800    0.25093200

C        -1.36793800    1.64972100    0.05522100

C        -0.20609600    0.93109700   -0.40373900

H         0.47808400   -1.04358700   -0.99286900

H        -1.71388800   -2.16165500   -0.62892400

H        -3.44611600    1.58840500    0.59802600

H        -1.25088200    2.72014400    0.24145700

C        -4.00127300   -1.02728300    0.21248400

H        -3.99304000   -2.12153400   -0.01202600

O        -5.03244000   -0.49563600    0.59377300

O         0.90750300    1.51882700   -0.58804700

H         2.11869200    0.50243600   -0.94215300

O         2.84809500   -0.17864000   -0.99084000

C         3.23060600   -0.42622400    0.34437500

H         2.33975100   -0.71392700    0.94128800

C         4.20261700   -1.59291000    0.34705800

C         3.83580000    0.82271600    0.97463900

H         5.09347100   -1.34003800   -0.24971300

H         4.52584800   -1.84163900    1.36830800

H         3.73640100   -2.48486200   -0.09715900

H         3.10925600    1.64806400    0.93837000

H         4.11358500    0.65080900    2.02556400

H         4.73615100    1.12867600    0.41818300

h1(2 iPrOH)

C       -1.42170500   -1.49459600    0.02169200

C       -2.76807400   -1.53965400    0.32701700

C       -3.60547500   -0.43048100    0.09940600

C       -3.03974400    0.74040700   -0.44853800

C       -1.69814300    0.80207600   -0.75930700

C       -0.83204200   -0.31953800   -0.54115500

H       -0.76841800   -2.35075300    0.20374800

H       -3.19906700   -2.45028900    0.75500800

H       -3.68895200    1.60229300   -0.62409500

H       -1.25834400    1.70868800   -1.18228800

C       -5.02141500   -0.50285100    0.42493000

H       -5.34949100   -1.47933000    0.85549900

O       -5.83329700    0.39222600    0.26435400

O        0.41738200   -0.26981000   -0.83706900

H        1.26273700   -1.68197100   -0.70512900

O        1.84917800   -2.44182400   -0.45578400

C        2.89643400   -1.87446600    0.30213700

H        2.47428100   -1.28485700    1.14176100

C        3.72276200   -3.00825000    0.88282100

C        3.73748500   -0.93988700   -0.56084300

H        4.16164300   -3.60804700    0.06969500

H        4.53889300   -2.62602600    1.51278900

H        3.09162100   -3.67004400    1.49423900

H        3.12095500   -0.11884100   -0.95840700

H        4.56786100   -0.49928800    0.01222100

H        4.15888700   -1.49854000   -1.41202100

H        1.16350000    1.18446400   -0.99378500

O        1.67187400    2.03710500   -0.99467800

C        2.06406600    2.29985500    0.33619800

H        2.66106600    1.44917000    0.72409100

C        2.95150000    3.53195800    0.32066800

C        0.85698500    2.47974100    1.24884600

H        2.38801100    4.39572600   -0.06661100

H        3.31407000    3.77553300    1.32969400

H        3.82133300    3.36956500   -0.33292100

H        0.24189400    1.56696000    1.26173000

H        1.16943900    2.69342700    2.28228100

H        0.23119100    3.31469900    0.89469000

h1(3 iPrOH)

C       -1.97534100   -1.08132900   -1.05975000

C       -3.35318800   -1.18561600   -0.99001100

C       -4.12739900   -0.17564300   -0.39229100

C       -3.47438100    0.95684100    0.13359200

C       -2.10042800    1.07361100    0.07146900

C       -1.29888500    0.05224700   -0.52364400

H       -1.37707400   -1.86307800   -1.53362000

H       -3.85520100   -2.06418000   -1.40665100

H       -4.07795600    1.74462300    0.59142400

H       -1.59225500    1.95494300    0.46953700

C       -5.57905000   -0.30539600   -0.32909100

H       -5.98351600   -1.24195400   -0.78172000

O       -6.33733200    0.50892400    0.16458800

O       -0.00796500    0.16168900   -0.57848400

H        0.96385000   -1.06452200   -1.21947400

O        1.62619400   -1.74233400   -1.49459500

C        2.90672900   -1.14806100   -1.39975800

H        3.11456700   -0.88464500   -0.34336800

C        3.92595000   -2.17986000   -1.84844200

C        2.97980600    0.12644200   -2.23159000

H        3.73682100   -2.46294000   -2.89615100

H        4.94994300   -1.78676400   -1.77174800

H        3.85533800   -3.08829500   -1.23164900

H        2.22440900    0.85489400   -1.89975400

H        3.96970900    0.60070500   -2.14491800

H        2.79362100   -0.10337100   -3.29317100

H        0.54387400    1.74341200   -0.66776700

O        0.96966300    2.63468400   -0.68811400

C        1.92253400    2.65431500    0.35680000

H        2.51320300    1.71647900    0.33556100

C        2.86044800    3.82173700    0.10605900

C        1.23898200    2.74822200    1.71541000

H        2.28969000    4.76402900    0.09076300

H        3.62820000    3.89174600    0.88995800

H        3.36386900    3.71022100   -0.86589800

H        0.56668900    1.89086000    1.86516900

H        1.97634400    2.74400200    2.53268100

H        0.64880100    3.67667400    1.77890400

H        0.98931700   -0.27713700    0.81996800

O        1.51418000   -0.47742800    1.62345900

C        1.50139800   -1.87416600    1.85462000

H        2.23654200   -2.36610600    1.18602000

C        1.93000000   -2.10127400    3.29300600

C        0.13154900   -2.46296500    1.55606500

H        1.20143300   -1.64375300    3.98085700

H        2.00132500   -3.17483700    3.51915700

H        2.91240000   -1.64187200    3.47722700

H       -0.10903400   -2.32797500    0.49205600

H        0.10717000   -3.54015300    1.77865000

H       -0.64234100   -1.95991100    2.15846500

Reference

[S1] Chen Y., Ji S., Wang Y., Dong J., Chen W., Li Z., Shen R., Zheng L., Zhuang Z., Wang D., Li Y. Isolated single iron atoms anchored on N-doped porous carbon as an efficient electrocatalyst for the oxygen reduction reaction. Angew. Chem. Int. Ed. 56, 6937–6941 (2017).

[S2] Mironenko A., Vlachos D. Conjugation-driven “Reverse Mars-van Krevelen”-type radical mechanism for low-temperature C−O bond activation. J. Am. Chem. Soc. 138, 8104−8113 (2016).

[S3] Panagiotopoulou P., Martin N., Vlachos D. Effect of hydrogen donor on liquid phase catalytic transfer hydrogenation of furfural over a Ru/RuO2/C catalyst. J. Mol. Catal. A: Chem. 392, 223−228 (2014).

[S4] Ma M., Hou P., Zhang P., Cao J., Liu H., Yue H., Tian G., Feng S. Magnetic Fe3O4 nanoparticles as easily separable catalysts for efficient catalytic transfer hydrogenation of biomass-derived furfural to furfuryl alcohol. Appl. Catal. A 602, 117709 (2020).

[S5] Frisch M., Trucks G., Schlegel H., Scuseria G., Robb M., Cheeseman J., Scalmani G., Barone V., Mennucci B., Petersson G., Nakatsuji H., Caricato M., Li X., Hratchian H., Izmaylov A., Bloino J., Zheng G., Sonnenberg J., Hada M., Ehara M., Toyota K., Fukuda R., Hasegawa J., Ishida M., Nakajima T., Honda Y., Kitao O., Nakai H., Vreven T., Montgomery J., Peralta J., Ogliaro F., Bearpark M., Heyd J., Brothers E., Kudin K., Staroverov V., Keith T., Kobayashi R., Normand J., Raghavachari K., Rendell A., Burant J., Iyengar S., Tomasi J., Cossi M., Rega N., Millam J., Klene M., Knox J., Cross J., Bakken V., Adamo C., Jaramillo J., Gomperts R., Stratmann R., Yazyev O., Austin A., Cammi R., Pomelli C., Ochterski J., Martin R., Morokuma K., Zakrzewski V., Voth G., Salvador P., Dannenberg J., Dapprich S., Daniels A., Farkas O., Foresman J., Ortiz J., Cioslowski J., Fox D. Gaussian 09, Revision D.01; Gaussian, Inc., Wallingford, CT (2013).

[S6] Zhao Y., Truhlar D. The M06 suite of density functionals for main group thermochemistry, thermochemical kinetics, noncovalent interactions, excited states, and transition elements: two new functionals and systematic testing of four M06-ClassFunctionals and 12 other functionals. Theor. Chem. Acc. 120, 215–241 (2008).

[S7] Marenich A., Cramer C., Truhlar D. Universal solvation model based on solute electron density and on a continuum model of the solvent defined by the bulk dielectric constant and atomic surface tensions. J. Phys. Chem. B 113, 6378–6396 (2009).

[S8] Weigend F., Ahlrichs R. Balanced basis sets of split valence, triple zeta valence and quadruple zeta valence quality for H to Rn: design and assessment of accuracy. Phys. Chem. Chem. Phys. 7, 3297–3305 (2005).

[S9] For recent examples considering energy correction for standard state change: (a) Li H., Hall M. Role of the chemically non-innocent ligand in the catalytic formation of hydrogen and carbon dioxide from methanol and water with the metal as the spectator. J. Am. Chem. Soc. 137, 12330–12342 (2015). (b) Jiang Y., Yan L., Yu H., Zhang Q., Fu Y. Mechanism of vanadium-catalyzed selective C−O and C−C cleavage of lignin model compound. ACS Catal. 6, 4399–4410 (2016). (c) Yu J., Zhang S., Hong X. Mechanisms and origins of chemo- and regioselectivities of Ru(II)-catalyzed decarboxylative C–H alkenylation of aryl carboxylic acids with alkynes: a computational study. J. Am. Chem. Soc. 139, 7224–7243 (2017). (d) Jiang Y., Li G., Yang D., Zhang Z., Zhu L., Fan X., Bi S. Mechanism of Cu-catalyzed aerobic C(CO)–CH3 bond cleavage: a combined computational and experimental study. ACS Catal. 9, 1066–1080 (2019).

[S10] Internet bond-energy databank (pKa and BDE)--iBonD Home Page. http://ibond.chem.tsinghua.edu.cn or http://ibond.nankai.edu.cn.

[S11] Fu Y., Liu L., Li R., Liu R., Guo Q. First-principle predictions of absolute pKa’s of organic acids in dimethyl sulfoxide solution. J. Am. Chem. Soc. 126, 814–822 (2004).