[bookmark: _Hlk44011789][bookmark: _Hlk44011886]Table 4.0: The average result of each parameter for condition of raw coconut husks with limestone and raw coconut husks.
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Table 4.1: The average result of each parameter for condition of raw sugarcane bagasse with limestone and raw sugarcane bagasse.
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[bookmark: _Hlk44012235]Table 4.2: The average result and percentage removal of turbidity for condition of raw coconut husks with limestone, raw coconut husks, raw sugarcane bagasse with limestone and raw coconut husks.
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Table 4.3: The average result and percentage removal of colour for condition of raw coconut husks with limestone, raw coconut husks, raw sugarcane bagasse with limestone and raw coconut husks.
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Table 4.4: The average result and percentage removal of pH for condition of raw coconut husks with limestone, raw coconut husks, raw sugarcane bagasse with limestone and raw coconut husks.
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Table 4.5: The average result and percentage removal of Copper for condition of raw coconut husks with limestone, raw coconut husks, raw sugarcane bagasse with limestone and raw coconut husks.
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Table 4.6: The average result and percentage removal of Zinc (Zn) for condition of raw coconut husks with limestone, raw coconut husks, raw sugarcane bagasse with limestone and raw coconut husks.
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Table 4.7: The average result and percentage removal of Iron (Fe) for condition of raw coconut husks with limestone, raw coconut husks, raw sugarcane bagasse with limestone and raw coconut husks.

[image: ]

image6.png
Parameter Sample/Filter
Raw After treated Raw After treated
(before Raw Raw (before Raw Raw
treated) coconut coconut | treated) | sugarcane | sugarcane
husks with husks bagasse with | bagasse
limestone limestone
Averageof | 3.72 127 139 3.67 134 1.42
Copper
(mg/L)
Percentage 0 66 63 0 63 61
removal (%)
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Parameter Sample/Filter
Raw After treated Raw After treated
(before Raw Raw (before Raw Raw
treated) coconut coconut | treated) | sugarcane | sugarcane
husks with husks bagasse with | bagasse
limestone limestone
Averageof | 125 038 0.44 1.10 035 048
Zine (mg/L)
Percentage 0 70 65 0 68 56
removal (%)
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Parameter Sample/Filter
Raw After treated Raw After treated
(before Raw Raw (before Raw Raw
treated) coconut coconut | treated) | sugarcane | sugarcane
husks with husks bagasse with | bagasse
limestone limestone
Averageof | 2.65 0.42 0.73 2.63 0.51 0.92
Iron (mg/L)
Percentage 0 84 72 0 81 65
removal (%)
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Parameter Sample/ Filter
Raw After treated
(before treated) Raw coconut husks | Raw coconut husks
[20 January 2020] with limestone

Turbidity (NTU) 426.0 614 732

Colour (PtCo) 1847 879 959

pH 4.59 577 5.57

Copper, Cu (nglL) | 3.72 127 139

Zinc, Zn (mg/L) 125 038 0.44

Tron, Fe (ng/L) 2.65 0.42 0.73
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Parameter Sample/ Filter
Raw After treated
(before treated) Raw sugarcane bagasse | Raw sugarcane
[27 January 2020] with limestone bagasse
Turbidity (NTU) 3200 684 814
Colour (PtCo) 1445 755 891
pH 4.67 538 533
Copper, Cu (mgL) | 3.67 134 L42
Zinc, Zn (mg/L) 1.10 035 048
Tron, Fe (ng/L) 2.63 051 092
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Parameter Sample/Filter
Raw After treated Raw After treated
(before Raw Raw (before Raw Raw
treated) coconut coconut | treated) | sugarcane | sugarcane
husks with husks bagasse with | bagasse
limestone limestone
Average of | 426.0 614 732 3200 68.4 814
turbidity
(NTU)
Percentage 0 86 83 0 77 75
removal (%)
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Parameter Sample/Filter
Raw After treated Raw After treated
(before Raw Raw (before Raw Raw
treated) coconut coconut | treated) | sugarcane | sugarcane
husks with husks bagasse with | bagasse
limestone limestone
Average of | 1847 879 959 1445 755 891
colour
(PtCo)
Percentage 0 52 48 0 48 38
removal (%)
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Parameter Sample/Filter
Raw After treated Raw After treated
(before Raw Raw (before Raw Raw
treated) coconut coconut | treated) | sugarcane | sugarcane
husks with husks bagasse with | bagasse
limestone limestone
Average of 4.59 577 5.57 4.67 538 533
pH





