Solar overall water-splitting by a spin-hybrid all-organic semiconductor

Xinyu Lin1, Yue Hao1, Yanjun Gong2, Peng Zhou3, Dongge Ma4, Zhonghuan Liu1, Yuming Sun1, Hongyang Sun1, Yahui Chen1, Shuhan Jia1, Wanhe Li1, Chengqi Guo1, Yiying Zhou1, Pengwei Huo1, Yan Yan1*, Wanhong Ma2*, Shouqi Yuan1*, Jincai Zhao2

1School of Chemistry & Chemical Engineering/Research Center of Fluid Machinery Engineering and Technology, Jiangsu University, Zhenjiang, China, 212013.

2Key Laboratory of Photochemistry, Institute of chemistry, Chinese Academy of Sciences, Beijing, China, 100190; University of Chinese Academy of Sciences, Beijing, China, 100049.

3Electrical Engineering & Computer Science, University of Michigan, Michigan, USA, 48109-2122.

4Department of Chemistry, College of Chemistry and Materials Engineering, Beijing Technology and Business University, Beijing, China, 100048.

Corresponding authors:

Prof. Yan Yan (dgy5212004@163.com)

Prof. Wanhong Ma (whma@iccas.ac.cn)

Prof. Shouqi Yuan (shouqiy@ujs.edu.cn)

Supplementary Figures

Supplementary Fig. 1. (a) Standard curves for Fe(III)-1, 10-phenanthroline back titration measurements. (b) UV-vis absorption spectra of Fe(II)-1, 10-phenanthroline after the titration of reductive electrons on PDI and :PDI2-/PDI2-.

Supplementary Fig. 2. Cyclic voltammetry curves of PDI. The polarization curves in 0.15 M TBATFB/DMSO at a scan rate is 10 mV s-1, and the loading amounts of all catalysts on carbon papers are 0.5 mg cm-2.

Supplementary Fig. 3. Mass spectra of PDI and :PDI2-/PDI2-.

Supplementary Fig. 4. NAP-XPS (a) C 1s and (b) O1s spectra of PDI and :PDI2-/PDI2-.

Supplementary Fig. 5. NAP-XPS N 1s spectra of PDI and :PDI2-/PDI2-.

Supplementary Fig. 6. 1H NMR spectra of PDI and :PDI2-/PDI2-.

Supplementary Fig. 7. SEM images to show the morphology evolution of pristine PDI during the self-assembly.

Supplementary Fig. 8. SEM images of (a) freshly prepared :PDI2-/PDI2- nanobelt (120 h) and (b) :PDI2-/PDI2- nanobelt stored in N2 glove box for 6 months. (c) XRD patterns of :PDI2-/PDI2- nanobelt (120 h) freshly prepared and stored in N2 glove box for 6 months. (d) ESR spectra of :PDI2-/PDI2- nanobelt (120 h) freshly prepared and stored in N2 glove box for 6 months.

Supplementary Fig. 9. XRD patterns of PDI and :PDI2-/PDI2-.

Supplementary Fig. 10. Photoluminescence spectra (λex=450 nm) of :PDI2-/PDI2- (solid) with different self-assembly times.

Supplementary Fig. 11. (a) Water-splitting performances on PDI with different self-assembly time. (b) Water-splitting experiments without catalysts, light or H2O over :PDI2-/PDI2- nanobelt (120 h) catalyst.

Supplementary Fig. 12. The water contact angle measurement on PDI and :PDI2-/PDI2-.

Supplementary Fig. 13. Radical self-assembly strategy applies to five PDI derivatives (PDI1-PDI5) with ESR spectra and optical microscope photos.

Supplementary Table 1. Wavelength-dependent AQYs and corresponding H2 production amount on PDI2-/PDI2- nanobelt (120 h).

| Wavelength (nm) | H2 evolution (μmol) | Light intensity (mW cm-2) | Irradiation area (cm2) | Irradiation time (h) | AQY (%) |
| --- | --- | --- | --- | --- | --- |
| 365 | 0 | 23.7 | 4 | 5 | 0 |
| 420 | 12.5 | 236.6 | 4 | 5 | 0.4247 |
| 425 | 26.2 | 241.5 | 4 | 5 | 0.8494 |
| 450 | 37.6 | 275.2 | 4 | 5 | 1.0138 |
| 475 | 45.9 | 266 | 4 | 5 | 1.1097 |
| 500 | 43.8 | 240.7 | 4 | 5 | 1.2193 |
| 530 | 56.8 | 195.2 | 4 | 5 | 1.5755 |
| 550 | 87.5 | 269.8 | 4 | 5 | 1.9591 |
| 580 | 61.3 | 210.5 | 4 | 5 | 1.6714 |
| 600 | 38.3 | 166.9 | 4 | 5 | 1.2741 |
| 630 | 56.1 | 201.2 | 4 | 5 | 1.4796 |
| 650 | 45.3 | 154.7 | 4 | 5 | 1.5344 |
| 670 | 46.4 | 143.1 | 4 | 5 | 1.6166 |
| 700 | 28.4 | 100.5 | 4 | 5 | 1.3426 |
| 725 | 26.9 | 99.5 | 4 | 5 | 1.2467 |
| 760 | 28.2 | 102.7 | 4 | 5 | 1.2056 |
| 850 | 18.7 | 80.2 | 4 | 5 | 0.9453 |

Supplementary Table 2. Wavelength-dependent AQYs and corresponding H2 production amount on PDI2-/PDI2- nanorod (24 h).

| Wavelength (nm) | H2 evolution (μmol) | Light intensity (mW cm-2) | Irradiation area (cm2) | Irradiation time (h) | AQY(%) |
| --- | --- | --- | --- | --- | --- |
| 365 | 0 | 15.9 | 4 | 5 | 0 |
| 420 | 3.3 | 154.2 | 4 | 5 | 0.17 |
| 425 | 5.3 | 220.5 | 4 | 5 | 0.19 |
| 450 | 7.8 | 253.2 | 4 | 5 | 0.23 |
| 475 | 9.7 | 260 | 4 | 5 | 0.26 |
| 500 | 12.9 | 244.7 | 4 | 5 | 0.35 |
| 530 | 12.4 | 200 | 4 | 5 | 0.39 |
| 550 | 17.4 | 250.7 | 4 | 5 | 0.42 |
| 580 | 10.4 | 170.5 | 4 | 5 | 0.35 |
| 600 | 7.6 | 155 | 4 | 5 | 0.27 |
| 630 | 5.2 | 180.7 | 4 | 5 | 0.16 |
| 650 | 2.7 | 100.8 | 4 | 5 | 0.13 |
| 670 | 2.6 | 131.1 | 4 | 5 | 0.1 |
| 700 | 1.7 | 98 | 4 | 5 | 0.08 |
| 725 | 1.3 | 82.7 | 4 | 5 | 0.072 |
| 760 | 0.8 | 69.5 | 4 | 5 | 0.05 |
| 850 | 0.6 | 70.2 | 4 | 5 | 0.034 |

Supplementary Table 3. AQYs and corresponding H2 production amount on PDI2-/PDI2- with different self-assembly time under λ=550 nm illumination.

| Self-assembly time (h) | H2 evolution (μmol) | Light intensity (mW cm-2) | Irradiation area (cm2) | Irradiation time (h) | AQY(%) |
| --- | --- | --- | --- | --- | --- |
| 0 | 0.99 | 200 | 4 | 5 | 0.03 |
| 24 | 23.8 | 200 | 4 | 5 | 0.72 |
| 48 | 31.4 | 200 | 4 | 5 | 0.95 |
| 72 | 43.6 | 200 | 4 | 5 | 1.32 |
| 96 | 59.2 | 200 | 4 | 5 | 1.79 |
| 120 | 64.8 | 200 | 4 | 5 | 1.96 |