Supplementary Information

Spontaneously Sn Doped Bi/BiOx Nanowires Toward High-Performance CO2 Electroreduction to Formate

Yang zhao1, Xunlin Liu2, Zhixiao Liu2, Xin Lin1, Jiao Lan1, Yanlong Zhang1, Ying-Rui Lu3, Ming Peng1, Ting-Shan Chan3, Yongwen Tan1*

1 College of Materials Science and Engineering, State Key Laboratory of Advanced Design and Manufacturing for Vehicle Body, Hunan University, Changsha, Hunan 410082, China

2College of Materials Science and Engineering, Hunan University, Changsha, Hunan 410082, China

3National Synchrotron Radiation Research Center, Hsinchu 300, Taiwan

*Corresponding Author: tanyw@hnu.edu.cn

Supplementary Figures

Supplementary Figure 1. The linear sweep voltammetry (LSV) curve of Bi1Sn99 in 0.25 M H2SO4. The oxidation (or dissolution) peak of Sn phase is from ~-0.48 V vs. Ag/AgCl, we selected the corrosion potential of -0.3 V for the selective dissolution of the Sn phase.

Supplementary Figure 2. EDS elemental distributions of Bi/Bi(Sn)Ox NWs after dealloying.

Supplementary Figure 3. Ternary phase diagram of the Bi–Sn–O system calculated at 300 °C, 1 atm1.

Supplementary Figure 4. Schematic illustration of the flow cell configuration.

Supplementary Figure 5. XRD patterns of commercial Bi2O3, Bi, and SnO2.

Supplementary Figure 6. SEM images of commercial Bi2O3 (a), Bi (b), and SnO2 (c).

Supplementary Figure 7. A representative GC spectrum of gas product, which was produced on Bi/Bi(Sn)Ox NWs catalyst at -0.7 V vs. RHE.

Supplementary Figure 8. (a) A representative 1H-NMR spectrum of a liquid sample, which was produced on Bi/Bi(Sn)Ox NWs catalyst at -0.7 V vs. RHE after 1 hour of electrolysis, (b) Established calibration curve.

Supplementary Figure 9. H2, CO, and formate FEs of commercial (a) Bi2O3, (b) SnO2, (c) Bi.

Supplementary Figure 10. Energy efficiency of Bi2O3, Bi, SnO2, and Bi/Bi(Sn)Ox NWs at different applied potentials.

Supplementary Figure 11. Tafel plots of the Bi2O3, Bi, SnO2, and Bi/Bi(Sn)Ox NWs in 1 M KOH.

Supplementary Figure 12. CO2 adsorption isotherms of the Bi2O3, Bi, and Bi/Bi(Sn)Ox NWs.

Supplementary Figure 13. Electrochemical impedance spectroscopy (EIS) of the different Bi2O3, SnO2, Bi, and Bi/Bi(Sn)Ox NWs catalysts. EIS plots were performed in the frequency range of 0.01 to 106 Hz at -0.4 V vs. RHE.

Supplementary Figure 14. (a-c) Cyclic Voltammetry (CV) curves of the catalysts (a) Bi, (b) Bi2O3, (c) SnO2, and (d) Bi/Bi(Sn)Ox NWs. (e) The capacitive current densities plotted against scan rate.

Supplementary Figure 15. ECSA-corrected current density of formate (a), CO (b), H2 (c) for the Bi, Bi2O3, SnO2 and Bi/Bi(Sn)Ox NWs catalysts at various applied potentials.

The calculation of ECSA was according to the formula, ECSA = Rf*S, in which S represents the geometric area of work electrode (1 cm2). The roughness factor (Rf) was obtained from the formula, Rf = Cdl/Cs, in which double layer capacitance (Cdl) was the half of the slope in Fig.S14. And the Cs (general specific capacitance of metal oxide) corresponds to the average double layer capacitance of a smooth oxide surface about 70 μF cm-2.

Supplementary Figure 16. (a) SEM and (b) TEM images of Bi/Bi(Sn)Ox NWs after 10 h stability testing.

Supplementary Figure 17. (a) Bi 4f, (b) Sn 3d and (c) O 1s XPS spectra of Bi/Bi(Sn)Ox NWs after 10 h CO2 reduction at -0.7 V vs. RHE.

Supplementary Figure 18. A photograph of In-situ Raman electrolysis cell.

Supplementary Figure 19. DFT calculation models of *OCHO, and *H adsorption on Bi/BiOx and Bi/Bi(Sn)Ox. Bi, pink; Sn, Bule; C, grey; O, red; H, white.

Supplementary Table 1. Elemental compositions of Bi/Bi(Sn)Ox NWs based on XPS and EDS characterizations.

|  | Bi (at%) | Sn (at%) | O (at%) |
| --- | --- | --- | --- |
| XPS | 34.5 | 5.1 | 60.4 |
| XPS (after Ar+ etch) | 51.5 | 3.4 | 45.1 |
| EDS | 95.2 | 4.8 | / |

Supplementary Table 2. Free energy of *OCHO, *H absorption and Ep on various DFT models.

| Catalysts | *OCHO (eV) | *H (eV) | Ep (eV) |
| --- | --- | --- | --- |
| Bi/BiOx | -0.65 | 0.32 | -2.68 |
| Bi/Bi(Sn)Ox | -0.13 | 0.6 | -2.25 |

Supplementary Table 3. Electrochemical CO2 reduction performance of recently Bi, Sn-based catalysts in flow cell.

| Catalyst | Electrolyte | Potential range for FEs of >90% (V vs. RHE) | Potential window (mV) | j @ -1.0 V (mA cm-2) | Ref. |
| --- | --- | --- | --- | --- | --- |
| Bi/Bi(Sn)Ox NWs | 1 M KOH | -0.5 ~ -0.9 | 400 | 301.4 | This work |
| Bi nanosheets | 0.5 M KHCO3 | -0.7 ~ -0.8 | 100 | ~120 | 2 |
| Sn80Bi20@Bi-SnOx | 0.5 M KHCO3 | −0.67 ~ −0.92 | 250 | ~40 | 3 |
| Bi NSs | 1 M KOH | -0.48 ~-0.67 | 190 | ＞400 | 4 |
| Bi@Sn NPs | 2 M KHCO3 | -0.81 ~ -1.15 | 340 | ~150 | 5 |
| Bismuthene nanosheets | 1 M KHCO3 | −0.65 ~ −1.4 | 750 | ~110 | 6 |
| Bi2O3@C-800 | 1 M KOH | -0.4 ~ -1.1 | 700 | ~220 | 7 |
| Bi-ene | 1 M KOH | -0.57 ~ -0.75 | 180 | ＞300 | 8 |
| NTD-Bi | 1 M KOH | -0.52 ~-0.58 | 60 | ＞300 | 9 |
| SnO2 nanosheet | 1 M KOH | -1.01~-1.13 | 120 | ~200 | 10 |
| Sn2.7Cu | 1 M KOH | -0.4~-0.7 | 300 | ＞400 | 11 |
| H–Sn3O4 NS | 1 M KOH | -1.02 | / | 421 | 12 |

References

1	Tang, J. et al. Advantages of eutectic alloys for creating catalysts in the realm of nanotechnology-enabled metallurgy. Nat. Commun. 10, 4645 (2019).

2	Yi, L. et al. Molten salt assisted synthesis of bismuth nanosheets for long-term continuously electrocatalytic conversion CO2 to formate. Angew. Chem. Int. Ed. 59, 2-10 (2020).

3	Yang, Q. et al. Novel Bi-doped amorphous SnOx nanoshells for efficient electrochemical CO2 reduction into formate at low overpotentials. Adv. Mater. 32, 2002822 (2020).

4	Yang, J. et al. Bi-based metal-organic framework derived leafy bismuth nanosheets for carbon dioxide electroreduction. Adv. Energy Mater. 10, 2001709 (2020).

5	Xing, Y. et al. Bi@Sn core-shell structure with compressive strain boosts the electroreduction of CO2 into formic acid. Adv. Sci. 7, 1902989 (2020).

6	Ma, W. et al. Monoclinic scheelite bismuth vanadate derived bismuthene nanosheets with rapid kinetics for electrochemically reducing carbon dioxide to formate. Adv. Funct. Mater. 31, 2006704 (2020).

7	Deng, P. et al. Metal-organic framework-derived carbon nanorods encapsulating bismuth oxides for rapid and selective CO2 electroreduction to formate. Angew. Chem. Int. Ed. 59, 10807-10813 (2020).

8	Cao, C. et al. Metal-organic layers derived atomically thin bismuthene for efficient carbon dioxide electroreduction to liquid fuel. Angew. Chem. Int. Ed. 59, 15014–15020 (2020).

9	Gong, Q. et al. Structural defects on converted bismuth oxide nanotubes enable highly active electrocatalysis of carbon dioxide reduction. Nat. Commun. 10, 2807 (2019).

10	Li, J. et al. Two-dimensional SnO2 nanosheets for efficient carbon dioxide electroreduction to formate. ACS Sustain. Chem. Eng. 8, 4975-4982 (2020).

11	Ye, K. et al. In situ reconstruction of hierarchical Sn-Cu/SnOx core/shell catalyst for high-performance CO2 electroreduction. Angew. Chem. Int. Ed. 59, 4814 –4821 (2020).

12	Liu L. X. et al. Tuning Sn3O4 for CO2 reduction to formate with ultra-high current density. Nano Energy 77, 105296 (2020).