Supporting information

Methylene Orange and Methyl Blue Adsorption Behavior on Pine Leaves Biomass (Pinus kesiya)

Phuong Thao Huynh1, Duy-Khoi Nguyen2,4, Bich-Ngoc Duong3, Phi-Ho Nguyen5, Van-Phuc Dinh3,*

1Faculty of Chemistry and Environment, Dalat University, 01 Phu Dong Thien Vuong Street, Ward 8, Dalat City, Lam Dong Province, Vietnam.

2Institute of Fundamental and Applied Sciences, Duy Tan University, Ho Chi Minh City 700000, Viet Nam

3Institute of Applied Technology and Sustainable Development, Nguyen Tat Thanh University, Ho Chi Minh City 700000, Vietnam.

4Faculty of Natural Sciences, Duy Tan University, Da Nang, 550000, Vietnam

5Graduate student at the Faculty of Chemistry and Environment, Dalat University, 01 Phu Dong Thien Vuong Street, Ward 8, Dalat City, Lam Dong Province, Vietnam.

Corresponding authors: dvphuc@ntt.edu.vn

1. Kinetic studies

To evaluate physiochemical interactions between biomass and dyes, the nature of sorption process, and rate-limiting step, all of which play an vital role for the design of commercial sorption systems, adsorption kinetic modeling is fitted with experimental data to determine kinetic parameters. As a consequence, the nonlinear equations indicated below were used to fit adsorption kinetic models to the biomass kinetic study data:

| Pseudo-first-order | qt= qe(1-e-k1t) | (1) |
| --- | --- | --- |
| Pseudo-second-order | qt=qe2.k2.t1+k2.qe.t | (2) |
| Elovich | qt= 1βln⁡(1+α.β.t) | (3) |
| Intra-diffusion | qt= kdt1/2+C | (4) |

Where	qt (mg.g-1): adsorbed amount of the adsorbate at time t

qe (mg.g-1): adsorption capacity at equilibrium

k1 (1.min-1): pseudo-first-order rate constant

k2 (g.mg-1.min): pseudo-second-order rate constant

α (mg.g-1.min-1): initial adsorption rate of the Elovich model

β (mg.g-1): the desorption constant in a single experiment

kd (mg.g-1.min): the Intra-diffusion model's rate constant

C (mg.g-1): a constant representing the boundary layer thickness

2. Adsorption Isotherm Modeling

Using equilibrium isotherm modeling plays an instrumental role in determining the distribution of dye molecules on the biomass surface, leading to an understanding of the dye-biomass adsorption mechanism. For this study, four isotherm models (Langmuir, Freundlich, Sips, Temkin) were applied to examine the sorption processes of cationic and anionic dyes onto the biomass. The fomulars and meanings of these models were shown in SI.

The Langmuir model of adsorption assumes monolayer adsorption, which means that all active binding sites are energetically similar and absorb just one color molecule. The nonlinear version of the model is as follows:

| qe=qm.KL.Ce1+KL.Ce | (5) |
| --- | --- |

Where, qm (mg/g) is the maximum adsorption capacity of the biomass and KL (L/mg) is the affinity constant for the Langmuir model.

The Freundlich model covers surface heterogeneity on sorbents, including multilayer adsorption and uneven energy distribution of active sorption sites. The nonlinearized Freundlich model is written as follows:

| qe=KF.Ce1/n | (6) |
| --- | --- |

Where KF and 1/n represent the Freundlich constant and the intensity parameter, respectively (dimensionless). If the value of n is more than one, it implies that dyes are adsorbing on the surface of the adsorbent and that a physical process is taking place. Furthermore, n less than one suggests that adsorption is a chemical process, but n equal to one indicates that adsorption is linear.

The Temkin isotherm model includes a component that explicitly considers interactions between adsorbate and adsorbent species. This model assumed that binding energy was distributed uniformly. The Tempkin equation is as follows:

| qe= RTbT.ln⁡(KTCe) | (7) |
| --- | --- |

Where bT (J/mol) represents the heat of sorption and KT (L/mg) represents the Temkin equilibrium binding constant corresponding to the highest binding energy.

The Sips isotherm is a mixture of the Langmuir and Freundlich models designed for anticipating adsorption in heterogeneous systems while avoiding the rising adsorbate concentration limitation of the Freundlich isotherm. In linear form, the Sips model is as follows:

| qe= qS.CeβS1+αS.CeβS | (8) |
| --- | --- |

Where qS (L/g): Sips constant; αS (L/mg): Sips isotherm model constant; βS: Sips isotherm model exponent.