Table 1. Qualitative and quantitative characteristics of coumarone-indene-containing raw materials

| Component | Structural formula | Content [wt. %] |  |
| --- | --- | --- | --- |
|  |  | Fraction 140-190 °С | Fraction 140-200 °С |
| Methylbenzene (toluene) |  | 4,44 | 7,34 |
| Ethylbenzene |  | 1,98 | – |
| 1,4-Dimethylbenzene (p-xylene) |  | 27,61 | 39,40 |
| 1,3-Dimethylbenzene (m-xylene) |  |  |  |
| 1,2-Dimethylbenzene (o-xylene) |  | 5,15 | 8,26 |
| Methylbenzene (toluene) |  | 1,46 | – |
| Ethenylbenzene (styrene) |  | 18,13 | 3,86 |
| 1-Methyl-2-ethylbenzene |  | – | 2,11 |

Continuation of table 1

| 1,3,5-Trimethylbenzene (mesitylene) |  | 0,33 | – |
| --- | --- | --- | --- |
| 2,3-Dimethyloctane |  | 3,81 | – |
| 1,2,4-trimethylbenzene (pseudocumene) |  | 4,31 | 2,69 |
| 2,3-Benzofuran (coumarone) |  | 1,65 | 2,69 |
| Benzocyclopentadiene (indene) |  | 22,15 | 27,24 |
| 1,2,4,5-Tetramethylbenzene (durene) |  | – | 1,11 |
| Naphthalene (naphthalin) |  | 2,08 | 3,54 |
| Other hydrocarbons1 and unidentified compounds | – | 6,90 | 1,76 |
| Total | – | 100,00 | 100,00 |
| Quantity of resin-forming2 components [wt. %] | – | 41,93 | 33,79 |
| The content of styrene in resin-forming2 components [wt. %] | – | 43,23 | 11,42 |

Continuation of table 1

| The content of coumarone in resin-forming2 components [wt. %] | – | 3,94 | 7,96 |
| --- | --- | --- | --- |
| The content of indene in the resin-forming2 components [wt. %] | – | 52,83 | 80,62 |

1 – components, the content of which in all samples did not exceed 1.0% wt.

2 – styrene, coumarone, indene.